University of Oklahoma

Graduate College

EXPERIMENTAL INVESTIGATION, CORRELATION, AND DIMENSIONAL ANALYSIS OF NEAR-WELLBORE FORMATION TREATMENT BY GEL PARTICLES and particle-gel system

A Dissertation

submitted to the Graduate Faculty

in partial fulfillment of the requirements for the

Degree of

Doctor of Philosophy

By

ADNAN L. muhsin AL-IBADI

Norman, Oklahoma

2014

EXPERIMENTAL INVESTIGATION, CORRELATION, AND DIMENSIONAL ANALYSIS OF NEAR-WELLBORE FORMATION TREATMENT BY GEL PARTICLES and particle-gel system

A Dissertation approved for the

Mewbourne School of Petroleum and Geological Engineering

By

______________________________

Dr. Faruk Civan, Chair

______________________________

Dr. Deepak Devegowda

______________________________

Dr. Ramadan Ahmed

______________________________

Dr. Maysam Pournik

______________________________

Dr. Jeffrey Harwell

© Copyright by ADNAN AL-IBADI 2014

All Rights Reserved.

# Acknowledgements

I would like to express sincere gratitude to Dr. Faruk Civan, chairman of my committee and advisor of this dissertation work, for providing the best graduate school experience that I could have hoped for. I am deeply indebted for his ultimate support, guidance, patience, and generosity throughout this dissertation work.

I would like to thank Dr. Deepak Devegowada, Dr. Ramadan Ahmed, Dr. Maysam Pournik, and Dr. Jeffrey Harwell for serving in my dissertation committee and their helpful comments, and suggestions.

I would like to thank Dr. Ian Robb of Halliburton Energy Services, who past away, of his valuable discussions and support during the initiation of our experimental studies related to the near-wellbore formation treatment by gel particles suspension. I would also like to thank Dr. Larry Eoff with Halliburton for his support on the work related to the near-wellbore water shutoff treatment studies, both supplying equipment and chemicals for lab testing and discussion of lab results. I would also like to thank Dr. Cengiz Altan and Dr. Levent Aktas of the University of Oklahoma for use their microscope to obtain the photomicrographs included in this work.

Finally, I would like to thank my wife, my two sons, and my sweet daughter for their understanding, support, and encouragement. This work is dedicated to the memory of my parents.

# Table of Contents

Acknowledgements..........................................................................................................iv

List of Tables.....................................................................................................................x

List of Figures.................................................................................................................xii

Abstract .....................................................................................................................xxxvi

Chapter 1: Introduction.....................................................................................................1

1.1  Near-Wellbore Formation Treatment ………………..………………......……..1

1.2  Objectives of the Study …………………………………………………......….3

1.2.1  Experimental approaches................................................................................3

1.2.2  Data analysis approaches................................................................................3

1.3  Description of Materials Presented in Various Chapters ………...………....….4

Chapter 2: Literature Review ………………………......……………….……….....….10

2.1  Review of Experimental Studies……………………………….….…….….…10

2.2  Review of Theoretical Studies ……………………………….…….……….....24

Chapter 3: Factors   Affecting    the   Near- Wellbore    Formation   Treatment   by   Gel

Particles...........................................................................................................................31

3.1   Introduction……………………………………………………………....…...31

3.2  Gel Particle Properties........................................................................................31

3.2.1   Gel particle deformation and break-up………………………………....…32

3.2.2   Gel particle coagulation and detachment…………...................…….…....34

3.3   Carrier Fluid Properties.....................................................................................37

3.4   Gel Particle Suspension Properties....................................................................37

3.4.1   Viscosity......................................................................................................38

3.4.2   Gel particle diameter...................................................................................39

3.4.3   Suspension concentration............................................................................40

3.5   Porous Media.....................................................................................................41

3.6    Operation Conditions........................................................................................42

3.6.1   Flow rate......................................................................................................42

3.6.2   Temperature.................................................................................................43

Chapter 4: Experimental Studies of Near-Wellbore Formation Treatment.....................45

4.1  Introduction………….……………………………..…………………..…..….45

4.2.  Experimental Systems and Procedure……………………………………..….45

4.2.1. Experimental flow apparatus………………………………………………45

4.2.1.1 Apparatus for gel particle suspensions process………………………..…46

4.2.1.2 Apparatus for silica flour particle-gel system process………………..….40

Chapter 5: Investigation   of    Treatment  in   High-Permeability   Formations .  by   Gel

Particles Suspension………………………………………..………………………......54

5.1  Introduction……………………………………………………………...….....54

5.2  Experimental Results and Discussion ………………………………......….....55

5.2.1  Particle size distribution …………………………….……………...…......55

5.2.2  Effect of suspension concentration ………………………………......……60

5.2.3  Effect of flow rate…………………………………………………...……..63

5.2.4  Effect of particle size ……………………………….......…........................64

5.3  Development of Empirical Correlations …………………………………..…..66

5.3.1 Suspended particle size distribution before and after flow …………...…...66

5.3.2  Differential pressure across propant pack…………………………….…...68

5.3.3  Permeability impairment (reduction)………………………………...……73

5.3.4  Resistance factor ……………………………………………………..……78

5.4  Plugging Criteria Correlated by Use of Dimensionless Groups…………..…..82

5.5  Identification of Particle Retention Mechanisms……………………......….…86

5.6  Conclusions …………………………………………………………....……...90

Chapter 6:  Thermal    Effects    on    Near- Wellbore    Formation   Treatment   by   Gel

Particles Suspension…………………………………………………………..…......…92

6.1  Introduction ……………………………………………………………....…...92

6.2  Experimental Results, Data Analysis, and Discussion …………………..........93

6.3  Correlation of Measurements ………………………………………….......….96

6.4  Correlation of Thermal Effect on Plugging/Unplugging Processes …........…104

6.4.1  Simultaneous fitting of correlation……………………………….....……114

6.5  Conclusions ……………………………………………………………...…..118

Chapter 7: Dimensional   Analysis of   Near- Wellbore  Formation   Treatment  by   Gel

Particles Suspension……………………………………………..……….......…….…120

7.1  Introduction ……………………………………………………..…………...120

7.2  Relevant Dimensionless Groups …………………………………....………..121

7.3  Data Analysis and Correlation ………………………………………...……..124

7.3.1  Dimensionless groups selected for correlations ………………....………124

7.3.2  Dimensionless plots of experimental data ……………………..........…...126

7.3.3  Normalized experimental data …………………………………....…...…132

7.3.4  Permeability reduction correlations ………………………………...……136

7.4  Correlated Versus Measured Permeability Reduction ………………….…...141

7.5  Effect   of   Particle-Diameter   to  Pore-Throat   Size    Ratio   on  .Permeability

Reduction ……………………………………………………………….……149

7.6  Discussion and Conclusions ………………………………………….….…..152

Chapter 8:  Experimental  Investigation  and   Correlation  of   Particle-Gel  Systems for

Near-Wellbore Water Shutoff  Treatments ...………........………….……..........……154

8.1 Introduction…………………………………………………………….…..…154

8.2 Analysis and Investigation of Experimental Results ………………….…...…156

8.3 Development of Empirical Correlations………………………………..…..…157

8.3.1 Fluid Loss………………………………………… …………………...…157

8.3.2 Critical Silica Flour Concentration………………..………………….…...164

8.3.3 Pressure Initiate Flow………………………………………………….….166

8.4 Thermal Effects.................................................................................................170

8.4.1 Correlation of Thermal Effects…………………….............…………..…171

8.5 Conclusions……………………………………………………………….…..175

Chapter 9: Filtration   Analysis of   Particle- Gel   Systems  for   Near- Wellbore  Water

Shutoff  Treatments…….......................................................................….…......…….177

9.1 Introduction …………………………………………………………….….…177

9.2 Development of Empirical Correlations of Filtrate Volume …........................177

9.3 Correlations of Rate Constant of Filtrate and Spurt Loss Volume…………....186

9.4 Conclusions………………………………………………………………...…191

Chapter 10: Field Application for Near-Wellbore Formation Treatment Design.........192

10.1 Introduction......................................................................................................192

10.2 Synthetic Field Application of Gel-Particle Suspension..................................192

10.3 Synthetic Field Application of Silica Flour Particle-Gel System.....................199

Chapter 11: Summary, Discussion, and Conclusions .......................…………........…206

11.1 Experimental Investigations.............................................................................206

11.2 Theoretical Investigation..................................................................................207

11.3 Overall accomplishment and benefits..............................................................209

References …………………………………………………………………........…....210

Appendix A ………………………………………………………………………..…220

Appendix B ………………………………………………………………………...…228

Appendix C ………………………………………………………………………...…232

Appendix D ………………………………………………………………………..…239

Appendix E ………………………………………………………………………...…241

Appendix F …………………………………………………………………….…..…252

Appendix G ………………………………………………………………………..…256

Appendix H ………………………………………………………………………..…272

Appendix I ………………………………………………………………………....…275

Appendix J ……………………………………………………………………....……287

Appendix K ………………………………………………………………........…......292

# List of Tables

Table 2-1: Summary of the experimental studies ……………………………….…..…19

Table 2-2: Summary of the theoretical studies ……..................………………….……27

Table 3-1: Components and properties of the gel-particle suspensions..........................41

Table 4-1: Properties of the proppant pack....................................................................48

Table 4-2:Components  of the particle-gel systems……………….……………..….…52

Table 5-1: Best-estimate fitting parameters ………………………………………...…84

Table 5-2: Wojtanowicz et al. (1987) diagnostic equations ……………….……..…....86

Table 5-3: Rate  constants  of  plugging  regions for  pore throat plugging  mechanism at

different particle volume concentration …….……………………….………………....89

Table 5-4: Rate  constants  of  plugging   regions for pore surface deposition mechanism

at different particle volume concentration ……………………………………..…....…89

Table 6-1: Rate and intercept constants of plugging at T= 23.5 °C …………….........110

Table 6-2: Rate and intercept constants of unplugging at T= 23.5 °C ……….…..…..111

Table 6-3: Rate and intercept constants of plugging at T= 40 °C ………………....…111

Table 6-4: Rate and intercept constants of unplugging at T= 40 °C ……………..…..112

Table 6-5: Rate and intercept constants of plugging at T= 60 °C ………………....…112

Table 6-6: Rate and intercept constants of unplugging at T= 60 °C ……………....…113

Table 6-7: Rate and intercept constants of plugging at T= 75 °C ……………....……113

Table 6-8: Rate and intercept constants of unplugging at T= 75 °C …………....……114

Table 7-1: Summary of primary variables ……………………………….…..…….…122

Table 7-2: Step-by-step of the fundamental dimensions ……………………......……123

Table 8-1:Critical silica flour concentrations……………………………….…..….…159

Table 9-1: Rate constants of filtrate and spurt loss volumes of 35 micron pore diameter filter disc at different sand sizes and different silica flour concentrations……………………………………………………………….....….…..189

Table 10-1: Parameters of synthetic well and field reservoir........................................193

Table 10-2: Parameters of  the  gel-particle  suspension and the near-wellbore formation

modification...................................................................................................................194

Table 10-3: Summary of the empirical correlations of the gel-particle suspension......194

Table 10-4: Results  of the  design of the neae-wellbore  formation treatment by the gel-

particle suspension.........................................................................................................197

Table 10-5: Parameters of synthetic oil producing well................................................200

Table 10-6: Perforation zones of synthetic oil producing well.....................................201

Table 10-7: Components of the silica flour particle-gel system developed from fluid loss experiments....................................................................................................................203

Table 10-8: Summary  of   the  empirical  correlations  of   the  silica  flour  particle- gel

system............................................................................................................................203

Table 10-9: Comparison between field particle- particle system and experiment particle-gel system......................................................................................................................204

List of Figures

Figure 1.1: Schematic of various zones and gel particles suspension and silica flour particle-gel system applications in the near-wellbore formation …………….…………2

Figure 3.1: Difference between rigid and deformable  particles passing through pore throat: (a) rigid particles    (b) deformable particles …………………………………...32

Figure 3.2: General motion and deformation of a particle……………..………...…….33

Figure 3.3: Pseudoplastic behavior of 3 vol% suspension at T= 23.5 °C ……………..39

Figure 3.4: Viscosity of the 3 vol% gel particle suspension with temperature...............44

Figure 3.5: Effect of temperature on gel particles passing through pore: (a) at low temperature   (b) at high temperature …………………………………………....…….44

Figure 4.1: Schematic diagram of the experimental apparatus ......................................47

Figure 4.2: Schematic diagram of the experimental apparatus with heating system......49

Figure 4.3: Heating system of the experimental apparatus ……………………………50

Figure 4.4: Schematic of the filtrate test apparatus ………………………..………….52

Figure 4.5: Heating system of the filtrate test apparatus………………….....…...……53

Figure 5.1: Particles  distribution  of  3 vol%  original  and effluent samples at 50 cm³/hr

after 1 and 5 PVI ………………………………………………………….…………...57

Figure 5.2: Particles  distribution  of 3 vol% original and effluent samples at 100 cm³/hr

after 1 and 5 PVI ……………………………………………………………………….58

Figure 5.3: Particles  distribution  of 3 vol%  original and effluent samples at 200 cm³/hr

after 1 and 5 PVI ……………………………………………………………………….58

Figure 5.4: Particles  distribution  of 3 vol%  original and effluent samples at 280 cm³/hr

after 1 and 5 PVI ……………………………………………………………………….59

Figure 5.5: Particles  distribution of 3 vol%  original and effluent  samples at 400 cm³/hr

after 1 and 5 PVI ……………………………………………………………………….59

Figure 5.6: Photomicrographs of effluent samples at 100 cm³/hr: (a) after 1 pore volume

Injection (PVI)  (b) after 5 pore volume injection (PVI) ………………………………60

Figure 5.7: Permeability   reduction  at  100  cm³/hr  for   different   volume   suspension

Concentrations at T= 23.5 °C ………………………………………………………….62

Figure 5.8: Suspension viscosity at 100 cm³/hr for different particle volume concentrations at T= 23.5 °C …………………………………………………………..62

Figure 5.9: Permeability  reduction  at 3 vol%  concentration  for  different  flow rates at

T= 23.5 °C ……………………………………………………………………………..64

Figure 5.10: Permeability    reduction  at  100 cm³/hr   for   different   particle   sizes   at

T= 23.5 °C ……………………………………………………………………………..65

Figure 5.11: Particle  size distribution for the original and effluent suspensions at 1 PVI for different flow rates …………………………………………………………………67

Figure 5.12: Calculated particle size distribution for the original and effluent suspensions at 1 PVI for different flow rates ………………………………………....68

Figure 5.13: Exponential relationship between gel particle concentration and differential pressure at 100 cm³/hr and 23.5 °C ……………………………………………………69

Figure 5.14: The relationship between injection flow rate and differential pressure at 3 vol% and 23.5 °C ………………………………………………………………..…….71

Figure 5.15: The relationship between gel particle diameter and differential pressure at 3 vol% and 23.5 °C ………………………………………………………………...…..72

Figure 5.16: The  relationship  between  gel  particle   concentration   and   permeability

reduction at 3 vol% and 23.5 °C ………………………………………………...……..74

Figure 5.17: Exponential relationship between injection flow rate of 3 vol% suspension and permeability reduction at T= 23.5 °C ……………………………………..………75

Figure 5.18: The relationship between gel particle diameter and permeability reduction at 100 cm³/hr and 23.5 °C ……………………………………………………..………76

Figure 5.19: Variation of permeability reduction with particle diameter to pore throat size for different suspensions at 100 cm³/hr …………………………………..……….77

Figure 5.20: Polynomial relationship between gel particle concentration and resistance factor at 100 cm³/hr and 23.5 °C …………………………………………………..…..79

Figure 5.21: The relationship between injection flow rate and resistance factor at 3 vol% and 23.5 °C …………………………………………………………………………….80

Figure 5.22: The relationship between gel particle diameter and resistance factor at 100 cm³/hr and 23.5 °C ……………………………………………………………….……81

Figure 5.23: Experimental and correlation results from power-law model as a function of particle Reynolds number …………………………………………………………..85

Figure 5.24: Experimental and  correlation results from exponential-law model as a function of particle Reynolds number …………………………………………..….….85

Figure 5.25: Pore throat plugging mechanisms for different particle volume concentrations at 100 cm³/hr and 23.5 °C ………………………………………..……87

Figure 5.26: Pore surface deposition mechanisms for different particle volume concentrations at 100 cm³/hr and 23.5 °C ……………………………………….….…88

Figure 6.1: Permeability  reduction  at 3 vol% concentration for different temperature at

100 cm³/hr ……………………………………………………………………...………95

Figure 6.2: Straight-line VTF plot for the 3 vol% suspension viscosity…………...…..98

Figure 6.3: Comparison  between suspension viscosity obtained from the VTF equation and the measured data …………………………………………………………………99

Figure 6.4: Straight-line VTF plot for the differential pressure …………….……....…99

Figure 6.5: Comparison between differential pressure obtained from the VTF equation and the experimental data …………………………………………………….........…100

Figure 6.6: Straight-line VTF plot for the permeability reduction …………...…..…..101

Figure 6.7: Comparison between permeability reduction obtained from the VTF equation and the experimental data ……………………………..……………...….…101

Figure 6.8: Straight-line VTF plot for the resistance factor ……………..………...…103

Figure 6.9: Comparison between resistance factor obtained from the VTF equation and the experimental data ……………………………………………………………....…103

Figure 6.10: Permeability reduction at 3 vol% concentration for different temperatures at 100 cm³/hr ……………………………………………………………………….…104

Figure 6.11: Plugging events trends at T= 23.5 °C ………………………….....…….106

Figure 6.12: Unplugging events trends at T= 23.5 °C ……………………….….……107

Figure 6.13: Plugging events trends at T= 40 °C ………………………...……..……107

Figure 6.14: Unplugging events trends at T= 40 °C ……………………………….…108

Figure 6.15: Plugging events trends at T= 60 °C ……………………………...….….108

Figure 6.16: Unplugging events trends at T= 60 °C ………………………………....109

Figure 6.17: Plugging events trends at T= 75 °C ……………………………...….….109

Figure 6.18: Unplugging events trends at T= 75 °C …………...………………….....110

Figure 6.19: Rate  constant of  plugging  at different pore volumes injected and different

temperatures…………………………………………………………..................……116

Figure 6.20: Rate   constant   of   unplugging   at   different  pore  volumes  injected  and

different temperatures……………………………………………………....…………116

Figure 6.21: Intercept  of   plugging  regions  at  different   pore  volumes   injected  and

different temperatures…………………………………………………………....……117

Figure 6.22: Intercept  of  unplugging  regions  at  different  pore  volumes  injected and

different temperatures…………………………………………………………....……117

Figure 7.1: The dimensionless groups for permeability reduction at 3 vol% concentration for different temperatures at 100 cm³/hr …………………………...….127

Figure 7.2: The dimensionless groups for permeability reduction at 3 vol% concentration for different temperatures at 100 cm³/hr …………………………...….127

Figure 7.3: The dimensionless groups for permeability reduction at 100 cm³/hr  for different concentrations  at T= 23.5 °C ………………………………………………128

Figure 7.4: The dimensionless groups for permeability reduction at 3 vol% concentration for different flow rates at T= 23.5 °C …………………………………128

Figure 7.5: The dimensionless groups for permeability reduction at 100 cm³/hr  for different  gel   particle   sizes   at  T= 23.5 °C  for   the  sand   pack  of  1015  µm   grain

diameter ………………………………………………………………………………129

Figure 7.6: The dimensionless groups for permeability reduction at 100 cm³/hr  for different   gel    particle    sizes   at  T= 23.5 °C   for   the   sand   pack of 1015 µm grain

diameter ………………………………………………………………………………129

Figure 7.7: The dimensionless groups for permeability reduction at 100 cm³/hr  for different   gel   particle    sizes  at  T= 23.5  °C  for  the   sand   pack  of  1015 µm  grain

diameter ………………………………………………………………………………130

Figure 7.8: The dimensionless groups for permeability reduction at 100 cm³/hr  for different   gel   particle   sizes   at  T= 23.5  °C  for   the   sand  pack  of  650  µm   grain

diameter ………………………………………………………………………………130

Figure 7.9: The dimensionless groups for permeability reduction at 100 cm³/hr  for different   gel    particle   sizes  at  T= 23.5  °C  for   the   sand   pack  of  650  µm  grain

diameter ………………………………………………………………………………131

Figure 7.10: The dimensionless groups for permeability reduction at 100 cm³/hr  for different   gel    particle   sizes  at  T= 23.5  °C  for   the   sand   pack  of  650  µm  grain

diameter ………………………………………………………………………………131

Figure 7.11: Correlation of the normalized  dimensionless groups for permeability reduction at 3 vol% concentration for different temperatures at 100 cm³/hr…………133

Figure 7.12: Correlation of the normalized  dimensionless groups for permeability reduction at 3 vol% concentration for different temperatures at 100 cm³/hr……...….134

Figure 7.13: Correlation of the normalized  dimensionless groups for permeability reduction at 100 cm³/hr for different concentrations at T= 23.5 °C……..………..…..134

Figure 7.14: Correlation of the normalized  dimensionless groups for permeability reduction at 3 vol% concentration for different flow rates at T= 23.5 °C……...….….135

Figure 7.15: Correlation of the normalized  dimensionless groups for permeability reduction  at 100 cm³/hr for  different gel  particle  sizes at T= 23.5 °C for the sand pack

of 1015 µm grain diameter ……..…………………………………………….……....135

Figure 7.16: Correlation of the normalized  dimensionless groups for permeability reduction  at 100 cm³/hr for  different gel particle  sizes at T= 23.5 °C for the  sand pack

of 650 µm grain diameter ……..…………………………………………….…….….136

Figure 7.17: Measured  permeability  reduction  and  correlated  permeability  reduction

( from K∆pµovozo/Ko∆poµvz and (µt/ρz²)*  correlation)  at 3 vol% concentration for different temperatures at 100 cm³/h ………………..…...........................................….138

Figure 7.18: Measured  permeability  reduction  and  correlated  permeability  reduction

( from K∆pµovozo/Ko∆poµvz and (t²Cθ/z²)*  correlation)  at 3 vol% concentration for different temperatures at 100 cm³/h………………….....................................….....….139

Figure 7.19:  Measured  permeability  reduction  and  correlated  permeability reduction

( from K∆pµovozo/Ko∆poµvz and (µt/ρz²)*  correlation)  at 100 cm³/h for different concentrations at T= 23.5 ˚C ………………………...…....................…..…139

Figure7.20: Measured   permeability  reduction  and  correlated  permeability  reduction

( from K∆pµovozo/Ko∆poµvz and (vt/z)*  correlation)   at 3 vol% concentration for different flow rates at T= 23.5 ˚C ………………........................................……….…140

Figure 7.21: Measured  permeability  reduction  and  correlated  permeability  reduction

( from K∆pµovozo/Ko∆poµvz and (µt/ρDp²)* correlation) at 100 cm³/h for different gel particle sizes at T= 23.5 ˚C for the sand  pack of 1015 µm grain diameter .................140

Figure 7.22: Measured  permeability  reduction  and  correlated  permeability  reduction

( from K∆pµovozo/Ko∆poµvz and (µt/ρDp²)* correlation) at 100 cm³/h for different gel particle sizes at T= 23.5 ˚C for the sand pack of 650 µm grain diameter.................    141

Figure 7.23: Comparison between measured permeability reduction and correlated permeability    reduction   at   3 vol%  concentration    for    different    temperatures   at

100cm³/h ……………………………………………………………...………………143

Figure 7.24: Comparison  between  measured  permeability   reduction   and   correlated

permeability   reduction  at  3 vol%  concentration   for   different   temperatures  at  100

cm³/h ……………………………………………………………………………….…143

Figure 7.25: Comparison between measured permeability reduction and correlated permeability reduction at 100 cm³/h for different concentrations at T= 23.5 ˚C ….....144

Figure 7.26: Comparison between measured permeability reduction and correlated permeability  reduction  at 3  vol%  concentration  for   different  flow  rates  at  T= 23.5

˚C...................................................................................................................................144

Figure 7.27: Comparison between measured permeability reduction and correlated permeability reduction at 100 cc/h for different gel particle sizes at T= 23.5 ˚C for the sand pack of 1015 µm grain diameter ………………………………………......……145

Figure 7.28: Comparison between measured permeability reduction and correlated permeability reduction at 100 cc/h for different gel particle sizes at T= 23.5 ˚C for the sand pack of 650 µm grain diameter ……………………………………..….......…...145

Figure 7.29: Comparison between constant limit value of steady measured permeability reduction and correlated permeability reduction at 5 PVI for different temperatures..146

Figure 7.30: Comparison between constant limit value of steady measured  permeability reduction and correlated permeability reduction at 5 PVI for different temperatures..146

Figure 7.31: Comparison between constant limit value of steady measured permeability reduction   and    correlated     permeability     reduction    at     5    PVI    for     different

concentrations................................................................................................................147

Figure 7.32: Comparison between constant limit value of steady measured  permeability

reduction    and    correlated    permeability    reduction    at  5  PVI  for  different   flow

rates................................................................................................................................147

Figure 7.33: Comparison between constant limit value of steady measured  permeability

reduction  and correlated permeability reduction at 5 PVI for different gel  particle sizes

for the sand pack of 1015 µm grain diameter ……………………………………...…148

Figure 7.34: Comparison between constant limit value of steady measured permeability reduction and correlated permeability reduction at 5 PVI for different gel particle sizes for the sand pack of 650 µm grain diameter …………………………………….....…148

Figure 7.35: Limit value of steady measured permeability reduction and correlated permeability reduction at 100 cm³/h for 3 vol% concentration at T= 23.5 ˚C for different particle diameter to pore-throat size ratios (Al-Ibadi and Civan, 2012 and 2013a) ….150

Figure 7.36: Limit value of steady measured and correlated π10 ″  and  π2  dimensionless groups for permeability reduction at 100 cm³/h for 3 vol% concentration at T= 23.5 ˚C for different particle diameter to pore-throat size ratios ……………………..…….…150

Figure 7.37: Measured  permeability  reduction  and  correlated  permeability  reduction

( from K∆pµovozo/Ko∆poµvz and Dp/DT dimensionless  groups) at 100 cm³/h for 3 vol%

at T= 23.5 ˚C for different particle diameter to pore-throat size ratios.........................151

Figure 7.38: Comparison between constant limit value of measured permeability reduction and correlated permeability reduction at 100 cc/h for 3 vol% concentration at T= 23.5 ˚C for different particle diameter to pore-throat size ratios …………………151

Figure 8.1: Convert the filtrate test from laboratory scale to field scale ……………..156

Figure 8.2: The filtrate cake for same filter disc and same silica flour concentration and different sand sizes (a) 12/20  mesh (b) 20/40 sand   (c) 40/70 mesh ………..............157

Figure 8.3: Experimental and correlated fluid loss at different silica flour concentrations and  different  sand  sizes  for  35  micron  average  pore  diameter  of filter disc (Plot of

Eq. 8.3)…….............................................................................................................….163

Figure 8.4: Experimental and correlated fluid loss at different silica flour concentrations and  different  sand  sizes  for 10  micron  average  pore  diameter of  filter  disc (Plot of

Eq. 8.3)…….............................................................................................................….163

Figure 8.5: Experimental and correlated fluid loss at different silica flour concentrations and  different  sand  sizes  for  5  micron  average  pore  diameter  of  filter  disc (Plot of

Eq. 8.3)….................................................................................................................….164

Figure 8.6: Experimental and correlated fluid loss at different silica flour concentrations and different pore diameters of filter discs for 12/20 sand mesh (Plot of Eq. 8.4)…...164

Figure 8.7: The  filtrate  cake for  same sand  mesh and  same  silica flour  concentration

and different pore diameters of filter discs (a) 5 micron (b) 10 micron (c) 35 micron.165

Figure 8.8: Experimental    and   correlated     critical   silica    flour    concentration    at

different    sand   sizes   and    different   (Plot of Eq. 8.5)    pore    diameters     of   filter

discs…………………………………………..............................………...….....……165

Figure 8.9: Experimental and correlated pressure initiate flow at different silica flour concentrations and different sand sizes for 35 micron average pore diameter of filter disc (Plot of Eq. 8.7)…….........................................................................................….168

Figure 8.10: Experimental and correlated pressure initiate flow at different silica flour concentrations and different sand sizes for 10 micron average pore diameter of filter disc (Plot of Eq. 8.7)…….........................................................................................….169

Figure 8.11: Experimental and correlated pressure initiate flow at different silica flour concentrations and different sand sizes for 5 micron average pore diameter of filter disc (Plot of Eq. 8.7)……................................................................................................….169

Figure 8.12: Experimental and correlated pressure initiate flow at different silica flour concentrations and different pore diameters of filter discs for 12/20 sand mesh (Plot of Eq. 8.7)…….............................................................................................................….170

Figure 8.13: Straight-line VTF plot for the 2.8 vol% particle-gel system viscosity….172

Figure 8.14: Straight-line VTF plot for the fluid loss………………………….……..173

Figure 8.15: Straight-line VTF plot for the pressure initiate flow……………………173

Figure 8.16: Comparison between silica flour particle-gel system viscosity obtained from the VTF equation and the measured data……………………………...…..……174

Figure 8.17: Comparison  between  fluid loss obtained from the VTF equation and the measured data…………………………………………………………………………174

Figure 8.18: Comparison between pressure initiate flow obtained from the VTF equation and the measured data………………………….……………………………175

Figure 9.1: Exponential relationship between filtrate time and filtrate volume at 35  micron pore diameter of filter disc and 12/20 sand mesh for different silica flour concentrations…………………………....................................................................…179

Figure 9.2: Exponential relationship between filtrate time and filtrate volume at 35  micron pore diameter of filter disc and 20/40 sand mesh for different silica flour concentrations…………........................................................…............………………180

Figure 9.3: Exponential relationship between filtrate time and filtrate volume at 35  micron pore diameter of filter disc and 40/70 sand mesh for different silica flour concentrations…………………....................................................................…………180

Figure 9.4: The  filtrate  cake  for  same  sand mesh  and same filter disc  and   different

silica    flour    concentrations      (a)  0.21  vol%       (b)  0.53  vol%      (c)     1.06  vol%

(d)  1.60 vol%................................................................................................................181

Figure 9.5: The filtrate cake for  same filter  disc  and  same  silica  flour   concentration

and different sand sizes (a) 12/20  mesh (b) 20/40 sand   (c) 40/70 mesh……………181

Figure 9.6: Exponential relationship between filtrate time and filtrate volume at 10  micron pore diameter of filter disc and 12/20 sand mesh for different silica flour concentrations…………….............................................................…………….......…182

Figure 9.7: Exponential relationship between filtrate time and filtrate volume at 10  micron pore diameter of filter disc and 20/40 sand mesh for different silica flour concentrations…………………....................................................................…………183

Figure 9.8: Exponential relationship between filtrate time and filtrate volume at 10  micron pore diameter of filter disc and 40/70 sand mesh for different silica flour concentrations………………....................................................................……………183

Figure 9.9: Exponential relationship between filtrate time and filtrate volume at 5  micron pore diameter of filter disc and 12/20 sand mesh for different silica flour concentrations………………....................................................................……………184

Figure 9.10: Exponential relationship between filtrate time and filtrate volume at 5  micron pore diameter of filter disc and 20/40 sand mesh for different silica flour concentrations………….................................................................…...………………184

Figure 9.11: Exponential relationship between filtrate time and filtrate volume at 5 micron pore diameter of filter disc and 40/70 sand mesh for different silica flour concentrations………………………....................................................................……185

Figure 9.12: The filtrate cake for same sand mesh and same silica flour concentration and different pore diameter of filter discs (a) 5 micron  (b) 10 micron (c) 35 micron..185

Figure 9.13: Experimental  and  correlated  filtrate  volume of 35 micron  pore  diameter

filter disc and 12/20 sand mesh for different silica flour concentrations………..……187

Figure 9.14: Experimental  and  correlated  filtrate  volume of 35 micron  pore  diameter

filter disc and 20/40 sand mesh for different silica flour concentrations…………..…188

Figure 9.15: Experimental  and  correlated  filtrate  volume of 35 micron  pore  diameter

filter disc and 40/70 sand mesh for different silica flour concentrations…………..…188

Figure 9.16: Rate  constant of  filtrate of 35 micron pore diameter  filter disc at different

silica flour concentrations and  different sand sizes……………………………..……190

Figure 9.17: Spurt loss volume of 35 micron  pore diameter  filter disc at different  silica

flour concentrations and  different sand sizes……………………………………...…190

Figure 10.1: Schematic of synthetic well under drilling process..................................193

Figure 10.2: Process  of    the    near- wellbore   formation    treatment   by   gel- particle

suspension......................................................................................................................198

Figure 10.3: Schematic of synthetic oil producing well................................................200

Figure 10.4: Process  of   the   near- wellbore   water   shutoff     treatment   by  particle-

gel system......................................................................................................................205

Figure C.1: Straight  line  plot  of  Eq. B-1  at  50  cm³/hr and 100  cm³/hr  flow  rates to

develop  the  empirical  correlation of the differential pressure at 3 vol% and 23.5 °C, as

shown in Fig. 5.14.........................................................................................................232

Figure C.2: Straight  line plot of Eq. B-2 at 100 cm³/hr, 200 cm³/hr, 280  cm³/hr and 400

cm³/hr flow  rates to  develop  the  empirical correlation of the  differential pressure at 3

vol% and 23.5 °C, as shown in Fig. 5.14.......................................................................233

Figure C.3: Straight  line plot of  Eq. B-3 at  different  gel- particle diameters to develop

the  empirical correlation of the  differential   pressure at 3 vol%  and 23.5 °C, as  shown

in Fig. 5.15.....................................................................................................................233

Figure C.4: Straight  line   plot  of   Eq. B-4  at  different  gel-particle  concentrations  to

develop   the  empirical  correlation of   the   permeability  reduction  at  100 cm3/h  and

23.5 °C, as shown in Fig. 5.16.......................................................................................234

Figure C.5: Straight  line  plot of Eq. B-4 at  different gel-particle diameters  to  develop

the  empirical   correlation  of   the   permeability  reduction  at  100 cm3/h  and 23.5 °C,

as shown in Fig. 5.18.....................................................................................................235

Figure C.6: Straight  line plot of Eq. B-4 at different particle diameter to pore throat size

ratios to  develop  the  empirical correlation of  the  permeability reduction at 100 cm3/h

and 23.5 °C, as shown in Fig. 5.19................................................................................235

Figure C.7: Straight    line   plot  of   Eq. B-5   at   0.5 vol%   and   1 vol%    gel-particle

concentrations to develop the empirical correlation of the  resistance factor at 100 cm3/h

and 23.5 °C, as shown in Fig. 5.20................................................................................236

Figure C.8:  Straight  line  plot of  Eq. B-6  at  1 vol%,  2 vol% and 3 vol%  gel- particle

concentrations to develop the empirical correlation of the  resistance factor at 100 cm3/h

and 23.5 °C, as shown in Fig. 5.20................................................................................237

Figure C.9: Straight  line  plot  of  Eq. B-7   at  50 cm³/hr  and  100 cm³/hr flow  rates to

develop  the  empirical correlation of   the  resistance  factor  at 3 vol%  and  23.5 °C, as

shown in Fig. 5.21.........................................................................................................237

Figure C.10: Straight line plot of Eq. B-6 at 100 cm³/hr, 200 cm³/hr, 280 cm³/hr and 400

cm³/hr  flow  rates to develop the empirical correlation of the resistance factor at 3 vol%

and 23.5 °C, as shown in Fig. 5.21................................................................................238

Figure C.11: Straight  line  plot of  Eq. B-5 at  different gel-particle diameter to develop

the empirical correlation of  the  resistance factor at 100 cm3/h and 23.5 °C, as shown in

Fig. 5.22.........................................................................................................................238

Figure D.1: Straight  line  plot of   Eq. B-8  at  different gel particle  concentrations  and

different    gel    particle   diameters  to   develop   the   power-law   equation,  shown  in

Fig. 5.23.........................................................................................................................239

Figure D.2: Straight  line  plot of  Eq. B-9  at  different  gel  particle  concentrations and

different   gel   particle   diameters   to   develop   the   power-law   equation,  shown   in

Fig. 5.23.........................................................................................................................240

Figure E.1: The  relationship  between  rate  constant  of  plugging   and   pore  volumes

injected at various temperatures....................................................................................241

Figure E.2: The relationship between  rate  constant  of  unplugging  and  pore  volumes

injected at various temperatures....................................................................................242

Figure E.3: Straight   line   plot  of  Eq. B-6   at  different   temperature  to  develop  the empirical   correlation  of   the   rate  constants  of  the   plugging  regions, as  shown  in

Fig. E.1..........................................................................................................................242

Figure E.4: Straight   line  plot  of   Eq. B-6   at   different   temperature to  develop  the  empirical   correlation of  the  rate  constants  of  the  unplugging  regions, as  shown  in

Fig. E.2..........................................................................................................................243

Figure E.5: The  relationship  between   intercept of plugging regions and pore volumes

injected at various temperatures....................................................................................244

Figure E.6: The   relationship   between   intercept   of   unplugging  regions   and   pore

volumes injected at various temperatures......................................................................244

Figure E.7: Straight   line   plot of   Eq. B-4   at  different   temperature  to  develop  the empirical    correlation  of   the   intercepts  of     the   plugging    regions, as   shown   in

Fig. E.5..........................................................................................................................245

Figure E.8: Straight   line   plot  of   Eq. B-2   at  different  temperature  to  develop  the empirical   correlation of   the   intercepts   of   the   unplugging   regions, as   shown   in

Fig. E.6..........................................................................................................................245

Figure E.9: Linear  function plot of A values at different temperatures for rate constants

of plugging………………………………………………………...……………..……246

Figure E.10: Linear function plot of B values at different temperatures for rate constants

of plugging…………………………………………………………………...……..…247

Figure E.11: Linear  function plot of β values at different temperatures for rate constants

of plugging……………………………………………………………   …………..…247

Figure E.12: Linear function plot of A values at different temperatures for rate constants

of unplugging…………………………………………………………………...…..…248

Figure E.13: Linear function plot of B values at different temperatures for rate constants

of unplugging…………………………………………………………………   …..…248

Figure E.14: Linear function plot of β values at different temperatures for rate constants

of unplugging………………………………………………………………….....……249

Figure E.15: Linear function  plot  A values at  different temperatures   for   intercept of

plugging regions…………………………………………………………………….…249

Figure E.16: Linear function  plot of B values at  different  temperature for intercept  of

plugging regions……………………………………………………….…………....…250

Figure E.17: Linear function  plot of β values at different temperatures for  intercept  of

plugging regions…………………………………………………………………....…250

Figure E.18: Linear function plot of A values at different temperatures for  intercept  of

unplugging regions……………………………………………………………....……251

Figure E.19: Linear function plot of  B values at different temperatures for  intercept of

unplugging regions………………………………………………………………....…251

Figure F.1: Straight line plot of Eq. B-2 for  the  normalized dimensionless group π4   for

the permeability reduction at different temperatures, as shown in Fig.7.11…….........252

Figure F.2: Straight line plot of Eq. B-2 for  the normalized dimensionless  group π9   for

the permeability reduction at different temperatures, as shown in Fig.7.12…....…….253

Figure F.3: Straight  line  plot of  Eq. B-7 for  the   normalized  dimensionless  group π4

for  the  permeability  reduction  at  different  gel  particles  concentrations, as  shown in

Fig.7.13………..............................................................................................................253

Figure F.4: Straight line  plot  of  Eq. B-7  for  the normalized  dimensionless   group π6

for the permeability reduction at different flow rates, as  shown in Fig.7.14...............254

Figure F.5: Straight  line plot  of  Eq. B-2 for the normalized dimensionless group π5 for

The  permeability reduction of  the sand pack of 1061 µm grain diameter at different gel

particles sizes, as  shown in Fig.7.15.............................................................................254

Figure F.6: Straight  line plot of  Eq. B-2 for the normalized dimensionless group π5  for

the  permeability reduction of  the sand  pack of 650 µm grain diameter  at different gel

particles sizes, as  shown in Fig.7.16.............................................................................255

Figure G.1: Correlate  the  experimental   results of   fluid loss  at  different   silica  flour

concentrations  for 35 micron  average  pore diameter of  filter  disc  and  different  sand

sizes...............................................................................................................................256

Figure G.2: Correlate  the  experimental   results of   fluid loss  at  different   silica  flour

concentrations  for 10 micron  average  pore diameter of  filter  disc  and  different  sand

sizes...............................................................................................................................257

Figure G.3: Correlate  the  experimental   results of   fluid loss  at  different   silica  flour

concentrations  for 5 micron  average  pore  diameter of  filter  disc  and  different  sand

sizes...............................................................................................................................257

Figure G.4: Straight  line  plot of  Eq. B-6  to develop the exponential relationship of the

fluid   loss at  different  silica  flour  concentration for  35 micron pore diameter of filter disc at different sand sizes, as shown in Fig. G.1..........................................................258

Figure G.5: Straight  line  plot of  Eq. B-6  to develop the exponential relationship of the

fluid   loss at  different  silica  flour  concentration for  10 micron pore diameter of filter disc at different sand sizes, as shown in Fig. G.2..........................................................258

Figure G.6: Straight  line  plot of  Eq. B-6  to develop the exponential relationship of the

fluid   loss at   different  silica  flour  concentration for  5 micron pore  diameter of filter disc at different sand sizes, as shown in Fig. G.3..........................................................259

Figure G.7: Correlate  the experimental results of fluid loss with the critical silica   flour

concentrations  for  35 micron average  pore diameter  of filter  disc  and  different  sand

sizes...............................................................................................................................260

Figure G.8: Correlate  the experimental  results of fluid loss with the critical silica  flour

concentrations  for  10 micron average  pore diameter  of filter  disc  and  different  sand

sizes...............................................................................................................................260

Figure G.9: Correlate  the experimental  results of fluid loss with the critical silica  flour

concentrations  for  5 micron average   pore diameter  of filter  disc  and  different  sand

sizes...............................................................................................................................261

Figure G.10: Straight  line  plot  of  Eq. B-10  to correlate  the fluid loss with the critical

silica  flour  concentration   for  35 micron pore diameter of filter disc at different sand sizes, as shown in Fig. G.7............................................................................................261

Figure G.11: Straight  line  plot of  Eq. B-10  to  correlate  the fluid loss with the critical

silica  flour  concentration   for  10 micron pore diameter of filter disc at different sand sizes, as shown in Fig. G.8............................................................................................262

Figure G.12: Straight  line  plot  of  Eq. B-10  to correlate  the fluid loss with the critical

silica  flour  concentration   for  5 micron  pore diameter of filter disc at different sand sizes, as shown in Fig. G.9............................................................................................262

Figure G.13: Linear  function plot of B values at different sand sizes for 35 micron  pore

diameter of filter disc………………………………………………………………….263

Figure G.14: Linear  function plot of α values at different  sand sizes for 35 micron pore

diameter of filter disc………………………………………………………………….264

Figure G.15: Linear function plot of xcr values at different sand sizes for 35 micron pore

diameter of filter disc………………………………………………………………….264

Figure G.16: Linear  function plot of B values at different  sand sizes for 10 micron pore

diameter of filter disc………………………………………………………………….265

Figure G.17: Linear  function plot of α values at different sand  sizes for 10 micron pore

diameter of filter disc………………………………………………………………….265

Figure G.18: Linear function plot of xcr values at different sand sizes for 10 micron pore

diameter of filter disc………………………………………………………………….266

Figure G.19: Linear function plot of B values at different  sand  sizes for 5 micron   pore

diameter of filter disc………………………………………………………………….266

Figure G.20: Linear function plot of α values  at different  sand  sizes for 5 micron  pore

diameter of filter disc………………………………………………………………….267

Figure G.21: Linear function plot of xcr values at different  sand  sizes for 5 micron pore

diameter of filter disc………………………………………………………………….267

Figure G.22: Linear function plot of a1 at different pore diameters of filter discs........268

Figure G.23: Linear function plot of b1 at different pore diameters of filter discs........269

Figure G.24: Linear function plot of a2 at different pore diameters of filter discs........269

Figure G.25: Linear function plot of b2 at different pore diameters of filter discs........270

Figure G.26: Linear function plot of a3 at different pore diameters of filter discs........270

Figure G.27: Linear function plot of b3 at different pore diameters of filter discs........271

Figure H.1: Correlate  the  critical silica  flour  concentrations  for 35, 10, and 5  micron

pore diameter of filter discs and different sand sizes....................................................272

Figure H.2: Linear  function   plot  of  A  values   at  different   pore   diameter   of  filter

discs...............................................................................................................................273

Figure H.3: Linear   function   plot  of  A   values  at   different   pore  diameter  of  filter

discs...............................................................................................................................274

Figure I.1: Correlate   the  experimental  results of pressure initiate flow with the critical

Silica  flour  concentrations  for  35  micron  average  pore  diameter  of  filter  disc  and

different sand sizes........................................................................................................275

Figure I.2: Correlate   the  experimental  results of pressure initiate flow with the critical

Silica  flour  concentrations  for  10  micron  average  pore  diameter  of  filter  disc  and

different sand sizes........................................................................................................276

Figure I.3: Correlate   the  experimental  results of pressure initiate flow with the critical

Silica   flour  concentrations  for  5  micron  average   pore  diameter  of  filter  disc  and

different sand sizes........................................................................................................276

Figure I.4: Straight  line  plot of  Eq. B-11  to develop  the  relationship  of  the pressure

Initiate  flow at different  silica flour  concentration for 35 micron pore diameter of filter disc at different sand sizes, as shown in Fig. I...1.........................................................277

Figure I.5: Straight  line  plot of  Eq. B-11  to develop  the  relationship  of  the pressure

Initiate  flow at different  silica flour  concentration for 10 micron pore diameter of filter disc at different sand sizes, as shown in Fig. I.2...........................................................277

Figure I.6: Straight  line  plot of  Eq. B-11  to develop  the  relationship  of  the pressure

Initiate  flow at different  silica flour  concentration for 5 micron pore diameter of filter disc at different sand sizes, as shown in Fig. I.3...........................................................278

Figure I.7: Linear  function   plot  of A values at different sand sizes for 35 micron  pore

diameter of filter disc....................................................................................................379

Figure I.8: Linear   function   plot of  B values at different sand sizes for 35 micron pore

diameter of filter disc.....................................................................................................379

Figure I.9: Linear   function   plot of α values at different  sand sizes for 35 micron  pore

diameter of filter disc.....................................................................................................280

Figure I.10: Linear  function  plot of A values at different sand sizes for 10 micron  pore

diameter of filter disc.....................................................................................................280

Figure I.11: Linear  function  plot of B values at different sand sizes for 10 micron  pore

diameter of filter disc.....................................................................................................281

Figure I.12: Linear  function  plot of α values at different sand sizes for 10 micron  pore

diameter of filter disc.....................................................................................................281

Figure I.13: Linear  function  plot of  A values at different  sand sizes for 5 micron  pore

diameter of filter disc.....................................................................................................282

Figure I.14: Linear  function  plot of B values  at different  sand  sizes for 5 micron pore

diameter of filter disc……………….…………………………………………………282

Figure I.15: Linear  function  plot of α values at different  sand  sizes for 5 micron  pore

diameter of filter disc……………….…………………………………………………283

Figure I.16: Linear function  plot of a1 at different  pore diameters of filter discs.......284

Figure I.17: Linear function  plot of b1 at different pore diameters of filter discs........284

Figure I.18: Linear  function plot of  a2 at different pore diameters of filter discs.......285

Figure I.19: Linear  function plot of b2 at different pore diameters of filter discs.......285

Figure I.20: Linear  function plot of a3 at different pore diameters of filter discs........286

Figure I.21: Linear   function plot of b3 at different pore diameters of filter discs.......286

Figure J.1: Straight  line  plot of  Eq. B-6 for 35  micron  pore diameter of  filter  disc  at

12/20 sand mesh and different silica flour concentrations............................................287

Figure J.2: Straight  line  plot of  Eq. B-6 for 35  micron  pore diameter of  filter  disc  at

20/40 sand mesh and different silica flour concentrations............................................288

Figure J.3: Straight  line  plot of  Eq. B-6 for 35  micron  pore diameter of  filter  disc  at

40/70 sand mesh and different silica flour concentrations............................................288

Figure J.4: Straight  line   plot  of  Eq. B-6 for 10  micron  pore  diameter  of  filter  disc

at 12/20 sand mesh and different silica flour concentrations........................................289

Figure J.5: Straight  line  plot  of   Eq. B-6 for 10  micron  pore  diameter  of  filter  disc

at 20/40 sand mesh and different silica flour concentrations........................................289

Figure J.6: Straight  line   plot  of  Eq. B-6 for 10  micron   pore  diameter  of  filter  disc

at 40/70 sand mesh and different silica flour concentrations........................................290

Figure J.7: Straight   line   plot  of   Eq. B-6  for 5  micron  pore  diameter  of  filter  disc

at 12/20 sand mesh and different silica flour concentrations........................................290

Figure J.8: Straight   line   plot  of  Eq. B-6   for 5  micron  pore  diameter  of  filter  disc

at 20/40 sand mesh and different silica flour concentrations........................................291

Figure J.9: Straight   line   plot  of  Eq. B-6   for 5  micron  pore  diameter  of  filter  disc

at 40/70 sand mesh and different silica flour concentrations........................................291

Figure K.1: The   relationship   between   rate  constant    of    filtrate   and   silica   flour

concentration at 35 micron pore diameter filter disc and different sand sizes..............292

Figure K.2: The relationship between spurt loss volume and silica flour concentration at

35 micron pore diameter filter disc and different sand sizes.........................................293

Figure K.3: Straight  line  plot of  Eq. A-6  at  35  micron  pore  diameter of filter disc to

develop  the   exponential  correlation of the  rate constant of  filtrate of  different  sand

sizes, as shown in Fig. K.1............................................................................................293

Figure K.4: Straight  line  plot  of Eq. A-6  at  35  micron  pore  diameter of filter disc to

develop the exponential correlation of the spurt loss volume of different  sand   sizes , as

shown in Fig. K.2..........................................................................................................294

Figure K.5: Linear function plot of A values at different sand sizes for the rate constants

of filtrate of 35 micron pore diameter filter disc...........................................................295

Figure K.6: Linear function  plot of B values at different sand sizes for the rate constants

of filtrate of 35 micron pore diameter filter disc...........................................................295

Figure K.7: Linear function  plot of β values at different sand sizes for the rate constants

of filtrate of 35 micron pore diameter filter disc............................................................296

Figure K.8: Linear  function  plot of A values at  different  sand  sizes   for the  spurt loss

volume of filtrate of 35 micron pore diameter filter disc...............................................296

Figure K.9: Linear  function plot of B values at  different  sand   sizes  for  the  spurt loss

volume of filtrate of 35 micron pore diameter filter disc..............................................297

Figure K.10: Linear function  plot of β values at  different  sand  sizes  for the  spurt loss

volume of filtrate of 35 micron pore diameter filter disc..............................................297

# Abstract

Reservoir permeability heterogeneity with high permeability zones can create many problems in petroleum reservoirs such as lost circulation of drilling fluids and high water production in hydrocarbon producing wells. These problems cause high cost to the oil and gas industry. Thus, the conditions leading to plugging of the high permeability zones during the treatment and conditioning of high permeability porous formations by suspended gel particles and silica flour particle-gel systems were studied and useful empirical correlations, dimensionless correlations, and charts were developed which can be used for effective and successful design of formation-plugging treatment.

First, conditioning and plugging of high permeability formations and the resulting permeability impairment occurring during injection of suspensions of deformable gel particles are investigated experimentally to treat reservoir permeability heterogeneity which can  prevent lost circulation of drilling fluids. Appropriate dimensionless groups are used to develop several empirical correlations of the experimental data, which can assist in choosing suitable gel-particle suspensions and proper conditions required for effective near-wellbore-formation treatment.

Second, the plugging and permeability impairment processes involved in the treatment and conditioning of high permeability porous formations is investigated at various temperatures by flowing a suspension of gel particles through unconsolidated proppant packs. The effective mechanisms of the consecutive plugging and unplugging processes occurring during the flow of gel particles suspension through the proppant pack are identified and the best-estimate values of their rate coefficients are determined. Various empirical correlations of practical importance developed in this work can be used for effective design of the suspended gel particles treatment in highly permeable near-wellbore formations. These correlations can predict the effect of temperature on conditioning of the high permeability formations by injection of suspensions of gel particles.

Third, analysis and interpretation of experimental data of laboratory tests of porous formation treatment by gel particles conducted at different gel particles suspension and application conditions are presented based on the dimensional analysis method. The measured permeability reduction caused by gel particles suspension injection into sand packs is correlated successfully by using the dimensionless groups developed from the relevant variables of sand packs, gel particles suspensions, and application operation conditions. Dimensionless correlations are developed from the dimensionless groups which can assist in evaluating the treatment of highly permeable  near-wellbore formations by suspension of gel particles under varying application conditions.

Fourth, the performance of several particle-gel systems is investigated for near-wellbore formation treatment to prevent or control water production in waterflooded mature oil fields. Effects of particulate concentration, leak-off, and threshold-pressure are investigated by the laboratory fluid loss tests conducted at constant pressure. Useful empirical correlations and charts for the fluid loss, pressure initiation for flow, and critical silica flour concentration are developed for practical applications which can assist in choosing suitable particle-gel systems for effective near-wellbore-formation treatment. A methodology using these correlations and charts is presented for design of optimal conformance control treatments for effective mitigation of water production in waterflooded mature oil fields.

Fifth, analysis and interpretation of experimental data of laboratory tests of several particle- gel systems and different application conditions are presented based on empirical correlations. The rate constant of filtrate and spurt loss volume are determined and correlated at different silica flour concentrations, sand sizes, and pore diameters of filter discs. Exponential relationship is used to correlate the experimental filtrate volume during  the leak off tests at different sand sizes, pore diameters of filter discs, and silica flour concentrations. The present empirical correlations can predict the evolving filtrate volume of particle-gel system under  varying conditions. The proposed empirical correlations can assist in effective design of particle-gel systems used for treatment of high-permeability near-wellbore formations for avoiding and mitigation of water production in waterflooded mature oil fields.

Sixth, treatment design for near-wellbore field application is demonstrated using the empirical correlations that developed by this study. Two synthetic field cases, involving the drilling of an oil well and producing from an oil well, are studied for treatment design. The treatment fluid properties and the conditioning and treatment of high permeability near-wellbore formation are determined.

# Chapter 1: Introduction

The high permeability zones of the  heterogeneous   petroleum reservoirs can cause many problems to the oil and gas industry such as lost circulation of drilling fluids and high water production in hydrocarbon producing wells. Injection of suspension of deformable gel particles and silica flour particle-gel systems as methods of near-wellbore formation treatment is considered in the present study. The goal of the present study is to determine the effects of various factors that participate in plugging of high permeability zones during the treatment and conditioning of high permeability porous formations by suspended gel particles and silica flour particle-gel systems and to develop empirical correlations, dimensionless correlations, and charts which can assist in choosing suitable conditions for effective near-wellbore formation treatment.

1.1  Near-Wellbore Formation Treatment

The lost circulation of drilling fluids during drilling operations and excessive water production in oil producing fields are undesirable problems because of high cost to the oil industry. These problems are caused by reservoir heterogeneity in high permeability zones with large and highly connective pores, open fractures, and worm holes. Therefore,  near-wellbore formation treatment by injection of suspensions of deformable gel particles and silica flour particle-gel system is explored as a method of preferentially plugging  the large  pores, thus  reducing  the  undesirable  high formation permeability and handling of reservoir permeability heterogeneity to prevent lost circulation of drilling fluids and control  water production in  mature waterflooded oil fields containing highly permeable zones. The gel particles suspension and silica flour particle-gel system are insensitive to lithology. Thus, these can be applied in sandstone, carbonate, and shale formations needing a near well-bore treatment.

Fig. 1.1 shows a schematic of the various zones and the gel particles suspension and silica flour particle-gel system applications in the near- wellbore formation. Study of the performance of gel particles during the injection into the porous media and the factors affecting the gel particles plugging mechanisms are important issues to consider for successful applications for this technology.

High Permeability Zone

High Permeability Zone

Fig. 1.1: Schematic of various zones and the gel particles suspension and silica

flour particle-gel system applications in the near- wellbore formation

Gel Particles Suspension or

Particle-Gel System

# 1.2  Objectives of the Study

The primary objectives of this study are several fold described as follows.

1.2.1 Experimental approaches

- Investigate the conditions leading to plugging of highly permeable formations by studying the permeability impairment of porous media during flow of a suspension of deformable gel particles and by studying the pressure required to initiate flow after the silica flour particle-gel process.

- Describe the relevant processes and mechanisms of pore plugging by gel particle suspensions and silica flour particle-gel system at different operation conditions.

- Describe the effect of the variation in gel particle and silica flour concentrations, flow rates, gel particle diameter, ratio of gel particle sizes-to-pore-throat diameter, pore space of the permeable filter disc, and sand sizes on the plugging conditions of the high-permeability formations.

- Determine the thermal effect on treatment of high permeability formations and the relevant processes and mechanisms of pore plugging by a suspension of deformable gel particles and silica flour particle-gel system.

- Evaluate the near well-bore treatment of high permeability formations by gel particles suspension using dimensional analysis.

1.2.2 Data analysis approaches

- Determine and describe the relevant dimensionless groups of gel particles application processes at different operation conditions and develop dimensionless    correlations    from    these   dimensionless   groups   for   the

- permeability reduction by gel particles injection and investigate the functional trends of these correlations to assist in scaling from laboratory to field conditions.

- Develop empirical correlations and charts from the experimental data of the gel particles process and silica flour particle-gel system for the suspended gel particle size distributions before and after flow, differential pressure build-up across porous media, permeability reduction of porous media, resistance factor against suspended flow, fluid loss, pressure required to initiate flow, and critical silica flour concentration.

- Investigate the permeability-impairment trapping mechanisms of gel particles by means of the diagnostic equations of Wojtanowicz et al. (1987).

- Apply a Vogel-Tammann-Fulcher (VTF) - type equation to develop empirical correlations for the viscosity, differential pressure build-up across porous media, permeability reduction of porous media, resistance factor against the suspended gel particles flow, fluid loss and pressure required to initiate flow of the silica flour particle-gel system from the experimental data involving the temperature effects.

- Correlate the thermal effects on the sequential plugging and unplugging events during the injection of gel particles suspension into porous media.

# 1.3  Description of Various Chapters

Chapter  2  presents  a  literature  review  of   the  experimental  studies  of   the

operation conditions involving the  particulate processes which lead to plugging in the pores of porous media. A literature review of the mathematical and numerical models of the particulate processes of porous formations is also presented.

Chapter 3 describes the factors affecting the near-wellbore formation treatment

by gel particles such as  gel particle deformation and break-up, gel particle coagulation and detachment, carrier fluid properties, suspension viscosity, gel particle diameter, suspension concentration, porous media, and operation conditions which can  affect  the  plugging of  pores and  thus the conditioning of the high permeability formations.

Chapter 4 presents the experimental studies undertaken to investigate the conditions favorable for plugging in highly permeable formations by gel particle suspensions and silica flour particle-gel systems. The experimental flow apparatus used at isothermal and thermal conditions, the experimental testing procedures, gel particle suspension preparation, silica flour particle-gel system preparation, and the measurements of viscosity, pore throat size, and particle gel size are described in this chapter.

Chapter 5 presents the conditioning and plugging of high permeability formations by suspension of deformable gel particles. The Effect of concentration, flow rate, gel-particle sizes of suspensions, and particle diameter to pore-throat size on the prevailing pore- plugging processes is inferred by flow tests conducted with 3800-md 16- to 20-mesh sandpacks. Prevailing particle-entrapment and –permeability impairment  mechanisms are identified under various conditions by means of specially formulated diagnostic equations and the results of data analysis for pore plugging are described. This reveals valuable insights and information about the functional trends of

sandpack plugging by gel-particle suspensions, which can help in successful design and mitigation of formation-plugging treatment in the field. Empirical correlations of the experimental data are developed which can assist in choosing suitable operation conditions for successful near-wellbore formation treatment.

Chapter 6 studied the thermal effects on near-wellbore formation treatment by suspension of gel particles. Gel particles treatment applications in reservoirs are subject to high temperature conditions significantly different than the above-mentioned laboratory test conditions and hence the characteristics of the in situ gel particles plugging mechanisms are affected by the prevailing temperature conditions, as demonstrated in the present studies. Consequently, an experimental study was undertaken to gain an understanding of the effect of temperature on the transient behavior of gel particles plugging in high permeability porous media for purposes of treating the reservoir heterogeneity to prevent the loss circulation and control  water production.

The permeability reduction and resistance factor are inferred by measurements of the pressure differentials with time across the proppant pack. Temperature effect is observed to be an important factor in suspended gel treatment of high permeability near-wellbore zones because temperature affects the gel properties and placement rate processes significantly. The effect of temperature on viscosity, differential pressure,  permeability reduction, and resistance factor are investigated and useful correlations are developed from the experimental data by using the Vogel-Tammann-Fulcher (VTF)-type equations. Mechanisms of plugging and unplugging phenomena are investigated during the near-wellbore formation treatment by gel particles. The rate constants of plugging and unplugging processes are determined at various temperatures and correlated by using the Vogel-Tammann-Fulcher (VTF)-type equations.

Chapter 7 presents the dimensionless analysis for interpretation of near-wellbore formation treatment by gel particles at different application conditions. Several dimensionless groups are developed from the relevant variables of sand packs, gel particles suspensions, and operation conditions. The dimensionless correlations are shown to assist in quantifying the effect of the particle-diameter to pore-throat size ratio on permeability reduction, evaluating the treatment of highly permeable and weak near well-bore formations by gel particles, and extrapolating from laboratory to field conditions. The present dimensionless correlations can predict the evolving permeability reduction under the varying conditions of gel particles suspension injection processes. The proposed dimensionless correlations can assist in effective design and mitigation of treatment of high-permeability near-wellbore formations by gel particles for avoiding drilling-fluids lost circulation.

Chapter 8 studied  the performance of silica flour particle-gel system for near-wellbore formation treatment. Effects of particle concentration,  leak off, and threshold pressure gradient on controlling water production in waterflooded mature oil fields are investigated. The filtrate volume is measured to determine the leak off under different treatment and formation conditions. Effects of particle concentration, pore space of the permeable filter disk, sand sizes and temperature on the leak off and the pressure required to initiate flow are measured by adding different amounts of silica flour to the gel systems and using permeable filter disks with different size pore spaces and sand of different sizes at different temperatures. The sand represents a gravel pack and the filter

disc represents the formation. The threshold pressure gradients which must be overcome

to initiate water flow after the fluid loss tests were determined in each case. The experimental results show that the filtrate loss decreases with increasing silica flour concentration and increases with increases in the pore size of the permeable filter disk, the sand mesh size, and temperature. The threshold pressure gradient increases with increase in the silica flour concentration and decreases with increase in the sand mesh size, with increase in the pore size of the permeable filter disk, and with increase in temperature. Correlations and charts for the fluid loss, the pressure required to initiate flow, and the critical silica flour concentration are developed for practical applications.

Chapter 9 presents filtration analysis of the leak off tests of the silica flour particle-gel system. Exponential relationship is used to correlate the filtrate time with the filtrate volume of the silica flour particle-gel system. Empirical correlations of the filtrate volume were developed at different sand sizes, pore diameters of filter discs, and silica flour concentrations. The empirical correlations can assist in successful design of silica flour particle-gel system used for near-wellbore formation treatment for mitigation of water production in waterflooded muture oil fields.

The filtrate volumes of the silica flour particle-gel system during the fluid loss tests are modeled and represented as straight line plots at different silica flour concentrations, pore diameters filter discs, and sand sizes. The rate constants of filtrate and the spurt loss volumes are determined from the straight line plots of relevant equations and correlated by using the exponential relationship at different sand sizes and pore diameters filter discs. The empirical correlations of the rate constant of filtrate and spurt loss volume can be used to predict the filtrate volume at any conditions.

Chapter 10 demonstrated the importance of the empirical correlations, which developed in this study, in the treatment design of the near-wellbore formation. Synthetic oil well under drilling operations, which have fluid loss problem, is studied. Gel-particles suspension is used to treat the near-wellbore formation and the developed empirical correlations are used to determine the gel-particle properties and the modification of the near-wellbore formation. Synthetic oil producing well is studied for high water cut problem. Silica flour particle-gel system is used to plug the perforation zone that produce high water. The components of the silica flour particle-gel system and the treatment design for the near-wellbore formation are presented using the developed empirical correlations.

Chapter 11 summarizes the accomplishments and conclusions of the present study.

# Chapter 2: Literature Review

This chapter is a review of the relevant literature on the experimental and theoretical studies which may be applicable for the present gel-particles treatment.

# 2.1   Review of Experimental Studies

Lost circulation of drilling fluids is an undesirable problem because it can increase the wellbore non-productive time (NPT) in drilling operations, especially in  highly permeable formations. The flow paths causing a fluid leak-off may be of the natural and induced types (Wang et al. 2008). Natural lost circulation occurs when drilling operations penetrate formations of large and highly connective pores, classified as highly permeable and high-coordination-number (high degree of pore connectivity) porous formations. Taking proper measures for drilling of wells of various types in such formations without losing a substantial amount of drilling fluid is of great concern. Injection of gel- particle suspensions into these formations can help avoid the lost circulation during a drilling operation by plugging large pores,  thus  reducing the undesirable high formation permeability.

Gruesbeck  and Collins (1982), Civan  and  Nguyen  (2005), and  Civan  and

Rasmussen (2005) have shown  that the pathways in porous media can be classified into

two  groups as  being the  plugging and  nonplugging  pathways, relative to  the  particle

size. Hence,  particle  retention  in plugging  pathways  can  occur  by  bridging  across

porethroats,   and    particle    retention   in    nonplugging    pathways    can   occur   by

deposition  over the  pore surface. The first  mechanism  leads to a severe  permeability

reduction, and the  latter  usually causes a negligible permeability reduction. Therefore,

particles   with   sizes   comparable  to   pore-throat   sizes   can  accomplish   effective

permeability impairment in  high-permeability  formations, as demonstrated  by Civan

(2000, 2007, 2010), Iscan and Civan (2006), and Iscan et al. (2009).

In many cases, lost circulation problems can be circumvented conveniently by using suitable lost circulation materials (LCM) as additives in drilling fluids, including certain types of granular and fibrous materials, calcined petroleum coke, calcium carbonate, and gelling polymers (Messenger 1981). Several researchers (Bai et al. 2007; Chaveteau et al. 2000, 2001, 2003; Coste et al. 2000; Feng et al. 2003) investigated the use of gel particles for plugging of pores for circumventing the problems associated with the high permeability of “thief zones” by conditioning and preparing such unfavorable formations for drilling operations.

Polymer-crosslinker mixtures, frequently referred to as gelants, are commonly applied in high-permeability reservoirs for controlling of the fluid-loss during drilling operations, improving the conformance, and reducing the water or gas channeling. Injection of gels into formations containing fractures or channels (high permeability) has been studied extensively (Fielding et al. 1994; Lane and Seright 2000; Sydansk and Southwell 2000; Wang et al. 2001). Mostly the preformed gels instead of in-situ formed gels are preferred to avoid the difficulties associated with controlling of the gelation time and gel compositions during gel placement in porous media. Seright (1997, 2000) studied the performance of gel behavior and placement in fractured formations and determined that preformed gel can penetrate deeper into a fracture than in-situ formed gel and  causes  much less gel damage in oil-bearing formations or matrix. Chaveteau et

al. (2000, 2001, and 2003) investigated the performance of preformed soft and size-controlled microgel particles which can crosslink by the shear effect which are insensitive to the physico-chemical conditions of reservoir formations. Preformed microgels were found to achieve an in-depth permeability treatment by adsorbing over the pore surface.

Coste et al. (2000) examined the effectiveness of the preformed gel particles (PPG) prepared by using 15wt% acrylamide monomer in a 400 mg/L crosslinker. They crushed and then sieved dry gels to obtain powdered gel particles which can swell several folds to their original size in water to form a suspension. Preformed gel particles effectively resist the high salinity and high temperature reservoir conditions. They conducted glass micro-models and core experiments using the PPG suspensions and observed the three distinct processes, namely deformation, shrinking, and breaking, which occur during a big PG particle passing through a pore throat. They demonstrated that weaker-strength gels penetrate deeper into porous media.

Bai et al. (2007) investigated the movement of the preformed particle gel (PPG) through porous media by visual micro-model experiments. They observed that the transport of PPG through porous media can occur in six different ways: direct pass and adsorption (for particle sizes smaller than the pore-throat size), deform and pass, snap-off and pass, shrink and pass, and entrap (for particle sizes greater than the pore-throat size). Three ways of the PPG motion through porous media were determined from the macroscopic scale (coreflooding) experiments: pass, break-into-pieces and pass, and plugging or jamming. The occurrence of these gel transport patterns depends on  the  pressure  change  over  time, injected  to produced suspension particle size ratio,

and residual resistance factor of porous formation. PG particle can move through porous media only when the driving pressure gradient exceeds the threshold pressure gradient (Prada et al. 2000) which in turn depends on the particle-to-pore throat size ratio (Civan 2000, Iscan and Civan 2006) and the particle strength.

Zhang and Bai (2010) studied the factors  affecting PPG injectivity and plugging

efficiency during  transport of PPG through  open fractures. They observed that the PPG

injection  pressure  increases with  injection  flow rates  and  decreases with  the fracture

width   and   the   resistance   factor   decreases   when   the   flow  rate   increases. They

correlated  the  injection   pressure   and   resistance   factor   vs.   flow   rate   by  use of

empirical power-law equations.

Zheng et al. (2012) developed a fuzzy ball working fluid with pocket air inside for plugging of fluid-losing channels in depleted reservoirs. The fuzzy ball working fluids of density 0.80, 0.85, 0.90, and 0.95 g/cm³  were prepared by mixing 100 mL of water with a predetermined weight of sodium carbonates, caustic soda, nucleating agent, film-forming agent, layering agent, and spotting agent. The rheological properties of the fuzzy ball working fluid at the room temperature and at HPHT were measured by using an adequate rheometer. The observed relationship between the shear-rate and shear-stress indicate a Bingham fluid. It is a plastic fluid having high yield points and plastic viscosity ratios. They determined that the fuzzy ball working fluid can be used for cuttings removal in the oil and gas wells as normal working fluid. They studied the microstructure of the fuzzy ball working fluid by using a microscope by enlarging 1000-2000 times which show a size of 15-150 µm and thickness  of  3-10  µm. The   density  of  the  fuzzy  ball   working   fluid  decreases  by

temperature and increases by pressure at constant  temperature  because  the  fuzzy  ball  contains  air. Their  plugging tests using static sand filling, static core, and dynamic core proved that the fuzzy ball working fluid can plug effectively the losing channels in the lost circulation formations.

Wang et al. (2012) examined pre-gelled particle (PPG) flow through single and double sand packs to determine the flow behavior in porous media, analyze the mechanism of profile control, and investigate the effect of the surface and plugging depositions on permeability reduction. Sand pack of 30 cm long and 2.5 cm diameter was filled with 20-mesh unconsolidated sand and the porosity and permeability were estimated at 0.32 and 6.53 µm², respectively. During the injection process, the pressure of the sand pack is recorded by a data acquisition system at four pressure taps located at the inlet,  the outlet, and the two locations in between them. The effluent sample is collected at a cylinder and tested by Malvern Mastersize 2000 to obtain the particle size distribution. The particle shape is approximately sphere and the particle expanded in volume because of the water swelling. PPG suspension of 20,000 parts per million (ppm) concentration is injected at 5 mL/min flow rate into the sand pack and the pressure at the four equally-spaced different points is recorded. They proved that there is a critical pressure below which the particles will deposit at the pore-throat and above which the particles can pass through the pore-throat without plugging. Double parallel sand packs with a permeability ratio 4:1 were used to study the fractional flow. They show that for the low permeability sand pack, the particles will accumulate at the inlet side of the pore throats and form new pores causing a small decrease in the permeability. For  the  high  permeability  sand pack, the PPG suspension initially flows

into the high permeability sand pack leading to a pressure increase because the occurring deposition causes deformation and pushing of the particle to move ahead and decreases the permeability and therefore the fractional flow. For the surface deposition experiments, they used particles of diameters smaller than the pore-throat size and show that for low injection concentration, the bridging pore-blocking did not occur and only the pore surface deposition happened. For the higher injection velocity, the amount of particle deposition at the surface decreased and particles concentration at the outlet increased, because the drag force causes mobilization of particles at the high injection velocity (Pu 2008; Zamani and Maini 2009). For the plugging deposition experiments, they used particles of diameter greater than the pore-throat size to cause particle deposition or plugging at the throat. They showed that the permeability variation happened by retention of the PPG because the deposition of particles on the surface causes a porosity decrease and hence permeability decrease, and the plugging deposition causes a decrease in the quantity of filtering channels which lead to permeability reduction.

Tran et al. (2010a) studied the formation damage caused by the suspended particles of the drilling fluid by using the Nuclear Magnetic Resonance (NMR) and X- ray (CT) methods. Water-based drilling fluid of suspended barite particles with different diameters and concentrations injected into Berea core samples saturated with 3% KCl brine and the permeability reduction was measured. The pore size distribution and the porosity of the core samples were measured before and after porous media damage by using the NMR technique and showed that the porosity reduced due to particle capturing  and  blocking  in  the  pores. By  the  injection  process, the  small pores were

blocked and the large interconnected pores provided the flowing path. Thus, when the capture probability decreased, then the porosity reduction decreased. The particle size distribution of the original and effluent fluids was measured by using the laser diffraction particle size distribution analysis (LDPSDA) technique and showed that the large particles were captured inside the pores while the small particles were remained in the flowing fluid. The X- ray computed tomography (CT) method was used to estimate the porosity of the core samples. Tran et al. proved that the particle capture probability and permeability reduction increase by increase in the particle size and concentration. They developed a model of fines migration and deposition in porous media from the empirical parameters determined from the injection processes.

Tran et al. (2010b) studied the conditions leading to plugging of natural fractures and slotted liners by suspended particles of different diameters and concentrations. The carrier fluid consisted from water and Diutan with concentration of 1.86% and viscosity of 65 cp to avoid particle settling. The suspended particles in the carrier fluid are the glass beads of 2.54 g/cm³ density and the ceramic proppant of 2.72 g/cm³ density. To study the plugging conditions, the Diutan particles suspension was injected into different slot geometries and the weight of the effluent during the injection process was measured. The experimental data were correlated by using the slot width-to-particle size ratio and the particle volume fraction Reynold number dimensionless groups. They developed exponential curve from the empirical dimensionless groups and the region below the curve is shown to represent the plugging conditions. They showed that the plugging conditions were affected essentially by the width and length of the fracture  opening, and  the  particle  size  and  concentration. They  studied also the time

required for plugging of fractures and slots at different particle concentrations and different shape factors, and developed empirical correlations of dimensionless plugging time versus particle volume fraction.

Feng et al.  (2013)  studied   experimentally   the   gel  particles  migration  and

deposition in porous media after polymer flooding. The shear breaking, synergy with remaining polymer, deformation migration, and swelling of gel particles were examined after polymer flooding. For swelling process of gel particles in water, the particle diameter was measured at different times by laser particle size analyzers which indicated that the aging time of gel particle swelling is very short. For synergy with remaining polymer, they demonstrated that the gel particle diameter increases by the polymer concentration because the gel particles adsorbed the remaining polymer in porous media. They proved that because of the shearing breaking of the gel particles when migration through porous media, the diameters of gel particles decrease quickly to ultimate value. To demonstrate the deformation and migration of gel particles in porous media, they studied the injection pressure during the gel particles injection process in cores. They  showed  that oscillation phenomenon happened because of the deformation

during the migration of the gel particles.

Muhammed et al. (2014) evaluated experimentally the strength of gel particles by using a simple apparatus which consists of a hand pump and a specially designed piston accumulator with screen plate having multiple holes. The threshold pressure gradient was determined during the experiments as the minimum pressure gradient required for the gel particles to pass through the screen holes. The same apparatus  was  also  used to measure the apparent viscosity. They showed that there is a

significant effect of the hole size and hole density per screen on the threshold pressure gradient but they do not effect the apparent viscosity. They observed that the threshold pressure  gradient increased when the brine salinity increased. The gel particles elastic modulus was measured using a rheometer and correlated with the threshold pressure gradient. Two models were developed based on the experimental data. First model represents the correlation of the threshold pressure gradient with the gel strength and the other represents the correlation of the apparent viscosity with the shear rate.

Almohsin et al. (2014) studied the effects of the nanogel particle concentration, flow rate, particle deformability, and rock permeability on the resistance factor and the particle propagation. Sandstone cores of permeabilities 42 to 1038 mD were used in the core flooding tests  of deformable nanoparticles of diameters 100 to 285 nm. The experimental results show that the resistance factor increased when the nanogel particles concentration increased and the resistance factor decreased when the rock permeability and flow velocity increased. For the same dry nanoparticles size, the resistance factor decreased when the swollen particles size increased because the larger particle is weaker than the smaller particle. They showed that the nanogel adsorption layer thickness increased when the nanoparticle concentration and decreased with the shear rate.

A summary of the findings by the above review and evaluation of the previous experimental studies is presented in Table 2-1.

- PPG concentration:        - Fracture length:        - The Injection pressure         - The resistance factor

0.903, 1.597, 2.731, and    55 cm.                         increased by the flow             is the ratio of the gel

2.961 %.                             - Fracture height:       rate and the brine conce-       particle injection

-Flow rates: 5,10, 15, 25   10 cm.                          ntration and decreased         pressure drop to the

, and 30 mL/min.               – Fracture width:        by the fracture width.          particle-free water

-Brine concentration:        0.55, 1.0, and 1.5        - The resistance factor             injection pressure

0.05, 0.25, 1, and 10%.    cm.                               increased by the fracture       drop.

width and the brine con-      - The PPG injectivity

centration and decreased      is the ratio of the flow

by the flow rate.                     rate to the pressure

-The PPG injectivity              difference.

increased by the flow rate

and the fracture width

and decreased by the

brine concentration.

Zheng et al. (2012)  - Density of the fuzzy         - Permeability of the   - The fuzzy ball working      -The fuzzy ball working

ball working fluid: 0.80,   sand packs are 15-       fluid can be used for           fluid composite from

0.85, 0.90, and 0.95          20, 40-60, and 140-     cuttings removal in the         water, sodium carbo-

g/cm³.                                300 µm² for 80-100,   oil and gas wells and can     nates, caustic soda,

- Size of the fuzzy ball is  40-60, and 20-40         plug effectively the losing   nucleating agent, film-

15-150 µm and thickness  mesh, respectively.       channels in the lost              forming agent, layering

is 3-10 µm.                        - Range of permea-     circulation formations.         agent, and spotting

- PH of the fuzzy ball          belities of the cores                                                   agent and the fuzzy ball

working fluid is 9.               are 2.36-244.2*10¯³                                                  contains air.

- Maximum injection           µm².

pressure of the sand

packs and the cores are

6 and 20 µPa, respecti-

vely.

Wang et al. (2012)    - PPG concentration is    -The sand pack          -Below the critical pressu-  - At high injection

20,000 ppm.                   length and diameter re particles deposit at po-    velocity, the drag

- Flow rate is 5 mL/min. are 30 and 2.5 cm,    re throat and above it pa-  forces caused mobil-

- The range of the injec-  respectively.              rticles deform and pass      ization of particles

tion pressure is 0.03-      -The permeability       through pore throat          which decreased the

0.23 µPa.                           and porosity of           causing permeability          particles deposition

- The range of the PPG    20 mesh sand pack    decreasing.                          at the surface.

diameter is 130-700       are 6.53 µm² and     -Pore surface deposition

µm.                                    0.32, respectively.    happened for particles

- Pore throat diameter    and for 80 mesh       smaller than pore throat

for 20 mesh sand pack    sand pack are 1.62   size and plugging deposi-

is 128.4 µm.                      µm² and 0.29, resp-  tion happened for particl-

-The injection velocities  ectively.                     es greater than pore thro-

range is 0.075-0.12                                              at size caused porosity an-

cm/s.                                                                      d permeability decreased.

d permeability decreased.

TABLE 2-1: SUMMARY OF THE EXPERIMENTAL STUDIES

Investigators                  Operation Conditions         Porous Media         Results and Analysis                    Comments

Zhang and Bai

(2010)

Investigators          Operation Conditions         Porous Media           Results and Analysis                Comments

Tran et al. (2010a)    - The core samples are   -Berea core samples   – The porosities of the       - External filter cake

saturated with 3% KCl.   of 6 in long and 1 in  core samples reduced fr-   observed because of

- Barite particles of          diameter are used.   om 0.209 to 0.176 and fr-  the pore-throat brid-

diameter range 0.5-15   - The permeabilities  om 0.175 to 0.169 after 5  ging mechanism.

µm are added to water- of the core samples  hrs flooding.                         - The pore deposition

based drilling muds.         are 1240 and 265    - For 5.4 µm mean diame-  and pore filling are

- The flow rate for per-   mD, the porosities    ter of particles injected,     the dominant mecha-

meability impairment    are 0.206 and 0.175 the large particles are         nisms.

experiments is 90 cm³/  , and the mean pore captured inside the pores

hr and for porosity va-   diameters are 26.1   while the smaller are flu-

riation experiments is     and 15.7 µm.             shed out.

36 cm³/hr.

Tran et al. (2010b)   - Geovis XT fluid of 1.86  - Transparent-plastic – No plug is observed for  - β΄ is a modified slot

% Diutan concentration  testing cell of 2 ft     β΄˃2 and the plug happe-    size-to-particle size

and 65 cp apparent vis-  long and 1.5 in ID.     ned for 0.795˂β΄˂2.           ratio.

cosity at ambient tem-   - For glass beads su- - No plug is observed up

perature 75 °F is used.    spended, slots of      to concentration of 0.25

- The suspended particl-  0.32 cm width and   by volume fraction and

es are glass beads of       different lengths of   the plug happened at

2.54 g/cm³ density and  0.64, 1.28, and 2.56   0.30 concentration.

0.10, 0.12, 0.15, 0.20,     are used.

and 0.25 cm diameters  - For ceramic propp-

and ceramic proppants  ant suspended, slots

of 2.72 g/cm³ density     of 0.16 cm width an-

and 20/40, 30/50, and   d different lengths

30/70 mesh.                     of 0.64, 1.28, and

2.58 cm are used.

Investigators           Operation Conditions         Porous Media              Results and Analysis        Comments

Feng et al. (2013)     - Bicarbonate-sodium      - Artificial quartz        - The agin time of gel pa-  - The oscillation phe-

type water of salinity      sandstone cores of     rticle swelling is about      nomenon of the pre-

2841.2 mg/L is used.         porosities 0.20, 0.21  4 hr.                                      ssure is happened

- Polymer of  16-19 mil-   , and 0.24, and per-   - The gel particle diame-    because of the defo-

lion molecular weight,     meabilities 1.037,       ter increases by the pol-   rmation migration of

20% hydrolyzing degree,  3.674, and 4.409        ymer concentration.         the gel particles.

and 1000 mg/L concen-    µm² are used.            - Because of the shearing

tration is used.                                                         braking, the gel particle

- Cationic gel particles                                            diameter decreases by

with 2000 mg/L conce-                                         about 27.3%.

nitration are used.              –The threshold pressure

- The median gel partic-     gradient is 16.7 µPa/m.

le diameter is 160 µm.

- The temperature is

45 °C.

- The injection pressure

is 2-10 µM.

Muhammed et al.     – Medium size of the dry  - Screen plates were     - The threshold pressure   - Threshold pressure

(2014)                        PPGs is 0.92 mm.            used as porous media    were 84.1 Kpa of 122       is the minimum

- Brine (NaCl) concentra- of  40 holes/plate and  holes/plate and 372.3 kPa  pressure required of

tion are (0.05, 0.1, 0.25,    and 122 holes/plate.     of 40 holes/plate for         the gel particle to

0.5, 1.0, and 5.0 wt%)       – The screen plates      PPGs swollen in water.     pass through hole.

- Flow rates are 0.1,0.2,    have hole sizes (0.5, 1 – The stabilized pressure

0.5, 0.75, 1.0, 1.5, 2.5, 3,  , 1.5, and 5.0 mm).       was 300 kPa for 0.5 mm

5.0, 7.5, and 10 ml/min.                                         hole and PPGs swollen in

5 wt% and decreased for

1.5 mm hole size.

- Threshold pressure

increased by salinity.

Investigators           Operation Conditions         Porous Media              Results and Analysis        Comments

Coste et al.         – PPG consists from 15%   - Glass plates with pore – Three mechanisms of   - The PPG particles

(2000)                acrylamide monomer and    network saturated with particles passing were      can be used for

400 mg/L crosslinker.           water were used.         investigated: deformation water control

- Concentration of the sus-  - Sand-packed columns , shrinking, and breaking. applications.

Pension was 1000 mg/L.    at residual oil saturation – Weaker-strength gels

- Flow rate was 2 ml/min.    with 30 cm long and     penetrate deeper into

2.2 cm diameter filled   porous media.

with sand of 40 to 120

mesh were used.

Bai et al. (2007) - PPG is a kind of xerogel   - Two etached glass      - PPG transport ways       – PPG particle moves

that can swell by water.      micromodels were used through micromodels are when the driving

- For sand-packed experim- : irregular and regular   : direct pass, adsorption,  pressure gradient is

ents, 1000 mg/L particle su- pore models.                 deform and pass, snap-    greater than the thre-

spension was injected at 1   - sand- packed core      off and pass, shrink and   shold pressure

cm³/hr flow rate and 3 MPa model of 30 cm long    pass, and entrap.              gradient.

pressure.                              and 2.2 diameter was    - PPG motion through

- 5 cm³ of PPG suspension   used.                             sand packed are: pass,

with a concentration of      - The sandpacked filled break and pass, and

0.1% was injected into the  with quartz sands of      plugging.

micromodels.                        20 to 100 meshes

- Average particle diameter size.

is 150 µm.

- Pore-throat diameters

varies from 90 µm to 250

µm.

Investigators           Operation Conditions         Porous Media              Results and Analysis        Comments

Wang et al.         – Concentration of PPG     - Sand pack of 30 cm    – There is a critical pres- - For high velocity,

(2012)                 suspension is 20,000 ppm.   long and 2.5 cm diam-   sure below which the     the drag force causes

- Injection flow rate is 5 ml eter filled with 20 mesh particles deposit at the     mobilization of the

/min.                                     sand was used with       pore-throat and above     deposited particles.

- Stable injection pressure    0.32 porosity and 6.53  which the particles pass

is 0.24 MPa.                          µm² permeability.        through the pore-through.

- Double parallel sand   - At high injection velo-

packs with permeability city, the particle depos-

ratio 4:1 were used to    ition decreases.

study the fractional flow

Almohsin et al.  – The nanogel was an acryl- Berea sandstone cores – The resistance factor     - The nanoparticles

(2014)                amide-based crosslinked      of 41.2 to 555.4 mD     increased by the particles adsorption layer thick-

polymer.                              permeability and Miss- concentration.                  ness decreased by the

- 1 wt% of potassium chlor- ouri sandstone cores     - The resistance factor     shear rate.

ide (KCl) was used to prep- of 1038 mD were used decreased by the rock

are the nanoparticle solut-   - The cores of 6.95 to  permeability and the flow

ions.                                     7.1 cm length and 2.5   velocity.

- Average particle diameter to 2.53 diameter.          – The resistance factor

was 158 µm.                                                             decreased with the swo-

- Injection flow rate is 0.25                                       llen particle size increas-

to 5 ml/min.                                                                ed.

- The injection pressure is

2379.21 psi at 1.75 ml/min

flow rate.

2.2  Review of Theoretical Studies

Zeinijahromi et al. (2012) derived the basic equations required for detachment and mobilization of fine particles by the drag and lifting forces applied on the particles during flow through porous media, and the size exclusion of the pores which causes formation permeability decrease and hence the well productivity decrease. They developed analytical models for steady-state well production, velocity, and particles suspension concentration near the wellbore. The reservoir fine particles production and accumulation cause a skin factor growth by time. The productivity index and the skin factor versus time are studied by the analytical model showing that the skin factor growth coefficient increases by the filtration coefficient. The analytical model assumes small retention concentration. Therefore, the model can be applied to predict the well behavior only at the early stage of the well clogging process and cannot be applied at the late stages of well clogging. The analytical modeling results show good agreement of matching with the field producing data.

Goldszten (2005) developed a mathematical model to predict the volume of suspension flowing through a small orifice until clogging occurs. The mathematical model describes the clogging and choking of a single pore throat present in a container as a circular hole on its wall and filled with a suspension of incompressible liquid and spherical particles. The mathematical model assumed that the liquid is incompressible, the particle velocity is same as the liquid velocity, uniform flow, and the particle is randomly placed in the container before opening the hole to allow flow. The mathematical model provides an understanding of pore throat clogging in porous media and efficient numerical algorithm for upper and lower bounds of the effluent volume.

Civan (2010) developed a practical phenomenological mathematical model which considered temperature variation and particle transport by dispersion and advection. The particle deposition and migration and the permeability impairment resulting from particle deposition and migration are investigated by this model. Effects of temperature and particle deposition on the permeability impairment of porous media are described by dimensionless numbers and special correlations of the relevant variables. The permeability impairment is affected strongly by temperature variation because the filter coefficient, pore-throat constriction, and porous matrix thermal deformation depends on temperature. The numerical simulation results obtained with and without considering the dispersion and temperature effects are compared to show the effect of temperature and dispersion on the fines deposition and migration, and the resulting permeability impairment. This improved model can assist in scientifically guided experimentation, analysis, and design of fines particles transport process through porous media.

Sato et al. (2013) numerically studied the effect of the trapping fines particles on formation permeability by using a three-dimensional (3D) Lattice Boltzmann method (LBM). They showed that the absolute permeability of porous media is reduced by 60-90% due to fine particles trapping for the volume fraction of the fine particles to the pore volume of 0.15-0.29. However, the permeability reduction is not only due to fine particle saturation but also the fine particle size distribution. The geometrical properties of sand grains are digitally described by series expansion of spherical harmonics using computed tomography (CT) scans of real sand grains. The migrating fine particles are assumed spherical and the volume distributions are log-normal. The permeability alteration is modeled theoretically using volume saturations and specific surface areas of the fine particles and the frame sands.

Tran et al. (2009) analyzed their experimental data and developed empirical correlations for perforation and pore plugging conditions and plugging time by suspended particles which can be help in avoiding the perforation/pore plugging in the field by migrating particles. The pore throat-to-particle size ratio was correlated satisfactorily against the particle volume fraction Reynolds number depending on the experimental data and using an exponential-law model. They showed that the exponential-law model worked well for the suspension of nylon particles of diameters range of 0.16-0.48 cm and of different particles size distributions and for the Carbo proppant suspension particles in Geovis XT fluid. They developed exponential curves, below which indicates the conditions leading to plugging and above which shows the conditions leading to non-plugging. Therefore, to avoid the plugging of the pores or the perforations, the value of perforation diameter to particle diameter ratio versus particle volume fraction Reynolds number should be located above the correlated curves. They correlated also the time for perforation and pore throat plugging by using exponential model of the particle volume fraction and demonstrated that higher the volume fraction of particles in the suspension, shorter the plugging time. They studied the effect of the particle size distribution on the plugging time and showed that the fines particles did not affect the plugging time but after plugging the fine particles deposited at the pore throats to form a bridge and worked as a membrane.

Feng et al. (2013) developed a numerical model to interpret their experimental data  which  demonstrates  the gel particles transportation after polymer flooding causes

permeability reduction in thief zones by retention of particles and pore volume reduction. The flow equations are solved implicitly to obtain the pressure and the saturation profiles and solved explicitly to obtain the concentration of the polymer by using the IMPSAT finite-difference numerical method because of its high accuracy. To weaken numerical dispersion, the convection-diffusion differential equation of polymer transport is solved by using the fourth-order Runge-Kutta method. The operator-splitting method is used to solve the continuity equation of gel particles. The new numerical method is validated by the experimental and field data and show satisfactory results.

The findings of the above review and evaluation of the theoretical studies are summarized in Tabe 2-2.

TABLE 2-2: SUMMARY OF THE THEORETICAL STUDIES

Investigators                                             Equations                                                                    Comments

- Assume small retention concentration.

- Can be applied at the early stages of

well clogging.

- Can not be applied at the late stages of

well clogging.

- Results show good matching with the

field production data.

Zeinijahromi et al(2012)   -

- Assume incompressible liquid, particle

velocity equal to liquid velocity, and

uniform flow.

- Clogging occurs when k(v)˃kmax.

- k(v) is the number of particles arriving

almost simultaneously at the opening.

-                                 -                               -

Goldsztein (2005)           -

-

- The model considers temperature variation

and particle transport by dispersion and

advection.

- The model shows that the permeability

is affected strongly by the temperature

variation because the porous matrix

thermal deformation, the filter coefficient,

and the pore-throat construction depend

on temperature.

Investigators                                             Equations                                                                    Comments

Civan (2010)                 -

-

- The effect of the trapping fines particles

on the formation damage is numerically

studied by using a 3D LBM simulation.

- The domain edges are approximately

300 µm length, each edge discretises into

60 lattice nodes.

Sato et al. (2013)             -

-

- To avoid plugging, the value of perforat-

ion diameter (β) versus Rep should be

above the correlated curve.

- Showed that the fines particles did not

affect the plugging time but after plugging

deposited and worked as a membrance.

Tran et al. (2009)              -

-

-

- The IMPES method is used to solve the

flow equations.

- The convection diffusion differential equ-

ation of polymer is descreted by using

fourth rank Ruge-Kutta method.

Feng et at. (2013)

-

-

where U is the flow velocity, m/s; k is the absolute permeability, md; Krowi  is the oil relative permeability at initial water saturation, md; P is the differential pressure, kPa; q is the injection flow rate, cm3/h; µ is the viscosity, Pa.s; βa is the formation damage coefficient  for  attachment, dimensionless;   a  is the volumetric concentration of attached fines, %;  βs is the formation  damage coefficient  for  straining, dimensionless;

s  is the volumetric concentration of strained fines, %;  r is the radius, µm; t is the time, min; λs is the filtration coefficient for size exclusion fines capture, m-1; cw is produced fines concentration, %; rw is the well radius, m; pi is the productivity index, dimensionless; j is the impedance, dimensionless; re is the drainage radius, m; rw is well radius, m; M = skin growth coefficient, dimensionless; Ct  = total amount of produced fines per unit well length, m2; λ is the ratio of volume of dashed cylinder and volume of a particle, dimensionless; A is the cross sectional  area of the sand pack, cm2;  kmax  is threshold number of particles for the first time, dimensionless; γ is the empirical material parameter, dimensionless; Ko is initial permeability, md; T is the temperature, °C; Tik is the reference absolute temperature, K; Ak is the fitting constant (E/Rg), K; Tck is the characteristic-limit absolute temperature, K; K is the permeability, md,  Ø  is the porosity, dimensionless; β is the empirical parameter, dimensionless; Pq is the position vector for a fine particle, µm; Pf  is the position vector for a frame sand grain, µm; df  is the diameter of a frame sand grain, µm; dq is the diameter of a fine particle, µm; x is the ratio of the distance, dimensionless; uq  is the particle velocity before the collision, m/s; β is the pore throat to- particle diameter ratio, dimensionless; A is the empirical parameter, dimensionless; B is the empirical parameter, dimensionless; Rep is the particle  Reynolds  number, dimensionless; C is the empirical parameter, dimensionless;

td is the dimensionless plugging time, dimensionless; a is the empirical parameter, dimensionless; b is the empirical parameter, dimensionless;    p is the fraction of particle, %; ν  is the velocity , cm/s; DT is the pore throat diameter, µm; DP is the particle diameter, µm; νw  is the water flow velocity, m/s; cgp is the gel particles mass concentration, mg/L; qw is the water flow rate, cm3/h;         is the retention coefficient of gel particles, dimensionless; Øo  is the initial porosity, dimensionless; Sw is the water saturation, %; SHRgp is the gel particle shear breaking ratio, dimensionless; SWRgp is the gel particle swelling ratio in polymer solution, dimensionless.

# Chapter 3: Factors Affecting the Near-Wellbore Formation Treatment by Gel Particles

Part of  this  chapter  has  been   previously  published   as  ‘‘Experimental  Study of Gel

Particles    Transport    Through   Porous   Media’’ in   the   SPE   Latin  American    and

Caribbean   Petroleum   Engineering    Conference,  Mexico  City, Mexico, 16-18  April,

2012 and is used here by permission.

Part  of  this  chapter   has   been  previously  published as ‘‘Experimental   Investigation

and   Correlation   of   Treatment  in   Weak   and   High- Permeability   Formations   by

Gel   Particles’’ in Production    and    Operations    Journal, Vol. 28, No. 4, pp. 387-401,

2013 and is used here by permission.

3.1   Introduction

Understanding the plugging mechanisms and the transport behavior of the gel particles through the porous media during the gel particles suspension injection is very important for successful near-wellbore formation treatment by the gel particle suspension. Two plugging mechanisms were investigated and illustrated in details in this study. These two mechanisms are the deposition of the gel particles on the pore-surface and the capture of the particles at the pore-throat.

There are many factors that affect the plugging mechanisms and the transport behavior of the gel particles including gel particle properties, carrier fluid properties, gel particle suspension properties, porous media, and operation conditions. These factors are described and investigated in details in this chapter and this study.

3.2  Gel Particle Properties

There  are only a  limited amount of  studies about the gel particles properties,

as discussed  in the following.

3.2.1 Gel particle deformation and break-up

Because of its deformable nature, the gel particle can deform  and pass through the pore-throat to deposit on the pore-surface, break-into pieces and pass through the pore-throat  to deposit on the pore-surface, or be captured at the pore-throat

during injection into porous media (Bai et al. 2007). Fig. 3.1 illustrates the difference between the rigid and deformable particles passing through a pore throat. The rigid particles cannot pass through the pore throat if their size is greater than the pore- throat size, but the deformable particles can deform and pass through at sizes greater than the pore-throat size.

(b)

(a)

(b) deformable particles

(a) rigid particles

Fig. 3.1: Difference between rigid and deformable particles passing through pore

throat:

Bonet and Wood (2008) describe the motion and the deformation of a particle, as shown in Fig. 3.2. The general measure of deformation is the measure of the strain and the strain is the change in the initial elemental vectors dX1 and dX2 after they

deform to dx1 and dx2.  Then, the deformation gradient tensor is given by:

or	                                                                     (3.1)

Fig. 3.2: General motion and deformation of a particle (modified after Bonet and

Wood 2008)

Gao et al. 2011 describe the deformation of an ellipsoidal elastic particle in a Newtonian viscous fluid in quantitative terms as follows:

(3.2)

where a and b refer to the semi-axes of the ellipsoidal particle, w= b/a and G is the ratio of the viscous forces in the fluid to the elastic forces in the elastic solid particle.

(3.3)

where  µf  is the fluid viscosity, ηs  is the shear modulus of the elastic solid particle.

(3.4)

where   τs is the extra stress tensor,                       is the Finger or left Cauchy-Green tensor,     is the shear rate or the velocity gradient.

(3.5)

v is the fluid velocity and d is the distance to the reference surface. As G increases, the D increases, therefore larger elastic deformation of the particle happens at the larger number of G and the elliptical particle become thread-like. Taylor (1932, 1934) studied the break-up of droplets and showed  that a droplet can be break-up when the D value is larger than 0.5.

3.2.2   Gel particle coagulation and detachment

The gel particles can stick together to coagulate and form larger aggregates without involving chemical reaction between the particles. The gel particles stickiness (coagulation) was not investigated sufficiently before, but Burya et al. (2001) studied the asphaltene particles stickiness and aggregation in crude oil.  The asphaltene particles can stick together with a chemical reaction between them. Burya et al. (2001) showed that the aggregation kinetics of asphaltene particles consist from the diffusion-limited aggregation (DLA) and reaction-limited aggregation (RLA) mechanisms with a crossover behavior between them given by:

(3.6)

where N is the average number of particles forming fractal aggregation, dimensionless, given by:

(3.7)

Ro and R are initial particle radius and the instantaneous mean aggregate radius, respectively, µm; df  is the fractal dimension, dimensionless, γ is a constant, dimensionless, given by:

(3.8)

τD  and τR represent the characteristics times τchar for the DLA and RLA mechanisms, respectively, dimensionless. Burya et al. (2001) used the analytical solution of Eq. 3.6 to correlate the experimental data of the mean number of asphaltene particle in an aggregate and mean radius of the asphaltene aggregates with the scaled time and obtained a satisfactory matching.

Engel (2000) defined the efficiency of stickiness (coagulation) (α) between two particles as the probability that two particles which collide can stick together with a value ranging from 0 to 1. Thus, the stickiness(α) is defined as the ration of the adhesion rate/collision rate. Kiorboe et al.  (1990)   determined   the  stickiness and aggregates of  diatom blooms experimentally  by  use  of   Couette Chamber system and the following empirical correlation:

Ct = C0 exp–(7.82 α Φ Gm/π)t                                                       (3.9)

where Ct and C0 are the particle concentration at times t and 0, respectively, (no. dm-3), Φ is the volume concentration of particles (ppm), and Gm is the mean shear rate of the Coutte Chamber system (s-1) which can be calculated by using the following equation (van Duuren 1968):

Gm = 4 πω r2 r1 (r22 – r12)–1                                               (3.10)

where ω is the angular velocity (s-1), and r2 and r1 are the radii of the outer and the inner cylinders of this system, respectively (cm). Engel (2000) used the Coutte Chamber to determine the variation in the particle stickiness according to the decline of a diatom bloom at low shear rate (G = 0.86 s-1). Engel investigated that the apparent particle stickiness (α) increases with the transparent exopolymer particles (TEP) and can exceed a value of 1, which means the collision rate is underestimated because the stickiness parameter (α) is calculated based on the conventional particle counting only.

The critical shear stress is the minimum shear stress required to detach and lift-off the deposited particles at the pore surface. Civan (1990, 1996) proposed an  empirical equation of the critical shear stress (τcr) as a power-law function of the particle stickiness to the surface according to the particle concentration at pore surface by:

τcr = krCpα                                                                                       (3.11)

where α is an empirical constant, kr is a constant and Cp is the particle mass concentration. Potanin and Uriev (1991) developed theoretical equation to calculate the critical shear stress required for detachment of particles.

τcr = H/24Dpl2                                                                                   (3.12)

where H is the Hamaker coefficient of particle and surface interacting through the pore fluid present in between them, J; Dp is the average particle diameter, cm; and l is the separation distance between the particle surfaces in filter cake.

The  plugging  probability of  the pores  increases by the gel particles stickiness

(coagulation) on the pore-surface and pore-throat. Thus, the efficiency of the near-wellbore formation treatments by the gel particles increases by the gel particles stickiness (coagulation) and decreases by the detachment of the deposited particles at the pore-surface.

3.3 Carrier Fluid Properties

The main functions of the carrier fluid are to suspend and carry the gel particles and prevent the particles from settling. The carrier fluid consists from water and Xanthan and the important properties of the carrier fluid are the viscosity and the density. In the present study, for example, 0.25 gm of Xanthan powder was mixed with 500 ml of water to get the proper viscosity and density that prevent the settling of gel particles.

3.4 Gel Particle Suspension Properties

The gel particle suspension is used for the near-wellbore formation treatment. In the present study, the gel particle suspension was prepared by mixing a predetermined weight of polyacralamide gel, consisting of acrylamide (< 0.2%), sodium azide (0.02%) and water (balance), with carrier fluid using a commercial blender to obtain the desired concentration of the suspension and the desired gel-particles size. The gel-particle suspension was colored with red by using a liquid color for clear visual observation of the progress of the suspension through the proppant pack. The properties of importance for using the suspension for treatment are the following.

3.4.1 Viscosity

There is a direct relationship between the suspension viscosity and the gel particle deformation. The ratio of the viscous forces in the fluid to the elastic forces in the elastic solid particle increases by the suspension viscosity, as shown in eq. 3.3, and thus the deformation of the gel particle increases, as shown in eq. 3.2. The gel particle suspension viscosities were measured at ambient temperature 23.5°C with a Chann 35 viscometer at shear rate of 511 s -¹. The suspension rheology was studied by using six speeds of viscometer to obtain the shear-rate/shear-stress graphs. These graphs demonstrate  the  pseudoplastic  characteristics of the  gel-particle  suspensions. Fig. 3.3

shows the shear-rate/shear-stress graph of a 3-vol% suspension.

Fig. 3.3: Pseudoplastic behavior of 3 vol% suspension at T= 23.5 °C (exponent n =

0.38)

3.4.2 Gel particle diameter

There is a direct relationship between the plugging of pore throats or capture of gel particles in porous media and the ratio of particle/pore-throat size because plugging occurs when gel particles block the pore throats (Civan 2000, 2007a, and 2010; Iscan and Civan, 2006). Measurement and understanding of the gel-particle size distribution are important in investigation of the mechanism of plugging of porous media by gel particles. The gel particles are irregular shaped and deformable. Thus, the equivalent diameter of a gel particle was calculated by considering the projected area of an irregular particle in two dimensions. This is equal to the projected area of the circular particle with an equivalent diameter (Bai et al. 2007). An optical procedure was used to measure the gel particle size because of the unavailability of an instrument that can be used to measure the gel particle size distribution like Mastersizer instrument and Elzone analyzer. However, there is no accurate method available for measurement of the actual particle size distribution in a suspension. The optical procedure was applied using a suspension placed under a microscope and digitally photographed by a camera. The dimensions of the irregular gel particles in the photomicrographs were measured in pixels and then converted from pixels to micrometers using a calibration scale. Then, the projected area of a plane of the irregular particle was calculated and converted to the equivalent diameter of a circular particle, and then the following equation was applied (Bai et al. 2007).

(3.13)

Dp indicates the equivalent diameter of a circular particle, S is the projected area of a plane of the irregular particle. The gel particles were grouped into chosen ranges according to their diameter values. A particle-size frequency distribution was obtained similar to a normal-size distribution, which represents approximately the gel particle size distribution in the suspension.

3.4.3 Suspension concentration

The concentration of the gel particle in the carrier fluid effects the near-wellbore formation treatment significantly. The permeability reduction increases when the suspension concentration increases because the tendency of plugging increases with the particle concentration and the suspension viscosity increases when the gel particle concentration increases. Properties of the suspensions used in this study are presented in Table 3-1.

TABLE 3-1: COMPONENTS AND PROPERTIES OF THE GEL-PARTICLE

SUSPENSIONS

Constituent and                 Suspension      Suspension        Suspension        Suspension

Properties                            1                        2                        3                         4

Polymer (vol%, g)              0.5%, 2.63          1%, 5.25           2%, 10.50       3%, 15.75

Water (cm³)                             500                    500                    500                   500

Xanthan powder (g)                0.25                   0.25                   0.25                  0.25

Particles size range (µm)      14- 350              14- 350              14- 350            14- 350

Viscosity at 511 s ̄¹ (Pa.s)      0.0035               0.0040               0.0045              0.0055

3.5 Porous Media

The pore-throat size is an important parameter of porous media that effect the near-wellbore formation treatment by gel particles. The permeability reduction increases when the pore-throat size decreases. For the same gel particle diameter, the particle diameter to pore-throat size ratio increases when the pore-throat size decreases and thus the tendency of the pore-throat plugging increases.

The pore-throat size distribution in a core sample is measured typically using the mercury injection capillary pressure method. In this method, the dry core sample is subjected to vacuum and then helium gas is injected at high pressure to indicate even the smaller pore throats that open up at high pressures to obtain the distribution of pore-throat sizes of the core. The core sample used is an unconsolidated proppant pack and the core holder is a cylindrical plastic holder. Therefore, the mercury injection capillary pressure method could not be applied. Instead, the pore throat size had to be estimated by considering a circular pore throat model of porous media according to Peifeng et al. (2010). Db indicates the cell body diameter, expressed by:

(3.14)

DT  indicates the pore-throat diameter, given by:

(3.15)

where     is the porosity and Dg is the mean grain diameter of the sieved sample pack.

3.6  Operation Conditions

The important parameters of the operation conditions that effect the near-wellbore treatment by gel particles are described in the following.

3.6.l  Flow rate

According to the definition of the particle deformation, the shear rate is an important parameter that can affect the gel particle deformation. The ratio of the viscous forces in the fluid to the elastic forces in the elastic solid particle increases by the shear rate, as shown in eq. 3.3. Thus the deformation of the gel particle increases, as shown in eq. 3.2. The shear rate increases by the flow rate, as shown in eq. 3.5 and thus the deformation and break-up increases by the flow rate. When the gel particles deformation  and  break-up  increase, the  transport of the gel particles through the pore-

throat increases and they are not captured at the pore-throat. Thus, the permeability reduction of the high permeability formation decreases at the high  deformation and break-up of the gel particles. Baghdikian et al. (1989) determined  that the particles deposition  over the pore   surface  decreases  when  the  flow  rate  increases and the    hydrodynamic   lift   force increases by the flow rate and thus the plugging decreases.

3.6.2  Temperature

There  are  two  effects  of   temperature  on  the   near-wellbore   formation

treatment  by gel  particle suspension. First, the viscosity of the suspension decreases when the temperature  increases. The viscosity of the 3 vol% gel particle suspension decreases  from  0.0055 Pa.s to 0.0035 Pa.s by  increasing the  temperature from 23.5 °C

to 75 °C, as shown  in  Fig. 3.4. Second, the  gel   particles  are   soft  and  more deformable  particles  and increased  temperature  makes  them softer and  deformable. These two effects make the gel  particles  less effective because they can  pass easily  through porous media without causing pore-throat  plugging and pore-surface deposition. Therefore, plugging of pores by gel  particles  becomes  less  pronounced at high temperatures, as shown in Fig. 3.5.

Fig. 3.4: Viscosity of the 3 vol% gel particle suspension with temperature

Fig. 3.5: Effect of temperature on gel particles passing through pore

(a) at low temperature         (b) at high temperature

# Chapter 4: Experimental Studies of Near-Wellbore Formation Treatment

part  of  this  chapter  has  been  previously  published  as  ‘‘Experimental  Study  of Gel

Particles   Transport   Through   Porous   Media’’ in   the   SPE    Latin   American   and

Caribbean   Petroleum   Engineering    Conference,  Mexico  City, Mexico, 16-18  April,

2012 and is used here by permission.

part of  this  chapter  has been previously published as ‘‘Experimental  Investigation and

Correlation  of   Treatment   in   Weak   and  High- Permeability   Formations    by   Gel

Particles’’ in Production    and    Operations    Journal, Vol. 28, No. 4, pp. 387-401, 2013

and is used here by permission.

4.1   Introduction

The following experimental studies were undertaken to investigate the transient behavior of gel particles and silica flour particles during plugging of porous media and the effect of the variation in gel particle and silica flour concentrations, flow rates, ratio of gel particle sizes-to-pore-throat diameter, pore space of the permeable filter disc, sand sizes, and temperatures on the plugging conditions of the high-permeability formations. This is inferred by monitoring the variation of the differential pressure across the proppant pack, the effluent particle size distributions during experiments by flowing deformable gel particles, the filtrate loss and the pressure gradient required to initiate flow across the fluid loss cell. Thus, the conditions for inducing pore plugging by injecting gel particle suspensions and silica flour particle-gel systems into porous media were investigated.

4.2  Experimental Systems and Procedure

4.2.1 Experimental flow apparatus

The experimental studies utilized two separate experimental apparatus as described in the following.

4.2.1.1  Apparatus for gel particle suspensions processes

The schematic experimental flow apparatus (Fig. 4.1); the experimental testing

procedure; suspension preparation; and the measurements of viscosity, pore throat size, and gel particle size are described in the following.

A- Tests under isothermal conditions

A Ruska pump was used to flow the gel particle suspension from the accumulator into the proppant pack at a constant rate by the mineral oil. The pump flow rate varies from 5 to 1120 cm³/hr and the pressure ranges from 0 to 10000 psig. A 500 cm³ stainless steel accumulator was filled with the particles suspension and contains a steel piston disk to separate the suspension from the mineral oil. An 18.4 cm long and 2.5 cm diameter plastic cylindrical column was used to simulate a core sample . For our study, the sandpack should have sufficiently  large and highly connective pores so that we can investigate the conditions for plugging of these pores and reduce the high permeability. Therefore, the ceramic proppant is more suitable than natural sand to create sufficiently large pores and high permeability required in this work. Thus, the plastic column was filled with 16-20 mesh proppant sands.  A 30 mesh sieve was used at the inlet and outlet ends of the sand pack to contain the proppant inside the plastic column. Absolute permeability and porosity were measured as 3800 md and 38%, respectively. The properties of the proppant pack are given in Table 4-1. Smart Differential   Pressure  Transmitter  ST3000  Series was used to measure the differential

pressure across the sandpack during the tests. A NI SC 2345 Data Acquisition System was used to record the differential pressure during the tests by the Labview software version 7.

The gel-particle suspension was injected at a constant rate at the bottom of the proppant pack at the ambient laboratory temperature of 23.5 °C using the Ruska pump as a piston-like front from the accumulator and the differential pressure across the sandpack was measured during the experiments by the pressure transducer and recorded by a computer- assisted data-acquisition system. The flow was continued until attaining a constant differential pressure across the proppant pack. The effluent gel particle suspension was collected in a beaker at various times to determine the gel-particles size distribution. The proppant was removed from the plastic cylindrical holder after each run and then washed and dried for reuse again in the next test.

Fig. 4.1: Schematic diagram of the experimental  apparatus

TABLE 4-1: PROPERTIES OF THE PROPPANT PACK

Properties                                                                    Data

Porosity (%)                                                                  38

Absolute permeability (md)                                         3800

Grain density (g/cm³)                                                    3.3

Average pore throat diameter (µm)                              127

Mesh size                                                                   16 – 20

B- Tests under thermal conditions

A glass-made water bath is added to the experimental apparatus as shown in Fig. 4.2 for purposes of studying the temperature effect on gel particles placement in porous media as described briefly in the following.

The experimental flow apparatus consists of the following major parts: (1) A Ruska pump used to inject the gel particles suspension into the proppant pack at a constant rate using a mineral oil, (2) A 500 cm³ stainless steel accumulator filled with the gel particles suspension, (3) Plastic cylindrical column of 18.4 cm long and 2.5 cm internal diameter filled with 16-20 mesh proppant sands to represent a core sample, the absolute permeability and the porosity of which are 3800 md and 38%, respectively, (4) Smart Differential Pressure Transmitter of ST3000 Series used to measure the differential pressure during the tests, (5) A NI SC 2345 Data Acquisition System equipped with Labview software version 7 used to record the differential pressure during the tests, and (6) Immersion Coiled Heater with Thermostatic Temperature Controller  having  a  sensitivity of ±2°F (±1°C) placed at  the bottom of the glass water

vessel used to maintain the proppant pack at the required experiment temperatures, and Pocket-Size K Thermometer of temperature operating range -50 to 750 ˚C using to register the water bath temperature, as shown in Fig. 4.3.

A 3 vol% concentration gel particle suspension at different temperatures of 23.5 °C, 40 ˚C, 60 ˚C, and 75 ˚C was injected into the proppant pack at a 100 cm³/hr flow rate from an accumulator by using the Ruska pump. The pressure transducer was used to measure the differential pressure across the proppant pack during the experiments  by using a computer- assisted  data acquisition  system and the experiment

continued until attaining a final constant differential pressure. Suspension viscosities were measured at different temperatures of 23.5 °C, 40 ˚C, 60 ˚C and 75 ˚C by using a Chann 35 viscometer at shear rate of 511 s-1.

Fig. 4.2: Schematic diagram of the experimental apparatus with heating system

Thermometer

Coiled Heater

Glass Water Vessel

Temperature Controller

Fig. 4.3: Heating system of the experimental apparatus

4.2.1.2  Apparatus for silica flour particle-gel processes

The following describes the filtrate test apparatus (Fig. 4.4), the experimental procedure, and the particle-gel system preparation.

- Tests under isothermal conditions

A nitrogen tank was used to apply pressure to the particle-gel system in the fluid loss cell at a 3447 kPa pressure. A fluid loss cell with a filter disc at the bottom of the cell and 1-in. column of sand on the filter disc was filled with the particle-gel system. The average pore diameter of the filter discs were 5, 10, and 35 micron, and the sand sizes were 12/20, 20/40, and 40/70 mesh. A graduated glass cylinder was used to measure the filtrate volume during the test.

The particle-gel system was filtered from the fluid loss cell at 3447 kPa pressure using a  nitrogen  tank  and gas pressure  regulator at an ambient temperature of 23.5°C,

and the filtrate volume was measured during the test using a graduated glass cylinder. The filtrate test was continued until no gel was filtered or after a 30-minute period of time had elapsed. The remaining particle-gel system was removed from the fluid loss cell and replaced with water to measure the pressure to initiate flow. To measure the value of the pressure to initiate water flow, pressure was applied on the fluid loss cell using the nitrogen tank and the pressure was increased gradually using a gas pressure regulator until the first drop was filtered from the fluid loss cell. The pressure that caused the first filtrate drop was the value of the pressure to initiate water flow.

The particle-gel system was prepared mixing potassium chloride (KCl) with water using a commercial blender and Polymer 1 was added slowly to the water; mixing continued until the polymer was completely hydrated and no lumps or ҅ fish eyes ҆ were present (a minimum of 30-minute mixing time). Polymer 2 was added to the solution and mixed using the blender until homogeneous, and crosslinker was then added to the solution and mixed until homogeneous. Silica flour was added slowly to the solution at the desired concentration and mixed until homogeneous. Components of the particle-gel system are presented in Table 4-2.

Fig. 4.4- Schematic of the filtrate test apparatus.

TABLE 4-2:COMPONENTS  OF THE PARTICLE-GEL SYSTEMS

Constituent                     System 1      System 2       System 3      System 4

Water (gm)                               78.7             78.7               78.7             78.7

KCl (gm)                                    9.3               9.3                 9.3               9.3

Polymer1 (gm)                            0.4               0.4                0.4               0.4

Polymer2 (gm)                          46.7             46.7              46.7             46.7

Crosslinker (gm)                         8                  8                   8                  8

Silica flour (wt%)                     0.56             1.40               2.80             4.20

- Tests under thermal conditions

Temperature affects the fluid loss of the silica flour particle-gel system and the  pressure  initiate  and  thus  the  thermal  effects  is  an  important factor in the near-

wellbore formation treatment by particle-gel system. To study the temperature effect, a heating system was added to the experimental system. The heating system consists from heating tape, temperature controller and thermometer, as shown in Fig. 4.5.

Thermometer

Heating Tape

Temperature Controller

Fig. 4.5: Heating system of the filtrate test apparatus

# Chapter 5: Investigation of Treatment in High-Permeability       Formations by Gel Particles Suspension

This  chapter  have  been  previously  published as ‘‘Experimental Study of Gel Particles

Transport  Through   Porous    Media’’ in   the   SPE   Latin   American   and   Caribbean

Petroleum Engineering  Conference,  Mexico  City, Mexico, 16-18 April, 2012 and is used here by permission.

This  chapter  has   been   previously   published  as  ‘‘Experimental   Investigation   and

Correlation  of   Treatment   in   Weak   and   High- Permeability   Formations   by   Gel

Particles’’ in Production    and    Operations    Journal, Vol. 28, No. 4, pp. 387-401, 2013

and is used here by permission.

5.1   Introduction

This study investigates the behavior and transport of particle gels through porous media and the conditions favorable for plugging of highly permeable formations and develops useful empirical correlations from the experimental data to assist in controlling of such conditions. These correlations can be used to determine the conditions which induce pore plugging by injecting gel particle suspensions into porous formations.

The diagnostic equations of Wojtanowicz et al. (1987) are applied to investigate the prevailing plugging mechanisms causing permeability reduction under various conditions. The gel particle size distributions are an important part in understanding the mechanism of plugging of porous media, following Civan (2000, 2007a, and 2010), Iscan and Civan (2006), and Iscan et al. (2009). The capture of gel particles in porous media was directly correlated to the ratio of the particle size to the pore throat diameter. The measurements of gel particle sizes of injected and effluent samples were made optically under a microscope equipped with a camera connected to a computer which can store the photomicrographs. The particle size distribution was studied  and useful correlations were developed for the cumulative particle distribution as a function of particle diameter. The experimental study provides an understanding of the transient flow behavior of gel particles through porous media and can assist in choosing suitable parameters for controlling the plugging of the pores and reducing the high permeability of formations to avoid the loss circulation during a drilling operation and control water production in waterflooded mature oil fields. The correlations of experimental data obtained here can be used for determination of the optimal conditions for mitigation and treatment of high permeability formations.

5.2  Experimental Results and Discussion

Because of the deformable nature of the gel particles, the experimental investigation and phenomenological description of the movement and retention of gel particles in porous media is a complicated task. Several transport mechanisms can occur simultaneously during particles transfer through pores and pore throats depending on the local pore and suspension conditions. It is difficult to determine the relative importance of the various particulate mechanisms during the transport process.  Hence, an evaluation index was used to determine the dominant mechanism based on the gel particle size distribution of the initial (original) and effluent suspension samples.

5.2.1  Particle size distribution

The  total  concentration  of  all  particles  ranging  in  the 14- to  350-µm  diameter   sizes   present  in  the  original  3-vol%   suspension  used  in  our   tests   was

determined approximately  as 1.7*104  particles/mL of suspension. Particles with  diameter sizes smaller than 14 µm cannot be counted  with the present  equipment. However, such extremely small particles (significantly  smaller than pore throats in high-permeability zones) can be ignored because they cannot really contribute to the plugging process unless without having a sufficient time to coagulate. The particle size distribution of the original sample indicates that 30% of these gel particles are larger than the average pore-throat size of 127 µm.

Figs. 5.1 to 5.5 show comparison of the particle size distributions of the collected effluent samples and the 3-vol% original injected sample for the gel-particle suspension at different flow rates after 1 and 5 pore volumes injected (PVI), respectively. The particle size distribution of the original sample shows that 30 % of the gel particles are larger than the average pore throat size. At 1 PVI most of the larger particles are trapped at the pore throat or are first deformed and then captured at the pore surface. There is also a possibility that some smaller particles are captured at the pore surface or some larger particles are broken into pieces and then pass through the pore throats. For 50 cm³/hr all particles greater than 150 µm, for 100 cm³/hr the particles greater than 110 µm, for 200 cm³/hr the particles greater than 130 µm, for 280 cm³/hr the particles greater than 150 µm, and for 400 cm³/hr the particles greater than 210 µm are trapped in porous media. These results indicate that at low flow rates the percentage of larger particles trapped at the pore throat or deformed and then captured at the pore surface increases by the flow rate but at high flow rates the percentage of larger particles trapped at the pore throat or deformed and then captured at the pore surface  decreases  by  the  flow  rate. At  5 PVI, the effluent particle size distribution is

approximately the same as the original. This indicates that all the particles pass through the pore throats of the non- plugging pores without entrapment or deposition. Fig. 5.6 shows samples of photomicrographs indicating the difference in size and concentration of the particles at 1 PVI and 5 PVI, respectively.

Fig. 5.1: Particles distribution of 3 vol% original & effluent sample at 50cm³/hr

after 1 and 5 PVI

Fig. 5.2: Particles distribution of 3-vol% original & effluent sample at 100cm³/hr

after 1 and 5 PVI

Fig. 5.3: Particles distribution of 3-vol% original & effluent sample at 200 cm³/hr

after 1 and 5 PVI

Fig. 5.4: Particles distribution of 3-vol% original & effluent sample at 280 cm³/hr

after 1 and 5 PVI

Fig. 5.5: Particles distribution of 3-vol% original & effluent sample at 400cm³/hr

after 1 and 5 PVI

(a)

(b)

Fig. 5.6: Photomicrographs of effluent samples at 100 cm³/hr: (a) after 1 pore

volume injection (PVI)          (b) after 5 pore volume injection (PVI)

5.2.2   Effect of suspension concentration

The effect of the concentration of gel particle in the carrier fluid on the differential pressure and permeability reduction during proppant pack flow tests was investigated by conducting several tests in which the flow rate of the injected suspension was kept constant but the concentration of gel particles in the injected suspension was varied. In these tests, a constant flow rate of 100cm³/hr was used to inject suspension with particle concentrations of 0.5, 1, 2, and 3 vol% into the sandpack.

As   previously  demonstrated  by  Gruesbeck  and  Collins (1982), plugging  of

pathways   in   porous    media    occurs   mainly  when   large   particles   form   bridges

across    pore   throats   and   cause  a   significant    permeability    reduction.  However,

particles   smaller  than   pore   throats    can    pass   through,  which,  under    favorable

conditions   only,  can   deposit   over   the    pore    surface,  and   cause    a    negligible

permeability-reduction   effect.  Fig. 5.7   shows   the    variation  of   the   permeability-

reduction ratio across the  sandpack  with PVI for different suspension concentrations at

a constant 100-cm3/h  flow  rate. By injecting   the  gel   particles, differential   pressure

is  built  up   by  particles   trapped  at  the  entrance of   the   pore  throats,  causing   the

suspension particles to  deform  and  pass   through the  pore   throats  or to be  captured

at  the  pore  surface. However, a  constant steady pressure is established as the injection

continues.

The results of the particle size distribution of the effluent samples at 1 PVI show

that  the   particles with  different  diameters were retained  inside  the  sandpacks, with

consequences  of the  plugging caused essentially by gel particles with sizes comparable

to  or larger  than  the  pore-throat  sizes, while  the larger  pores serving as nonplugging

flow  paths  were only  slightly  impaired by surface  deposition. Fig. 5.7 shows  that the

permeability-reduction ratio  changes from 0.81 to 0.36 by increasing  the concentration

of  the  gel  particles  from  0.5 to 3 vol%. This  happened because the plugging of pores

occurs  more  rapidly  as the  amount of particles trapped at the pore throats or deformed

and  then  captured  at the  pore  surface  increases  by  concentration   increase. Also, as

shown  in Fig. 5.8, for a  constant  flow  rate, the   suspension  viscosity   increases from

0.0035 to 0.0055 Pa.s when the gel-particle concentration increases from 0.5 to 3 vol%.

This causes an increase in the differential pressure and permeability reduction.

Fig. 5.7: Permeability reduction at 100 cm³/hr for different volume suspension

concentrations  at T = 23.5 °C

Fig. 5.8: Suspension viscosity at 100 cm³/hr for different particle volume

concentrations at T= 23.5 °C

5.2.3   Effect of flow rate

The effect of the suspension injection flow rate on the pressure drop and permeability reduction in the sand pack was investigated by several experiments at a constant 3 vol% concentration for the flow rates of 50 cm³/hr, 100 cm³/hr, 200 cm³/hr, 280 cm³/hr, and 400 cm³/hr. Fig. 5.9 shows the permeability-reduction with pore volumes injected at different flow rates and constant concentration. The permeability reduction increased from 0.46 to 0.36 when the flow rate increased from 50 cm³/hr to 100 cm³/hr but the permeability reduction decreased from 0.36 to 0.60 when the flow rate increased from 100 cm³/hr to 400 cm³/hr. This is because at the low flow rate the differential pressure increased as much as the injection flow rate (the differential pressure increased from 16.13 kPa to 41.15 kPa when the flow rate increased from 50 cm³/hr to 100 cm³/hr), but at the high flow rate, the differential pressure did not increase as much as the injection flow rate (the differential pressure only increased from 41.15 kPa to 98.19 kPa when the flow rate was increased four times from 100cm³/hr to 400 cm³/hr). This indicates that the gel particles were able to pass through the pore throats easily at the high flow rate, as we shown from the previous results of the particle size distribution of the effluent sample at 1 PVI for different flow rates. Thus, plugging of pores becomes less pronounced by increasing flow rates.

Baghdikian et al. (1989) investigated the hydrodynamic lift force acting on the rate of particle deposition over and mobilization of particles from pore surfaces. They showed that an increase in the hydrodynamic force with flow rate decreased the particles deposition and increased the particles mobilization, and thus decreased the plugging effect and therefore permeability reduction in porous media. Consequently, increase of differential pressure and reduction of permeability with increase of flow rate become less pronounced.

Fig. 5.9: Permeability reduction at 3-vol% concentration for different flow rates

at T= 23.5 °C

5.2.4   Effect of particle size

The effect of gel- particle size on the differential pressure and permeability reduction was investigated a number of experiments at a constant 3-vol% suspension concentration and 100-cm³/hr constant flow rate using average particle diameters of 50 µm, 75 µm, 100 µm, 125 µm, and 140 µm, respectively. Fig. 5.10 shows the permeability reduction with pore volumes injected at different particle sizes, and constant flow rate and concentration. The permeability reduction changes from 0.54 to 0.30 with the average particle size increasing from 50 µm to 140 µm. This indicates that the amount of  pores  being plugging by the gel particles can be increases by increasing particle size.

It is difficult to determine exactly the prevailing particular processes of gel- particle transport through porous media during the tests because the gel particles are deformable and not rigid. We can consider that the particle will pass through the pore throat if the particle diameter is less than pore-throat size, and the particle will deform and pass through the pore throat to deposit on the pore surface if the particle diameter is larger than the pore-throat size. The rigid particles in diameters larger than the pore- throat size cannot pass through the pore throat. The analysis of the effluent samples at 1 PVI for 100 cm³/hr showed that the effluent samples contain only small particles because almost all the particles larger than pore throat size are captured in porous media. In this case, the pore surface deposition is the relevant process of the gel- particles transport through porous media.

Fig. 5.10: Permeability reduction at 100 cm³/hr for different particle sizes at T=

23.5 °C

5.3  Development of Empirical Correlations

Empirical correlations were developed from the experimental data by using the relevant parameters of flow rate, concentration, and particle diameter leading to plugging of pores by suspended particles. Instead of resorting to ordinary polynomial regressions which are prone to various limitations (Civan, 2011), special correlation equations were developed and implemented, as described in the Appendix B. It is demonstrated by the correlations presented in this section that these equations can represent the experimental data satisfactorily over the full range of the experimental conditions. The advantage of the particular equations of correlations described in  Appendix B that are used here is the elimination of any problems inherent to polynomial regression, such as polynomial oscillations causing inaccurate interpolation values for conditions between measured data.

5.3.1  Suspended particle size distribution before and after flow

The normal size distribution of the suspended particles of the original suspension with minimum particle diameter of 14 micrometer and maximum particle diameter of 350 micrometer and the effluent suspensions at different flow rates were showed in Fig. 5.11. Approximately 30 % of the particles have size greater than the pore-throat size (127 micrometer). For the effluent suspensions, Fig. 5.11 shows that at 50 cm³/hr 18 % of the particles are about 30 micrometer in diameter , while the largest particles (at 150 micrometer) are 5 %; at 100 cm³/hr, 22 % of the particles are approximately 30 micrometer in diameter, while the largest particles (at 110 micrometer)   are   12 %; at  200  cm³/hr, 20 %  of  the  particles   are   approximately 30

micrometer in diameter, while the largest particles (at 130 micrometer) are 10 %; at 280 cm³/hr, 19 % of the particles are approximately 30 micrometer in diameter, while the largest particles (at 150 micrometer) are 4 %; and at 400 cm³/hr, 17 % of the particles are approximately 30 micrometer in diameter, while the largest particles (at 210 micrometer) are 2 %. These results indicate that at the high flow rate, the percentage of the largest particles that are trapped at the pore throat or deposited at the pore surfaces decreases by the flow rate, and thus, the permeability reduction is less.

Fig. 5.11: Particle size distribution for the original and effluent suspensions at 1 PVI for

different flow rates

Empirical correlations were developed from the histogram of the particle size distribution for the original suspension and the effluent samples at different flow rates, as shown in Fig. 5.12. These correlations show an exponential relationship between the

cumulative particle distribution and the particle diameter with high regression coefficient (R²) so that we can use it to predict the cumulative particle distribution at any diameter of the suspended particles for these flow rates, and, from the cumulative particle distribution we can know the percentage of the particles that are trapped and deposited in the porous media, which can demonstrate the permeability reduction. Note F(x) represents the cumulative particle distribution, %; and the normalized particle diameter is given by X = (Dp - Dpmin)/(Dpmax - Dpmin).

Fig. 5.12: Calculated particle size distribution for the original and effluent

suspensions at 1 PVI  for different flow rates

5.3.2  Differential pressure across proppant pack

The experimental results show that differential pressure increases from 11.58 to

41.15 kPa when increasing  the gel- particle- suspension  concentration   from  0.5  to  3

vol%   because  the  amount  of  particles  that  deform  and  deposit at the  pore surface

increases  when   the   concentration   increases. Also,  the  viscosity  of  the  suspension

increases from  0.0035  to 0.0055  kPa.s when increasing  the concentration  from 0.5 to

3 vol%,  which   leads to an  increase in  the  differential   pressure. Fig. 5.13  shows  an

exponential relationship between the gel-particle concentration and differential pressure

across  the proppant  pack. The following   relationship correlates the  experimental data

satisfactorily:

(5.1)

where P indicates differential pressure across proppant pack, kPa; and CP is gel- particle concentration, vol%.

Fig. 5.13: Exponential relationship between gel particle concentration and

differential pressure at 100 cm³/hr and 23.5 °C

For  low  flow  rate, the differential  pressure  increases from 0 to 16.13 kPa by

increasing the  flow  rate from 0 to 50 cm3/h and from 16.13 to 41.15 kPa by increasing

the   flow  rate   from 50 to 100 cm3/h. For   high   flow  rate, the   differential   pressure

increases   from  41.15  to 75.10 kPa,  75.10  to  92.10 kPa,  and  92.10  to 98.19  kPa by

increasing  the  flow  rate from 100 to 200 cm3/h, 200 to 280 cm3/h, 280  to 400 cm3/h,

respectively. These  results  show  that  for  the  high  flow rate, the differential pressure

does  not  increase  as  much as the injection  flow rate. Increasing  the flow rate leads to

an  increase in the  hydrodynamic  lift  force, which  causes  a decrease  in  the  particles

deposition over the pore surface and an enhancement in the release of particles from the

pore   surface; consequently,  plugging   decreases  and  the  increase  in the  differential

pressure  decreases (Baghdikian et al., 1989). For the  high flow rate, the  percentage  of

larger  particles that  are trapped at the pore throat or deformed and then captured  at the

pore   surface  decreases  as  the  flow  rate  increases. Fig. 5.14  shows  the  relationship

between   injection  flow  rate  and  differential  pressure  across the  proppant pack. The

following relationship correlates the experimental data satisfactorily:

(5.2)

where P indicates differential pressure across proppant pack, in kPa, and q is injection flow rate, in cm³/hr. The empirical parameters -6.65 and 0.0001 were determined first by applying Eq. B-1, given in Appendix B, and then the empirical parameters 1.80, 115, and 7136 were determined by applying  Eq. B-2 given in Appendix B, as shown in Figs. C.1 and C.2 in Appendix C.

Fig. 5.14: The relationship between injection flow rate and differential pressure at

3 vol% and 23.5 °C

The differential pressure increases from 27.40 kPa to 50.01 kPa by increasing the average particle size from 50 µm to 140 µm because the amount of the pores that are plugging by the gel particles increases with increase in particle size. Fig. 5.15 shows the relationship between the gel-particle diameter and differential pressure across the proppant pack. The following relationship correlates the experimental data satisfactory.

(5.3)

where ∆P indicates differential pressure across proppant pack, in kPa, and Dp is the gel- particle  diameter, in µm. The empirical  parameters 122 and  265  were  determined  by

applying Eq. B-3, given in Appendix B, as shown in Fig. C.3 in Appendix C.

These simple empirical correlations can be used to predict the differential pressure across the proppant pack for a similar material and operation conditions at any gel particle concentration, flow rate, or gel-particle diameter because the regression coefficients (R²) of these relationships are high (0.99- 1).

Fig. 5.15: The relationship between gel-particle diameter and differential pressure

at 100 cm³/hr and 23.5 °C

It is very important to know the change in the differential pressure during the gel-particle-suspension injection because the differential pressure was built up by the plugging of the pores, thus reducing the high permeability of porous media. Therefore, the parameters that give higher differential pressure should be used to achieve a successful field applications of gel-particle-suspension injection for treating the reservoir permeability heterogeneity to avoid the loss of circulation during a drilling operation and control water production in mature waterflooded oil fields.

5.3.3  Permeability impairment (reduction)

The permeability reduction increased from 0.81 at 0.5-vol% suspension concentration to 0.36 at 3-vol% suspension concentration because the tendency of plugging increased with particle concentration. Fig. 5.16 shows the relationship between gel-particle concentration and permeability reduction at 100-cm³/hr flow rate and ambient temperature of 23.5 °C. The following relationship correlates the experimental data satisfactorily:

(5.4)

where (K/Ko)  indicates the permeability reduction (dimensionless) and Cp is gel- particle  concentration, vol%. The empirical parameters 0.64, 5.55 and -19.42 were determined by applying Eq. B-4 given in Appendix B, as shown in Fig. C.4 in Appendix C.

Fig. 5.17 shows the exponential relationship between the injection flow rate of 3-vol% suspension and the permeability reduction at ambient temperature of 23.4 °C. The permeability reduction increases for the low flow rate and decreases for the high flow because of the hydrodynamic force and the viscosity. The following exponential relationship correlates the experimental data satisfactorily.

(5.5)

where (K/Ko)  indicates permeability reduction (dimensionless) and q is injection flow rate, in cm³/hr.

Fig. 5.16: The relationship between gel particle concentration and permeability

reduction at 100 cm³/hr and 23.5 ˚C

Fig. 5.17: Exponential relationship between injection flow rate of 3 vol%

suspension and permeability  reduction at T= 23.5 °C

The permeability reduction increases from 0.54 to 0.30 with increasing average particle size from 50 µm to 140 µm because the amount of  pores that are plugging by the gel particles increases with increase in  particle sizes. Fig. 5.18 shows the relationship between the gel particle diameter and the permeability reduction at 100 cm³/hr flow rate and ambient temperature  of 23.5 °C. The following relationship correlates the experimental data satisfactory.

(5.6)

where K/Ko indicates permeability reduction (dimensionless) and Dp is gel-particle diameter, in µm. The values of the empirical parameters were determined by applying Eq. B-4 given in Appendix A, as shown in Fig. C.5 in Appendix C.

Fig. 5.:18 The relationship between gel particle diameter and permeability

reduction at 100 cm³/hr and 23.5 °C

Another  proppant  pack with 3600-md permeability, 34% porosity, and 59 µm

pore- throat size was used to study the variation of permeability reduction with particle diameter/pore-throat size for different suspensions. Fig. 5.19 shows the relationship between particle diameter /pore-throat size and the permeability reduction at 100 cm³/hr flow rate and ambient temperature 23.5 °C. The following relationship correlates the experimental data satisfactory:

(5.7)

where (K/Ko)  indicates permeability reduction (dimensionless) and Dp/DT particle diameter /pore-throat size (dimensionless). The values of the empirical parameters were determined by applying Eq. B-4 given in Appendix B, as shown in Fig. C.6 in Appendix C.

Fig. 5.19: Variation of permeability reduction with particle diameter to pore-

throat size for different suspensions at 100 cm³/hr

These empirical correlations can be used to predict the permeability reduction across the proppant pack for a similar material and the operation conditions at any gel- particle concentration, flow rate, gel-particle diameter or particle diameter/pore-throat size because the regression coefficients (R²) of these correlations are high (0.98- 1).                               The permeability  reduction of the porous media was caused  from the plugging of the pores by the gel particles. Therefore, the parameters that lead to the best plugging of the pores and  the best reducing of the high permeability of the formations should be used for successful field applications of treating the reservoir permeability heterogeneity to avoid  the  loss of circulation during a drilling operation and control water production in

mature waterflooded oil fields having highly permeable zones.

5.3.4  Resistance factor

Fig. 5.20 shows the relationship between the gel-particle concentration and resistance factor. The resistance factor is the ratio of the water mobility (Kw/µw) before suspension injection to the suspension mobility (K/µ) during suspension injection at the same flow rate (Littmann 1988):

(5.8)

Where Fr indicates the resistance factor (dimensionless); Kw is the effective water permeability, in md; µw is the water viscosity, in Pa.s; K is the suspension permeability, in md; and µ is the suspension viscosity, in Pa.s. The resistance factor increased from 4.3 at suspension concentration of 0.5 vol% to 15.3 at suspension concentration of 3 vol%. This means that an increase in plugging of the pores occurs when the suspension concentration increases. The following relationship correlates the experimental data satisfactory.

(5.9)

where Fr  indicates resistance factor (dimensionless) and Cp is gel-particle concentration, vol%. This correlation was obtained by regression of a weighted-sum combination of Eqs. B-5 and B-6, both given in Appendix B, as shown in Figs. C.7 and C.8 in Appendix C.

Fig. 5.20: Polynomial relationship between gel-particle concentration and

resistance factor at 100 cm³/hr and 23.5 °C

Fig. 5.21 shows the relationship between injection flow rate and resistance factor. The resistance factor increases for the low flow rate and decreases for the high flow rate because of the hydrodynamic force and the viscosity, the resistance factor increased from 12.01 to 15.29 when the flow rate increased from 50 cm³/hr to 100 cm³/hr and the resistance factor decreased from 15.3 to 9.1 when the flow rate increased from 100cm³/hr to 400cm³/hr. The following relationship correlates the experimental data satisfactorily.

(5.10)

where Fr  indicates resistance factor (dimensionless) and q is injection flow rate, in

cm³/hr. This correlation was obtained by regression of a weighted-sum combination of  Eqs. B-6 and B-7, both given in Appendix B, as shown in Figs. C.9 and C.10 in Appendix C.

Fig. 5.21: The relationship between injection flow rate and resistance factor at 3

vol% and 23.5 °C

Fig. 5.22 shows the relationship between gel-particle diameter and resistance factor. The resistance factor increases from 15.3 to 17.7 by increasing the gel particle diameter from 100 µm to 125 µm because the plugging of the pores increases as the gel- particle diameter increases. The following relationship correlates the experimental data satisfactory.

(5.11)

where Fr  indicates resistance factor (dimensionless) and Dp is gel-particle diameter, in µm. The empirical parameters of this correlation were determined by applying Eq. B-5 given in Appendix B, as shown in Fig. C.11 in Appendix C.

Fig. 5.22: The relationship between gel particle diameter and resistance factor at

100 cm³/hr and 23.5 °C

These correlations can be used to predict the resistance factor across the proppant pack for a similar material and the operation conditions at any gel-particle concentration, flow rate, or gel-particle diameter because the regression coefficients (R²) of these correlations are high (0.99- 1). According to the definition of the resistance factor, high resistance factor means that there was a high reduction in the permeability of the porous media. Therefore, the parameters that lead to higher resistance factor should be chosen to achieve successful application of gel-particle-suspension injection for field applications to avoid the loss of circulation during a drilling operation and control water production in mature waterflooded oil fields having highly permeable zones.

5.4  Plugging Criteria Correlated by Use of Dimensionless Groups

The experimental data generated in this study illustrate the effect of particle concentration, flow rate, and pore-throat/particle size ratio on the plugging mechanisms. To determine the conditions that lead to pore plugging (i.e., the plugging criteria), two dimensionless variables and the power- law and exponential-law equations presented by Civan (2000, 2007a) were applied to correlate the measured data:

(5.12)

(5.13)

(5.14)

(5.15)

Eq. 5.15 is a modified form of the exponential- law equation presented by Civan (2000, 2007a). Here, β indicates the pore-throat/particle-diameter ratio, which is the first dimensionless variable; Rep is the particle Reynolds number which is the second dimensionless group of variables; Cp is the particle concentration in the suspension; μ is the viscosity of the suspension; ѵ is the velocity of the particles (assuming the particle velocity is equal to the suspension velocity);  is an empirical exponent; A1, A2, B1, B2, C1, and C2 are the empirical fitting parameters; DT is the average pore-throat diameter; and Dp is the average particle diameter calculated as:

(5.16)

where σi is the volume fraction of particle i; and (Dp)i is the diameter of particle i.

Eqs. 5.14 and 5.15 describe the occurrence of pore plugging with certain fluid/ particle conditions such as the particle concentration, fluid viscosity, pore-throat/ particle diameter ratio, and fluid velocity. Applying the power- law and exponential- law correlations of the two dimensionless groups, a correlation curve can be developed with two regions. The region above the curve represents the non-plugging conditions, and region below the curve represents the plugging conditions. The physical meaning of the coefficient C is that the plugging always occurs when 0<DT/Dp<1 (the particle size equal to or greater than pore-throat size), so C in Eqs. 5.14 and 5.15 assumes a value of unity. However, this physical interpretation is not always valid because the deformable gel particles with diameter greater than pore-throat size may be able to squeeze and move through a pore throat. The empirical parameters A1, B1, C1, A2, B2 and C2 and the empirical exponent λ were determined by using the linearized forms of Eqs. B-8 and B-9 given in Appendix B. The best straight- line that matches the experimental data was obtained by the method of least squares, and the values of the fitting parameters were determined as the highest  coefficient of regression of this straight line, as shown in Table 5-1 and Figs. D.1 and D.2 in Appendix D. Figs. 5.23 and 5.24 present the successful power- law and exponential correlations, respectively, of the experimental data by use of the gel suspensions of different particle concentrations and different average particles diameter. The regression coefficients of the experimental data are 0.97 for the power- law and 0.96 for the exponential- law. The power- law and exponential correlations curves, given in Figs. 5.23 and 5.24, respectively, indicate that no plugging occurs if β > 1.35 at any value of Rep because all the points are above the curve. Pore plugging occurs at low particle concentration when β is close to 1.0. Thus, the condition can change from non-plugging to plugging position by a small increase in particle concentration in the range of 1<β<1.35. According to the correlations of the dimensionless groups, the plugging occurs under certain conditions of particles concentration, flow rate, and pore-throat/ particle diameter ratio. Pore plugging induces permeability reduction, thus the dimensional analysis can assist in determining the functional trends of the correlations of the present experimental data, such as the differential pressure, the permeability reduction, and the resistance factor.

TABLE 5-1: BEST- ESTIMATE FITTING PARAMETERS

Model                                                                  Parameters

(dimensionless)

Power- Law                  A1 = 54         B1 = 0.511       C1 = 1.00                         R² = 0.97

Exponential- Law       A2 = 690       B2 = -0.07        C2 = 1.00        λ= 0.50      R² = 0.96

Fig. 5.23: Experimental and correlation results from power- law model as a

function of particle Reynolds number

Fig. 5.24: Experimental and correlation results from exponential- law model as a

function of particle Reynolds number

5.5  Identification of  Particle Retention Mechanisms

Wojtanowicz et al. (1987) proposed a quantitative approach for analyzing the single-fluid phase formation-permeability-reduction trends because of fine-particles invasion and deposition. Three different mechanisms of particulate injection processes were recognized, and the corresponding diagnostic equations were derived for these mechanisms by assuming that one mechanism dominates at a time of suspension injection, as summarized in Table 5-2. These three mechanisms are (a) pore-surface deposition in which gradual pore reduction occurs when particle size smaller than pore- throat size; (b) pore-throat plugging in which single pore blocking occurs when the particle size is comparable or larger than the average size of the pore throat; and (c) pore filling, which occurs as a result of internal filter cake (neglecting the external cake) (Civan 2007a). The fundamental assumptions of the method of Wojtanowicz et al. (1987) are homogeneous formation and constant flow rate, low solid concentration, and  pore-volume reduction caused by particle capture, but neglecting the gravity effect.

TABLE 5-2: WOJTANOWICZ ET AL. (1987) DIAGNOSTIC EQUATIONS

Permeability Reduction                 Diagnostic Equations                 Straight Line

Mechanisms                                                                           Plotting Scheme

Pore surface deposition                     (K/Ko)½ = 1- C3t                    (K/Ko)½ vs. t

Pore throat plugging                             K/Ko = 1- C4t                        K/Ko vs. t

Pore filling                                             Ko/K = 1+ C5t                      Ko/K vs. t

Figs. 5.25 and 5.26 present the permeability-change tendency during the injection of gel particles into the proppant pack. These figures show a wavy-shape trend for alteration of permeability observed during the experiments, indicating the occurrence of consecutive plugging and unplugging phenomena. Thus, the gel particles in the suspension tend to be captured at the small pore throats initially, then the gel particles with diameter larger than the pore-throat sizes are diverted to the larger unplugged  pore throats and accumulate behind them, leading to generation and building up of high differential pressure. This differential pressure causes deformation of the gel particles captured at some pore throats and induces them to pass through these pores. After the deformation and passing of these gel particles, the process of pressure build up by particle accumulation begins again until the gel particles deform and pass through the pore throat once more. The frequent plugging and unplugging processes continue until a steady flow at a constant differential-pressure and permeability reduction level is attained, at which the gel-particle-suspension injection process should

be terminated.

1

2

2

2

2

1

1

1

Fig. 5.25: Pore-throat-plugging mechanism for different particle concentrations

at 100 cm³/hr and 23.5 °C

2

2

2

2

1

1

1

1

Fig. 5.26: Pore-surface-deposition mechanism for different particle concentrations

at 100 cm³/hr  and 23.5 °C

The diagnostic equations of Wojtanowicz et al. (1987) consider an initial condition that K/Ko = 1.0 at t = 0. Therefore, they can be applied over various regions only after shifting the time so that the initial reference time considered in our data analysis becomes zero for each consecutive period. Figs. 5.25 and 5.26 represent the straight- line plotting of the diagnostic equations of the pore-throat-plugging mechanism and the pore-surface-deposit mechanism for regions 1 and 2 for different gel-particle- suspension concentrations (0.5 , 1, 2, and 3 vol%) at a constant flow rate of 100 cm³/hr and ambient temperature of 23.5 °C. These figures indicate that the pore-throat-plugging mechanism and the pore-surface-deposition mechanism are dominant, indicated with high regression coefficients. Tables 5-3 and 5-4 show that the values of the rate-constants of the plugging regions increase with particle concentration because the amount of particles that are trapped at the pore throats or deformed and then captured at the pore surface increases when the concentration increases. The pore filling dose not occur because an internal filter cake cannot be formed in the proppant pack.

TABLE 5-3: RATE CONSTANTS  OF PLUGGING REGIONS FOR PORE-     THROAT- PLUGGING MECHANISM AT DIFFERENT PARTICLE  CONCENTRATIONS

Particle                                      Regions                  Rate Constants                  R²

Concentrations (vol%)                                                     (min  ̄¹)

0.5                                       1                               0.0070                      0.98

0.5                                       2                               0.0050                             0.99

1.0                                       1                               0.0140                      0.96

1.0                                       2                               0.0052                      1.00

2.0                                       1                               0.0310                      0.97

2.0                                       2                               0.0250                      0.99

3.0                                       1                               0.0400                      0.96

3.0                                       2                               0.0248                      0.99

TABLE 5-4: RATE CONSTANTS  OF PLUGGING REGIONS FOR PORE- SURFACE -DEPOSITION MECHANISM AT DIFFERENT PARTICLE CONCENTRATIONS

Particle                                      Regions                   Rate Constants                   R²

Concentrations (vol%)                                                 (min  ̄¹)

0.5                                      1                            0.0035                         0.98

0.5                                      2                            0.0025                                 0.99

1.0                                      1                            0.0070                         0.96

1.0                                      2                            0.0026                         1.00

2.0                                      1                            0.0160                         0.97

2.0                                      2                            0.0138                         0.99

3.0                                      1                            0.0210                         0.96

3.0                                      2                            0.0145                         0.99

5.6  Conclusions

The main findings of the present  flow tests conducted using 3800- md, 16-  to 20-mesh sand packs can be summarized as the following:

- This is a relatively  new  technology, and,  therefore, quantitative  evaluation the

effect  of  various  factors  on  the  performance of gel-particle  applications presented in

this study  is significant  for  practical  applications of gel-particle-suspension  injection.

Therefore,  important correlations were developed that can assist in controlling plugging

in  highly  permeable  formations and  treating  these  formations  by reducing  the  high

permeability to avoid loss of circulation during drilling operations  and to control  water

production  in mature waterflooded oil fields containing highly permeable zones.

- Consecutive  plugging  and  unplugging   phenomena  occur  during  gel-particle

injection  into  proppant packs. Accumulation of  the  particles  behind the pore  throats

leads to a differential  pressure buildup, and  the  particles can pass  through other pores

because of the ability of the gel particles to deform or break, which causes a subsequent

reduction in the differential pressure.

- The  plugging and unplugging processes continue until a steady flow is attained

in  which the  differential-pressure level  and permeability reduction  approach constant

limit   values, at  which  time  the  gel-particle-suspension-injection  process  should  be

stopped. The values of the rate constants of  the plugging regions  increase with particle

volume  concentration   because the   amount  of  particles  that are  trapped  at the pore

throats or deformed and then captured at the pore surface increases with the gel-particle

concentration.

- The  gel-particle distribution  of the  suspensions  before and after  injection was

studied to determine which particles can be trapped and deposited inside the sandpacks,

to  determine  the   percentage of  these  particles, and  to demonstrate  the  permeability

reduction    effect.  Empirical    correlations   were   developed   from   the   gel-particle

distribution  to  predict   the  cumulative  particle  distribution  at  any  diameter  of  the

suspended particles for certain conditions.

- Conditions  leading   to pore  plugging  in highly  permeable  formations  can  be

quantified in terms of  the  relevant  dimensionless groups, such as the particle Reynolds

number (Rep) and pore-throat/particle size ratio (β). Plugging occurs if the Rep vs. β is in

the region  indicated  below the  curve  obtained by plotting  of the developed  empirical

correlations.

- The   diagnostic   equations   of   Wojtanowicz   et al.  (1987)   can  be   used  for

identification  of the  relevant  governing  mechanisms of  impairment of  porous  media

during   the   injection   of   gel-particle  suspensions   into  the  sandpacks   at   different

conditions.

# Chapter 6: Thermal Effects on Near-Wellbore Formation Treatment by Gel Particles Suspension

This   Chapter   has   been   previously   published  as ‘‘Experimental   Investigation  and

Correlation  of   Thermal   Effects  on   Near-Wellbore   Formation   Treatment  by   Gel

Particles’’ in the  SPE   International Symposium on Oilfield Chemistry, Woodland, TX,

8-10 April, 2013 and is used here by permission.

6.1   Introduction

Temperature plays an important factor in suspended gel particles treatment of high permeability near-wellbore zones because temperature affects the gel particles properties. Thus, temperature is affect the transient behavior of gel particles through porous media by influencing the plugging mechanisms and their rates. Practically, there are no correlations reported that can be used for designing of suspended gel particles placement for near-well bore formation treatment by considering the effect of near-wellbore zone temperatures. For this purpose, an experimental study of thermal effects on conditioning and reducing the high permeability of formations is undertaken to investigate the relevant processes and correlate the experimental results for successful gel particles applications in oil fields.

The effect of temperature on plugging of highly permeable near-wellbore formations is investigated by injection of suspension of gel particles into proppant packs at different temperatures and useful correlations are developed for field applications. The effect of temperature on permeability impairment at various temperatures (23.5 ˚C, 40 ˚C, 60 ˚C, and 75 ˚C) is investigated at a constant 100 cm³/hr flow rate and a 3 vol% gel   particles  concentration. Experiments  are  conducted  using  unconsolidated plastic

glass proppant packs. The resulting pressure differentials across the proppant pack are measured during the experiments and the permeability reductions and resistance factors are inferred by the variation of differential pressures with time. Further, we investigate the mechanisms of plugging and unplugging phenomena during the injection of gel particles into the proppant pack at various temperatures. The permeability reduction increases during plugging and decreases during unplugging. The plugging and unplugging processes occur repetitively over consecutive periods of times. The frequency of the plugging and unplugging regions decreases by increase in temperature. The rate constants of plugging and unplugging processes are determined at various temperatures. The experimental data of the differential pressure, permeability reduction, and resistance factor, and the rate constants determined at various temperatures are correlated by using Vogel-Tammann- Fulcher (VTF) - type equations similar to Civan (2008, 2011a). Excellent agreement is observed between the experimental data and the correlations. Hence, these correlations can be used to predict the effect of temperature on conditioning of the high permeability formations by means of injection of suspension of gel particles.

6.2  Experimental Results, Data Analyses, and Discussion

Differential pressure build up is a key issue during the gel particle suspension injection by plugging of the pores and thus reducing the high permeability and increasing the resistance factor of porous media. Therefore, it is very important to study the effect of temperature on the differential pressure during the gel particle suspension injection because higher differential pressure should be attained to achieve a successful

field applications of the gel particle suspension injection to treat the reservoir permeability heterogeneity and thus prevent the loss circulation during a drilling operation  and  control  the  water  production  in  waterflooded  mature  oil  fields.  The

empirical correlations for the viscosity, differential pressure, and permeability reduction and resistance factor across proppant pack are developed from the experimentally measured data at different temperatures. It is demonstrated that these equations can represent the measured and experimental data satisfactorily over the range of the experimental conditions.

Several tests were carried out in which the flow rate of the injected suspension and the concentration of gel particles in the injected suspension were kept constant at 100 cm³/hr and 3 vol%, respectively, but the temperature of the proppant pack was varied at 23.5 ˚C, 40 ˚C, 60 ˚C, and 75 ˚C in each experiment in order to investigate the effect of temperature on the differential pressure and permeability reduction of the proppant pack. Fig. 6.1 shows the variation permeability reduction across the proppant pack with pore volumes injected for different temperatures of 23.5 ˚C, 40 ˚C, 60 ˚C, and 75 ˚C at a constant 100 cm³/hr flow rate and a constant 3 vol% gel concentration. Differential pressure is build up during the injection of the gel particles suspension when particles are trapped at the pore throats causing the gel particles to deform and pass through the pore throats or to be captured across the pores and the injection continues until a constant steady pressure is attained. Fig. 6.1 shows that the permeability reduction decreased from 0.36  to 0.42 by increasing the temperature of the sand pack from 23.5 ˚C to 75 ˚C. This happened because the gel particles became softer and  deformable by  temperature and the degree of pore-throat plugging and pore-

surface deposition decreased. Consequently, the gel particles were able to pass through the pore easily at high temperature and plugging of pores becomes less pronounced at increasing  temperatures. Thus, the  differential  pressure  decreased  from  41.15 kPa to

22.68 kPa when the temperature increased from 23.5 ˚C to 75 ˚C.  Also, for a constant flow rate and concentration, the suspension viscosity decreases from 0.0055 Pa.s to 0.0035 Pa.s when the temperature increased from 23.5 ˚C to 75 ˚C. This causes a decrease in the differential pressure and permeability reduction.

Fig. 6.1: Permeability reduction at 3 vol% concentration for different

temperatures at 100 cm³/hr

6.3  Correlation of Measurements

Several empirical correlations of practical importance are developed from the experimental data at different temperatures for effective design of the suspended gel particles treatment in weak and highly permeable near- wellbore formations. The empirical correlations will be developed by using a VTF- type equation. The results are compared to measured and experimental data to determine the reliably for design of treatment of  highly permeable formations by gel particles under different temperature	The Vogel- Tammann- Fulcher-type equations (VTF) are widely used to correlate the experimental data for the temperature dependent parameters (Vogel 1921; Tammann and Hesse 1926; Fulcher 1925). Civan (2004, 2005, 2006a and b, 2007b and c, and 2008, 2010) described the VTF equation as an asymptotic exponential function in the following general form:

(6.1)

where f is a temperature dependent parameter (unit determined by the type of property); fc is a pre- exponential coefficient (unit determined by the type of property); T is the actual temperature, K;  Tc is the critical temperature, K; and C is defined as E/Rg, where E is the activation energy (J/kmol), and Rg is the universal gas constant (J/kmol- K). fc, Tc, and C are the fitting constants and are determined by using the special least- squares method developed by Monkos (2003) and then trial and error method of Tc is used in the straight- line VTF plot of the experimental data until get the best regression coefficient (R²) value. The  applications of  this equation are illustrated in the following.

The  viscosity of  the 3  vol % gel  particles  suspension  decreases  from  0.0055 Pa.s to

0.0035  Pa.s by increasing the temperature from 23.5 ˚C  to 75 ˚C. The measured data of a 3 vol% concentration gel suspension viscosity is correlated by using the VTF equation, given by:

(6.2)

where  µ is the  suspension  viscosity, Pa.s; and µc is the pre- exponential  coefficient of

viscosity is 0.03484  Pa.s. The fitting constants Tc and C are  550 K and -465 K, respectively. Fig. 6.2 shows the straight- line VTF plot of the measured data for the 3 vol% suspension viscosity. Fig. 6.3 shows comparison between the suspension viscosity values obtained from VTF equation and the measured data.

The differential pressure across the proppant pack decreases from 41.15 kPa to  22.68 kPa by increasing the temperature of the sand pack from 23.5 ˚C to 75 ˚C  because the gel particles were able to deform and then pass through the pore throats easily at high temperatures and hence, the amount of particles that deformed and deposited at the pore surface decreases when the temperature  increases. Also, the viscosity of the suspension decreases from 0.0055 Pa.s to 0.0035 Pa.s by increasing the temperature from 23.5 ˚C to 75 ˚C which leads to a decrease in the differential pressure.

The experimental data of the differential pressure across the proppant pack is correlated by using the VTF  equation, given by:

(6.3)

where ∆P  is  the  differential  pressure  across  proppant  pack, kPa; and  ∆Pc  is the pre-

exponential coefficient of differential pressure is 2703 kPa. The fitting constants Tc and C are 700 K and -1685 K, respectively. Fig. 6.4 shows the straight- line VTF plot of the experimental data for the differential pressure across proppant pack. Fig. 6.6 shows comparison between the differential pressure  values obtained from VTF equation and the experimental data.

Fig. 6.2: Straight- line VTF plot for the 3 vol% suspension viscosity

Fig. 6.3: Comparison between suspension viscosity obtained from the VTF

equation and the measured data

Fig. 6.4: Straight- line VTF plot for the differential pressure

Fig. 6.5: Comparison between differential pressure obtained from the VTF

equation  and the experimental data

The permeability reduction decreased from 0.36 at 23.5 ˚C temperature to 0.42 at 75 ˚C temperature because the tendency of plugging decreased with increasing temperature. The experimental data of the permeability impairment (reduction)  is correlated by using the VTF equation, given by:

(6.4)

where (K/Ko) is the permeability impairment (reduction), dimensionless; and (K/Ko)c is the pre- exponential coefficient of  permeability impairment (reduction) is 0.711. The fitting constants Tc and C are 100 K and 134 K, respectively. Fig. 6.6 shows the straight- line  VTF  plot  of  the  experimental   data  for  the   permeability   impairment

(reduction). Fig. 6.7 shows comparison between the permeability impairment (reduction)  values obtained from VTF equation and the experimental data.         Fig. 6.6: Straight- line VTF plot for the permeability reduction

Fig. 6.7: Comparison between permeability reduction obtained from the VTF

equation and the experimental data

The resistance factor is defined as the ratio of the water mobility before suspension injection to the suspension mobility during suspension injection at the same flow rate (Littmann 1988):

(6.5)

Fr indicates the resistance factor, dimensionless; Kw is the effective water permeability, md; µw is the water viscosity, Pa.s; K is the suspension permeability, md, and µ is the suspension viscosity, Pa.s. The resistance factor decreased from 15.3 at temperature of 23.5 ˚C to 8.43  at temperature of 75 ˚C. This indicates a decreasing in plugging of the pores occurs when increasing the temperature. The experimental data of the permeability impairment (reduction)  is correlated by using the VTF equation, given by:

(6.6)

where Fr is the resistance factor, dimensionless; (Fr)c is the pre- exponential coefficient of  resistance factor = 0.000223. The fitting constants Tc and C are -600 K and -10000 K, respectively. Fig. 6.8 shows the straight- line VTF plot of the experimental data for the resistance factor. Fig. 6.9 shows comparison between the resistance factor  values obtained from VTF equation and the experimental data. As can be seen, the VTF correlation values of viscosity, differential pressure, and permeability reduction and resistance factor are close to the experimental data because of the high regression coefficients (R²) of these relationships, around the unity. Thus, we can use the VTF equation to predict the viscosity, differential pressure across the proppant pack, permeability impairment (reduction) and resistance factor for a similar material and operation conditions at any temperature.

Fig. 6.8: Straight- line VTF plot for the resistance factors

Fig. 6.9: Comparison between resistance factor obtained from the VTF

equation and the experimental data

6.4  Correlation of Thermal Effect on Plugging/Unplugging Processes

A consecutive  plugging  and  unplugging  phenomena is observed  during  the

injection of gel  particles  into the proppant pack at various temperatures as seen in Fig.

6.10. The   permeability   reduction   increases  during  plugging  and  decreases  during

unplugging.  The  plugging  event  occurs  when  the  gel  is  captured and accumulated

behind  the  pore  throats, causing  a buildup  of  differential  pressure. The  unplugging

event occurs  when the  differential  pressure  leads to a deformation of the gel particles

captured  and  accumulated  at some  pore  throats  and  then  pass  through these pores,

decreasing  the  differential pressure (Al- Ibadi and Civan 2012 and 2013a). A series of

plugging  and  unplugging  processes  occurs  repetitively  over  consecutive periods of

times and  continues until attaining a steady flow at a constant differential pressure and

permeability reduction level.            Fig. 6.10: Permeability reduction at 3 vol% concentration for different

temperatures at 100 cm³/hr

Figs. 6.11 to 6.18 show the plugging and unplugging events occurring during the injection of gel particles into the proppant pack at various temperatures. The number of plugging and unplugging regions decreases by increase in temperature. The plugging and unplugging events can be modeled and represented as straight line plots shown in Figs. 6.11 to 6.18. The straight lines are not parallel because they have different slopes and not horizontal because the slopes are not equal zero. The slopes of the straight lines represent the rate constant values for the plugging and unplugging processes. Tables 6-1 to 6-8 show the rate and intercept constants values for plugging and unplugging processes at various temperatures. The values of the rate constants decrease by the pore volume injected, indicating that first the gel particles are captured at the small pore throat and then the gel particles of diameter larger than the pore throat size are diverted toward the larger unplugging pore throats and accumulate behind them, as described by Civan and Nguyen (2005). Thus, the rate constants of plugging and unplugging regions are determined and correlated for the rate of plugging and unplugging at various temperatures. Figs. E.1 and E.2 show the relationship between the rate constants of plugging and unplugging regions and the pore volumes injected for 3 vol% particles suspension at various temperatures. The rate constant of plugging and unplugging regions are correlated by using  Eq. B-6 given in appendix B, as shown in Figs. E.3 and E.4 in Appendix E. Further, the intercept of the plugging and unplugging regions are determined and correlated with the pore volumes injected at various temperatures as shown in Figs. E.5 and E.6. The intercept of the plugging regions are correlated by using equation B-4 given in Appendix B and the intercept of the unplugging regions are correlated by applying equation B-2 given in appendix B, as shown in Figs. E.7 and E.8 in appendix E.

The values of the rate constants and the intercepts of the plugging and unplugging regions were correlated by used of Eqs. 6.7 and 6.8, respectively, as shown in Figs. E.1, E.2, E.5, and E.6:

(6.7)

(6.8)

where y represent the rate constants of the plugging and unplugging regions, dimensionless or the intercept of the plugging and unplugging regions, dimensionless; x represents the pore volume injected, dimensionless; A, B, and β are empirical parameters, dimensionless.

Fig. 6.11: Plugging events trends at T= 23.5 ˚C

Fig. 6.12: Unplugging events trends at T= 23.5 ˚C

Fig. 6.13: Plugging events trends at T= 40 ˚C

Fig. 6.14: Unplugging events trends at T= 40 ˚C

Fig. 6.15: Plugging events trends at T= 60 ˚C

Fig. 6.16: Unplugging events trends at T= 60 ˚C

Fig. 6.17: Plugging events trends at T= 75 ˚

Fig. 6.18: Unplugging events trends at T= 75 ˚C

TABLE 6-1: RATE AND INTERCEPT CONSTANTS  OF PLUGGING

REGIONS AT T=23.5 ˚C

Regions                   Rate Constants                    Intercept Constants                R²

(dimensionless)                      (dimensionless)

1                                 0.78                                         1                               0.98

2                                 0.68                                       0.62                              1

3                                 0.54                                       0.59                              1

4                                 0.50                                       0.53                              1

5                                 0.23                                       0.48                            0.98

6                                 0.19                                       0.45                            0.89

7                                 0.17                                       0.44                            0.97

8                                 0.15                                       0.43                            0.99

9                                 0.10                                       0.42                              1

TABLE 6-2: RATE AND INTERCEPT CONSTANTS  OF UNPLUGGING

REGIONS AT T=23.5 ˚C

Regions                    Rate Constants                 Intercept Constants                  R²

(dimensionless)                    (dimensionless)

1                                0.45                                      0.61                                 1

2                                0.50                                      0.56                                 1

3                                0.38                                      0.51                                 1

4                                0.24                                      0.46                               0.97

5                                0.14                                      0.44                                 1

6                                0.09                                      0.43                                 1

7                                0.07                                      0.42                               0.99

8                                0.06                                      0.41                               0.98

9                                0.07                                      0.40                                 1

TABLE 6-3: RATE AND INTERCEPT CONSTANTS  OF PLUGGING

REGIONS AT T=40 ˚C

Regions                  Rate Constants                    Intercept Constants                 R²

(dimensionless)                      (dimensionless)

1                               0.83                                         1                                  0.98

2                               0.66                                       0.66                               0.99

3                               0.58                                       0.59                                 1

4                               0.37                                       0.54                               0.95

5                               0.18                                       0.50                               0.97

6                               0.25                                       0.48                               0.99

7                               0.18                                       0.46                                 1

8                               0.13                                       0.45                                 1

TABLE 6-4: RATE AND INTERCEPT CONSTANTS  OF UNPLUGGING

REGIONS AT T=40 ˚C

Regions                  Rate Constants                   Intercept Constants                 R²

(dimensionless)                     (dimensionless)

1                                0.35                                       0.64                               1

2                                0.55                                       0.56                               1

3                                0.25                                       0.53                               1

4                                0.09                                       0.49                             0.96

5                                0.26                                       0.47                               1

6                                0.10                                       0.45                               1

7                                0.09                                       0.44                               1

8                                0.05                                       0.43                               1

TABLE 6-5: RATE AND INTERCEPT CONSTANTS  OF PLUGGING

REGIONS AT T=60 ˚C

Regions                  Rate Constants                    Intercept Constants                   R²

(dimensionless)                      (dimensionless)

1                               0.85                                          1                                  0.97

2                               0.62                                        0.62                                 1

3                               0.41                                        0.58                               0.97

4                               0.19                                        0.55                                 1

5                               0.14                                        0.50                               0.99

6                               0.11                                        0.48                                 1

TABLE 6-6: RATE AND INTERCEPT CONSTANTS  OF UNPLUGGING

REGIONS AT T=60 ˚C

Regions                  Rate Constants                   Intercept Constants                   R²

(dimensionless)                     (dimensionless)

1                               0.30                                       0.62                                  1

2                               0.20                                       0.57                                  1

3                               0.19                                       0.54                                  1

4                               0.05                                       0.49                                0.89

5                               0.07                                      0.47                                  1

6                               0.05                                       0.45                                  1

TABLE 6-7: RATE AND INTERCEPT CONSTANTS  OF PLUGGING

REGIONS AT T=75 ˚C

Regions                  Rate Constants                    Intercept Constants                   R²

(dimensionless)                      (dimensionless)

1                               0.86                                          1                                  0.95

2                               0.73                                        0.69                                 1

3                               0.44                                        0.63                               0.99

4                               0.22                                        0.57                               0.94

5                               0.22                                        0.55                               0.98

TABLE 6-8: RATE AND INTERCEPT CONSTANTS  OF UNPLUGGING

REGIONS AT T=75 ˚C

Regions                  Rate Constants                   Intercept Constants                   R²

(dimensionless)                     (dimensionless)

1                               0.28                                       0.68                                  1

2                               0.23                                       0.62                                  1

3                               0.19                                       0.56                                  1

4                               0.09                                       0.54                                0.95

5                               0.01                                       0.51                                  1

The effect of temperature on the plugging mechanism is observed from the number of the plugging regions and the permeability reduction at various temperatures. The number of the plugging regions decreases by the temperature increases, the number of the plugging regions decreases from 9 to 5 when the temperature increases from 23.5 ˚C to 75 ˚C. Hence, the permeability reduction decreases from 0.36 to 0.42 when the temperature increases from 23.5 ˚C to 75 ˚C. This occurs because the gel particles become more deforming and pass easily through the pore throats at the high temperature. Therefore, plugging of pores by gel particles is less pronounced by increasing temperature and hence, permeability reduction decreases, as shown in Fig. 6.1.

6.4.1  Simultaneous fitting of correlation

Simultaneous  fitting  of  correlations  is developed by collecting the values of

A, B, and β from the exponential correlations of the thermal effects and plotted against temperatures, as shown in Figs. E.9 to E.19 given in Appendix E. The plotted A, B, and β were correlated as linear functions (y = ai + bix) where y represents A, B, and β; x represents temperatures; ai and bi represents initial guesses of parameters (See figures E.9 to E.19). By substituting the linear functions of A, B, and β in the relationships of the rate constants of plugging and unplugging and intercepts of plugging and unplugging regions, as shown in Eqs. 6.9 and 6.10, empirical correlations of the thermal effect on the rate and intercept constants of plugging and unplugging were developed which can be used for practical applications, as shown in Figs. 6.19 to 6.22. The rate constants of plugging and unplugging regions represent the slopes of the straight lines and not represent the permeability impairment (reduction), therefore the initial values of the curves are not 1, as shown in Figs. 6.19 and 6.20. The first region of the plugging starts from value 1 of the permeability impairment (reduction), therefore the curves of the intercept of plugging regions start from 1, as shown in Fig. 6.21.

(6.9)

(6.10)

where y represent the rate constants of the plugging and unplugging regions, dimensionless or the intercept of the plugging and unplugging regions, dimensionless; x represents the pore volume injected, dimensionless; T represents the temperature, °C; and a1, b1, a2, b2, a3, and b3 represent initial guesses, dimensionless.

Fig. 6.19: Rate constant of plugging at different pore volumes injected and

different temperatures

Fig. 6.20: Rate constant of unplugging at different pore volumes injected and

different temperatures

Fig. 6.21: Intercept of plugging regions at different pore volumes injected and

different temperatures

Fig. 6.22: Intercept of unplugging regions at different pore volumes injected and

different temperatures

6.5  Conclusions

The main findings of this experimental study can be summarized as the following:

- Quantitative evaluation of the thermal effect on the performance of gel particles applications was study for successful field applications of gel particle suspension injection. Thus, important empirical correlations for thermal effect were developed which can be used for controlling plugging in highly  permeable formations and conditioning of these formations by reducing the high permeability. Hence, we can  prevent loss circulation during drilling operations in formations having high permeability zones and control water production in waterflooded mature oil fields.

- The Vogel-Tammann- Fulcher (VTF) - type equation is used to correlate the experimentally measured data of the viscosity, differential pressure, permeability reduction, and resistance factor at various temperatures and an excellent agreement is observed between the experimental data and the correlations. Hence,  these correlations can be used to predict the effect of temperature on conditioning and reducing the high permeability of the formations by injection of a suspension of gel particles.

- The effect of temperature on plugging and unplugging phenomena which occurred during the injection of gel particles into the proppant pack was investigated and a decrease in  the number of plugging and unplugging regions  by increasing in temperature was observed. This occurs because the gel particles become more deforming and pass easily through the pore throats at high temperatures. Therefore, plugging of pores by gel particles becomes less pronounced by increasing temperature and   permeability   reduction   decreases. The   rate   constants   of   the   plugging   and

unplugging regions were determined and correlated successfully with temperature.

# Chapter 7:  Dimensional Analysis of Near-Wellbore Formation Treatment by Gel Particles Suspension

This  Chapter    has   been    previously    published   as ‘‘Evaluation  of   Near- Wellbore

Formation  Treatment   by   Gel   Particles   Using   Dimensional   Analysis’’ in  the SPE

Production  and  Operations Symposium, Oklahoma City, Ok, 23-26 March, 2013 and is

used here by permission.

7.1   Introduction

Several important factors affect the gel particles transport through porous media and hence the near-wellbore formation treatment by gel particles, including flow rate, gel particles concentration, gel particle diameter, pore-throat size, and temperature. However, concerning the transport of soft-gel particles through narrow pore throats in porous media, the deformation property is a particularly important factor that causes the oscillation phenomenon observed of the measured pressure differential and hence in the resulting permeability reduction trends. In fact, the dimensional analysis of the gel particles injection data presented in the following proves the importance of the deformation property of the gel particles. Because the overall phenomena of gel particles transport and entrapment in porous media involve many complicated processes, the difficulty of analyzing the experimental data is alleviated by developing dimensionless correlations which can assist in evaluating the near-wellbore formation treatment by gel particles.

The relevant dimensionless correlations of experimental data of gel particles plugging of porous media are developed based on the dimensional analysis method which can be used for effective design and monitoring of treatment of high-permeability

near-wellbore formation by gel particles suspension. The dimensionless groups are developed from the primary variables of the sand packs, gel particles suspension, and operation conditions. Step-by-step procedure of elimination of the basic dimensions was used for combination of variables into relevant dimensionless groups. The normalized dimensionless groups were used to correlate the measured permeability reduction by gel particles at different temperatures, concentrations, flow rates, and gel particles diameters. Comparison between correlated and measured permeability reduction indicates satisfactory results, especially for the limit value of the final permeability reduction. Hence, the effect of the ratio of the particle-diameter to pore-throat size on permeability reduction under various conditions is correlated successfully.

7.2  Relevant Dimensionless Groups

The permeability reduction data obtained from the tests of Al-Ibadi and Civan (2012, 2013a and 2013b) by gel particles suspension injection into sand packs at different temperatures, flow rates, gel particles diameters, and gel particles concentrations are now correlated by dimensional analysis. The dimensionless correlations of the experimental data are developed from dimensionless groups in normalized forms to accommodate for differences in the final limit values of permeability reduction attained under different conditions.

The actual variables used in this study are summarized in Table 7-1 and all the variables and their units are summarized in Table 7-2. The basic dimensions involved in this study are mass M, length L, time T, and temperature θ. Step-by-step procedure applied  for  derivation  of  the  relevant  dimensionless  groups involves the first step to

eliminate M, the second step to eliminate L, the third step to eliminate T, and the fourth step to eliminate K,  as illustrated in Table 7-2. The variables are grouped into several groups according to the initial system such as the porous media group, the gel particle suspension group, and the operation conditions group.

The dimensionless groups are obtained from the variables by means of the combination of variables method (Churchill 1997) and the number of dimensionless groups is equal to the number of the variables minus the number of the basic dimensions (Van Driest 1946). We have 14 variables and 4 basic dimensions as shown in Table 7-2. Therefore, the number of the dimensionless groups obtained from these variables is 10 as follows:

,                   ,    	             ,	                  ,                    ,

,                      ,                        ,                                               (7.1)

The dimensionless groups are manipulated to obtain conventional dimensionless group as the following, for example:

(7.2)

Table 7-1: Summary of Primary Variables

Variable Group       Variable     Unit                                 Values

Sand Pack                 Dg            µm          1015       650

Gel                     Dp                 µm           50          75         100        125          140

Cp            vol%        0.5%      1%         2%        3%

Test Conditions           v             cm/s        0.0072    0.0144    0.0288   0.0403    0.0576

θ                K           296.5      313        333       348

Table 7-2: Step-by-Step Elimination of the Fundamental Dimensions

Initial  Dimensions Step1 Eliminate Step 2 Eliminate Step 3 Eliminate Step 4 Eliminate

System                                     M                        L                         T                         K

Variables                  Vari.    Dimen.  Vari.    Dimen.    Vari.     Dimen.              Dimen.

Porous Media

K          L²            K           L²       K/z²:dim.    1

group

DT             L             DT         L        Dp/DT: dim. 1

group

A          L²            A           L²       A/z²: dim.   1

group

z           L              z           L         z: scaling    L

variable

L³/L³                     L³/L³                       L³/L³

Gel Particle Suspension

µ       M/LT         µ/ρ       L²/T          µ/ρ/z²     1/T    tµ/ρ/z²: dim.  1

group

µ/ρ/Dp²   1/T   tµ/ρ /Dp²: dim. 1

group

ρ       M/L³    ρ:scaling    M/L³

variable

Dp           L             Dp                L        Dp: scaling    L

variable

Cp     L³/L³          Cp         L³/L³              Cp         L³/L³

Operation Conditions

v      L/T             v         L/T	    v/z     1/T    tv/z: dim.     1

group

v/Dp     1/T     tv/Dp: dim.  1

group

t         T                t           T	      t        T      t: scaling      T

variable

∆p    M/LT²       ∆p/ρ     L²/T²          ∆p/ρ/z²  1/T²  t²∆p/ρ/z²: dim. 1

group

θ        K               θ          K                     θ       K                 θ	         K    θ: scaling    K

variable

c      L²/T²K          c     L2/T²K	   c/z2     1/T²K       t²c/z2     1/K      θt²c/z²        1

c/Dp²   1/T²K     t²c/Dp²   1/K     θt²c/Dp2       1

7.3.  Data Analysis and Correlation

The correlations of dimensionless groups, plots of data and correlations after normalization, and permeability obtained from dimensionless correlations are presented in the following.

7.3.1  Dimensionless groups selected for correlations

Although we determined 10 dimensionless groups, we only used 7 dimensionless groups to correlate the measure data obtained from the gel particle suspension injection into the sand pack at different concentrations, flow rates, gel particle diameter, and temperatures (Al-Ibadi and Civan 2012, 2013a, and 2013b). Dimensionless group Π2 combining Dp with DT show the effect of the ratio of the particle diameter (Dp) to the pore throat size (DT) (produced from the grain diameter (Dg) of the sand pack) on the permeability reduction (K/Ko). Dimensionless group Π4 combining µ, t, ρ and z variables show the effect of the suspension viscosity µ change with  the  gel  particle concentration (Cp) on the permeability reduction.   Dimensionless

group Π5 combining µ, t, ρ and Dp variables show the effect of the particle diameter (Dp) on the permeability reduction. Dimensionless group Π6 combining v, t, and z variables show the effect of the suspension velocity (v) on the permeability reduction.  Dimensionless group Π7 combining v, t, and Dp variables show the effect of the particle diameter (Dp) on the permeability reduction. Dimensionless group Π9 combining t, c, θ and z variables show the effect of the temperature (θ) on the permeability reduction. Dimensionless group Π10 combining t, c, θ and Dp variables show the effect of the particle diameter (Dp) on the permeability reduction. The following combined dimensionless group was also used to represent the permeability reduction (K/Ko):

(7.3)

To develop dimensionless correlations of the thermal effect on near well- bore formation treatment by gel particles, we used Π4 dimensionless group because it contains suspension viscosity (µ) affected by temperature and used Π9 dimensionless group because it contains the temperature (θ). The dimensionless correlation of the effect of the gel particle concentration on near well-bore formation treatment by gel particles is developed using Π4 dimensionless group because it contains suspension viscosity (µ) that increases by the gel concentration. To develop dimensionless correlation of the effect of the flow rate on near well-bore formation treatment by gel particles, we used Π6 dimensionless group because it contains suspension velocity (v). The dimensionless correlation of the effect of the gel particle diameter on near well- bore   formation   treatment   by   gel   particles  is  developed    using  Π5,  Π7,  and  Π10

dimensionless groups because they contain the particle diameter (Dp).

7.3.2  Dimensionless plots of experimental data

Figs. 7.1 and 7.2 show the Π4 and Π9 dimensionless groups for the permeability reduction at 3 vol% concentration for different temperatures at 100 cm³/h. These figures show that the maximum values of the dimensionless groups at 5 PVI different by the temperature. The values of  the Π4 dimensionless group are 1.04 at 23.5 ˚C, 0.95 at 40 ˚C, 0.76 at 60 ˚C, and 0.66 at 75 ˚C and for the Π9  dimensionless group are 1.50E+15 at 23.5 ˚C, 1.59E+15 at 40 ˚C, 1.69E+15 at 60 ˚C, and 1.77E+15 at 75 ˚C. Fig. 7.3 shows the Π4 dimensionless group for the permeability reduction at 100 cm³/hr for different concentrations at T= 23.5 ˚C. Fig. 7.3 shows that the maximum values of the Π4 dimensionless group at 5 PVI different by the gel particles concentration, 0.66 at 0.5% concentration, 0.76 at 1.0% concentration,  0.85 at 2.0% concentration, and 1.04 at 3.0% concentration. Fig. 7.4 shows the Π6 dimensionless group for the permeability reduction at 3 vol% concentration and 23.5 ˚C for different flow rates. The figure shows that the maximum values of the dimensionless group at 5 PVI different by the flow rate, 2.5 at 50 cm³/hr, 5 at 100 cm³/hr, 10 at 200 cm³/hr, 14 at 280 cm³/hr, and 20 at 400 cm³/hr. Figs. 7.5 to 7.7 show the Π5, Π7, and Π10 dimensionless groups for the permeability reduction at 100 cm³/hr  and 23.5 ˚C for different particle sizes for the sand pack of 1015 µm grain diameter.  The maximum values of the Π5, Π7, and Π10 dimensionless groups at 5 PVI different by the particle diameters are shown in Figs. 7.5 to 6.7. Figs. 7.8 to 7.10 show the Π5, Π7, and Π10 dimensionless groups for the permeability reduction at 100 cm³/hr  and 23.5 ˚C for different particle sizes for the sand pack of 650 µm grain diameter and  the maximum values of the dimensionless groups at 5 PVI different by the particle diameter.

Fig. 7.1: The dimensionless groups for permeability reduction at 3 vol%

concentration for different temperatures at 100 cm³/h

Fig. 7.2: The dimensionless groups for permeability reduction at 3 vol%

concentration for different temperatures at 100 cm³/h

Fig. 7.3: The dimensionless groups for permeability reduction at 100 cm³/h for

different concentrations at T= 23.5 ˚C

Fig. 7.4: The dimensionless groups for permeability reduction at 3 vol%

concentration for different flow rates at T= 23.5 ˚C

Fig. 7.5: The dimensionless groups for permeability reduction at 100 cm³/hr for

diameter different gel particle sizes at T= 23.5 ˚C for the sand pack of

1015 µm grain

Fig. 7.6: The dimensionless groups for permeability reduction at 100 cm³/hr for

different gel particle sizes at T= 23.5 ˚C for the sand pack of 1015 µm

grain diameter

Fig. 7.7: The dimensionless groups for permeability reduction at 100 cm³/h for

different gel particle sizes at T= 23.5 ˚C for the sand pack of 1015 µm

grain diameter

Fig. 7.8: The dimensionless groups for permeability reduction at 100 cm³/h for

different gel particle sizes at T= 23.5 ˚C for the sand pack of 650 µm grain

diameter

Fig. 7.9: The dimensionless groups for permeability reduction at 100 cm³/h for

different gel particle sizes at T= 23.5 ˚C for the sand pack of 650 µm grain

diameter

Fig. 7.10: The dimensionless groups for permeability reduction at 100 cm³/h for

different gel particle sizes at T= 23.5 ˚C for the sand pack of 650 µm

grain diameter

7.3.3  Normalized experimental data

The above direct plotting of the dimensionless groups revealed that the maximum limit values of the various dimensionless groups are different by their final limit values. Thus, it is inconvenient to correlate with the dimensionless groups directly. We resort to the following normalized values method in order to avoid this problem according to Civan (2011b).

(7.4)

where x is the value of the actual dimensionless group; x* is the normalized value of the dimensionless group; xmin is the minimum value of the dimensionless group; and xmax is the maximum value of the dimensionless group.

Figs. 7.11 and 7.12 show the normalized Π4 and Π9 dimensionless groups for the permeability reduction at 3 vol% concentration for different temperatures at 100 cm³/h and the correlation curves obtained by applying equation  B-2 given in Appendix B on the normalized dimensionless groups data, as shown in Figs. F.1 and  F.2 in Appendix F. Fig. 7.13 shows the normalized Π4 dimensionless group for the permeability reduction at 100 cm³/h for different concentrations at T= 23.5 ˚C and the correlation curve obtained by applying equation B-7 given in Appendix B on the normalized dimensionless group data, as shown in Fig. F.3 in Appendix F. Fig. 7.14 shows the normalized Π6 dimensionless group for the permeability reduction at 3 vol% concentration and 23.5 ˚C for different flow rates and the correlation curve obtained by applying equation  B-7 given in Appendix B on the normalized dimensionless group data, as  shown in Fig. F.4 in Appendix F. For  the permeability  reduction at 100 cm³/h

and 23.5 ˚C for different particle sizes for the sand pack of 1015 µm grain diameter, we obtained same values of the normalized dimensionless groups of Π5 , Π7 , and Π10 and same correlation curves by applying equation  B-2 on the normalized dimensionless group data. Therefore, we used only Π5 dimensionless group to correlate the data as shown in Fig. 7.15 for the sand pack of 1015 µm grain diameter and in Fig. 7.16 for the sand pack of 650 µm grain diameter, as shown in Figs. F.5 and  F.6 in Appendix F.

Fig. 7.11: Correlation of the normalized dimensionless groups for permeability

reduction at 3 vol% concentration for different temperatures at 100

cm³/h

Fig. 7.12: Correlation of the normalized dimensionless groups for permeability

reduction at 3 vol% concentration for different temperatures at 100

cm³/h

Fig. 7.13: Correlation of the normalized dimensionless groups for permeability

reduction at 100 cm³/h for different concentrations at T= 23.5 ˚C

Fig. 7.14: Correlation of the normalized dimensionless groups for permeability

reduction at 3 vol% concentration for different flow rates at T= 23.5 ˚C

diameter at different gel particles sizes

Fig. 7.15: Correlation of the normalized dimensionless groups for permeability

reduction at 100 cm³/hr for different gel particle sizes at T= 23.5 ˚C for

the sand pack of 1015 µm grain diameter

Fig. 7.16: Correlation of the normalized dimensionless groups for permeability

reduction at 100 cm³/hr for different gel particle sizes at T= 23.5 ˚C for

the sand pack of 650 µm grain diameter

7.3.4  Permeability Reduction Correlations

Figs. 7.17 and 7.18 show the measured permeability reduction (K/Ko) and the correlated permeability reduction obtained from the dimensionless correlations of the normalized Π4 and Π9 dimensionless groups for permeability reduction at 3 vol% concentration for different temperatures at 100 cm³/h. The measured data show permeability reduction from 0.36 to 0.415 by increasing the temperature from 23.5 ˚C to 75 ˚C. This means that the plugging of pores and pore- throats decreases by the temperature because the gel particles became more soft and deformable by temperature. The correlated data of  the normalized Π4 dimensionless group show permeability reduction from 0.366 to 0.427 and the normalized Π9 dimensionless group show permeability reduction from 0.358 to 0.417 by increasing the temperature from 23.5 ˚C to 75 ˚C.

Fig. 7.19 shows the measured permeability reduction and the correlated permeability reduction obtained from the dimensionless correlations of the normalized Π4 dimensionless group for permeability reduction at 100 cm³/h for different concentrations at T = 23.5 ˚C. The measured data show permeability reduction from 0.81 to 0.36 by increasing the gel particles concentration from 0.5% to 3.0% because the amount of particles plugging the pores increases by concentration. The correlated data of the normalized Π4 dimensionless group show permeability reduction from 0.80 to 0.354 by increasing the gel particles concentration from 0.5% to 3.0%.

Fig. 7.20 shows the measured permeability reduction and the correlated permeability reduction obtained from the dimensionless correlations of the normalized Π6 dimensionless group for permeability reduction at 3 vol% concentration and 23.5 ˚C for different flow rates. The measured data show permeability reduction increasing from 0.0.46 to 0.36 by increasing the flow rate from 50 cc/h to 100 cc/h and decreasing from 0.36 to 0.60 by increasing the flow rate from 100 cc/h to 400 cc/h because at the high flow rate the particles can pass easily through the pore throats and the plugging of pores decreases. The correlated data of the normalized Π6 dimensionless group show the same values of the measured permeability reduction when the flow rate increases from 50 cc/h to 100 cc/h and from 100cc/h to 400 cc/h.

Fig. 7.21 shows the measured permeability reduction and the correlated permeability reduction obtained from the dimensionless correlations of the normalized Π5  dimensionless  group   for   permeability  reduction   at 100 cm³/h   and  23.5  ˚C  for

different particle sizes for the sand pack of 1015 µm grain diameter. The measured data show permeability reduction from 0.54 to 0.30 by increasing the particle diameter from 50 µm to 400 µm because the plugging of pores increases by gel particle size. The correlated data of the normalized Π5 dimensionless group show permeability reduction from 0.544 to 0.30 by increasing the particle size from 50 µm to 140 µm.

Fig. 7.22 shows the measured permeability reduction and the correlated permeability reduction obtained from the dimensionless correlations of the normalized Π5 dimensionless group for permeability reduction at 100 cm³/hr  and 23.5 ˚C for different particle sizes for the sand pack of 650 µm grain diameter. The measured data show permeability reduction  from 0.34 to 0.27 by increasing the particle diameter from 50 µm to 100 µm and the  correlated data of the normalized Π5 dimensionless group show permeability reduction from 0.346 to 0.273 by increasing the particle size from 50 µm to 75 µm.

Fig. 7.17: Measured permeability reduction and correlated permeability reduction

( from  K∆pµovozo/Ko∆poµvz  and  (µt/ρz²)*  correlation) at  3 vol%

concentration for different temperatures at 100 cm³/h

Fig. 7.18: Measured permeability reduction and correlated permeability reduction

( from  K∆pµovozo/Ko∆poµvz  and  (t²cθ/z²)*  correlation) at  3 vol%

concentration for different temperatures at 100 cm³/h

Figure 7.19: Measured permeability reduction and correlated permeability

reduction ( from K∆pµovozo/Ko∆poµvz and (µt/ρz²)* correlation) at

100 cm³/h for different concentrations at T=23.5˚C

Figure 7.20: Measured permeability reduction and correlated permeability

reduction ( from K∆pµovozo/Ko∆poµvz and (vt/z)* correlation) at

3 vol% concentration for different flow rates at T= 23.5 ˚C

Figure 7.21: Measured permeability reduction and correlated permeability

reduction ( from K∆pµovozo/Ko∆poµvz and (µt/ρDp²)* correlation)

at 100 cm³/h for different gel particle sizes at T= 23.5 ˚C for the sand

pack of 1015 µm grain diameter

Figure 7.22: Measured permeability reduction and correlated permeability

reduction ( from K∆pµovozo/Ko∆poµvz and (µt/ρDp²)* correlation)

at 100 cm³/h for different gel particle sizes at T= 23.5 ˚C for the sand

pack of 650 µm grain diameter

7.4  Correlated Versus Measured Permeability Reduction

The correlated data of all the normalized dimensionless groups presented above show satisfactory results in comparison with the measured data of the permeability reduction. Thus, the dimensionless correlations can be used to predict the permeability reduction across the sand pack during the gel particles injection at any temperature, particle concentration, flow rate, and particle diameter. Figs. 7.23 to 7.28 show comparison between the measured permeability reduction and the correlated permeability reduction obtained from all the dimensionless correlations of all the normalized    dimensionless    groups    for   the    permeability   reduction   at   different

temperatures, particle concentrations, flow rates, and particle diameters. The plot of the correlated versus measured permeability reduction clusters close the diagonal-line indicating that the dimensional correlations represent the data satisfactory. Also, the accuracy is lower during the early injection period but improves rapidly as more pore volumes of suspension injected, as shown in the Figs. 7.29 to 7.34 of the steady limit value of correlated versus measured permeability reduction at 5 pore volumes injected (PVI). The reason of the scatter of the points and the lower accuracy during the early injection period is the consecutively occurring plugging and unplugging phenomena that were demonstrated in our previous studies (Al-Ibadi and Civan 2012, 2013a and 2013b). At the beginning of the gel particles injection, the particles are trapped at the entrance of the pore-throats causing a buildup in the differential pressure which subsequently leads to deformation and passing of the trapped particles through the pore-throats decreases the differential pressure. The plugging and unplugging processes induced by suspension injection repeat continuously until attaining a constant steady differential pressure and the permeability reduction reaches approximately a constant limit value.

Fig. 7.23: Comparison between measured permeability reduction and correlated

permeability reduction at 3 vol% concentration for different

temperatures at 100 cm³/h

Fig. 7.24: Comparison between measured permeability reduction and correlated

permeability reduction at 3 vol% concentration for different

temperatures at 100 cm³/h

Fig. 7.25: Comparison between measured permeability reduction and correlated

permeability reduction at 100 cm³/h for different concentrations at T=

23.5 ˚C

Fig. 7.26: Comparison between measured permeability reduction and correlated

permeability reduction at 3 vol% concentration for different flow rates

at T= 23.5 ˚C

Fig. 7.27: Comparison between measured permeability reduction and correlated

permeability reduction at 100 cc/h for different gel particle sizes at T=

23.5 ˚C for the sand pack of 1015 µm grain diameter

Fig. 7.28: Comparison between measured permeability reduction and correlated

permeability reduction at 100 cc/h for different gel particle sizes at T=

23.5 ˚C for the sand pack of 650 µm grain diameter

Fig. 7.29: Comparison between constant limit value of steady measured

permeability reduction and correlated permeability reduction at 5 PVI

for different temperatures

Fig. 7.30: Comparison between constant limit value of steady measured

permeability reduction and correlated permeability reduction at 5 PVI

for different temperatures

Fig. 7.31: Comparison between constant limit value of steady measured

permeability reduction and correlated permeability reduction at 5 PVI

for different concentrations

Fig. 7.32: Comparison between constant limit value of steady measured

permeability reduction and correlated permeability reduction at 5 PVI

for different flow rates

Fig. 7.33: Comparison between constant limit value of steady measured

permeability reduction and correlated permeability reduction at 5 PVI

for different gel particle sizes for the sand pack of 1015 µm grain

diameter

Fig. 7.34: Comparison between constant limit value of steady measured

permeability reduction and correlated permeability reduction at 5 PVI

for different gel particle sizes for the sand pack of 650 µm grain

diameter

7.5 Effect of Particle-Diameter to Pore-Throat Size Ratio on Permeability Reduction

The limit value of the steady measured permeability reduction at 100 cm³/h for 3 vol% concentration at T = 23.5 ˚C for different particle-diameter to pore-throat size ratios was correlated satisfactory in our previous studies (Al-Ibadi and Civan 2012 and 2013a) as shown in Fig. 7.35. The experimental data show a permeability reduction from 0.54 to 0.27 by increasing the ratio of particle-diameter to pore-throat size from 0.40 to 1.7 because pore plugging is enhanced by increase in the particle-diameter to pore-throat size ratio.

To correlate the effect of the ratio of the gel particle-diameter to the pore- throat size on the permeability reduction by gel particles, we used the Π2 dimensionless group that represents (Dp/DT). Figs. 7.36 and 7.37 show the limit value of steady measured and correlated dimensionless group and permeability reduction, respectively, at 100 cm³/h for 3 vol% concentration at T = 23.5 ˚C for different particle-diameter to pore-throat size ratios. The correlated data of the dimensionless group show satisfactory results compared with the measured data. Fig. 7.38 shows a comparison and satisfactory correlation between the constant limit values of the measured and correlated permeability reductions at 100 cc/h for 3 vol% concentration at T = 23.5 ˚C for different particle-diameter to pore-throat size ratios.

Fig. 7.35: Limit value of steady measured permeability reduction and correlated

permeability reduction at 100 cm³/h for 3 vol% concentration at T= 23.5

˚C for different particle diameter to pore-throat size ratios (Al-Ibadi and

Civan 2012 and 2013a)

Fig. 7.36: Limit value of steady measured and correlated π10 ″and  π2

dimensionless groups for permeability reduction at 100 cm³/h for 3 vol%

concentration at T= 23.5 ˚C for different  particle diameter to pore-

throat size ratios

Figure 7.37: Measured permeability reduction and correlated permeability

reduction ( from K∆pµovozo/Ko∆poµvz and Dp/DT dimensionless

groups) at 100 cm³/h for 3 vol% at T= 23.5 ˚C for different particle

diameter to pore-throat size ratios

Fig. 7.38: Comparison between constant limit value of measured permeability

reduction and correlated permeability reduction at 100 cm3/h for 3 vol%

concentration at T= 23.5 ˚C for different particle diameter to pore-throat

size ratios

7.6  Discussion and Conclusions

The dimensional analysis of the gel particles injection into the sand packs provided the following results and conclusions of practical importance:

- The evaluation of the near well-bore formation treatment by gel particles using dimensionless correlations was presented and various important dimensionless correlations were developed which can assist in designing for conditioning of the high permeability formations with gel particles.

- The original 14 variables of the sand packs, gel particles suspensions, and the operation conditions, were reduced to 10 dimensionless groups by means of the method of dimensional analysis. However, only 7 out of these 10 dimensionless groups were sufficient to obtain meaningful correlations of our experimental data.

- The maximum limit values of the dimensionless groups were observed to be different for different experimental conditions. This problem was alleviated conveniently by using the normalized dimensionless groups to obtain an effective correlation of the permeability reduction of the sand packs at different temperatures, concentrations, flow rates, and gel particles diameters.

- Comparison between the measured and correlated permeability reduction obtained from the normalized dimensionless groups was shown to yield a satisfactory match, especially at the steady limit values of permeability reduction.

- The effect of the ratio of the gel-particle to pore-throat size ratio on the permeability reduction by gel particles was correlated successfully using the dimensionless group involving the ratio of the gel-particle to pore-throat size.

- The outstanding advantage of using the normalized dimensionless groups rather than the actual variables is to be able to develop empirical correlations which are applicable also at field conditions which are different than the laboratory test conditions.

- The present dimensionless correlations can predict the evolving permeability reduction under the varying conditions of gel particles suspension injection processes. In contrast, the previous empirical correlations of gel particles injection can only provide an estimate of the final permeability reduction attained at the end of treatment.

- The particles trapped across the pore throats initially cause a pressure build-up (and permeability decrease) which eventually leads to deformation and passing of the particles through pore-throats resulting in a subsequent reduction of the differential pressure (and permeability increase). Thus, the measured and correlated permeability reduction show consecutively decreasing and increasing permeability trends (oscillation phenomenon) caused by the plugging and unplugging phenomena.

Chapter 8: Experimental Investigation and Correlation of Particle-Gel Systems for Near-Wellbore Water Shutoff  Treatments

8.1  Introduction

The particle- gel system was used as a method of near-wellbore formation treatment to prevent or control water production in waterfloooded mature oil fields. This system consists from a polymer/crosslinker as the gel and a silica flour as the particles to provide leak off control and act as a diverting filter cake ( Dalrymple et al. 2008; Ali et al. 2008; van Eijden et al. 2005). The gel squeezes into the matrix, developing a shallow matrix seal. One application of this system has been in wells where the water producing zones were identified and separated from the oil producing zones, wherein zonal isolation was not an option. The entire interval was treated and, following a shut-in period to allow the system to crosslink, the wellbore was cleaned with coiled tubing (CT) and the hydrocarbon zone could then be re-perforated. Dalrymple et al. (2008) applied 50 wt% silica flour concentration to achieve sufficient fluid loss control of the gel but it is desirable to lower this concentration.

Optimization particulate concentration, leak off, and threshold pressure are studied qualitatively and quantitatively by laboratory testing. To study the leak off, fluid loss tests are performed at constant pressure and the volume of the filtrate water is measured during the test. Effects of silica flour concentration, pore space of the permeable filter disk, sand size and temperature on the leak off and the pressure initiate flow  are  studied  by  adding different amount of silica flour to special gel system using

permeable filter disks of different pore spaces and sand of varying sizes and temperatures. The sand represents a gravel pack and the filter disc represents the formation. To study the threshold pressures, the pressures that initiate water flow  are measured after the fluid loss tests.

In the present study Empirical correlations and charts are developed from the experimental data which can be used to predict the fluid loss, the pressure necessary to initiate flow, and the filtrate volume at any silica flour concentration, pore diameter of formation, sand size, and temperature. Additionally, correlations for the critical silica flour concentration are developed which can be used to predict the critical silica flour concentration at any pore diameter of filter disc and sand size. The critical silica flour concentration is the concentration below which there is no effect on the filtrate volume and the pressure to initiate flow and above which the filtrate volume can decreases and the pressure initiate flow can increase. This study can aid the successful design to achieve optimal conformance control for reducing high permeability and controlling water production in waterflooded mature oil fields. Rather than correlating the individual data set, correlating the data in groups for similar tests to develop general correlations is preferred. This can help ensure the similar trends in correlations of all the data points of the measurement in a consistent manner so that the trends of correlations will be similar. Therefore, correlating data in groups is advantageous to obtain the best meaningful generalized correlations, which can aid the design of field scale applications at any conditions which could differ from conditions of the experimental study or measurements.

8.2  Analysis and Investigation of Experimental Results

Described next are the experimental investigation and phenomenological description of the filtrate loss and the pressure to initiate flow. The silica flour-gel system during fluid loss testing was passed through sand (gravel pack) similarly to filtration through a disc (formation), as shown in Fig. 8.1. Silica flour concentration in the system that reached the filtration disc was an important factor affecting filtrate loss and pressure to initiate flow because the silica flour became trapped in the pores of the filtrate disc, forming a filter cake.

Fig. 8.1- Convert the filtrate test from laboratory scale to field scale

For the same filter disc and silica flour concentration, the fluid loss of the silica flour-gel system were increased and the pressure to initiate flow was decreased by increasing the sand mesh because the sand and pore sizes were decreased. This leads to silica flour entrapment in the pores of the sand, causing the filter disc to have low concentration of silica flour, which caused low silica flour to be trapped in the pores of the filter disc and low filter cake formation on the filter disc, as shown in Fig. 8.2.

(c)

(b)

(a)

Fig. 8.2: The filtrate cake for same filter disc and same silica flour  concentration

and different sand sizes (a) 12/20  mesh (b) 20/40 sand   (c) 40/70 mesh

8.3   Development of Empirical Correlations

8.3.1  Fluid Loss

Empirical correlations from the experimental data were developed by considering several relevant parameters, such as silica flour concentration, sand size, and pore size of filter disc that effect fluid loss. Charts for practical applications of fluid loss were constructed by performing the following steps:

- Develop a relationship which correlates the experimental data of fluid loss percent with silica flour concentration.

- Determine the critical silica flour concentration for all experimental conditions.

- Correlate the experimental data at various conditions with the critical silica flour concentration.

- Apply the correlations of the experimental data developed above to construct charts of fluid loss  that can be used for practical applications at other conditions.

1-   Correlation of the Experimental Data of Fluid Loss

Experimental data were correlated by the following exponential relationship.

(8.1)

where y represents the fluid loss of the particle-gel system (%); x is the silica flour concentration (wt%); A, B, and α are empirical parameters (dimensionless), determined by applying Eq. B-6, given in Appendix B. For the same filter disc and different sand sizes, Figs. G.1 to G.3 show an exponential relationship between the fluid loss and silica flour concentration for 35, 10, and 5 micron average pore diameter of filter disc at different sand sizes. Figs. G.4 to G.6 show straight line plot of Eq. B-6 for 35, 10, and 5 micron pore diameter of filter disc at different sand sizes, given in Appendix G.

2-     Determination of the Critical Silica Flour Concentrations

The critical silica flour concentration is the concentration below which there is no effect on the fluid loss% and the pressure initiate flow and above which the fluid loss will decreases and the pressure initiate flow increases. The critical silica flour concentration represents the minimum value at which the fluid loss equal 100%. The critical silica flour concentrations were determined from the correlations developed in the following section at 100% fluid loss for all the experimental conditions, as shown in Table 8-1.

Table 8-1: CRITICAL SILICA FLOUR CONCENTRATIONS

Pore diameter of         Sand size               Critical silica

filter disc                                             flour concentration

(micron)                 (mesh)                          wt%

35                        12/20                           0.60

35                        20/40                           0.70

35                        40/70                           0.84

10                        12/20                           0.28

10                        20/40                           0.32

10                        40/70                           0.38

5                         12/20                           0. 08

5                         20/40                           0.15

5                         40/70                           0.20

3-     Correlation of the experimental data with the critical silica flour concentration

The experimental data were correlated with the critical silica flour concentration as a minimum value by used of the following exponential relationship.

(8.2)

where y represents the fluid loss of the particle-gel system (%); x is the silica flour concentration (wt%); xcr is the critical silica flour concentration (wt%); B, and α are empirical   parameters,  dimensionless,   determined  by  applying    Eq. B-10,  given  in

Appendix B. For the same filter disc and different sand sizes, Figs. G.7 to G.9 show an exponential relationship between the fluid loss and silica flour concentration for 35, 10, and 5 micron average pore diameter of filter disc at different sand sizes. Figs. G.10 to G.12 show straight line plot of Eq. B-10 for 35, 10, and 5 micron pore diameter of filter disc at different sand sizes, given in Appendix G.

4-      Development of charts for fluid loss

Charts of fluid loss were developed based on the exponential relationships of the experimental data with the critical silica flour concentrations which can be used to estimate the fluid loss of the particle-gel system at any silica flour concentration, pore diameter of filter disc, and sand size. The values of B, α, and xcr  were collected from the exponential relationships of same pore diameter of filter disc and different sand sizes and plotted against sand sizes, as shown in Fig. G.13 to G.21.  The plotted B, α, and xcr were correlated as linear functions (y = aix + bi) where y represents B, α, or xcr; x represents sand size; and ai and bi represent initial guesses of parameters (Figs. G.13 to G.21). By substituting the linear functions of B, α, and xcr in the exponential relationship, as shown in Eq. 8.3, empirical correlations were developed and used to construct charts of fluid loss at 35, 10, and 5 micron pore diameter of filter disc and different sand mesh, and different silica flour concentrations, as shown in Figs. 8.3 to 8.5.

(8.3)

where F.L. represents the fluid loss (vol%); Ds represents the sand diameter (micron); Cs represents the silica flour concentration (wt%); and a1, b1, a2, b2, a3, and b3 represent initial guesses (dimensionless). The values of the initial guesses of a1, b1, a2, b2, a3, and b3 in Eq. 8.3 were collected from the linear functions of 35, 10, and 5 micron pore diameter of filter disc and plotted against pore diameter of filter disc, as shown in Figs. G.22 to G.27 given in Appendix G. The parameters of a1, b1, a2, b2, a3, and b3 were correlated as linear functions (y = aix + bi) where y represents a1, b1, a2, b2, a3, or b3; x represents pore diameter of filter disc; and ai and bi represent initial guesses of parameters (Figs. G.22 to G.27). The linear functions of a1, b1, a2, b2, a3, and b3 were substituted in Eq. 8.3 and general empirical correlation of the fluid loss was developed which can be used at any pore diameter of filter disc, sand mesh, and silica flour concentration.

(8.4)

where DF represents pore diameter of filter disc, micron.  Fig. 8.6 shows the chart of fluid loss at 12/20 sand mesh and different pore diameters of filter disc and different silica flour concentrations which was developed by the general empirical correlation (Eq.8.4). Fig. 8.6 shows that for the same sand mesh and same silica flour concentration, the filtration volume of the silica flour-gel system increased by increasing the pore diameter of the filter disc because the silica flour was passed through the large pores of the filter disc and low silica flour was trapped in the pores and low filtrate cake was formed on the filtrate disc, as shown in Fig. 8.7.

Fig. 8.3: Experimental and correlated fluid loss at different silica flour

concentrations and different sand sizes for 35 micron pore diameter of

filter disc (Plot of Eq. 8.3)

Fig. 8.4: Experimental and correlated fluid loss at different silica flour

concentrations and different sand sizes for 10 micron pore diameter of

filter disc (Plot of Eq. 8.3)

Fig. 8.5: Experimental and correlated fluid loss at different silica flour

concentrations and different sand sizes for 5 micron pore diameter of

filter disc (Plot of Eq. 8.3)

Fig. 8.6: Experimental and correlated fluid loss at different silica flour

concentration and different pore diameters of filter discs for 12/20 sand

mesh (Plot of Eq. 8.4)

(c)

(b)

(a)

Fig. 8.7: The filtrate cake for same sand mesh and same silica flour  concentration

and different pore diameters of filter discs (a) 5 micron  (b) 10 micron  (c)

35 micron

8.3.2   Critical Silica Flour Concentration

The critical silica flour concentration represents the value of concentration at which the fluid loss and the pressure initiate flow change. The determination of the critical silica flour concentration is very important because it represents the initial condition of the empirical correlation for practical application. Charts of critical silica flour concentration were developed from the experimental data which can be used to estimate the critical silica flour concentration at any pore diameter of filter disc and sand size. The values of xcr of same pore diameter of filter disc and different sand sizes were calculated from the linear functions of figures G. 15, G.18, and G. 21 and plotted against sand sizes, as shown in Fig. H.1. The plotted xcr in Fig. H.1were correlated as linear functions and the values of A, and B were collected from the linear functions and plotted against sand size, as shown in Figs. H.2 and H.3. The plotted As and Bs were correlated again as linear functions (y = aix + bi) where y represents A, or B; x represents sand size, and ai and bi represent initial guesses of parameters (Figs. H.2 and H.3). The empirical correlation was developed by substituting the linear functions of A, and  B  in  the  critical  silica flour concentration  relationship, as shown in Eq. 8.5. This

empirical correlation was used to construct chart of critical silica flour concentration which can be used for practical applications, as shown in Fig. 8.8.

(8.5)

where xcr represents critical silica flour concentration (wt%); Ds represents sand diameter (micron); and DF represents pore diameter of filter disc (micron).

Fig. 8.8: Experimental and correlated critical silica flour concentration at

different sand sizes and different  pore diameter of filter discs (Plot of Eq. 8.5)

Fig. 8.8 shows that the critical silica flour concentration increased by increasing  the  pore  diameter  of  filter  disc because the silica flour passed through the

large pores of the filter disc and low silica flour trapped in the pores of the filter disc. The maximum value of the critical silica flour concentration is determine at the sand size equal zero. The maximum value of the critical silica flour concentration for 5, 10, 15, 25, 35, and 45 micron pore diameter of filter disc are 0.25, 0.36, 0.47, 0.68, 0.89, and 1.10 wt%, respectively. Fig. 8.8 shows that the critical silica flour concentration was decreased by increasing the sand size because the silica flour passed through the pores of the sand and the gel-particle system reached the filter disc at a high concentration of the silica flour. The minimum value of the critical silica flour concentration is zero and for 5, 10, 15, 25, 35, and 45 micron pore diameter of filter disc the minimum value of the critical silica flour concentration is determined at the sand size 2400, 3200, 3500, 3900, 4200, and 4400 micron, respectively.

8.3.3  Pressure Initiate Flow

Charts and empirical correlations were developed from the experimental data of several relevant parameters, such as pore size of filter disc, silica flour concentration, and sand size that effect pressure initiate flow. The experimental data of the pressure initiate flow were correlated with the critical silica flour concentration as an initial condition by the following relationship.

(8.6)

where y represents  the  pressure  initiate  flow (kPa); x is the  silica flour  concentration

(wt%); xcr is the critical silica flour concentration (wt%), were determined by applying Eq. 8.5; A, B, and α  are  empirical  parameters  (dimensionless),  were  determined   by

applying Eq. B-11, given in Appendix B. For the same filter disc and different sand sizes, Figs. I.1 to I.3 show the relationship between the pressure initiate flow and silica flour concentration for 35, 10, and 5 micron average pore diameter of filter disc at different sand sizes. Figs. I.4 to I.6 show straight line plot of Eq. B-11 at different sand sizes for 35, 10, and 5 micron pore diameters of filter disc.

To develop charts of pressure to initiate flow of same pore diameter of filter disc and different silica flour concentration and sand sizes, the values of A, B, and α  of the correlations were  plotted against sand sizes, as shown in Figs. I.7 to I.15, and correlated as linear functions (y = aix + bi) where y represents A, B, and α; x represents sand size, ai and bi represent initial guesses of parameters. These linear functions were substituted in Eq. 8.6 to get new empirical correlations used to construct charts of pressure initiate flow at 35, 10, and 5 micron pore diameter of filter disc and different sand sizes and silica flour concentrations, as shown in Figs. 8.9 to 8.11.

(8.7)

where P represents the pressure initiate flow (kPa); Ds represents the sand diameter, micron; Cs represents the silica flour concentration (wt%); xcr represents critical silica flour concentration (wt%); and a1, b1, a2, b2, a3, and b3 represent initial guesses (dimensionless). The  values  of   a1, b1, a2, b2, a3, and  b3  in  Eq. 8.7   were  plotted   against   pore diameter of filter disc and correlated as linear functions, as shown in Figs. I.16 to I.21 and substituted in Eq. 8.7 to develop a general empirical correlation of the pressure initiate flow which can be used at any pore diameter of filter disc, silica flour concentration, and sand size.

(8.8)

Fig. 8.12 shows application of Eq. 8.8 to calculate the pressure initiate flow at 12/20 sand mesh and different pore diameters of filter disc and different silica flour concentrations. Fig. 8.12 demonstrated that the pressure initiate flow for the same sand mesh and same silica flour concentration decreased by increasing the pore diameter of the filter disc because low silica flour was trapped in the large pores and low filtrate cake was formed, as shown in Fig. 8.7.

Fig. 8.9: Experimental and correlated pressure initiate flow at different silica flour

concentrations and different sand sizes for 35 micron pore diameter of

filter disc (Plot of Eq. 8.7)

Fig. 8.10: Experimental and correlated pressure initiate flow at different silica

flour concentrations and  different sand sizes for 10 micron pore diameter

of filter disc (Plot of Eq. 8.7)

Fig. 8.11: Experimental and correlated pressure initiate flow at different silica

flour concentrations and different sand sizes for 5 micron pore diameter

of filter disc (Plot of Eq. 8.7)

Fig. 8.12: Experimental and correlated pressure initiate flow at different silica

flour concentrations and different pore diameters of filter discs for 12/20

sand mesh (Plot of Eq. 8.8)

8.4  Thermal Effects

The fluid loss of the 2.8 wt% silica flour particle-gel system is studied at 35 micron pore diameter filter disc, 12/20 sand mesh and different temperatures of 23.5, 51, 68, and 83 °C. The filtrate tests results show an increase in the fluid loss of the silica flour particle-gel system by increasing the temperature. The fluid loss was increased from 11 to 12.5% by increasing the temperature from 23.5 to 83 °C. This happened because the viscosity of the silica flour particle-gel system decreases by temperature which lead to the particle-gel system pass through the pores easily. The viscosity decreases  from  0.059 to 0.027 Pa.s when the temperature increases from 23.5 to 83 °C.

The pressure initiate flow after the filtrate tests of the silica flour particle-gel system is studied at different temperatures of 23.5, 51, 68, and 83 °C. The experimental results show decreases in the pressure initiate flow by increasing the temperature. The pressure initiate flow  was decreased from 3100 to 2070 kPa by increasing the temperature from 23.5 to 83 °C. This happened because the degree of pore plugging by the silica flour particle-gel decreased by temperature.

8.4.1  Correlation of Thermal Effects

Empirical correlations of practical importance are developed from the experimental data at different temperatures for effective design of the silica flour particle-gel system application of near-wellbore formation treatment. The Vogel-Tammann- Fulcher (VTF)-type equations (Eq. 6.1) was used to correlate the experimental data for viscosity, the fluid loss, and the pressure initiate flow of the silica flour particle-gel system, as follows:

(8.9)

where µ is the viscosity (Pa.s), T is the actual temperature (K), µc is the pre-exponential coefficient of the viscosity = 0.0027 Pa.s, and Tc and C are 120 and -545 K, respectively.

(8.10)

where F.L. is the fluid loss (vol%), T is the actual temperature (K), (F.L.)c is the pre-exponential coefficient of fluid loss = 8.60 vol%, and Tc and C are 470 and 42.80 K, respectively. Further,

(8.11)

where P is the pressure to initiate flow (kPa), T is the actual temperature (K), Pc is the pre-exponential coefficient of pressure to initiate flow = 4824 kPa, and Tc and C are 420 and -54.18 K, respectively.

Figs. 8.13 to 8.15   show the straight- line VTF plots of the experimental data of the 2.8 wt% silica flour particle-gel viscosity, fluid loss, and pressure initiate flow . Figs. 8.16 to 8.18 show comparisons between the viscosity, fluid loss, and pressure to initiate flow values obtained from VTF equation and the experimental data.

Fig. 8.13: Straight- line VTF plot for the 2.8 wt% particle-gel system viscosity

Fig. 8.14: Straight- line VTF plot for the fluid loss

Fig. 8.15: Straight- line VTF plot for the pressure initiate flow

Fig. 8.16: Comparison between silica flour particle-gel system viscosity obtained

from the VTF equation and the measured data

Fig. 8.17: Comparison between fluid loss obtained from the VTF equation  and the

experimental data

Fig. 8.18: Comparison between pressure initiate flow obtained from the VTF

equation  and the experimental data

The experimental results show that when the temperature increased from 23.5 to 83°C, the viscosity of the 2.8 wt% silica flour particle-gel system deceased from 0.059 to 0.027 Pa.s, the fluid loss increased from 12.5 to 11%, and the pressure to initiate flow decreased from 3100 to 2070 kPa. The VTF correlations of viscosity, fluid loss, and pressure to initiate flow are close to the experimental data. Thus, the VTF equation can be used to predict viscosity, fluid loss, and pressure to initiate flow for a similar material and operational conditions at any temperature.

8.5   Conclusions

The primary findings of this experimental study can be summarized as follows:

- Quantitative  evaluation of various factors affecting the performance of silica

flour particle-gel applications was studied for successful field applications of particle-gel system injection. Thus, important empirical correlations were developed which can assist in conditioning of highly permeable formations by reducing the high permeability and increasing the pressure to initiate flow. Hence, operators can treat near-wellbore formations having high permeability zones and prevent or control water production in waterflooded mature oil fields.

- Instead of correlating individual data set, the data was correlated as groups and best meaningful generalized correlations and charts were developed which can help design silica flour particle-gel field trip applications at any operation conditions for near-wellbore formation treatment.

- The effects of temperature on the fluid loss and the pressure to initiate flow of the silica flour particle-gel process were investigated and an increase to fluid loss and a decrease to pressure initiate flow were observed. This occured because the silica flour particle-gel viscosity decreased by temperature which leads to the particle-gel system transport easily through the pores.

- Important empirical correlations for thermal effect with high agreement between the experimental data and correlations were developed using (VTF)- type equations, which can be used for successful design of the silica flour particle-gel system application of near-wellbore formation treatment.

# Chapter 9: Filtration Analysis of Particle-Gel Systems for Near-Wellbore Water Shutoff  Treatments

9.1   Introduction

The high permeability formations are prone to high water production occurrence in oil or gas producing wells which causes several undesirable problems to the oil industry. Using silica flour particle- gel system is a method to reduce or condition the high permeability of reservoir formation and thus avoid the water production problem. The leak off of the silica flour particle-gel system is studied by fluid loss tests at different silica flour concentrations, pore space of the permeable filter disc, and sand sizes. The rate constant of filtrate and spurt loss volume are determined and correlated with the silica flour concentration at different sand sizes and pore diameters filter discs. Exponential relationship is used to correlate the experimental data of the leak off tests of the silica flour particle-gel system and empirical correlations are developed of the filtrate volume of the silica flour particle-gel system at different sand sizes, pore diameters of the filter disc, and silica flour concentrations. The developed  empirical correlations can be used to predict the evolving filtrate volume and thus can assist in effective and successful design of silica flour particle-gel system used for near-wellbore formation treatment under varying conditions.

9.2   Development of Empirical Correlations of Filtrate Volume

The experimental data obtained from the tests of Al-Ibadi et al. (2015) by silica

flour particle- gel system are correlated by exponential relationship. Empirical correlations of filtrate volume of the silica flour particle-gel system were developed from the experimental data of the leak off tests at different silica flour concentrations, pore diameters of filter discs, and sand sizes. The experimental data were correlated by the following exponential relationship.

(9.1)

where y represents the filtrate volume of the particle-gel system, cm3; x is the filtrate time, min; A, B, and α are empirical parameters, dimensionless, were determined by applying Eq. B-6, given in Appendix B. Figs. 9.1 to 9.3 show the experimental filtrate volume (Vf) and the correlated filtrate volume obtained from the exponential relationship at 35 micron pore diameter of filter disc  for different sand sizes at 12/20, 20/40, and 40/70 sand mesh and different silica flour concentrations at 0.21, 0.53, 1.06, and 1.60 vol%. Figs. J.1 to J.3 show straight line plot of Eq. B-6 for 35 micron pore diameter of filter disc at different sand sizes and different silica flour concentrations. For same filter disc and same sand mesh, the experimental data show filtrate volume reduction  by increasing the silica flour concentration, for 35 micron pore diameter of filter disc and 12/20 sand mesh, the filtrate volume deceases from 76 cm3 to 5.5 cm3 by increases the silica flour concentration from 0.21 vol% to 1.60 vol%, as shown in Fig. 9.1. This happened because the amount of the silica flour trapped in the pores of the filter disc increased by silica flour concentration and high filtrate cake was formed on the filtrate disc, as shown in Fig. 9.4. For same filter disc and same silica flour concentration, the  experimental  data  show  filtrate volume increases  as the sand mesh

increases. For  35  micron   pore  diameter  of  filter  disc  and  1.06  vol%   silica   flour

concentration, the filtrate volume increases from 11 cm3 to 25 cm3 by increase of the sand mesh from 12/20 to 20/40, as shown in Figs. 9.1 and 9.2. This happened because the sand size was decreased and the pores size was decreased which lead to the silica flour entrapment in the pores of the sandpack and the silica flour particle-gel system that reached to the filter disc have low concentration of the silica flour. This causes low silica flour entrapment in the pores of the filter disc and low filtrate cake formation on the filter disc, as shown in Fig. 9.5.

Fig. 9.1: Exponential relationship between filtrate time and filtrate volume at 35

micron pore diameter of filter disc and 12/20 sand mesh for different

silica flour concentrations

Fig. 9.2: Exponential relationship between filtrate time and filtrate volume at 35

micron pore diameter of filter disc and 20/40 sand mesh for different

silica flour concentrations

Fig. 9.3: Exponential relationship between filtrate time and filtrate volume at 35

micron pore diameter of filter disc and 40/70 sand mesh for different

silica flour concentrations

(b)

(a)

(c)

(d)

Fig. 9.4: The filtrate cake for same sand mesh and same filter disc and different

silica flour concentrations   (a) 0.21 vol%   (b) 0.53 vol%   (c) 1.06 vol%

(d) 1.60 vol%

(c)

(b))

(a)

Fig. 9.5: The filtrate cake for same filter disc and same silica flour  concentration

and different sand sizes (a) 12/20  mesh (b) 20/40 sand   (c) 40/70 mesh

Figs. 9.6 to 9.11 show the experimental filtrate volume (Vf) and the correlated filtrate volume obtained from the exponential relationship at 10 and 5 micron pore diameters filter discs for different sand sizes at12/20, 20/40, and 40/70  sand  mesh  and  different  silica  flour  concentrations at 0.21, 0.53, 1.06, and 1.60 vol%. Figs. J.4 to J.9

show straight line plot of Eq. B-6 for 10 and 5 micron pore diameters filter disc at different sand sizes and different silica flour concentrations. For the same sand mesh and same silica flour concentration, the experimental data show filtrate volume increases  as the pore diameter of the filter disc increases. For 12/20 sand mesh and 1.06 vol% silica flour concentration, the filtrate volume increases from 1 cm3 to 7 cm3 by increase of the pore diameter of the filter disc  from 5 micron to 10 micron, as shown in Figs. 9.6 and 9.9. This happened because the silica flour passed into the large pores of the filter disc and low silica flour was trapped in the pores and low filtrate cake was formed on the filtrate disc, as shown in Fig. 9.12.

Fig. 9.6: Exponential relationship between filtrate time and filtrate volume at 10

micron pore diameter of filter disc and 12/20 sand mesh for different

silica flour concentrations

Fig. 9.7: Exponential relationship between filtrate time and filtrate volume at 10

micron pore diameter of filter disc and 20/40 sand mesh for different

silica flour concentrations

Fig. 9.8: Exponential relationship between filtrate time and filtrate volume at 10

micron pore diameter of filter disc and 40/70 sand mesh for different

silica flour concentrations

Fig. 9.9: Exponential relationship between filtrate time and filtrate volume at 5

micron pore diameter of filter disc and 12/20 sand mesh for different

silica flour concentrations

Fig. 9.10: Exponential relationship between filtrate time and filtrate volume at 5

micron pore diameter of filter disc and 20/40 sand mesh for different

silica flour concentrations

Fig. 9.11: Exponential relationship between filtrate time and filtrate volume at 5

micron pore diameter of filter disc and 40/70 sand mesh for different

silica flour concentrations

(b)

(a)

Fig. 9.12: The filtrate cake for same sand mesh and same silica flour concentration

and different pore diameter of filter discs (a) 5 micron  (b) 10 micron

9.3   Correlations of Rate Constant of Filtrate and Spurt Loss Volume

The experimental results of the fluid loss tests showed a reasonable relationship between the filtrate volume and the silica flour concentration, sand size, and pore diameter of filter disc. The filtrate volume decreased by silica flour concentration and sand size increased and the filtrate volume increased as the pore diameter of the filter disc increased. For the fluid loss test, the rate constant of filtrate and the spurt loss volume are important variables because they give a good idea about the expected filtrate volume during the fluid loss test. Figs. 9.13 to 9.15 show the filtrate volume of the silica flour particle-gel system during the fluid loss test for different silica flour concentrations, pore diameters filter discs, and sand sizes. The filtrate volume is modeled and represented as straight line plots shown in Figs. 9.19 to 9.21. The slops of the straight lines represent the rate constants of filtrate and the intercepts represent the spurt loss volumes. Table 9-1  shows the rate constants of filtrate and the spurts loss volumes of the silica flour particle-gel system at different sand sizes, pore diameters of the filter discs, and silica flour concentrations. The rate constants of the filtrate and spurt loss volumes decreased by silica flour concentrations and sand sizes because the pores plugging increased and increased by pore diameters of the filter discs because the pores plugging decreased. Figs. K.1 and K.2 in Appendix K show the relationship between the rate constants of filtrate and spurt loss volumes and the silica flour concentrations of the particle-gel system at different sand sizes and pore diameters of the filter discs. The rate constant of the filtrate and the spurt loss volumes are correlated by using Eq. B-6 given in Appendix B, as shown in Figs. K.3 to K.8. The rate  constants  of  the  filtrate  and  the  spurt  loss  volumes  were  correlated  using  the

exponential relationship shown in Eq. 6.7. The correlations showed intersection between them because of the individual data correlation, as shown in Figs. K.1 and K.2. The correlations are simultaneously fitted by collecting the empirical parameters values from the correlations and plotted against the sand sizes and pore diameters of the filter discs  correlated as linear functions, as shown in Figs. K.9 to K.14. The linear functions of A, B, and β are substituted in the exponential relationships of the rate constants of the filtrate and spurt loss volumes and the empirical correlations are developed which can be used to predict the filtrate volume of the silica flour particle-gel system at any conditions, as shown in Figs. 9.16 and 9.17.

Fig. 9.13: Experimental and correlated filtrate volume of 35 micron pore diameter

filter disc and 12/20 sand mesh for different silica flour concentrations

Fig. 9.14: Experimental and correlated filtrate volume of 35 micron pore diameter

filter disc and 20/40 sand mesh for different silica flour concentrations

Fig. 9.15: Experimental and correlated filtrate volume of 35 micron pore diameter

filter disc and 40/70 sand mesh for different silica flour concentrations

TABLE 9-1:  RATE   CONSTANTS    OF    FILTRATE   AND   SPURT   LOSS VOLUME OF 35 MICRON PORE DIAMETER FILTER DISC AT DIFFERENT SAND SIZES AND DIFFERENT SILICA FLOUR CONCENTRATIONS

Sand size            Silica Flour                 Rate Constant          Spurt Loss              R²

(mesh)         Concentration (vol%)        (cm³/min1/2)          Volume (cm³)

12/20                      0.21                                 3.64                    67.80                0.99

0.53                                 1.23                    29.64                0.67

1.06                                 0.74                      7.10                0.94

1.60                                 0.67                      2.08                0.97

20/40                      0.21                                 6.17                    67.10                0.81

0.53                                 1.20                    44.20                0.60

1.06                                 0.61                    21.70                0.98

1.60                                 0.39                      8.00                0.90

40/70                      0.21                                 3.42                    73.00                 1

0.53                                 1.64                    56.00                0.60

1.06                                 0.99                    21.95                0.95

1.60                                 0.64                       9.51               0.99

Fig. 9.16: Rate constant of filtrate of 35 micron pore diameter filter disc at

different silica flour concentrations and  different sand sizes

Fig. 9.17: Spurt loss volume of 35 micron pore diameter filter disc at

different silica flour concentrations and  different sand sizes

9.4 Conclusions

The main findings of the filtrate analysis of performance of the silica flour particle-gel system are the following:

- Filtrate analysis was used to evaluate the performance of the silica flour particle-gel applications in near-wellbore formation treatment and various important empirical correlations were developed which can assist in effective and successful designing for near-wellbore formation treatment with silica flour particle-gel system.

- The correlated filtrate volume obtained from the exponential relationship showed satisfactory match with the experimental filtrate volume.

- The effect of the silica flour concentration, sand size, and pore diameter of filter disc on the filtrate volume of the silica flour particle-gel system was investigated and a decrease in the filtrate volume by increasing the silica flour concentration and sand size and an increase in the filtrate volume by increasing the pore diameter of the filter disc were observed.

- The rate constants of filtrate and spurt loss volumes were determined and correlated successfully with the silica flour concentration, sand size, and pore diameter filter disc.

Chapter 10: Near-Wellbore Formation Treatment Design

10.1  Introduction

The objective of this chapter is to demonstrate the importance of the empirical correlations developed in this study for choosing suitable treatment fluids and evaluating the near-wellbore formation treatment under optimum application conditions. The developed empirical correlations are used to determine the treatment fluid properties and the modification of the near-wellbore formation after the treatment process. Two cases of treatment design are presented involving synthetic examples of gel-particle suspension and silica flour particle-gel systems.

10.2  Synthetic Field Application of Gel-Particle Suspension

The synthetic field application represents a well under drilling operations (Fig. 10.1) and the parameters of the synthetic well and fiels reservor shown in Table 10-1. Drilling fluid loss occurred through the sandstone bed because of the high permeability of the sandstone bed. Gel-particle suspension is used to treat and modify the sandstone bed permeability to prevent the drilling fluid loss. Table 10-2 shows the properties of the gel-particle suspension and the modification of the sandstone bed after treatment that should be determined to design the treatment process. For the near-wellbore formation treatment by the gel-particle suspension, empirical correlations were used for the treatment design. Table 10-3 shows a summary of the empirical correlations developed in this study.

Fig. 10.1: Schematic of synthetic well under drilling process

operations

TABLE 10-1: PARAMETERS OF SYNTHETIC WELL AND FIELD

RESERVOIR

Hole size, casing ID = 8 in

Thickness of the sandstone bed = 200 ft

Penetrate of the invaded zone = 3ft

Porosity = 0.38

Permeability = 3800 md

BHT = 125 °F

TABLE 10-2: PARAMETERS OF THE GEL-PARTICLE SUSPENSION AND

THE NEAR-WELLBORE FORMATION MODIFICATION

Suspension volume required (bbl)

Carrier fluid volume required (bbl)

Xanthan powder weight required (lb)

Polymer (gel particles) weight required (lb)

Injection flow rate of the suspension (bbl/day)

Time required to inject the suspension (hr)

Suspension viscosity (Pa.s)

Permeability reduction (dimensionless)

Resistance factor (dimensionless)

TABLE 10-3: SUMMARY OF THE EMPIRICAL CORRELATIONS OF THE GEL-PARTICLE

SUSPENSION DEVELOPED IN THIS STUDY

Correlation Name                        Empirical Correlation	                                     Symbols

Viscosity correlation                                                                  µ: suspension viscosity, Pa.s

Cp: suspension concentration, vol%

Differential pressure	         ΔP: differential pressure, kPa

correlations                                                                         q: injection flow rate, cm3/hr

Dp: gel-particle diameter, µm

Permeability reduction                                                                                      : permeability reduction,

correlations                                                                                                   dimensionless

Correlation Name                      Empirical Correlation	                                            Symbols

Resistance factor                                                                                       Fr: resistance factor,

correlations                                                                                                  dimensionless

Power-law equation                                                                                 β: pore-throat/particle-diameter

ratio, dimensionless

Exponential-law                                                                                       Rep: particle Reynold number,

equation                                                                                                        dimensionless

Thermal effect                                                                                             T: temperature, k

correlations

The steps of the treatment design calculations are as follows.

The wellbore volume = 3.141 × 0.333² × 200 = 69.80 ft³. Wellbore + 3 ft penetration volume = 3.141 × 3.333² × 200 = 6980 ft³. Volume for 3 ft matrix penetration = (6980- 69.80) × 0.38 = 2626 ft³. Volume for casing fill + 20% = 69.80 + (0.2 × 69.80) = 83.76 ft³. Volume of suspension required = 83.76 + 2626 = 2709.76 ft³ (643.46 bbl). For 3 vol% gel particle suspension. Volume of gel particles required = 0.03 × 643.46 = 19.30 bbl. Volume of carrier fluid required = 643.46- 19.30 = 624.16 bbl. 0.25 gm of Xanthan powder was added to 500 cm³ (0.004193 bbl ) water to prepare the carrier fluid. Weight of  the  Xanthan  powder  required =                                         gm = 37.214 kg (16.88lb). For the suspension experiments, 100 cm³/hr injection flow rate was used for sandpack of 1 in diameter. The  suspension velocity (v) =         . where A is the cross sectional area of the sandpack.                                       cm/hr. For same suspension velocity in the formation, the injection flow rate of the suspension in the Field (q): q = v × A × Φ. where A is the cross sectional treatment area of the sandstone bed. A = π × d × h. where d is the diameter of the well and h is the thickness of the sandstone bed. A = 3.141 × 0.667 × 200 = 419 ft². v = 51.94 cm/hr = 1.704 ft/hr. q = 1.704 × 419 × 0.38 = 271.32 ft³/hr = 64.43 bbl/hr = 1546 bbl/day. Time required to inject the suspension to the wellbore and the formation (t): t = Total volume of the suspension/ Injection flow rate of the suspension. t = 643.46/64.43 = 10 hrs. Viscosity of 3 vol% gel particle suspension at 125 °F (324.82 K) temperature: By using the correlation given in Table 10-1, suspension viscosity = 0.00442 Pa.s. Permeability reduction of 3800 md permeability of the sandstone at 125 °F temperature: By using the correlation given in Table 10-1, permeability  reduction  (K/Ko) = 0.39. Permeability  decreased  from  3800

md to 1482 md by the suspension treatment. Resistance factor (Fr) at 125 °F = 11.1 by using the correlation given in Table 10-1. Table 10-4 shows the results of the design of the near-wellbore formation treatment by the gel-particle suspension to prevent the drilling fluid loss during the drilling operations. Fig. 10.2 shows flow chart of the process of the near-wellbore formation treatment by gel-particle suspension.

TABLE 10-4: RESULTES OF THE NEAR-WELLBORE FORMATION

TREATMENT DESIGNE BY THE GEL-PARTICLE SUSPENSION

Suspension volume required = 643.46 bbl

Carrier fluid volume required = 624.16 bbl

Xanthan powder weight required = 16.88 lb

Polymer (gel particles) volume required = 19.30 bbl

Injection flow rate of the suspension = 1546 bbl/day

Time required to inject the suspension = 10 hr

Suspension viscosity = 0.00442 Pa.s

Permeability reduction (K/Ko) = 0.39

Permeability after treatment = 1482 md

Resistance factor = 11.1

Near-wellbore formation treatment

by gel-particle suspension

Parameters of the well

and field reservoir

Suspension injection through

porous media experiments

Parameters of the gel-

particle suspension

Thermal effect

correlations

Permeability reduction

correlations

Resistance factor

correlations

Injection flow rate

required in the field

Volume of the suspension

required for treatment

Weight of Xanthan

Powder required

Time required to

inject the suspension

Volume of gel

particles required

Volume of carrier

fluid required

Resistance factor of the

treated formation

Permeability modification of

the treated formation

Fig. 10.2: Process of the near-wellbore formation treatment by gel-particle

suspension

10.3  Synthetic Field Application of Silica Flour Particle-Gel System

The synthetic field application represents oil producing well (Fig. 10.3) of parameters show in Table 10-5 and with three perforated zones (Table 10-6) (van Eijden et al. 2004). The middle sands were flushed and producing predominantly water. The well was producing 3000 bbl/day with a water cut of 63 %. Gel-cement system treatment was applied of the perforated zones at maximum pressure of 1500 psi for 30 minutes, thus the water shutoff was achieved by the cement plugged in the perforations and the gel penetrated three inch through the matrix (formation). The wellbore was washed to remove excess gel-cement and the well was shut in for 48 hrs. The upper and lower zones were re-perforated and the initial production was 4500 bbl/day at 40% water cut. The production logging tool (PLT) showed no flow coming from the middle zone. It was found that the main problem for the gel-cement system is the interaction between the cement retarders and the gel. The cement worked as a fluid loss agent in the gel-cement system. van Eijden 2005 replaced the cement by a silica flour which is an inert material, and developed particle-gel system. 50 wt% of silica flour was used in the particle-gel system which causes logistics problem and  results in wellsite handling issues (Dalrymple et al. 2008). Fluid loss experiments were conducted on different silica flour particle-gel systems to minimize and optimize the silica flour concentration, as shown in chapter 8. Silica flour particle-gel system of 4.20 wt%  (1.60 vol%) silica flour concentration was developed from the fluid loss experiments, which can be used for the near-wellbore formation treatment. Table 10-7 shows the components of the silica flour-particle gel system developed from the fluid loss experiments.

Fig. 10.3: Schematic of synthetic oil producing well

TABLE 10-5: PARAMETERS OF SYNTHETIC OIL PRODUCING

WELL

Hole size, casing ID = 7.0 in

Tubing ID = 3.5 in

Oil production rate = 3000 bbl/day

Water cut = 63 %

Porosity = 0.22

BHP = 1500 psi

BHT = 90 °C

TABLE 10-6: PERFORATION ZONES OF SYNTHETIC PRODUCING

OIL WELL

Zone                       Perforation Interval, m	   Net Thickness, m

Upper zone                      2864.0- 2867.0                           3.0

2872.0- 2873.0                           1.0

2873.5- 2878.0                           4.5

2883.0- 2892.0                           9.0

Middle zone                    2892.5- 2896.0                            3.5

2901.0- 2904.0                           3.0

2905.0- 2914.0                           9.0

2917.0- 2925.0                           8.0

Lower zone                      2933.0- 2944.0                         11.0

2943.0- 2948.0                           5.0

The steps of the treatment design calculations as follows. The wellbore volume = 3.141 × 0.292² × 275.52 = 73.79 ft³. Wellbore + 3 in penetration   volume = 3.141 ×0.542² × 275.52 = 254.23 ft³.  Volume  for  3  in  formation  penetration  = (254.23- 73.79) × 0.20 = 36.09 ft³. Volume  for casing fill + 20% = 73.79 + (0.20 × 73.79) = 88.55 ft³. Volume of gel-particle system required = 36.09 + 88.55 = 124.64 ft³ = 932.29 gal = 29.60 bbl. Empirical correlations of the silica flour particle-gel system were developed from the experimental data, as shown in Table 10-8.

The  developed  empirical  correlations  were  used  for   treatment   design  as

follows. For pore diameter of filter disc (Ds) = 35 micron and sand diameter (Ds) = 1260 micron (12/20 sand mesh). The critical silica flour concentration = 0.62 wt% by using the correlation given in Table 10-8. By using the correlation given in Table 10-8, the fluid loss for 4.20 wt% silica flour particle-gel system = 6 vol% and for 50 wt% silica flour particle-gel system = 0 vol%. This fluid loss for 100 cm3 silica flour particle-gel system and the fluid loss for 29.60 bbl silica flour particle-gel system = 1.77 bbl. By using the correlation given in Table 10-8, the pressure initiate flow = 3478 kPa and for 50 wt% silica flour particle-gel system = 4510 kPa. By using the correlation given in Table 10-9, the filtrate rate constant for 4.20 wt% silica flour particle-gel system = 0.49 cm3/ min1/2 and for 50 wt% silica flour particle-gel system = 0 cm3/ min1/2. For 30 minute treatment time and 29.60 bbl particle-gel system, the filtrate volume = 0.49 × (30)1/2 = 2.68 cm3 for 100 cm3 = 0.79 bbl for 29.60 bbl. By using the correlation given in Table 10-8, the spurt loss volume for 4.20 wt% silica flour particle-gel system = 1.80 cm3 and for 50 wt% silica flour particle-gel system = 0 cm3. This spurt loss volume for 100 cm3  particle-gel system and for 29.60 bbl = 0.53bbl. Total filtrate volume = filtrate volume at 30 minutes + spurt loss volume = 0.79 + 0.53 = 1.32 bbl.

A comparison was conducted between the particle-gel system that was used for the field application and the particle-gel system that was developed from the experiments, as shown in Table 10-9. Table 10-9 shows that the difference between the results of the treatment design of both particle-gel systems is low, thus the 50 wt% silica flour concentration is very high and should be minimized. Fig. 10.4 shows flow chart of the process of the near-wellbore water shutoff treatment by silica flour particle-gel system.

TABLE 10-7: COMPONENTS OF THE SILICA FLOUR PARTICLE-GEL

SYSTEM DEVELOPED FROM FLUID LOSS EXPERIMENTS

Water = 16.02 bbl

Silica flour =  0.47 bbl

KCl = 1.89 bbl

Polymer 1 = 0.08 bbl

Polymer 2 =  9.51 bbl

Crosslinker =  1.63 bbl

Particle-gel system volume = 29.06 bbl

TABLE 10-8: SUMMARY OF THE EMPERICAL CORRELATIONS OF THE SILICA FLOUR

PARTICLE-GEL SYSTEM

Correlation Name                        Empirical Correlation	                                                                 Symbols

Critical silica flour	                                                                                                xcr: critical silica

flour conce-

concentration                                                                                                                            ntration, wt%

correlation                                                                                                                         DF: pore diameter

filter disc, micron

Fluid loss

Ds: sand diameter,

correlation                                                                                                                                  micron

F.L.: fluid loss, %

Pressure initiate                                                                                                                   Cs: silica flour

concentration,

flow correlation                                                                                                                        wt%

P: pressure initiate

flow, kPa

Thermal effect                                                                                                                    µ: silica flour

particle-gel

correlations                                                                                                                            viscosity, Pa.s

T: temperature, k

Correlation Name                       Empirical Correlation	                                         Symbols

y(0.21%) = 8.3exp(2.063x0.02)

y(0.53%) = 6exp(1.623x0.03)

Filtrate volume                                                                                    y: filtrate volume, cm3

correlations for 35                                                                                                x: filtrate time, min

y(1.06%) = 4exp(0.670x0.12)

micron disc and

y(1.60%) = 1exp(0.927x0.02)

12/20 mesh sand

y(12/20) = 16exp(-2.91x0.38)

Filtrate rate constant                                                                             y: filtrate rate constant,

cm3/min1/2

y(20/40) = 40exp(-3.80x0.31)

correlations for 35

x: silica flour

y(40/70) = 54exp(-4x0.29)

micron disc                                                                                                                 concentration, vol%

y(12/20) = 84exp(-2.155x1.20)

y(20/40) = 93exp(-1.588x1.10)

Spurt loss volume                                                                                y: spurt loss volume, cm3

correlations for 35                                                                                                x: silica flour

concentration, vol%

y(40/70) = 98exp(-1.304x1.05)

micron disc

TABLE 10-9: COMPARISON BETWEEN FIELD PARTICLE-GEL SYSTEM

AND EXPERIMENT PARTICLE-GEL SYSTEM

Properties                         Field Gel-Particle           Experiment Gel-Particle

System   	       System

Silica flour concentration (wt%)                     50                                         4.20

Fluid loss (vol%)                                               0                                            6

Pressure initiate flow (kPa)                           4510                                        3478

Filtrate rate constant (cm3/min1/2)                     0                                           0.49

Filtrate volume at 30 minutes (bbl)                   0                                           0.79

Spurt loss volume (bbl)                                     0                                           0.53

Total filtrate volume (bbl)                                 0                                           1.32

Near-wellbore water shutoff treatment

by silica flour particle-gel system

Parameters of the silica flour

Particle-gel system

Fluid loss and pressure

Initiate flow experiments

Parameters of the

Producing well

Volume of the particle-gel

system required for treatment

Filtrate rate constant

correlations

Pressure initiate

flow correlations

Spurt loss volume

correlations

Fluid loss

correlations

Thermal effect

correlations

Spurt loss

volume

Pressure initiate

flow

Filtrate rate

constant

Fluid loss

volume

Volume of KCl

required

Volume of crosslinker required

Volume of polymer

2 required

Volume of polymer

1 required

Volume of silica

flour required

Volume of water

required

Fig. 10.4: Process of the near-wellbore water shutoff treatment by particle-gel

system

Chapter 11: Summary, Discussion, and Conclusions

Heterogeneous formations around wellbore are been treated using gel particles suspensions and silica flour particle-gel slurry systems without much in depth investigations of the relevant and operating principles involved in the treatment of near-wellbore zones. Therefore, this work has focused on understanding of the operating principles and conditions by means of investigations of various issues involved in the effective treatment of heterogeneous formations by gel-particles suspensions injection and application of silica flour particle-gel systems. The discussion and conclusions of the various issues investigated in this dissertation can be summarized in the following sections. These will be presented in two groups experimental and theoretical studies.

11.1 Experimental Investigations

A- Fluid loss control treatment

In this study fluid loss control using gel particles suspension was investigated for the effect of gel particles concentration, gel particle diameter, flow rate, temperature, and particle diameter to pore-throat size on controlling lost circulation of drilling fluids during drilling operations. The experimental work demonstrated that the permeability modification of the high permeability formation increases by the gel particles concentration, gel particle diameter, and particle diameter to pore- throat size increases because the plugging of the pores by the gel particles increases. Also, the permeability modification  become  les s pronounced  with  flow  rate  increases because the particles

deposition over the pore surfaces decreases and mobilization of particles from pore surfaces increases by flow rate increases. The degree of pore-throat plugging and pore-surface deposition decreased when temperature increased and thus the permeability modification decreased when temperature increased.

B- Water shutoff treatment

In this study water shutoff treatment using silica flour particle-gel slurry system was investigated for the effect of silica flour concentration, temperature, sand size, pore diameter of formation material on controlling water production in hydrocarbon producing wells. The experimental work demonstrated that the fluid loss decreases and the pressure required to initiate water flow increases by silica flour concentration and sand size increase because the silica flour trapped in the pores of formation and forming a filter cake. The fluid loss increases and the pressure required to initiate flow decreases by pore diameter of formation and temperature increase because the particle-gel slurry system pass through the pores of formation easily without forming filter cake.

11.2 Theoretical Studies

A- Fluid loss treatment

a- Development of empirical correlations in actual variables of gel particles concentration, gel particle diameter, flow rate, temperature, and particle diameter to pore-throat size which effect on the permeability modification of the near-wellbore formation. Further, the dimensionless forms of these correlations were also developed.

b- Theoretical  descriptions of  various  plugging and  unplugging  mechanisms  causing

permeability modification. Further, the correlations of rate constant of plugging and unplugging processes at various temperatures were also developed.

B- Water shutoff treatment

a- Development of empirical correlations in actual variables of silica flour concentration, temperature, sand size, and pore diameter of formation which effect the fluid loss of silica flour particle-gel slurry systems and the pressure required to initiate water flow after water shutoff formation treatment.

b- Theoretical description of filtration analysis of silica flour particle-gel system and empirical correlations of the rate constant of filtrate and spurt loss volume were developed.

C- Field scale treatment design

a- Fluid loss treatment design

The developed correlations were used in designing of near-wellbore formation treatment by the gel particle suspension to control the drilling fluid loss of a well under drilling operations and the required volume of the gel particles suspension and the components of the suspension were determined. The permeability modification of the near-wellbore formation after the treatment was also determined.

b- Water shutoff treatment design

The developed correlations were used in the design of the near-wellbore water shutoff treatment by the silica flour particle-gel slurry system to control the water production of an oil producing well and the required volume of the silica flour particle-gel slurry system and the components of the slurry were determined. The fluid loss of the silica flour particle-gel slurry system and the pressure required to initiate water flow after the treatment were also determined.

11.3 Overall accomplishment and benefits

The correlations developed in this dissertation and the application demonstrated examples can be beneficial in scientifically-guided applications and understanding of fluid-loss control by gel particles  suspension and water shutoff treatment by silica flour particle-gel slurry system for field applications. Specifically, the investigations and studies presenting in this work provide:

a- Dimensionless empirical correlations can help in applications in the field for conditions that may be different than conditions of the experimental studies conducted in this work because dimensionless numbers are applicable under similar conditions.

b- The equations describing the various plugging and unplugging mechanisms can help in developing calculational  procedures for simulation and theoretical investigation of the consequences of field treatment.

c- The methodology demonstrating the applications of field fluid-loss control and water shutoff treatments provide a useful example of how the correlations developed in this study can be applied in optimal design of other practical field treatment cases.

# References

Al-Ibadi,  A.  and  Civan,  F.  2012.  Experimental   Study  of   Gel   Particles  Transport

through  Porous   Media. Paper SPE 153557 presented  at  the  SPE  Latin   American

and   Caribbean   Petroleum  Engineering   Conference, Mexico   City, Mexico, 16- 18

April.

Al- Ibadi,  A. and   Civan, F.  2013a: Experimental   Investigation   and   Correlation  of

Treatment   in   Weak   and    High- Permeability    Formations    by    Gel    Particles.

Paper  SPE 153557, Journal of  SPE  Production and  Operations, Vol. 28, No. 4, pp.

387-401.

Al- Ibadi,  A.  and   Civan, F.  2013b: Experimental   Investigation   and  Correlation  of

Thermal  Effects  on  Near-Wellbore  Formation  Treatment  by  Gel  Particles. Paper

SPE-164119      presented   at   the   SPE   International    Symposium    on     Oilfield

Chemistry,   The Woodlands, TX, USA, 8-10 April.

Al- Ibadi,   A.   and     Civan,  F.   2013c:  Evaluation    of    Near-Wellbore    Formation

Treatment    by   Gel   Particles   Using   Dimensional   Analysis.  Paper  SPE  164507

presented  at  the  SPE  Production and  Operations Symposium, Oklahoma City, OK,

USA, 23-26 March .

Al- Ibadi,   A.,    Civan,  F.,    and    Eoff, L.  2015:   Experimental    Investigation    and

Correlation  of  Particle-Gel  Systems  of  Near-Wellbore  Water  Shutoff  Treatments.

Paper   SPE   173627  will  be  presented   at  the  SPE   Production   and    Operations

Symposium, Oklahoma City, OK, USA, 1-5 March .

Ali, E.,  Bergen, F.,  Demestre, P.,  Biezen, E.,  and  van  Eijden, J. 2008.  Effective Gas

Shuttoff    Treatments  in  a  Fractured  Carbonate  Field in Oman. Paper SPE 102244

presented  at the Annual  Technical Conference and Exhibition, San Antonio, Texas,

24-27 September. DOI:10.2118/102244-MS.

Almohsin, A.,  Bai, B.,  Imqam, A.,  Wei, M.,  Kang, W.,  Delshad, M., Sepehrnoori, K.

2014. Transport of Nanogel through Porous Media and Its Resistance to Water Flow.

Paper SPE 169078  presented  at  SPE  Improved   Oil  Recovery  Symposium, Tulsa,

Oklahoma, USA, April 12-16.

Baghdikian, S., Sharma, M., Handy, L. 1989. Flow of Clay Suspensions Through Porous Media. Paper SPE  16257- PA, SPE Reservoir Engineering Journal, May 1989.

Bai, B., Liu, Y., and  Coste, J., P. 2007. Performed Particle Gel Conformance Control: Transport Mechanism through  Porous  Media. SPE Reservoir Evaluation and  Engineering 10176-184. SPE 89468- PA. DOI: 10.2118/89468- PA.

Bonet, J. and Wood, R.D. 2008. Nonlinear Continuum Mechanics for Finite Element Analysis, Second Edition, Cambridge University Press, New York.

Burya, Y. G., Yudin, I. K., Dechabo, V. A., Kosov, V. L., and Anisimov M. A. 2001. Light-Scattering Study of Petroleum Asphaltene Aggregation. Journal of Applied Optics, Vol. 40, No. 24, pp. 4028-4035.

Chauveteau, G., Omari, A., Tabary, R., Renard, M., and Rose, J. 2000. Controlling Gelatiom Time and Microgel Size for Water Shutoff. Paper SPE 59317 presented at the SPE/DOE Improved Oil Recovery Symposium, Tulsa, 3-5 April. DOI: 10.2118/59317- MS

Chauveteau, G., Omari, A Tabary, R., Renard, M.,Veerapen, J., and Rose, J. 2001. New Size- Controlled Microgels for Oil Production. Paper SPE 64988 presented at the SPE International Symposium on Oilfield Chemistry, Houston, 13-16 February. DOI: 10.2118/64988- MS.

Chauveteau, G., Tabary, R., Le Bon, C., Renard, M., Feng, Y., and Omari, A. 2003.In-Depth Permeability Control by Adsorption of weak size-Controlled Microgels. Paper SPE 82228 presented at the SPE European Formation Damage Conference, The Hague, 13-14 May. DOI: 10.2118/82228- MS.

Churchill, S.W. 1997. A new approach to teaching dimensionless analysis. Chemical Engineering Education, 30, pp. 158-165.

Civan,  F.  1990.  A  Generalized   Model   for   Formation    Damage   by   Rock-Fluid

Interactions  and Particulate Processes. Paper SPE 21183 presented at the SPE Latin

American  Petroleum  Engineering Conference, Rio de Janeiro, Brazil, October 14-19.

Civan, F. 1996. A Multipurpose Formation Damage Model. Paper SPE 31101 presented

at the  SPE Formation Damage Symposium, Lafayette, Louisiana, USA, February 14-

15.

Civan, F. 2000.Reservoir Formation Damage- Fundamentals, Modeling, Assessment, and Migration, Gulf Pub. Co., Houston,  TX,  742p.

Civan, F. 2004. Temperature  Dependence of  Wettability  Related  Rock  Properties  Correlated by  the  Arrhenius Equation. Petrophysics 45 (4): 350- 362.

Civan, F. 2005. Applicability of the VTF Type Asymptotic Exponential Functions for Ice, Hydrates, and Polystrene Latex. J. of Colloid and Interface Science 285: 429- 432.

Civan, F. and Nguyen, V. , 2005, “Modeling Particle Migration and Deposition in Porous Media by Parallel Pathways with Exchange,” Chapter 11, Handbook of Porous Media, Second Edition, Vafai, K. (Ed.), CRC Press,Taylor& Francis Group, LC, Boca Raton, FL, pp. 457-484.

Civan, F. 2006a. Viscosity Temperature Correlation for Crude Oils Using an Arrhenius Asymptotic Exponential Function. Petroleum Science and Technology 24 (6): 699- 706.

Civan, F. 2006b. Discusion of a Practical Method for Anticipating Asphaltene Problems. SPEPO 21 (3): 411. SPE- 104235- PA. DOI: 10.2118/104235- PA.

Civan, F. 2007a. Reservoir  Formation  Damage  Fundamentals, Modeling, Assessment

and Mitigation, Second Edition, Elsevi-er, Gulf Professional. Pub., Burlington, MA, 1114p.

Civan, F. 2007b. Temperature Effect on Power for Particle Detachment from Pore Wall Described by an Arrhenius- Type Equation. Transport in Porous Media 67 (2): 329- 334.

Civan, F. 2007c. Critical Modification to the Vogel- Tammann- Fulcher Equation for Temperature Effect on the Density of Water. Industral Engineering & Chemistry Research Journal 46 (17): 5810- 5814.

Civan, F. 2008. Use Exponential Functions to Correlate Temperature Dependence. Chemical Engineering Progress 104 (7): 46- 52.

Civan, F. 2010, Non-isothermal Permeability Impairment by Fines Migration and Deposition in Porous Media including Dispersive Transport, Transport in Porous Media: Vol. 85, Issue 1, pp. 233-258.

Civan, F. 2011a, Correlate Data Effectively, Chemical Engineering Progress, Vol. 107, No. 2, pp. 35-44.

Civan, F. 2011b. Porous Media Transport Phenomena. John Wiley and Sons, Hoboken, 463p.

Civan, F. and Rasmussen, M.L. 2005. Analytical Models for  Porous Media Impairment

by Particles in Rectilinear  and  Radial  Flows. In  Handbook of Porous Media, second

edition, ed. K. Vafai, Chap. 12, 485–542. Boca Raton, Florida: CRC Press.

Coste, J.P., Liu, Y., Bai, B. et al.2000. In Depth  Fluid Diversion by Pre Gelled Particles. Laboratory study and Pilot  Testing. Paper SPE 59362 presented at the SPE/DOE Improved Oil Recovery Symposium, Tulsa, 3-5 April. DOI: 10.2118/59362- MS.

Dalrymple,  D.,  Eoff,  L.,  Vasques, J.,  and  van  Eijden, J. 2008.  Shallow   Penetration

Particle-Gel  System  for Water  and  Gas Shuttoff  Applications. Paper SPE 114886

presented at the  Russian Oil & Gas Technical Conference and Exhibition, Moscow,

Russian, 28-30 October. DOI:10.2118/114886-MS.

Engel, A.  2000. The  role of  transparent  exopolymer  particle  (TEP) in the increase in

apparent  particle  stickiness  (α)  during  the  decline  of  a  diatom bloom. Journal of

Plankton Research 22: 485-497.

Feng, Q., Chen, X., and Zhang, G. 2013. Experimental and Numerical Study of Gel Particles Movement and Deposition in Porous Media After Polymer Flooding, Transport in Porous Media: Vol. 96. Issue 1.

Feng, Y., Tabary, R., Renard, M., Le Bon, Omari, A., and Chaveteau, G. 2003. Characteristics of Microgels Designed for  Water  Shutoff  and  Profile Control.  Paper  SPE  80203 presented at the SPE international.

Fileding, R. C. Jr., Gibbons, D. H,  and  Legrand, F. P. 1994 . In Depth  Drive Fluid Diversion   Using    An    Evaluation    of    Colloidal    Dispersion    Gels   and    New

Bulk Gels: An Operational Case History of North Rainbow  Ranch Unit. Paper SPE 27773 presented at the SPE/DOE Improved   Oil Recovery Symposium.  Tulsa ,  17-20  April .  DOI: 10.2118/ 27773- MS.

Fulcher, G.S. 1925. Analysis of Recent Measurements of the Viscosity of Glasses. J. Am. Ceram. Soc. 8: 339–355.

Gao, T., Hu, H.H. and Castaneda, P.P. 2011. Rheology of a Suspension of Elastic Particles in a Viscous Shear Flow. J. Fluid Mech., Vol. 687, pp. 209-237.

Goldsztein, G.H. 2005. Volume of Suspension that Flows through a Small Orifice before It Clogs. SIAM Journal of Appl. Math., Vol. 66, No. 1, pp. 228-236.

Gruesbeck, C. and  Collins, E. 1982. Entrapment   and   Deposition  of  Fine Particles in

Porous  Media. Journal of the Society of     Petroleum Engineers: 847-856.

Iscan,  A.G.   and   Civan, F.  2006. Correlation  of   Criteria  for   Perforation  and  Pore

Plugging by Particles, Journal of Porous Media, Vol. 9, No. 6, pp. 541-558.

Iscan, A.G., Kok, M.V., and Civan, F. 2009. Investigation of Porosity and Permeability Impairment in Sandstones by X-Ray Analysis and Simulation,” Energy Sources, Part A, Vol.31, No. 5, pp. 387-395.

Kiørboe, T., Andersen, K.P. and Dam, H.G. 1990. Coagulation efficiency and aggregate

formation in marine phytoplankton. Marine Biology Journal 107(2): 235–245.

Lane, R. H  and  Seright , R. S. 2000. Gel   Water  Shutoff  in Fractured or Faulted Horizontal  Wells.  Paper    SPE   65527  presented  at  the  SPE/ CIM  International   Conference on Horizontal Well Technology, Calgary, 6-8 November. DOI: 10.2118/ 65527- MS.

Littmann, w. 1988. Polymer Flooding, Elsevier Science Publishing Company Inc.

Messeenger  J. U.1981. Lost  Circulation,  Pennwell   Publishing  Co., Tulsa,112P.

Monkos, K., 2003.A  Method of  Calculations of  the Parameters in the VTFs Equation:

An Application to the Porcine Serum Albumin Aqueous Solutions. Current Topics in Biophysics 27 (1–2): 17–21.

Muhammed, F., Bai, B., and Al Brahim, A. 2014. A Simple Technique to Determine the Strength of Millimeter-Sized Particle Gel. Paper SPE 169106 presented at SPE Improved Oil Recovery Symposium, Tulsa, Oklahoma, USA, April 12-16.

Peifeng, H., Jianjun, L., and  Xiang, H.  2010. Pore Structure Effect on the Permeability

of   porous   Media. Proceedings   of  2010  International   Symposium  on  Multi-field

Coupling Theory of Rock and Soil Media and Its Applications, Chengdu  City, CH-   INA. ISBN: 978- 0- 9807687- 2- 5.

Potanin,  A. A.  and  Uriev,  N.B.  1991.  Micro-rheological   Models   of   Aggregated

Suspensions in Shear Flow. Journal of Colloid and Interface Science 142(2): 385-395.

Prada, A.,   Civan,  F., and  Dalrymple, D.  2000. Evaluation   of  Gelation  Systems  for

Conformance  Control.  Paper  SPE  59322  presented  at the Improved Oil Recovery

Symposium, Tulsa, Oklahoma, 3-5 April.

Pu, C.S. 2008. Surface  Deposition  and  Micro-Dispersed  Migration  Dynamics of  in

Liquid-Solid System. Petroleum Industry Press, Beijing.

Sato,  T.,   Mitsuhori, K.,  Hirabayashi, S.,  Brumby, P.E.,  Nagao, J.,  Temma, N.,  and

Narito, H. 2013. Microscale Numerical Simulation of the Permeability Reduction due

to  Trapping of Suspended  Fine  Particles Within Sand Sediments. Transport in Porou

Media, Vol. 96, pp. 153-167.

Seright, R.S.1997. Use of Preformed gels for Conformance Control in Fractured System

. SPEPE, 12(1): 59-65. SPE- 35351- PA. DOI: 10. 2118/35351-PA.

Seright, R. S.2000. Gel  Propagation Through Fractures. Paper SPE 59316 Presented at

The  SPE/ DOE    Improved    Oil   Recovery   Symposium,    Tulsa,  3-5  April.  DOI:

10.2118159316-MS.

Sydansk, R. D. and Southwell, G.P. 2000. More Than 12 Years Experience With a Successful Conformance- Control Polym-er- Gel Technology. SPEPF 15 (4): 270- 278. SPE – 66558- PA. DOI: 10.2118/66558- PA.

Tammann, G. and Hesse, W.1926.  Die  abhängigkeit der viskosität von der temperature bei unterkühlten flüssigkeitn. Z. Anorg. Allg. Chem. 156: 245–257.

Taylor, G.I. 1932. The Viscosity of a Fluid Containing Small Drops of Another Fluid. Proc. Roy. Soc., 138 A, pp. 41-48.

Taylor, G.I. 1934. The  Deformation of Emulsions in Definable Fields of Flow. Proc. Roy. Soc., 146 A, pp. 501-523.

Tran, T.V., Civan, F., and Robb, I. 2009. Correlating Flowing Time and Condition for Perforation Plugging by Suspended Particles. Paper SPE 120473, presented at the 2009 SPE Production and Operations Symposium, Oklahoma City, OK, USA, 5-7 April.

Tran, T.V., Civan, F., and Robb, I. 2010a. Effect of Permeability Impairment by Suspended Particles on Invasion of Drilling Fluids. Paper SPE IADC/SPE 133724, presented at the IADC/SPE Asia Pacific Drilling Technology Conference and Exhibition, Ho Chi Minh City, Vietnam, 1-3 November 2010.

Tran, T.V., Civan, F., and Robb, I. 2010b. Correlating Flowing Time and Condition for Plugging   of   Rectangular   Openings, Natural   Fractures, and   Slotted     Liners   by

Suspended Particles. Paper SPE 126310, presented at the 2010 SPE International Symposium and Exhibition on Formation Damage Control, Lafayette, Louisiana, USA, 10-12 February.

Van Driest, E.R. 1946. On  dimensional  analysis  and  the  presentation of data  in fluid

flow  problems. Journals of Applied Mechanics, 13, P. A34.

van  Duuren, F. A. 1968. Defined  velocity  gradient  model  flocculator. Journal  of  the

Sanitary  Engineering  Divison:  Proceeding   of   the   American   Society  of   Civil

Engineers 94: 671–682.

van Eijden, J., Arkesteijn, F.,  Akil, E., Vliet, J.,  Batenburg, D.,  and  McGinn, P. 2004.

Gel- cement, a   water   shut-off   system:  qualification  in  a  Syria  field. Paper   SPE

88765  presented  at  the  11th  Abu   Dhabi  International   Petroleum  Exhibition   and

Conference, Abu Dhabi, U.A.E., 10-13 October.

van Eijden, J., Arkesteijn, F., van  Batenburg, D.,  and  van Vliet, J. 2005. Development

and   Field   Application  of a Shallow   Perforation  Shuttoff  System  for  HP-HT  Oil

Wells.   Paper SPE 94518 presented at the 6th European Formation Damage

Conference, Scheveningen, The Netherlands, 25-27 May. DOI: 10.2118/94518-MS.

Vogel, H. 1921. Das temperature-abhängigketsgesetz der viskosität von flüssigkeiten. Phys. Zeit. 22: 645–  646.

Wang, H. G., Guo, W. K., and Jiang, H. F. 2001. Study and Application of Weak Gel   System Prepared by Complex  Polymer Used for Depth Profile Modification.

Paper SPE 65379 presented at the SPE International Symposium on Oilfield Chem-istry, Houston, 13- 16 February. DOI: 10.2118/65379- MS.

Wang, H., Sweatman, R., Engelman, B. et al. 2008. Best Practice in  Understanding and

Managing Lost Circulation Challenges. SPE Drill & Compl 23 (2): 168–175.

SPE95895-PA. http://dx.doi.org/10.2118/ 95895-PA.

Wang, J.,  Liu, H.,  and  Wang,  Z.  2012. Experimental   Investigation  on  the  Filtering

Flow  Law of  Pre-gelled Particle in Porous Media. Transport in Porous Media, Vol.

94, pp. 69-86.

Wojtanowicz, A. K.,  Krilow, Z., and  Langlinas, J. P. 1987. Study on the Effect of Pore Blocking Mechanisms on Formation   Damage. Paper SPE 16233, Presented at SPE Production Operations Symposiums, Oklahoma City, Oklahoma, USA, March 8-10.

Zamani, A.  and  Maini, B.  2009. Flow of Dispersed  Particles  through  Porous  Media-

Deep Bed Filtration. J. Pet. Sci. Eng., Vol. 69, pp. 71-88.

Zeinijahromi, A., Vaz, A. and Bedrikovetsky, P. 2012. Effects  of Fines  Migration  on

Well  Productivity  during   Steady  State  Production. Journal of  Porous  Media, Vol.

15, pp. 665-679.

Zhang, H., and Bai, B. 2010. Preformed Particle Gel Transport Through Open Fractures and its Effect on Water  Flow. Paper SPE-129908 presented at the SPE Improved Oil Recovery Symposium, Tulsa, OK, USA, 24-28 April.

Zheng, L.H., Kong, L., Cao, Y., Wang, H., and Han, Z. 2012. Anew Fuzzy Ball Working Fluid for Plugging Lost Circulation Paths in Depleted Reservoirs. Petroleum Science and Technology, Vol. 30, pp. 2517-1530.

Appendix A: Nomenclature

International system of units (SI units) were used in this dissertation and the units inside the parentheses represent the SI derived units that were used also in this dissertation.

a = empirical parameter, dimensionless

ai = initial guesses of parameters  (unit determined by the type of property)

a1 = initial guesses (unit determined by the type of property)

a2 = initial guesses (unit determined by the type of property)

a3 = initial guesses (unit determined by the type of property)

A = empirical parameter (unit determined by the type of property)

A = cross sectional area of the sand pack, m2 (cm2)

A1 = empirical parameter, dimensionless

A2 = empirical parameter, dimensionless

Ak and C = fitting constant (E/Rg), K

b = empirical parameter, dimensionless

bi = initial guesses of parameters  (unit determined by the type of property)

b1 = initial guesses (unit determined by the type of property)

b2 = initial guesses (unit determined by the type of property)

b3 = initial guesses (unit determined by the type of property)

b4 = initial guesses (unit determined by the type of property)

b5 = initial guesses (unit determined by the type of property)

b6 = initial guesses (unit determined by the type of property)

b7 = initial guesses (unit determined by the type of property)

b8 = initial guesses (unit determined by the type of property)

b9 = initial guesses (unit determined by the type of property)

B = empirical parameter (unit determined by the type of property)

Bs = left Cauchy-Green or Finger tensor, dimensionless

B1 = empirical parameter, dimensionless

B2 = empirical parameter, dimensionless

c = specific heat capacity, m²/s²K (cm²/s²K)

cgp = gel particles mass concentration, kg/m3 (mg/L)

cw = produced fines concentration, %

C = empirical parameter, dimensionless

Co = particle concentration at the time o, no.dm-1

Cp =  particle concentration, vol% or wt%

Cs = silica flour concentration, wt% or vol%

Ct  = total amount of produced fines per unit well length, m2

C1 = empirical parameter, dimensionless

C2 = empirical parameter, dimensionless

C3 = empirical parameter, s ̄ ¹ (min  ̄ ¹)

C4 = empirical parameter, s ̄ ¹ (min  ̄ ¹)

C5 = empirical parameter, s ̄ ¹ (min  ̄ ¹)

df = diameter of a frame sand grain, m (µm)

dq = diameter of a fine particle, m (µm)

Db = cell body diameter, m (µm)

DF = pore diameter of filter disc, m (µm)

Dg = grain diameter, m (µm)

DP = gel-particle diameter, m (µm or cm)

Dpmax = maximum gel-particle diameter, m (µm)

Dpmin = minimum gel-particle diameter, m (µm)

Ds = sand diameter, m (µm)

DT = pore throat diameter, m (µm)

en = restitution coefficient, dimensionless

eτ = friction coefficient, dimensionless

E = activation energy (J/kmol)

f = temperature dependent parameter (unit determined by the type of property)

fc = pre- exponential coefficient (unit determined by the type of property)

F = deformation gradient tensor, dimensionless

F.L. = fluid loss, vol%

(F.L.)c = pre-exponential coefficient of fluid loss, vol%

Fr = resistance factor, dimensionless

(Fr)c = pre- exponential coefficient of  resistance factor, dimensionless

F(x) = cumulative particle distribution, %

G = viscous forces in the fluid to the elastic forces in the elastic solid particle,

dimensionless

Gm = mean shear rate of the Coutte Chamber system, s-1

H = Hamaker coefficient of particle and surface interacting through the pore fluid

present in between them, J

j  = impedance, dimensionless

k = absolute permeability, 1 D= 9.869233*10-13 m²  (md)

kmax  = threshold number of particles for the first time, dimensionless

kr = constant, dimensionless

krowi = oil relative permeability at initial water saturation, 1 D= 9.869233*10-13 m²

(md)

k(V) = number of particles arriving simultaneously at the opening, dimensionless

K = suspension permeability, 1 D= 9.869233*10-13 m² (md)

Ko = initial permeability, 1 D= 9.869233*10-13 m² (md)

Kw = water permeability, 1 D= 9.869233*10-13 m² (md)

l = separation distance between the particle surfaces in filter cake, m (cm)

M = skin growth coefficient, dimensionless

N = average number of particles forming fractal aggregation, dimensionless

pi = productivity index, dimensionless

P = differential pressure, kPa

Pc = pre- exponential coefficient of pressure, kPa

Pf = position vector for a frame sand grain, m (µm)

Po = initial pressure, kPa

Pq = position vector for a fine particle, m (µm)

q = injection flow rate, m3/s (cm3/min)

qw = water flow rate, m3/s (cm3/h)

r = radius, m (µm)

r1 = radii of the inner cylinder of the system, m (cm)

r2 = radii of the outer cylinder of the system, m (cm)

re = drainage radius, m

rw = well radius, m

R = instantaneous mean aggregate radius, m (µm)

Rep = particle Reynolds number, dimensionless

Rg =  universal gas constant , J/kmol- K

Ro = initial particle radius, m (µm)

R2 = regression coefficient, dimensionless

S = gel particle area, m² (µm²)

Sw = water saturation, %

SHRgp = gel particle shear breaking ratio, dimensionless

SWRgp = gel particle swelling ratio in polymer solution, dimensionless

t = time, s (min)

td = dimensionless plugging time, dimensionless

T = temperature, K (°C)

Tc = critical temperature, K

Tck = characteristic-limit absolute temperature, K

Tik = reference absolute temperature, K

uq  = particle velocity before the collision, m/s

U = flow velocity, m/s

ν  = velocity , m/s (cm/s)

νw  = water flow velocity, m/s

Vf = volume of fluid loss, m³ (cm3)

VGel = volume of gel in 1 ml of suspension, m³ (µm³)

x = independent variable, dimensions determined by application

x = ratio of distance, dimensionless

x* = normalized value of the dimensionless group, dimensionless

xcr = critical silica flour concentration, wt%

xmin = minimum value of the dimensionless group, dimensionless

xmax = maximum value of the dimensionless group, dimensionless

X = normalized particle diameter, dimensionless

y = dependent variable, dimensions determined by application

z = length of the sand pack, m (cm)

zo = initial length of the sand pack, m (cm)

Greek

γ = empirical material parameter, dimensionless

= shear rate or velocity gradient, s-1

βa = formation damage coefficient for attachment, dimensionless

βs = formation damage coefficient for straining, dimensionless

β = pore throat to- particle diameter ratio, dimensionless

α, β and λ = empirical parameter, dimensionless

λs = filtration coefficient for size exclusion fines capture, m-1

λ = ratio of volume of dashed cylinder and volume of a particle, dimensionless

and   p = fraction of particle, %

a = volumetric concentration of attached fines, %

s  = volumetric concentration of strained fines, %

Ø  = porosity, dimensionless

Øo  = initial porosity, dimensionless

µc = pre- exponential coefficient of viscosity, Pa.s

µf  = fluid viscosity, Pa.s

µo  = initial viscosity, Pa.s

µ  = suspension viscosity, Pa.s

µw  = water viscosity, Pa.s

θ = temperature, K (°C)

ρ = suspension density, kg/m³ (g/cm³)

τcr = critical shear stress, Pa

τD = characteristics times τchar for the DLA, dimensionless

τR = characteristics times τchar for the RLA, dimensionless

τs = extra stress tensor, Pa

Φ = volume concentration of particle, p.p.m

ηs = shear modulus of the elastic solid particle, Pa

ω = angular velocity, s-1

= retention coefficient of gel particles, dimensionless

Abbreviations

BHP = bottom-hole pressure

BHT = bottom-hole temperature

CT = computed tomography

DLA = diffusion-limited aggregation

3D = three-dimensional

F.L. = fluid loss

HPHT = high pressure high temperature

LBM = Lattice Boltzmann method

LCM = lost circulation material

LDPSDA = laser diffraction particle size distribution analysis

NMR = Nuclear Magnetic Resonance

NPT = non- productive time

PG = preformed gel

PLT = production logging tool

PPG = preformed particle gel

PVI = pore volumes injected

RLA = reaction-limited aggregation

TEP = transparent exopolymer particle

VTF = Vogel- Tammann- Fulcher

# Appendix B: Special Correlation Equations

The  general  expressions of  the  special equations  used  for  correlations  of

experimental   data  are   presented   in   the   following, where   x   and  y   denote   the

independent and dependent variables considered in their applications. All these equations were correlated using Microsoft excel 2010.

Type 1:

(B-1)

where  y  is  the   steady-state  differential   pressure (kPa); x is  the  injection  flow  rate

(≤100) (cm3/h) and a and b are empirical parameters.

Type 2:

(B-2)

where  y   is   the  steady-state   differential   pressure  (kPa)  or intercept of the unplugging region (dimensionless) or  dimensionless  group (KΔPµovoZo/KoΔPoµvZ); x  is  the  injection  flow  rate (≥100) (cm3/h)  or pore volume injected (dimensionless) or  normalized dimensionless   group   (µt/ρZ²)*   or  normalized   dimensionless   group  (µt/ρDp²)*  or normalized dimensionless group (t²cθ/Z²)*; and a, b, and α are empirical parameters.

Type 3:

(B-3)

where  yo  is  the  initial  differential  pressure,  in  kPa;  y  is the steady-state differential

pressure, in  kPa;  x  is  the   gel-particle  diameter, in  µm;  and  a  and  b  are  empirical

parameters.

Type 4:

(B-4)

where   y   is   the   permeability    reduction     (dimensionless)   or intercept of the plugging region (dimensionless); x is the  gel-particle  volume fraction (%) or gel-particle diameter (µm) or  particle   diameter/pore-throat  size  (dimensionless) or pore volume injected (dimensionless); and  a,  b, and  α  are  empirical parameters.

Type 5:

(B-5)

where  y  is  the  resistance  factor  (dimensionless); x is the gel-particle volume fraction

(≤1) (%) or gel particle diameter (µm); and a and b are empirical parameters.

Type 6:

(B-6)

where  y  is  the  resistance  factor (dimensionless) or rate constant of the plugging and unplugging region (dimensionless) or fluid loss (%) or filtrate volume (cm3) or rate constant of filtrate (cm³/min1/2) or spurt loss volume (cm³); x is the gel-particle volume  fraction  (≥1)  (%)  or  injection   flow   rate  (≥100)   (cm3/h) or pore volume injected (dimensionless) or   silica   flour concentration (wt% or vol%) or filtrate time (min); and a, b, and α are empirical parameters.

Type 7:

(B-7)

where   y    is    the     resistance    factor    (dimensionless)    or    dimensionless    group

(KΔPµovoZo/KoΔPoµvZ)  or   dimensionless   group   (Vf/DF3)   or   dimensionless   group

(Vf/Ds3); x is  the  injection flow rate (≤100) (cm3/h) or normalized dimensionless group

(µt/ρZ²)* or normalized  dimensionless  group (vt/Z)* or dimensionless group (vt/DF) or

dimensionless group (vt/Ds); and a and b are empirical parameters.

Type 8:

(B-8)

where y is  the pore-throat/particle size  ratio (dimensionless); x is the particle Reynolds

number (dimensionless); and A1, B1, and C1 are empirical parameters (dimensionless).

Type 9:

(B-9)

where y is  the pore-throat/particle size  ratio (dimensionless); x is the particle Reynolds

number    (dimensionless); A2,  B2,  and  C2   are  empirical   parameters;  and  λ   is   the

empirical exponent.

Type 10:

(B-10)

where y is the  fluid loss (%); x is the  silica flour  concentration (wt%); xcr is the critical

silica flour concentration (wt%); and a, b, and α are empirical parameters.

Type 11:

(B-11)

where y is the pressure  initiate  flow (psig); x is the silica flour concentration (wt%); xcr

is the critical silica flour concentration (wt%); and a, b, and α are empirical parameters.

# Appendix C: Empirical correlations of  the differential pressure, permeability reduction, and resistance factor

A- The experimental data of the differential pressure across the proppant pack during the gel-particle-suspension injection were correlated with the injection flow rate and the gel particle diameter and empirical correlations were developed by applying Eqs. B-1, B-2, and B-3 given in Appendix B, as shown in Fgs. C.1 to C.3.

Fig. C.1: Straight line plot of Eq. B-1 at 50 cm³/hr and100 cm³/hr flow rates to

develop the empirical correlation of the differential pressure at 3 vol%

and 23.5 °C, as shown in Fig. 5.14

Fig. C.2: Straight line plot of Eq. B-2 at 100 cm³/hr, 200 cm³/hr, 280 cm³/hr and

400 cm³/hr flow rates to develop the empirical correlation of the

differential pressure at 3 vol% and 23.5 °C, as shown in Fig. 5.14

Fig. C.3: Straight line plot of Eq. B-3 at different gel- particle diameters to develop

the empirical correlation of the  differential pressure at 3 vol% and 23.5

°C, as shown in Fig. 5.15

B- The experimental data of the permeability reduction during the gel-particle-suspension injection were correlated with the gel-particle concentration, the gel particle diameter and the particle diameter to pore throat size ratio and empirical correlations were developed by applying Eq. B-4 given in Appendix B, as shown in Fgs. C.4 to C.6.

Fig. C.4: Straight line plot of Eq. B-4 at different gel-particle concentrations to

develop the empirical correlation of the  permeability reduction at 100

cm3/h and 23.5 °C, as shown in Fig. 5.16

Fig. C.5: Straight line plot of Eq. B-4 at different gel-particle diameters to

develop the empirical correlation of the  permeability reduction at 100

cm3/h and 23.5 °C, as shown in Fig. 5.18

Fig. C.6: Straight line plot of Eq. B-4 at different particle diameter to pore throat

size ratios to develop the empirical correlation of the  permeability

reduction at 100 cm3/h and 23.5 °C, as shown in Fig. 5.19

C- The experimental data of the resistance factor during the gel-particle-suspension injection were correlated with the gel-particle concentration, the gel particle diameter and the injection flow rate and empirical correlations were developed by applying Eqs. B-5, B-6, and B-7 given in Appendix B, as shown in Fgs. C.7 to C.11.

Fig. C.7: Straight line plot of Eq. B-5 at 0.5 vol% and 1 vol% gel-particle

concentrations to develop the empirical correlation of the  resistance

factor at 100 cm3/h and 23.5 °C, as shown in Fig. 5.20

Fig. C.8: Straight line plot of Eq. B-6 at 1 vol%, 2 vol% and 3 vol% gel-particle

concentrations to develop the empirical correlation of the  resistance

factor at 100 cm3/h and 23.5 °C, as shown in Fig. 5.20

Fig. C.9: Straight line plot of Eq. B-7 at 50 cm³/hr and 100 cm³/hr flow rates

to develop the empirical correlation of the  resistance factor at 3 vol%

and 23.5 °C, as shown in Fig. 5.21

Fig. C.10: Straight line plot of Eq. B-6 at 100 cm³/hr, 200 cm³/hr, 280 cm³/hr and

400 cm³/hr flow rates to develop the empirical correlation of the

resistance factor at 3 vol% and 23.5 °C, as shown in Fig. 5.21

Fig. C. 11: Straight line plot of Eq. B-5 at different gel-particle diameter to develop

the empirical correlation of the  resistance factor at 100 cm3/h and

23.5 °C, as shown in Fig. 5.22

# Appendix D: The power-law and exponential-law equations

The experimental data of the pore-throat/particle size ratio were correlated with the particle Reynolds number and power-law and exponential-law equations were developed by applying Eqs. B-8 and B-9 given in Appendix B.

Fig. D.1: Straight line plot of Eq. B-8 at different gel particle concentrations and

different gel particle diameters to develop the power-law equation, shown

in Fig. 5.23.

Fig. D.2: Straight line plot of Eq. B-9 at different gel particle concentrations and

different gel particle diameters to develop the power-law equation, shown

in Fig. 5.23.

# Appendix E: Correlations of Thermal Effect on plugging/Unplugging Processes

The correlations of the thermal effect on the rate and intercept constants of plugging and unplugging regions were developed by the following steps:

1- The rate constant of the plugging and unplugging regions were correlated with the pore volumes injected at various temperatures and empirical correlations were developed, as shown in Figs. E.1 and E.2, by applying Eq. B-6 given in Appendix B.

Fig. E.1: The relationship between rate constant of plugging and pore volumes

injected at various temperatures

Fig. E.2: The relationship between rate constant of unplugging and pore volumes

injected at various temperatures

Fig. E.3: Straight  line  plot  of  Eq. B-6  at  different  temperatures to  develop the

empirical correlation of the rate constants of the plugging regions, as shown in Fig. E.1

Fig. E.4: Straight line plot of Eq. B-6 at different temperatures to develop the empirical correlation of the rate constants of the unplugging regions, as shown in Fig. E.2

2- The intercept of the plugging and unplugging regions were correlated with the pore volumes injected at various temperatures and empirical correlations were developed, as shown in Figs. E.5 and E.6, by applying Eq. B-6 given in Appendix B.

Fig. E.5: The relationship between intercept of plugging regions and pore

volumes injected at various temperatures

Fig. E.6: The relationship between intercept of unplugging regions and pore

volumes injected at various temperatures

Fig. E.7: Straight line plot of Eq. B-4 at different temperature to develop the empirical correlation of the intercepts of the plugging regions, as shown in Fig. E.5

Fig. E.8: Straight line plot of Eq. B-2 at different temperature to develop the empirical correlation of the intercepts of the unplugging regions, as shown in Fig. E.6

3- The values of A,B, and β of the correlations in Figs. E.1, E.2, E.5 and E.6 were plotted and correlated as linear functions and substituted in Eqs. 6.7 and 6.8 to develop correlations of the thermal effect on the rate and intercept constants of plugging and unplugging regions, as shown in Figs. 6.20 to 6.23.

| Fig. E.9: Linear function plot of A values at different temperatures for rate constants of plugging Fig. E.10: Linear function plot of B values at different temperatures for rate constants of plugging Fig. E.11: Linear function plot of β values at different temperatures for rate constants of plugging Fig. E.12: Linear function plot of A values at different temperatures for rate constants of unplugging Fig. E.13: Linear function plot of B values at different temperatures for rate constants of unplugging Fig. E.14: Linear function plot of β values at different temperatures for rate constants of unplugging |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fig. E.15: Linear function plot of A values at different temperatures for intercept of plugging regions Fig. E.16: Linear function plot of B values at different temperatures for intercept of plugging regions |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fig. E.17: Linear function plot of β values at different temperatures for intercept of plugging regions |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Fig. E.18: Linear function plot of A values at different temperatures for intercept of unplugging regions Fig. E.19: Linear function plot of B values at different temperatures for intercept of unplugging region |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |

Appendix F: Correlations of the normalized dimensionless groups

The dimensionless groups values were normalized by used of Eq. 7.4 and were   correlated  at   different    concentrations,  flow   rates,  gel   particle   sizes,  and temperatures  by  applying  Eqs. B-2  and  B-7  given  in  Appendix B,  as  shown in the following figures:

Fig. F.1: Straight line plot of Eq. B-2 for the normalized dimensionless group π4

for the permeability reduction at different temperatures, as shown in Fig. 7.11

Fig. F.2: Straight line plot of Eq. B-2 for the normalized dimensionless group π9

for the permeability reduction at different temperatures, as shown in Fig. 7.12

Fig. F.3: Straight line plot of Eq. B-7 for the normalized dimensionless group π4

for the permeability reduction at different gel particles concentrations, as

shown in Fig. 7.13

Fig. F.4: Straight line plot of Eq. B-7 for the normalized dimensionless group π6

for the permeability reduction at different flow rates, as shown in Fig. 7.14

Fig. F.5: Straight line plot of Eq. B-2 for the normalized dimensionless group π5

for the permeability reduction of the sand pack of 1061 µm grain

diameter at different gel particles sizes, as shown in Fig. 7.15

Fig. F.6: Straight line plot of Eq. B-2 for the normalized dimensionless group π5

for the permeability reduction of the sand pack of 650 µm grain

diameter at different gel particles sizes, as shown in Fig. 7.16

Appendix G: Correlation of the fluid loss

General empirical correlation of fluid loss at any pore diameter of filter disc, sand size and silica flour concentration was developed as described in the following.

1- The experimental data of the fluid loss was correlated with the silica flour concentration and exponential relationships were developed for 35, 10, and 5 micron pore diameter of filter disc at different sand sizes, as shown in Figs. G.1 to G.3, by applying Eq. B-6 given in Appendix B, as shown in Figs. G.4 to G.6.

Fig. G.1: Correlate the experimental results of fluid loss at different silica flour

concentrations for 35 micron average pore diameter of filter disc and

different sand sizes

Fig. G.2: Correlate the experimental results of fluid loss at different silica flour

concentrations for 10 micron average pore diameter of filter disc and

different sand sizes

Fig. G.3: Correlate the experimental results of fluid loss at different silica flour

concentrations for 5 micron average pore diameter of filter disc and

different sand sizes

Fig. G.4: Straight line plot of Eq. B-6 to develop the exponential relationship of the

fluid loss for 35 micron pore diameter of filter disc at different silica flour

concentrations and different sand sizes, as shown in Fig. G.1

Fig. G.5: Straight line plot of Eq. B-6 to develop the exponential relationship of the

fluid loss for 10 micron pore diameter of filter disc at different silica flour

concentrations and different sand sizes, as shown in Fig. G.2

Fig. G.6: Straight line plot of Eq. B-6 to develop the exponential relationship of the

fluid loss for 5 micron pore diameter of filter disc at different silica flour

concentrations and different sand sizes, as shown in Fig. G.3

2- The fluid loss was correlated with the critical silica flour concentration for 35, 10, and 5 micron pore diameter of filter disc at different sand sizes, as shown in Figs. G.7 to G.9, by applying Eq. B-10 given in Appendix B, as shown in Figs. G.10 to G.12.

Fig. G.7: Correlate the  experimental  results of  fluid loss with  the critical silica

flour concentrations for 35 micron average pore diameter of filter disc

and different sand sizes

Fig. G.8: Correlate  the experimental  results of  fluid  loss with  the critical silica

flour concentrations for 10 micron average pore diameter of filter disc

and different sand sizes

Fig. G.9: Correlate the  experimental  results of  fluid loss with the critical silica

flour concentrations for 5 micron average pore diameter of filter disc

and different sand size

Fig. G.10: Straight line plot of Eq. B-10 to correlate the fluid loss with the critical

silica flour  concentration for 35 micron  pore  diameter of filter disc at

different sand sizes, as shown in Fig. G.7

Fig. G.11: Straight line plot of Eq. B-10 to correlate the fluid loss with the critical

silica flour  concentration for 10 micron  pore  diameter of filter disc at

different sand sizes, as shown in Fig. G.8

Fig. G.12: Straight line plot of Eq. B-10 to correlate the fluid loss with the critical

silica flour  concentration for 5 micron  pore  diameter of filter disc at

different sand sizes, as shown in Fig. G.9

3- The values of B, α, and xcr of the exponential relationships were plotted and correlated as linear functions and substituted in Eq. 8.2 to develop charts of fluid loss for same pore diameter of filter disc and different sand sizes, as shown in Figs. 8.3 to 8.5.

Fig. G.13: Linear function plot of B values at different sand sizes for 35 micron

pore diameter of filter disc

Fig. G.14: Linear function plot of α values at different sand sizes for 35 micron

pore diameter of filter disc

Fig. G.15: Linear function plot of xcr values at different sand sizes for 35 micron

pore diameter of filter disc

Fig. G.16: Linear function plot of B values at different sand sizes for 10 micron

pore diameter of filter disc

Fig. G.17: Linear function plot of α values at different sand sizes for 10 micron

pore diameter of filter disc

Fig. G.18: Linear function plot of xcr values at different sand sizes for 10 micron

pore diameter of filter disc

Fig. G.19: Linear function plot of B values at different sand sizes for 5 micron pore

diameter of filter disc

Fig. G.20: Linear function plot of α values at different sand sizes for 5 micron pore

diameter of filter disc

Fig. G.21: Linear function plot of xcr values at different sand sizes for 5 micron

pore diameter of filter disc

4- The values of a1, b1, a2, b2, a3, and b3  of Eq. 8.3 were plotted against pore diameter of filter disc and correlated as linear functions and substituted in Eq. 8.3 to develop general empirical correlation of fluid loss at any pore diameter of filter disc and sand size, as illustrated in Eq. 8.4.

Fig. G.22: Linear function plot of a1 at different pore diameters of filter discs

Fig. G.23: Linear function plot of b1 at different pore diameters of filter discs

Fig. G.24: Linear function plot of a2 at different pore diameters of filter discs

Fig. G.25: Linear function plot of b2 at different pore diameters of filter discs

Fig. G.26: Linear function plot of a3 at different pore diameters of filter discs

Fig. G.27: Linear function plot of b3 at different pore diameters of filter discs

Appendix H: Correlation of critical silica flour concentration

The empirical correlation of critical silica flour concentration at any pore diameter of filter disc and sand size was developed as described in the following.

1- The values of critical silica flour concentration of same pore diameter of filter disc were plotted against sand size and correlated as linear function, as shown in Fig. H.1.

Fig. H.1: Correlate the critical silica flour concentrations for 35, 10, and 5 micron

pore diameter of filter discs and different sand sizes

2- The values of As and Bs of the linear function of the critical silica flour concentration were plotted against the sand size and correlated as linear functions and substituted in the linear function of the critical silica flour concentration to develop general empirical correlation can be used at any pore diameter of filter disc and sand size, as shown in Eq. 8.5.

Fig. H.2: Linear function plot of A values at different  pore diameter of filter discs

Fig. H.3: Linear function plot of B values at different  pore diameter of filter discs

Appendix I: Correlation of the pressure initiate flow

The empirical correlation of pressure to initiate flow at any pore diameter of filter disc, sand size and silica flour concentration was developed as described in the following.

1- The experimental data of the pressure initiate flow was correlated with the critical silica flour concentration and relationships were developed for 35, 10, and 5 micron pore diameter of filter disc at different sand sizes, as shown in Figs. I.1 to I.3, by applying Eq. B-11 given in Appendix B.

Fig. I.1: Correlate the experimental results of pressure initiate flow with the

critical silica flour concentrations for 35 micron average pore diameter

of filter disc and different sand sizes

Fig. I.2: Correlate the experimental results of pressure initiate flow with the

critical silica flour concentrations for 10 micron average pore diameter

of filter disc and different sand sizes

Fig. I.3: Correlate the experimental results of pressure initiate flow with the

critical silica flour concentrations for 5 micron average pore diameter of

filter disc and different sand size

Fig. I.4: Straight line plot of Eq. B-11 to develop the relationship of the pressure initiate flow at different silica flour concentration for 35 micron pore diameter of filter disc at different sand sizes, as shown in Fig. I.1

Fig. I.5: Straight line plot of Eq. B-11 to develop the relationship of the pressure initiate flow at different silica flour concentration for 10 micron pore diameter of filter disc at different sand sizes, as shown in Fig. I.2

Fig. I.6: Straight line plot of Eq. B-11 to develop the relationship of the pressure initiate flow at different  silica flour concentration for 5 micron pore  diameter of filter disc at different sand sizes, as shown in Fig. I.3

2- The values of A, B, and α of the relationships were plotted and correlated as linear functions and substituted in Eq. 8.6 to develop charts of pressure to initiate flow for same pore diameter of filter disc and different sand sizes, as shown in Figs. 8.9 to 8.11.

Fig. I.7: Linear function plot of A values at different sand sizes for 35 micron

pore diameter of filter disc

Fig. I.8: Linear function plot of B values at different sand sizes for 35 micron

pore diameter of filter disc

Fig. I.9: Linear function plot of α values at different sand sizes for 35 micron

pore diameter of filter disc

Fig. I.10: Linear function plot of A values at different sand sizes for 10 micron

pore diameter of filter disc

Fig. I.11: Linear function plot of B values at different sand sizes for 10 micron

pore diameter of filter disc

Fig. I.12: Linear function plot of α values at different sand sizes for 10 micron

pore diameter of filter disc

Fig. I.13: Linear function plot of A values at different sand sizes for 5 micron pore

diameter of filter disc

Fig. I.14: Linear function plot of B values at different sand sizes for 5 micron pore

diameter of filter disc

Fig. I.15: Linear function plot of α values at different sand sizes for 5 micron

pore  diameter of filter disc

3- The values of a1, b1, a2, b2, a3, and b3  of Eq. 8.7 were plotted against pore diameter of filter disc and correlated as linear functions and substituted in Eq. 8.7 to develop general empirical correlation of fluid loss at any pore diameter of filter disc and sand size, according to Eq. 8.8.

Fig. I.16: Linear function plot of a1 at different pore diameters of filter discs

Fig. I.17: Linear function plot of b1 at different pore diameters of filter discs

Fig. I.18: Linear function plot of a2 at different pore diameters of filter discs

Fig. I.19: Linear function plot of b2 at different pore diameters of filter discs

Fig. I.20: Linear function plot of a3 at different pore diameters of filter discs

Fig. I.21: Linear function plot of b3 at different pore diameters of filter discs

Appendix J: Correlation of the filtrate volume

The  experimental  data  of  the filtrate volume of the silica flour particle-gel

system  were correlated with the filtrate time and empirical correlations were developed

for  35, 10, and 5  micron  pore  diameter  of  filter  disc,  12/20,  20/40,  and 40/70 sand

mesh, and  different silica  flour  concentrations, as shown  in Figs. 9.1 to 9.3  and 9.6 to

9.11, by applying Eq. B-6 given in Appendix B.

Fig. J.1: Straight line plot of Eq. B-6 to develop the exponential relationship of the filtrate volume at different silica flour concentration for 35 micron pore diameter

of filter disc and 12/20 sand mesh, as shown in Fig. 9.1

Fig. J.2: Straight line plot of Eq. B-6 to develop the exponential relationship of the filtrate volume at different silica flour concentration for 35 micron pore diameter

of filter disc and 20/40 sand mesh, as shown in Fig. 9.2

Fig. J.3: Straight line plot of Eq. B-6 to develop the exponential relationship of the filtrate volume at different silica flour concentration for 35 micron pore diameter

of filter disc and 40/70 sand mesh, as shown in Fig. 9.3

Fig. J.4: Straight line plot of Eq. B-6 to develop the exponential relationship of the filtrate volume at different silica flour concentration for 10 micron pore diameter

of filter disc and 12/20 sand mesh, as shown in Fig. 9.6

Fig. J.5: Straight line plot of Eq. B-6 to develop the exponential relationship of the filtrate volume at different silica flour concentration for 10 micron pore diameter

of filter disc and 20/40 sand mesh, as shown in Fig. 9.7

Fig. J.6: Straight line plot of Eq. B-6 to develop the exponential relationship of the filtrate volume at different silica flour concentration for 10 micron pore diameter

of filter disc and 40/70 sand mesh, as shown in Fig. 9.8

Fig. J.7: Straight line plot of Eq. B-6 to develop the exponential relationship of the filtrate volume at  different  silica flour concentration for 5  micron pore diameter

of filter disc and 12/20 sand mesh, as shown in Fig. 9.9

Fig. J.8: Straight line plot of Eq. B-6 to develop the exponential relationship of the filtrate volume at  different  silica flour concentration for 5  micron pore diameter

of filter disc and 20/40 sand mesh, as shown in Fig. 9.10

Fig. J.9: Straight line plot of Eq. B-6 to develop the exponential relationship of the filtrate volume at  different  silica flour concentration for 5  micron pore diameter

of filter disc and 40/70 sand mesh, as shown in Fig. 9.11

Appendix K: Correlation of the rate constant of filtrate and spurt loss volume

The exponential correlations of the rate constant of filtrate and spurt loss  volume of the silica flour particle-gel system were developed by the following steps:

1- The rate constant of filtrate were correlated with the silica flour concentration at different sand sizes and 35 micron pore diameter of filter disc and exponential correlations were developed, as shown in Figs. K.1 and K.2, by applying Eq. B-6 given in Appendix B.

Fig. K.1: The relationship between rate constant of filtrate and silica flour concentration at 35 micron pore diameter filter disc and different sand sizes

Fig. K.2: The relationship between spurt loss volume and silica flour concentration at 35 micron pore diameter filter disc and different sand size

Fig. K.3: Straight line plot of Eq. B-6 at 35 micron pore diameter of filter disc to

develop  the  exponential  correlation of the rate constant of filtrate of

different sand sizes, as shown in Fig. K.1

Fig. K.4: Straight line plot of Eq. B-6 at 35 micron pore diameter of filter disc to

develop  the  exponential  correlation of  the  spurt  loss  volume  of

sand sizes, as shown in Fig. K.2

2- The values of A,B, and β of the correlations in Figs. K.1 and K.2 were plotted and correlated as linear functions and substituted in Eq. 6.7 to develop correlations of rate constant of filtrate and spurt loss volume of the silica flour particle-gel system at 35 micron pore diameter of filter disc, as shown in Figs. 9.22 and 9.23.

Fig. K.5: Linear function plot of A values at different  sand sizes for the rate

constants of filtrate of 35 micron pore diameter filter disc

Fig. K.6: Linear function plot of B values at different  sand sizes for the rate

constants of filtrate of 35 micron pore diameter filter disc

Fig. K.7: Linear function plot of β values at different  sand sizes for the rate

constants of filtrate of 35 micron pore diameter filter disc

Fig. K.8: Linear function plot of A values at different  sand sizes for the spurt loss

volume of filtrate of 35 micron pore diameter filter disc

Fig. K.9: Linear function plot of B values at different  sand sizes for the spurt loss

volume of filtrate of 35 micron pore diameter filter disc

Fig. K.10: Linear function plot of β values at different  sand sizes for the spurt loss

volume of filtrate of 35 micron pore diameter filter disc