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[bookmark: _Toc102015396]ABSTRACT
Foams exhibit valuable properties such as high viscosity, low density, and good cutting carrying capacity. However, they are thermodynamically unstable due to gravitational drainage, bubble coalescence, and coarsening. As a result, they lose these functional properties with time. Therefore, this study investigates the effects of pressure and contaminant oil on the stability of aqueous foams. In a flow loop with a vertical drainage measurement section, nitrogen foam was generated. Drainage experiments were conducted for different (40 - 60%) foam qualities while varying the pressure from 100 to 400 psi. Water with 2% anionic surfactant was used as the base liquid. Tests were also conducted at 10% v/v oil concentration to study the effect of contamination. The foam images were captured using a viewport at regular intervals to examine bubble structure and determine the bubble size distribution with time.      	   	   
At constant pressure, lower-quality aqueous foams drained faster than higher-quality aqueous foams without oil contamination. On the contrary, when 10% oil was added to the base liquid, 50% quality foam exhibited lower drainage than 40% and 60% quality foams. The stability of aqueous foams also improved considerably when the pressure was increased for each foam quality, regardless of the presence of oil. 
[bookmark: _Hlk94479331]The data from image processing showed that as the pressure increases, the bubble size decreases at a constant foam quality. Besides this, bubble size approximately linearly increased with time, demonstrating bubble coalescence and coarsening. Furthermore, the size of the bubbles grew with foam quality. It can be concluded that the increase in pressure stabilizes the aqueous foam. At a given foam quality, the lower the bubble size more stable is the foam. Contaminants like oil affect the aqueous foam's stability and bubble size. This study helps understand the effect of pressure and oil contaminants on the stability of aqueous foam at different quality.
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1. [bookmark: _Toc99805600][bookmark: _Toc102015397]CHAPTER ONE 
[bookmark: _Toc99805601][bookmark: _Toc102015398]1.1 Overview 
Foam is created when a dispersed gas phase is trapped in a continuous liquid phase, resulting in a variety of bubble sizes. They contain large volumes of gas separated by thin liquid films. Mechanical agitation or shearing, as well as the presence of a surfactant to reduce surface tension and stabilize the interface between the two phases, are essential to produce foams. In many industrial applications, foams are efficient and economical. In foam drilling operations, the backpressure, and gas and liquid injection rates are all adjusted parameters to manage the foam quality (volumetric concentration of the gas phase). The liquid phase consists of water and surfactants, whereas the gas phase consists of either air, nitrogen, carbon dioxide, or hydrocarbon gas. 
Foams are used in a variety of industries, including food, petroleum, firefighting, pharmaceuticals, personal care goods, sewage treatment, chemical sector, textile, and paper (Kim and Dlugogorski 1996). Common examples of foam products are bath foam, whipped cream, fire retardant foam, and shaving foam. 
[bookmark: _Toc99805602][bookmark: _Toc102015399]1.2 Oil Field Applications
In the oil and gas industry, foams are used for a range of applications such as drilling, enhanced oil recovery (EOR), hydraulic fracturing, cementing, and stimulation amongst others. In refineries, unwanted foams form in distillation towers and oil-gas separators, which must be chemically broken down into their constituent chemicals. Foams are widely used because of their unique properties such as high viscosity and low density, which make them suitable for hole cleaning and downhole pressure management. In addition to their high viscosity, the bubble structure of the foam plays a vital role in increasing their carrying capacity. In field applications, the foam generated has a foam quality of 90% when measured at surface but the foam quality reduces in downhole conditions due change in pressure and temperature.
[bookmark: _Toc99805603][bookmark: _Toc102015400]1.1.1 Drilling
Formation damage is one of the leading causes of poor well performance (Falk and McDonald 1995). Underbalanced drilling with lightweight drilling fluid-like foam improves the rate of penetration, reduces formation damage with minimal or no stimulation required, reduces chances of differential pipe sticking, minimizes lost circulation, and faster payback due to production of formation fluids while drilling (Capo et al. 2006). Foam drilling is highly beneficial for water-sensitive formations and regions with water shortages. The use of high-quality foams with appropriate flow rate ensures good hole cleaning for inclined and horizontal wells (Martins et al. 2001). When applied for drilling in depleted zones and low-pressure formations, foams are more cost-effective than traditional fluids because they halt fluid leak off into the formation, reducing fluid loss and the amount of drilling fluid used. 
[bookmark: _Toc99805604][bookmark: _Toc102015401]1.1.2 Hydraulic Fracturing and Stimulation
Fracturing occurs when the wellbore pressure exceeds the formation's pore and overburden pressures and. Foams exhibits properties that are suitable for fracturing applications such as low fluid loss, high proppant carrying capacity, low hydrostatic head, quick fluid recovery, low formation damage, exceptional flow back, and good wellbore cleanout capability (Kumar et al. 2010; Blauer and Kohlhaas 1974). Frequently, foam fracturing is implemented in low permeability gas reservoirs, water-sensitive shale formations, coalbed, tight sandstones, and carbonates. The fluid used in the fracturing consists of 65-85% of the gaseous phase which is mostly made up of either nitrogen, carbon dioxide, or natural gas. The foam's high gas content aids in the rapid return of liquids in the form of mist. In addition, good post-treatment viscosity-breaking characteristics elevate the use of foam as fracturing fluid. Also, recent acid stimulation studies show that Nano surfactants are better suited for higher temperature applications (Omar et al. 2018).  
[bookmark: _Toc99805605][bookmark: _Toc102015402]1.1.3 Enhanced oil recovery
Enhanced oil recovery is a technique for increasing output in wells that have reached their inherent capacity for oil production. Carbon dioxide gas is the most widely used fluid for EOR along with nitrogen, hydrocarbons, air, and water (Worthen et al. 2012). These fluids are less successful in dislodging hydrocarbons from the pore space in the reservoir due to their low density and viscosity. The flowing of foam as an EOR fluid through the porous media is unique because its rheology and microstructure (Kovscek and Radke 1994). The ability of an aqueous foam stabilized with a surfactant to limit gas mobility in porous media which increases the sweep efficiency (Fried 1961). The gas mobility reduction factor is dependent on the surfactant concentration and injection velocities (Simjoo et al. 2013). Recent studies show that nano particle-stabilized carbon dioxide foams show greater efficiency in reducing gas mobility in gas-injected EOR (Ortiz et al. 2018). An optimized mixture of nitrogen and carbon dioxide for generating foams increases the recovery of oil when compared to recovery by pure carbon dioxide foams (Gajbhiye 2021).
[bookmark: _Toc99805606][bookmark: _Toc102015403]1.1.4 Cementing
Foam cement is employed when lower slurry densities are required for long-term performance in high-pressure, high-temperature zones (Ahmed et al. 2008). When the casing is pressured, foamed cement deforms but does not crack like conventional cement. Foamed cement slurries have superior displacement properties due to their high viscosity providing good zonal isolation. The low thermal conductivity of nitrogen foamed cement allows less heat to escape the casing boundary (Benge et al. 1982). Resistance to impact and cyclic loading improved due to improved physical and mechanical properties. Foam cement works well for cementing wells with lost circulation issues and removes the need for multi-stage cementing procedures, saving time and money (Peskunowicz and Bour 1987).
[bookmark: _Toc99805607][bookmark: _Toc102015404]1.2 Problem Statement
Although foam has many applications in the oil and gas sector, it is thermodynamically unstable fluid. Properties of foam such as low density and high viscosity are extremely critical but deteriorate with time. Foams have high sand carrying capacity which is due to their bubble structure. Therefore, it is necessary to have a better understanding of foam’s rheology, drainage, stability, bubble size, and hydraulics. In downhole conditions, foam is affected by the presence of contaminants like oil, salt, clay, and several other impurities. The effects of pressure and temperature on various foam characteristics must be thoroughly investigated. The quality of foam has a major influence on the foam properties and changes with temperature and pressure. 
Gravitational drainage, bubble coalescence, and Ostwald ripening all contribute to foam decay. The difference in density between the liquid and gas phases is the driving mechanism that causes gravity drainage. The walls of the bubbles get thinner as the liquid drains from the foam structure. Surfactants, on the other hand, slow down film thinning, a phenomenon known as the Gibbs-Marangoni effect (Zhou et al. 2020). Coalescence (Fig.1.1) of two bubbles in the foam structure to form a larger bubble destabilizes the foam structure as larger bubbles are unstable. Gas migration from smaller bubbles to bigger bubbles is known as Ostwald ripening. 
With increasing depth, downhole circumstances vary, affecting the downhole conditions for foam flowing through the annulus. In past few years, drilling inclined wells has increased and research showed that well inclination speeds up the drainage process (Govindu et al. 2021). Aqueous foams have demonstrated promising outcomes in geothermal drilling applications where lost circulation is a problem, but only at temperatures below 70°C. The bubble structure of aqueous foams breaks down at high temperatures, hence they can't be used at elevated temperatures.
High-quality aqueous foams show a hexagonal bubble structure, and low-quality foams display a normal spherical structure (Fig. 2.2). The average bubble size increases with time as the foam decays due to coalescence and coarsening, and consequently, the number of bubbles decreases with time.
[image: A picture containing text
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[bookmark: _Toc102015462]Figure 1.1: Coalescence (top) and coarsening (bottom) (Hill and Eastoe 2017)
	The application of oil-based drilling foams is limited due to environmental concerns. Using unstable aqueous foams for underbalanced drilling can cause temporary overbalance conditions, causing severe formation damage. Therefore, it is necessary to understand the drainage, rheology, and stability of aqueous foams. 
[bookmark: _Toc99805608][bookmark: _Toc102015405]1.3 Objectives & Scope of work 
The principal aim of this investigation to understand the drainage behavior and the half-life of oil-contaminated aqueous foams under various conditions, including different pressures and foam qualities. The specific goals of this investigation include:
· Studying the effects of pressure and oil contamination on the bubble size distribution and drainage behavior of foams.
· Examining the impact of pressure on the mechanism of foam drainage in the presence of contaminant oil. 
· Investigating the impact of oil contamination on the structure of foam under various conditions. 
· Developing correlations to relate to foam drainage and half-life to it is characteristics such as bubble size distribution, foam quality, and pressure.
The scope of the current study is focused on the experimental investigation of the drainage of aqueous foam in the presence of oil contaminants and different pressures. Therefore, aqueous nitrogen foams used in this study were tested with varying test parameters such as quality, pressure, and oil concentration. Foam quality and pressure were varied between 40-60%, and 100-400 psi. Oil contaminant concentration was from 0 to 20%. Bubble size and structure are studied in order to understand the drainage of aqueous foams. The quality of foam was regulated by adjusting liquid injected into the system, which was done in a closed-loop system. In the liquid mixture, a 2% concentration of anionic surfactant was added.
[bookmark: _Toc99805609][bookmark: _Toc102015406]1.4 Properties of Foams 
Foam has a number of useful properties that have been stated previously, allowing its utilization in a variety of applications. These properties largely depend on the method of foam generation, type of surfactant, properties of base fluid, pressure, temperature, and contaminants present in the fluid system. Some of the important properties of foam are discussed in this section.
[bookmark: _Toc99805610][bookmark: _Toc102015407]1.4.1 Quality
The foam quality is the in-situ volumetric concentration of the gas phase present in the foam. It is one of the most essential characteristics that gives foam its distinctive attributes. Foam quality affects the stability, viscosity, bubble size distribution, and structure of foams. Foam quality is mathematically defined as the ratio of the in-situ volume of gas to the total foam volume: 
                         							(1.1)
Where VG and VL are volume of gas (VG) and volume of liquid (VL), respectively. The in-situ gas volume varies with pressure and temperature; as a result, foam quality is a function of pressure and temperature. 
As the foam quality is increased from zero to unity, we see a transition in the foam structure (Fig. 1.2). Foams below 60% are identified as bubbly liquids. For aqueous foams, rigidity transition occurs at 63% (Kraynik 1983; Ahmed et al. 2003). Foams above 96% are classified as mists. Wet foams have high liquid content than dry foams. Due to thicker films, wet foams have a spherical structure and dry foams have thinner films with polyhedral structure. Foam density is majorly influenced by the change in density of the base fluid as change in gas density has negligible effect. The density of the foam structure changes with the foam quality. Foam density is calculated as a mixture of density of gas and liquid. As the quality of foam gets higher, the fraction of liquid present in the foam structure reduces and the fraction of gas present in the foam structure reduces. The drainage of the liquid phase from the foam structure reduces the amount of liquid and thus reducing the overall density of foam drastically. 
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[bookmark: _Toc102015463]Figure 1.2: Relative viscosity as a function of foam quality (Ahmed et al. 2003)
[bookmark: _Toc99805611][bookmark: _Toc102015408]1.4.2 Rheology
[bookmark: OLE_LINK6][bookmark: OLE_LINK7]The rheology of the foam is determined by the quality of the foam and the base liquid viscosity (Sherif et al. 2016; Mitchell 1971). The shear rate that is applied to the foam influences its rheology, while surfactant concentration has a slight effect. The liquid used is usually oil, water, or polymer with a gas phase consisting of nitrogen, carbon dioxide, or hydrocarbons. Wet foams made with these fluid mixtures exhibit Newtonian behavior. As the quality increases, non-Newtonian, pseudoplastic fluid behavior also increases. Besides this, foam rheology is affected by foam generation method, pressure, temperature, and shear rate. Foam made of a high-viscosity liquid phase often exhibits higher stability because the viscous force impedes liquid movement and opposes drainage. The viscosity of non-dry foam increases with quality.
[bookmark: _Toc99805612][bookmark: _Toc102015409]1.4.3 Stability
Foams exhibit unique properties, but they start to drain and lose their properties as soon as they are created. Foam’s stability is mainly influenced by its quality and base liquid rheological properties. Foams with higher qualities are found to be more stable. Wet foams decay faster than dry foams. The stability of foams is measured as the drainage of fluid from the foam structure. Drainage in foam occurs by gravitational drainage, coalescence, coarsening, and Ostwald ripening. As the liquid drains from the foam structure, the walls of the bubble become thinner and unstable. Furthermore, bubble size and structure impact foam stability. Foams containing bubbles of small size are proved to be more stable than foams with large bubbles. In dry foams, bubbles are so tightly packed that they start impacting the neighboring bubbles such that they take a polyhedral shape. The addition of surfactants increases foam stability by lowering the surface tension. However, increasing surfactant concentration beyond critical micelle concentrations does not improve the stability of foam.
[bookmark: _Toc99805613][bookmark: _Toc102015410]1.5 Factors Affecting the Foam Stability
Foam stability is mainly a function of its quality and base liquid rheology as mentioned earlier. Other factors that have effects on foam stability are pressure, temperature, contaminants, surfactant type, and foam generation techniques.
[bookmark: _Toc99805614][bookmark: _Toc102015411]1.5.1 Effect of Pressure
An increase in pressure at a constant foam quality doesn't have significant effect on the foam viscosity (Lourenco et al. 2003; Akhtar 2017; Akhtar et al. 2018). Experiments conducted with various surfactant types and gas combinations show that drainage time increases with pressure (Rand and Kraynik 1983). The improvement in drainage time at a constant quality can be linked to the decrease in bubble size (Rand and Kraynik 1983). The change is the size of the bubbles is attributed to the compressibility of gas phase (Fig. 1.3).
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[bookmark: _Toc102015464]Figure 1.3: Microscopic images of bubble size with varying pressure (Rand and Kraynik 1983)
An increase in pressure reduces the bubble size and creates a uniform foam texture. This uniform texture of the foam slows down the drainage and decay of the foam structure. Increasing pressure at constant foam quality affects foam stability by modifying surface elasticity (Ruckenstein and Jain 1974). This improved surface elasticity prevents rupture of thin films and delays bubble coalescence.  Moreover, when compared to anionic surfactant foam, amine oxide surfactant foam exhibited higher stability and delayed foam drainage when pressure was increased (Fuseni et al. 2014). Also, foam flooding experiments demonstrated that foam stability increases with increasing pressure (Holt et al. 1996). However, extremely high-pressure conditions might cause the lamella to rupture and destabilize the foam (Sheng 2013).
[bookmark: _Toc99805615][bookmark: _Toc102015412]1.5.2 Effect of Temperature
Increasing temperature can affect gas phase volume, foam quality, pressure, and viscosity of the base liquid. When quality is kept constant, the apparent viscosity of foam decreases significantly with temperature (Akhtar 2017). The reduction is mainly due to thermal thinning of the base liquid. Effect of temperature on foam viscosity is more pronounced in high-quality foams (Gu and Mohanty 2015). Foams swell with increase in temperature which is due to the expansion of gas phase in foams. When the temperature of foam is increased, foam volume reaches a peak value after which the foam volume decreases due to the evaporation of water from the foam structure (Li et al. 2012). Presence of solid particles increases the drainage rate initially and decreases later. Increase in temperature, rapidly decreases foam height in a static foam drainage test (Wei et al. 2020). Surfactants that are stable at high temperatures are used for creating stable foams at high temperatures. The addition of surface-modified nanoparticles increases the stability of aqueous foams at high temperatures (Singh and Mohanty 2017, Zhu et al. 2017).
[bookmark: _Toc99805616][bookmark: _Toc102015413]1.5.3 Effect of Contaminants
As drilling or completion foam circulates in the wellbore, it encounters contaminants like salt, oil, and clay. Lower concentrations of salt like NaCl and CaCl2 stabilize the foam. However, at higher concentrations, they destabilize the foams across all qualities (Obisesan et al. 2020). The effect of oil on the stability of foams is sensitive to foam qualities. At lower qualities, the presence of oil helps increase the stability of foams but as the foam quality increases above 60% the foam becomes unstable (Obisesan 2021). Clays like bentonite and kaolinite improve the stability of foam at all qualities with increasing clay concentrations (Obisesan 2021).  
[bookmark: _Toc99805617][bookmark: _Toc102015414]1.5.4 Effect of Additives
Foam stabilizing agents like fiber, polymer, and nanoparticles have been used to attain higher stability in foam structures. Nano particles along with surfactants provide stability to foam structure in presence of oil and salt (Qian et al. 2020). This is due to the change in curvature of lamella boundary and forming a barrier to minimize the contact area between bubbles which reduces the foam destabilizing process. Bentonite nanoparticles stabilize the foam and make them resistant to temperature and oil (Zhu et al. 2017). Fly-ash nanoparticles are inexpensive, and an exceedingly small amount of these nanoparticles show higher stability in presence of oil (Eftekhari et al. 2015). Addition of polymers improves the quality of foam and multiplies the half-life period and foam stability (Zvada et al. 2021). Sodium dodecyl sulfate surfactant with hydroxyethyl cellulose polymer is less stable as compared to their combination with nano silica (Parvaneh et al. 2022). 
[bookmark: _Toc99805618][bookmark: _Toc102015415]1.5.5 Surfactant Type
Surfactants lower the surface tension between the liquid phase and gas phase and stabilize the interface between the two phases created when the foam is generated by mixing or shearing. Experimenting with different surfactant types like anionic, amphoteric, cationic, and non-ionic showed that anionic surfactants take the highest time to reach half-life (Rand and Kraynik 1983). Besides this, recent studies show that nanoparticles and nano surfactants are better suited at higher temperatures (Omar et al. 2018, Singh and Mohanty 2017).
[bookmark: _Toc99805619][bookmark: _Toc102015416]1.5.6 Foam Generation Techniques
The primary requirements for aqueous foam generation is the presence of water containing a surface-active agent and mixing mechanisms. The method by which the foam is generated affects its properties. The bubble size distribution, rheological characteristics, drainage behavior, and half-life affected by foam generation technique. Different sizes of the mesh have been used to generate foam (Harris 1989). One of the methods includes in-situ generation of foam using a rotary mixer. Other methods used for generating foam involve the use of orifices, needle valves, and liquid phase vaporization.

2. [bookmark: _Toc99805620][bookmark: _Toc102015417]CHAPTER TWO
[bookmark: _Toc99805621][bookmark: _Toc102015418]Literature review
Foam is a multiphase fluid that exhibits instability affected by various factors. Quality and base-liquid viscosity are foam properties that directly impact its stability. Pressure, temperature, and contaminants can influence foam stability indirectly. Therefore, foam stability at high-pressure and high-temperature conditions is essential in underbalanced drilling. 
Oil is one of the most common downhole contaminants. Often foam drainage rate changes with the oil concentration in the base liquid (Obisesan 2021). Contaminants like oil can influence foam structure and bubble size distribution that are instrumental in determining the characterization of foams. Bubbles of various sizes and structures can be produced using different foam generation techniques and surfactants (Ozbayoglu 2005).  
[bookmark: _Toc99805622][bookmark: _Toc102015419]2.1 Foam Structure and Bubble Size
Properties of aqueous foams are related to their bubble structure. For a given quality, foam structure is determined by the minimization of surface energy. Plateau borders are edges formed when three bubble walls meet (Thomas et al. 2015). In 19th century, a Belgian physicist Joseph Plateau established some fundamentals, known as Plateau’s laws (Plateau 1873). It states the followings: 
a. Thin films are smooth and have a constant mean curvature
b. At the Plateau border, three films join together at an angle of 120°
c. The Plateau borders that link at one point come in a group of four and at an angle of 109.5 in a tetrahedral geometry (Fig. 2.1).
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[bookmark: _Toc102015465]Figure 2.1: Geometry and topology of aqueous foam at high qualities (Drenckhan and Hutzler 2015)
Bubble shape and structure depend on the foam quality (Drenckhan and Hutzler 2015). Bubble size increases with the gas volume fraction, more gas in the system means higher the bubble size. The bubbles get their opacity from the dispersion of light from the liquid film surface and plateau borders. Small bubbles scatter more light, thus making the foam appear whiter. An example of this is shaving foam and whipped cream. 
[bookmark: _Toc99805623][bookmark: _Toc102015420]2.1.1 Aqueous Foams
[bookmark: OLE_LINK1]High-quality aqueous foams show a hexagonal bubble structure, and low-quality foams display a normal spherical structure (Fig. 2.2). The average bubble size increases with time as the foam decays due to coalescence and coarsening, and consequently, the number of bubbles decreases with time.
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[bookmark: _Toc102015466]Figure 2.2: Spherical structure of aqueous foam at low quality (Left)  and Polyhedral structure of aqueous foams at high quality (Right)
The surface tension acting on the bubbles is given by the Young – Laplace law as excess pressure of a bubble inside a liquid is given by surface tension, and radius of bubble, R. Thus:
	[bookmark: _Hlk96199883]
	
	(2.1)


And the energy of the foam for n bubbles is given by: 
	[bookmark: _Hlk96202030]
	
	(2.2)


For a bubble of size of 100 µm, the surface energy is about 1013 times higher than the thermal energy which means that surface energy dominates the bubble packing over thermal energy (Drenckhan and Hutzler 2015). Thermal energy is the total internal kinetic energy of an object due to the random motion of its atoms and molecules. The average bubble size is smaller at the bottom of the foam structure because the foam at the bottom is wet foam, and the average bubble size is larger at the top of the foam structure because the foam at the top is dry foam. 
[bookmark: _Toc99805624][bookmark: _Toc102015421]2.1.2 Oil-Contaminated Foams
For aqueous foams, oil acts as a contaminant but doesn’t enter the bubbles. Oil droplets travel through the foam lamella overcoming the electrostatic interactions (Telmadarreie and Trivedi 2018). As the oil droplet approaches the gas-liquid interface, it forms an oil film at the gas interface called a pseudo emulsion film. Oil droplets cannot penetrate the bubble when the pseud emulsion film is stable. The presence of vesicles creates a thick film around the bubbles (Fig. 2.3) and contributes to the slowing down of the coarsening of bubbles (Rio et al. 2014). 
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[bookmark: _Toc102015467]Figure 2.3: Spherical structure of aqueous foam at an early stage (Left) and after 5 minutes (Right)
Oil-laden foams have a fragile structure and lose their pseudo emulsion property easily. Small oil droplets get trapped in between the plateau borders. Small oil globules come together to form big oil globules which deform the plateau border and destabilize the foam (Mensire and Lorenceau 2017). This process is also accelerated by drainage of liquid phase making bubble films thinner. 
[bookmark: _Toc99805625][bookmark: _Toc102015422]2.2 Drainage Mechanism
Foam structures are a part of non-equilibrium systems like emulsions or off-critical decomposing mixtures that change their shape and size with time (Carrier and Colin 2003). Foam destabilization can be explained by two methods: drainage and decay. Drainage is the loss of the liquid phase from the foam structure and is governed by capillary and gravitational forces. During foam decay, there is a loss of bubbles in the foam structure due to the merger of smaller bubbles into larger bubbles known as coarsening and bubble coalescence which is caused by the rupturing of the bubble film. In this study, the stability of aqueous foams is studied by measuring the drainage with respect to time. Foam drainage occurs because the trapped foam has a natural tendency to acquire static equilibrium. Constant drainage and decay cause changes in foam structure and thus alter the property of foam continuously (Cohen et al. 2015). Therefore, it is necessary to understand the drainage mechanism of the liquid phase in the foam structure. 
There are three drainage regimes in static foam columns (Fig. 2.4). In Regime 1, the drainage rate is transient and increases rapidly. After that, the drainage due to gravity is countered by viscous and capillary forces, which establish an equilibrium between them, and the drainage rate becomes constant represented in Regime 2. As the gravitational drainage increases, the amount of liquid fraction present in the foam structure decreases. This causes the liquid film to become thin and stop further drainage. In Regime 3, foam decaying is dominated by coalescence and coarsening as the foam film structure dries. 

[bookmark: _Toc102015468]Figure 2.4: Foam drainage curve (Redrawn using data from Agrillier et al. 1998)
When foam is directly exposed to the atmosphere without any covering, the liquid film evaporates from the top surface and accelerates the drainage process. The larger bubbles rise to the top of the foam structure as they have a large gaseous phase entrapped in them decreasing the overall density of the bubbles. The presence of fatty alcohols and oil on the film surface reduces the rate of water evaporation significantly (Barnes 1986). For a trapped foam, conventional drainage occurs through the plateau borders. 
Gravitational Drainage: Foam drainage can be explained as the flow of liquid through the plateau borders and nodes between bubble structures which is induced by gravity. Moreover, bubbles with large volumes rise quickly due to the buoyancy and the heavier liquid is collected at the bottom of the foam column. This phase-based segregation phenomenon is called Gravitational Drainage. As foam quality increases from 70% due to drainage, the bubble change from spherical to polyhedral. Close examination of the drainage process indicated that the maximum drainage occurs at the interconnected network of Plateau borders (Cohen et al. 2015).  One of the crucial factors for gravity drainage is the coupling of bulk and surface flows at plateau borders and nodes, which can be adjusted by the surfactant and base liquid viscosity (Saint-Jalmes 2006). Drainage time can be defined as the period of liquid drainage from the foam structure driven by gravity until an equilibrium state is found between the capillary effects and gravity. Basic foam drainage model was introduced by (Kraynik 1983) where simplifying assumptions were made to reduce the number of parameters. Assumptions made were: 
1) Rigid gas-liquid interface
2) Uniform Initial liquid volume fraction distribution
3) Liquid hold-up in the films is negligible
 Foam drainage time-dependent model was modified by (Koehler et al. 1998; Koehler et al. 2000): 
	
	
	(2.3)


where H is the foam height, R the average bubble radius, 𝜌 is liquid density, ɳ is viscosity, g is acceleration due to gravity, K is dimensionless permeability and α is an exponent between 0.5 and 1. This model is effective for wet foams and the drainage time for dry foams is negligible. K and α depend on the mobility of the surface layers protecting the bubbles which again depends on compression modulus and surface shear viscosity (Saint-Jalmes et al. 2004). Foam drainage can be stopped if the liquid phase manages to solidify or form a gel.
Coarsening: Foams attain their thermodynamic equilibrium by reducing total surface area as the average size of the bubbles increases with time and coarsening of bubbles occurs (Hilgenfeldt et al. 2001). Coarsening is a process that involves the movement of the gas phase from smaller bubbles to larger bubbles increasing the average bubble radius. The Laplace pressure is the driving mechanism for this process. Laplace pressure is the pressure difference between the curved surface or interface. This pressure jump arises due to surface tension or interfacial tension, which compresses the curved surface or interface. Coarsening follows the same principle as the phenomenon of Ostwald Ripening (Rio et al. 2014). The diffusion of gas happens through the thin film between the bubbles as it provides the smallest diffusion path. The gas's effective diffusion coefficient (Deff) and nature are the driving factors for the characteristic coarsening time. The coarsening effect becomes significant when the drainage curve reaches the plateau region and the period through which this coarsening effect lasts is called as coarsening time. Coarsening time is given by (Hilgenfeldt et al. 2001):
	
	
	(2.4)


[bookmark: OLE_LINK2]Coarsening time is observed as foams get drier and the liquid fraction is less than 0.36. Highly soluble gases such as carbon dioxide crate less stable foam because they dissolve in water and quickly diffuse through the thin film between the bubbles. The diffusion of gas can be slowed down by using less soluble gas like nitrogen instead of carbon dioxide (Weaire and Pageron 1990). Consequently, strong coarsening of bubbles causes faster liquid film drainage and foam degradation.
Coalescence: As the bubble structure attains equilibrium from the drainage and reaches a critical liquid volume fraction, the bubble films become thin and rupture. This process leads to bubble coalescence. Unlike coarsening, there is no diffusion of gas in coalescence. Due to rupturing of the bubble film, there is a loss of gas in the foam structure. Bubbles coalescence can be reduced by adding stabilizing agents like polymers, nanoparticles, proteins, low molecular weight surfactants, or their mixtures (Tcholakova et al. 2008).
[bookmark: _Toc99805626][bookmark: _Toc102015423]2.2.1 Aqueous Foams
The drainage process of foams in vertical columns can be explained by considering different natural phenomena. As the foam quality increases the drainage rate decreases. This is due to the increase of viscous force as the foam quality increases and liquid fraction decreases (Kruglyakov et al. 2008). The foam becomes dry, and the bubble films become thin. As the film becomes thin, the area of flow through the conduit decreases, and the effect of capillary and viscous forces increases which hinders the drainage of dry foams.
The drainage in inclined columns is more complex due to the presence of lateral drainage along with vertical drainage (Fig. 2.5). The lateral drainage results in forming a liquid layer on the low side of the column. Due to gravity, the liquid layer flows downward in the inclined wall and accumulates at the bottom of the column. As a result, a higher drainage rate is observed in the inclined column than in a vertical one (Govindu et al. 2021).
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[bookmark: _Toc102015469]Figure 2.5: (a) Drainage in Vertical column (b) Drainage in Inclined column (Govindu et al. 2021)
[bookmark: _Toc99805627][bookmark: _Toc102015424]2.2.2 Oil-Contaminated Foams
Foams show certain change in stability in presence of oil due to the interaction of contact phases between the oil phase and the porous phase of the foam structure (Schramm and Novosad 1992). Based on oil types in foam emulsions, there are three types of foam A, B, and C (Fig. 2.6) respectively as described by (Schramm and Novosad 1990). These foams can be classified on the basis of Lamella number. Lamella number is a dimensionless ratio of pressure drop between the plateau border and oil drop. Lamella number is calculated by:
	
	
	(2.5)

	Where, ΔPc = Pressure drop at the plateau border 
             ΔPR = Pressure drop at the oil-foam interface
             ϒF = Foaming aqueous solution surface tension
             ϒOF = Foaming aqueous solution/oil interfacial tension
                   rp = Radius at plateau border 
             ro = Radius of the oil drop
Later they found experimentally that the ratio of ro/rp is 0.15 (Schramm and Novosad 1992).  

	[bookmark: _Hlk96378233]
	
	(2.6)


Type A foams have L values less than unity. Type B foams exhibit L values ranging between 1 to 7, whereas Type C foams have L values greater than seven. Type A foams are the most stable in the presence of oil, and Type B and C foams become less stable with the increasing Lamella number. 
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[bookmark: _Toc102015470]Figure 2.6: Types of foam and their behavior after oil contact (Schramm and Novosad 1990)
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[bookmark: _Toc102015471]Figure 2.7: Oil particles trapped at the Plateau borders and nodes for 5% oil v/v (Vikingstad et al. 2005)
It is found that the stability of the foams with emulsified oil depends on the stability of the pseudo emulsion film that forms between oil and the gas-liquid interface (Koczo et al. 1991). If the pseudo emulsion film is stable, the oil does not enter the gas-liquid interface (Fig. 2.7) but if it is unstable then the oil droplets enter the bubble and destabilize the foam.  
[bookmark: _Toc99805628][bookmark: _Toc102015425]2.3 Foam Drainage Models
Foam drainage is studied over a macroscopic scale so that a continuum or coarse-grained approach is appropriate. Foam drainage is the flow of the liquid phase from the foam structure through interstitial spaces between the bubbles. The interstitial flow can be through three different ways:
a. Films formed between two neighboring bubbles that have almost flat bubble faces.
b. Plateau borders, where three films meet.
c. Nodes or junctions, where four plateau borders intersect.
Foam drainage models have been developed based on conservation laws as they can help predict the drainage characteristics of foams under various conditions. Various foam drainage models have been developed to predict foam quality profile during the drainage process. The models for node-dominated and channel nominated drainage are established by applying Darcy’s law to foam (Koehler et al. 2000). While deriving the general foam drainage equations, the following assumptions are made.
(a) All bubbles present in the foam structure are monodispersed. 
(b) The gas pressure and volume are constant across all bubbles
(c) Compression due to gravity is negligible due to the small weight of the foams.
(d) There is the no-slip interface boundary condition at the walls of the container
(e) The viscosity is assumed to be constant throughout the foam structure
(f) The liquid in the faces is stationary and any motion of channel walls is resisted by the surface viscosity
According to Koehler et al. (2000), the driving force (G) that causes the drainage of foam in vertical configuration is mathematically expressed as:
	
	
	(2.7)


Here the first term is the hydrostatic pressure gradient, and second term is pressure gradient due to the surface tension at the boundary. The radius in the second term can be approximated with channel length for dry foams where r<<L and bubbles have a polyhedral structure. G is the pressure gradient driving the flow, 𝜌 is the liquid density, g is acceleration due to gravity, r’ is the radius of curvature for channels, Ԑ is liquid volume fraction, ꝺԑ is a geometric constant for bubble and L is the channel length
The model considers the contributions of viscous dissipation in channels and nodes of liquid network. The driving force is opposed by the viscous force. Hence, balancing these two forces, the generalized foam drainage equation can be expressed as (Koehler et al. 2000):
	
	
	(2.8)


For equation 2.8, there are three forces involved i.e., viscous, gravitational and surface forces respectively. In the model development, foam is treated as a porous medium with a permeability that varies with liquid volume fraction. For channel dominated drainage, the permeability of the foam k(ԑ) is directly related to the liquid volume fraction by:
	
	
	(2.9)


where K1 is a dimensionless number that depends on the geometry of foam structural units.
For one-dimensional drainage, the drainage equation can be further simplified by considering channel dominated drainage (Koehler et al. 2000). Therefore:
	
	
	(2.10)


For node dominated drainage, the permeability of the foam is directly related to the square root of the liquid volume fraction. Thus:
	

	
	(2.11)


Combining Eqns. (6) and (9), the model for node dominated drainage can be formulated as (Koehler et al. 2000):
	
	(2.12)


where K1/2 is a dimensionless number. 
The node dominated drainage equation reproduces results from experiments with good accuracy, but the channel dominated equation fails to do so (Koehler et al. 2000). However, channel dominated model showed better accuracy with protein-based surfactants. 
Recently, node-dominated and channel-dominated drainage models have been utilized to simulate laboratory experiments conducted with aqueous foams (Govindu 2019). The numerical foam drainage models were formulated considering the following assumptions:
(a) Bubbles in the foam structure are assumed to be monodispersed.
(b) Drainage is considered to be in vertical model only 
(c) Uniform surfactant concentration throughout the vertical section 
(d) The bubbles are considered to be maintain a spherical shape. 
(e) Geometric constant (ꝺԑ) is assumed to be 0.1711. 
(f) Effects of wall slip, and container shape are neglected. 
Both the models were tested for aqueous and polymer foams of qualities 40%, 60 % and 80%. These models were unique as they included the effect of change in bubble size distribution as the drainage progresses with time. These models predict the change in liquid volume fraction over time in a static foam column. Since, we are working with aqueous foams, we will discuss the results between the experimental and predicted values of the model. 
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[bookmark: _Toc102015472]Figure 2.8: Experimental measurements and model predictions for 40% aqueous foams –(a) channel dominated and (b) node dominated models (Govindu 2019)
From (Fig. 2.8) results obtained for 40% quality foams, channel dominated model predicted liquid volume fraction values were slightly off from the values obtained through experimental results. While the node dominated model, over predicted the liquid volume fraction values. 
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[bookmark: _Toc102015473]Figure 2.9: Experimental measurements and model predictions for 60% aqueous foams –(a) channel dominated and (b) node dominated models (Govindu 2019)
For 60% foam quality (Fig. 2.9), node dominated models over predicts the liquid volume fraction while the channel dominated model values were closer to the experimental values. 
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[bookmark: _Toc102015474]Figure 2.10: Experimental measurements and model predictions for 80% aqueous foams – (a) channel dominated and (b) node dominated models (Govindu 2019)
For 80% foam quality (Fig. 2.10), both the models made decent predictions for liquid volume fraction, however the channel dominated model showed better fit to the experimental values. 
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[bookmark: _Toc102015475]Figure 2.11: (a) Mean bubble diameter correlation for aqueous foams and (b) Error % of correlations (Govindu 2019)
The correlation developed by (Govindu 2019) predicted the average bubble diameter for different foam qualities. However, there were few outliers with these model and majority of the predicted values lie within an error of +/- 25 %. This is because the Non-Newtonian behavior of the liquid phase was not considered. 
[bookmark: _Toc99805629][bookmark: _Toc102015426]2.4 Effects of Container Shape
Effects arbitrary container shape on capillarity and vertical gradients are studied and another set of equations were developed by (Saint-Jalmes et al. 2000). Most liquid in the foam structure resides in the random network of plateau borders. So, the average velocity of the liquid in the foam structure can be established by considering the balance of gravity, viscosity, and capillarity:
	
	
	(2.13)


where m is a parameter that depends on the nature of viscous dissipation, u is flow speed, uo is maximum flow speed, є is capillary rise, ԑc is critical liquid fraction and z is the height of container. For plateau borders, m = 1, and for vertices, m = 0.5. Assuming that the flow is only downwards, it is easier to deduce a drainage equation for container of any shape. Cross sectional area (A) and height of the container become important parameters to be considered in the analysis (Saint-Jalmes et al. 2000).  This:
	
	
	(2.14)


The first term in the bracket is the drainage equation and the second bracket is accounting for the container shape. For a container shaped like ‘Eiffel tower’ which flares at the bottom, an exact solution can be obtained (Saint-Jalmes et al. 2000). Therefore, the liquid volume fraction is expressed as a function of position and the time(t) as:
	 
	
	(2.15)


Here time (to) given used in equation 2.16, is given by equation 2.17,
	
	
	(2.16)


Where to = Initial time, t=0 
ԑo = liquid fraction at initial time
zo = Initial capillary rise
Volume of the corresponding drained liquid is given by (Saint-Jalmes et al. 2000).
	
	
	(2.17)


Where V(t) = Volume of liquid at time ‘t’	
	Vf = Final volume of liquid at t = 0
At late time, the model is inaccurate as it doesn’t take capillarity and coarsening (Saint-Jalmes et al. 2000). 
[bookmark: OLE_LINK3][bookmark: OLE_LINK4]The fluid velocity is zero at the plateau borders since they are assumed to be rigid. Also, the flow is considered to be Poiseuille-like. For forced drainage model, fluid velocity is given by (Saint-Jalmes et al. 2004):
	
	
	(2.18a)


Here Kc0 is the dimensionless permeability
But when the plateau borders are not rigid and coupling between bulk and surface flows are taken into consideration. New coupling parameter M is introduced into Eqn. (2.18b). Thus: 
	
	
	
	(2.18b)


The values of a and b are constants varying with liquid fraction. The coupling parameter (M) is defined as:
	 
	
	(2.19)


Here, µs = Surface shear viscosity  
A large value of M means more mobility of the surfaces and reduced hydrodynamic resistance of Plateau borders. Another coupling parameter N has been proposed to account for surface tension gradients of bulk and surface flow (Durand and Langevin 2002):
	
	
	(2.20)


Considering the coupling parameters M and N at the same time, the fluid velocity equation can be written as (Saint-Jalmes et al. 2004):
	
	
	(2.21)


The mobility control parameter (M) incorporates bubble size, liquid phase fraction and surface shear viscosity. The importance of this parameter is verified with a large number of experimental data. Hence, the assumption that flow of liquid is through the network of nodes and plateau borders with negligible transport in the thin films is reasonable and it demonstrates the importance of bubble geometries (Koehler et al. 2000). However, this parameter (M) fails for bubbles of small size (less than 0.2 mm diameter) and a bulk-surface coupling parameter N is introduced. For foams drainage with small bubble sizes, the surface mobility is determined by the node and plateau border resistances (Saint-Jalmes et al. 2004).
[bookmark: _Toc99805630][bookmark: _Toc102015427]2.5 Effects of Oil
Foam behavior for oil, gas, and surfactant mixture is characterized by spreading coefficient (Harkins 1941) and entering coefficients (Robinson and Woods 1948).
	
	(2.22)
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Where, ϒwg = Surface tension between water-gas phase
ϒwo = Surface tension between water-oil phase
ϒog = Surface tension between oil-gas phase

A positive entering coefficient means favorable energy for oil to enter the gas-water interface from the water phase side. Negative value of entering coefficient of oil is correlated to the stability of foam. The positive spreading coefficient of aqueous phase on gas-oil interface is an indication of foam stability in presence of oil. Foam stability varies with pressure for different surfactants for both conditions; presence and absence of oil (Holt et al. 1996). Later, it was found that entering and spreading coefficient values are not enough to judge foam’s stability, but the stability of Pseudo emulsion film stability is an important parameter to take into consideration while determining foam’s stability (Telmadarreie and Trivedi 2018; Vikingstad et al. 2005). 
The stabilizing effect of oil depends on its nature. If the oil is solubilized or emulsified and accumulated in the plateau border, it inhibits the liquid drainage due to increased hydrodynamic resistance (Koczo et al. 1992). 
Another factor known as Lamella rupture frequency (fb) is introduced for oil contaminated foams by (Schramm and Novosad 1992):
	
	
	(2.25)


This equation gives a good correlation between foam stability and lamella number (L). The addition of foaming agents like polymers enhance the stability of foam in presence of oil (Telmadarreie and Trivedi 2018; Govindu 2020). Also, smaller alkanes destabilize foam whereas larger alkanes stabilize it (Vikingstad et al. 2005). An overview of effect of oil in aqueous foam with regards to oil-foam interaction is shown in (Fig. 2.12).
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[bookmark: _Toc102015476]Figure 2.12: Foam stability classification in presence of oil (Reproduced from Koczo et al. 1991)


3. [bookmark: _Toc99805631][bookmark: _Toc102015428]CHAPTER THREE
In this investigation, aqueous foams were tested to study the influence of pressure, foam quality, oil contaminant on foam drainage and bubble size distribution at ambient temperature. The tests were conducted with maintaining the same procedure and environmental conditions to avoid any inconsistency in measurements and minimize the error. This chapter presents in detail the experimental setup, test material, and their properties, test procedure, scope of the experiment, data acquisition and analysis. 
[bookmark: _Toc99805632][bookmark: _Toc102015429]3.1 Experimental Setup
The experimental setup used for this investigation is a foam circulating flow loop (Fig. 3.1) consists mainly of two sections: (a) Drainage test section and (b) Rheology test section. A 1000 mL base liquid tank (liquid reservoir) was used for introducing base liquid containing a mixture of water, surfactant, and oil as needed. The mixture was introduced into the system by opening a valve installed below the tank. The entire system was filled with the surfactant mixture with the help of a gear pump powered by a motor with variable frequency drive (VFD) control (Fig. 3.2). Nitrogen was introduced in the foam generation section and mixed with the surfactant mixture. This mixture was foamed with help of a needle valve placed between two static mixers. A flow meter was used to monitor the flow rate and density of the generated foam. 
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[bookmark: _Toc102015477]Figure 3.1: Schematic of the experimental setup
The drainage test section contains a vertical column with a height of 1.93 m. The foam was trapped in this section with the help of two automated valves. The foam drainage is calculated by measuring the differential pressure with the help of 10 differential pressure transducers dividing the vertical column into 9 tests segments (Fig. 3.3). The vertical column was pressurized with the help of nitrogen gas and the pressure was controlled by a pressure regulator installed on nitrogen supply cylinder. 
[image: A picture containing indoor

Description automatically generated]
[bookmark: _Toc102015478]Figure 3.2: Motor and Pump
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[bookmark: _Toc102015479]Figure 3.3: Experimental setup of vertical drainage test section
An optical microscopic camera (Dinolite Model AD7013MT) and a viewport were installed at the inlet of the vertical column to capture images of the foam structure (Fig. 3.4). The camera has built-in illumination with the help of 8 white LED’s. The scope of the camera ranges from 10x-240x magnification. The camera has calibration features and accurately analyze the bubble size distribution in the image with the help of a software provided with the camera.
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[bookmark: _Toc102015480]Figure 3.4: Optical microscope with viewport at the side angle (left) and top angle (right)
[bookmark: _Toc99805633][bookmark: _Toc102015430]3.2 Test Materials
Aqueous foams of varying qualities (40%, 50 %, and 60%) were generated in the above-mentioned experimental setup using water, surfactant, and nitrogen gas. To study the effect of oil contaminant, Drakeol light mineral oil was added to the base liquid (water + surfactant). Tap water (from Norman, Oklahoma) was used in the base liquid mixture. 
[bookmark: _Toc99805634][bookmark: _Toc102015431]3.2.1 Surfactant
Aqueous foam was generated using anionic surfactant commonly known as Howco SudsTM (Fig. 3.5). Surfactant was used at 2% concentration which is higher than the CMC value of the surfactant as indicated in previous studies (Akhtar et al. 2018; Govindu 2019). The surfactant properties are given in Table.3.1:
[bookmark: _Toc100231222][bookmark: _Toc100231440]Table 3.1: Properties of the surfactant used
	Howco SudsTM

	Physical State
	Liquid

	Color
	Light Yellow

	Boiling Point
	>300oF

	pH range
	6.5 – 7.5
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[bookmark: _Toc102015481]Figure 3.5: Anionic surfactant used for foaming
[bookmark: _Toc99805635][bookmark: _Toc102015432]3.2.2 Oil
Light mineral oil (Fig. 3.6) was used to study the effects of oil contamination on the drainage and structure of foam. Concentration of mineral oil was in range of 0% to 20% by volume with an increment of 10%. White mineral oil is insoluble in hot and cold water. The properties of the oil are given in Table.3.2:

[bookmark: _Toc100231223][bookmark: _Toc100231441]Table 3.2: Properties of Mineral oil
	Mineral Oil

	Color
	Colorless

	Physical state
	Liquid

	Viscosity (cP)
	38.4

	Density (g/cm3)
	0.82

	API gravity
	35
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[bookmark: _Toc102015482]Figure 3.6: Drakeol Mineral Oil
[bookmark: _Toc99805636][bookmark: _Toc102015433]3.2.3 Nitrogen Gas
Technical grade nitrogen gas (99.9%) was used as a gaseous phase for generating foam. The gas was supplied in a high-pressure (20 MPa) cylinder (Fig. 3.7). The gas was injected into the flow loop to control foam quality and system pressurize. Using nitrogen foams has several benefits due to its properties like:
1. Inertness
1. Non-flammability
1. Low solubility
1. Low environmental impact.
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[bookmark: _Toc102015483]Figure 3.7: Compressed nitrogen cylinder with pressure gauge
[bookmark: _Toc99805637][bookmark: _Toc102015434]3.3 Test Procedure
This section describes the experimental procedure used to generate foam in the flow loop. Controlling the pressure in the system and achieving foam of desired quality are two major operations in this process. 
For the base liquid preparation, a mixture of water and surfactant is created. The surfactant concentration used was 2% v/v of water. So, for 2 L of water used, 40 mL of surfactant was added and mixed for 10 minutes with a laboratory stirrer for homogeneity (Fig. 3.8). Two drops of pink dye were added to improve the visibility of bubbles while capturing images. To study the effects of presence of oil contaminant at different concentrations, oil was added to the water-surfactant mixture and stirred for 10 minutes for dispersing mineral oil in water.  
[image: A picture containing indoor, device

Description automatically generated]
[bookmark: _Toc102015484]Figure 3.8: Laboratory stirrer controlled with a rheostat
Once the base liquid was ready, it was filled in the 1-L liquid tank (Fig. 3.9), and valve V1 was opened to fill up the entire flow loop. The reverse flow of the base liquid was prevented with the help of a check valve. The valve V2 is kept completely open to release back pressure from the system and allow the free flow of base liquid into the flow loop. After the system was filled with base liquid, both valves (V1 and V2) were closed, and the motor was started at full capacity. The base liquid was pumped through the entire system keeping all pipe viscometers open to allow maximum flow area for the fluid. Nitrogen gas was introduced into the system at the desired pressure, and the needle valve was kept open to allow circulation while mixing the gas and the liquid phases.
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[bookmark: _Toc102015485]Figure 3.9: Liquid tank filled with base liquid
[bookmark: OLE_LINK5]Then the needle valve was throttled to generate foam. For all experiments, a differential pressure of 500 inches of water between upstream and downstream of the valve was maintained to ensure uniform foam generation (Akhtar 2017; Akhtar et al. 2018; Obisesan et al. 2020). As the base liquid turned into a foam of constant quality, it was compared to the desired quality of foam. If the desired foam quality was not achieved, the liquid phase was slowly drained through Valve V7 while injecting nitrogen to maintain pressure. And the system was closed again to regenerate the foam and measure its quality. This step-by-step procedure was repeated until the desired quality of foam was achieved. The foam was circulated for an additional 5 minutes after the desired quality was achieved to make sure the foam has been fully generated and is stable while flowing. 
For the stability test, the foam was trapped in the vertical section to allow drainage of the liquid phase. During this test, the motor was shut off, and valves V3 and V6 were closed to trap the foam. The pressure distribution in the column was measured using differential pressure transducers for two hours. The images of the trapped foam were captured at 30, 60, 90, and 120 minutes of the stability test from the viewport (Fig. 3.10).
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[bookmark: _Toc102015486]Figure 3.10: Visual cell with base fluid
A commercial software (DinoCapture) supplied with the camera was used to capture images using the digital microscope. All the data collected from the stability test is analyzed and drainage of foam is calculated as a measure for foam stability. Bubble size distribution is obtained by digital image processing using DinoCapture and ImageJ software.
[bookmark: _Toc99805638][bookmark: _Toc102015435]3.4 Experimental Scope
In this study, we tested aqueous foams to see the influence of pressure, foam quality, and oil contaminant on drainage and bubble size distribution. The pressure rating on the viewport (425 psi) is the limiting factor for the test pressure. The data from the stability test is acquired using VBA in Excel from the sensors connected to the data acquisition board. The pressure variations along the vertical column are the important measurements to determine the drainage of the foam over two hours and observe the effect of test parameters on the half-life of the foams. While generating foam, data collected to ensure good quality foams include flowrate, density, temperature, system pressure, and pressure differential across the needle valve pressure. Foam densities are normalized with the initial foam densities of each section. Normalized foam density chart (Fig. 3.11) gives us information about the changing densities of trapped foam in each segment of the vertical column. As the drainage test starts, the liquid starts draining from the top sections which is monitored by pressure sensors. As a result of the drainage, lower sections start gaining liquid and their densities start increasing and later the curve flattens which means that the lower segments are filled with liquid.

[bookmark: _Toc102015487]Figure 3.11: Normalized foam column density for each section for the period of drainage test for 60% quality foam.
While generating foam, flowrate data has been captured from starting with base liquid till the achieving the desired foam quality. From Fig. 3.12, we can see that initially the density measurements were unstable. But as the foam is fully generated, we get homogenous foam with constant density.

[bookmark: _Toc102015488]Figure 3.12: Flowrate while generating foam
The test matrix is discussed in Table.3.3:
[bookmark: _Toc100231224][bookmark: _Toc100231442]Table 3.3: Test Matrix
	Foam type
	Aqueous Foam

	Liquid phase
	Tap water

	Surfactant used (v/v)
	Howco SudsTM at 2% concentration

	Gas phase
	Nitrogen

	Dye used
	Pink dye (does not change consistency)

	Contaminant used
	White mineral oil

	Contaminant concentration (v/v)
	0%, 10%, and 20%

	Foam qualities
	40%, 50 %, and 60%

	System pressure (psi)
	100, 250, and 400



A total of 27 tests were performed with each varying combination of pressure, foam quality, and oil concentration. The pink dye was used to give the generated foam a bright color to increase the quality of taken images and make the bubbles more visible. The foam stability was tested at ambient temperature for all 27 tests. 
[bookmark: _Toc99805639][bookmark: _Toc102015436]3.5 Data Analysis
[bookmark: _Toc99805640][bookmark: _Toc102015437]3.5.1 Analysis of Pressure Profiles
For data analysis, the differential pressure is measured across the vertical test section where the foam is trapped. Ten pressure transducers (with an accuracy of ± 5%) divide the vertical column into nine segments (Fig. 3.3). For instance, the segment between DP1 and DP2 is referred as Segment 1, the segment between DP2 and DP3 is named as Segment 2 and so on till Segment 9. The pressure profile measurement helps us to verify the homogeneity of the generated foam in the vertical column. When the pressure profile is linear, the foam in the column is considered as homogenous (Fig. 3.13), and as the liquid film starts draining from the foam structure, the pressure profile becomes non-linear with time. 

[bookmark: _Toc102015489]Figure 3.13: Differential pressure profile for generated homogeneous foam
The pressure data obtained from the pressure sensors has units (in. H20), so it is converted into Kilopascal (kPa). The foam drainage from each segment is determined by applying the pressure profile plots non-linear regression analysis using the second-degree polynomial (Eqn. 3.1). 
	
	
	(3.1)


Where, C1 and C2 are constants and are calculated using excel functions:
C2 = INDEX(LINEST(y, x^{1,2}),1)
C1 = INDEX(LINEST(y, x^{1,2}),1,2)
b = INDEX(LINEST(y, x^{1,2}),1,3)
The known pressure data is fitted as ‘x’ and the column height is fitted for ‘y’. LINEST function is used to calculate the statistics for a straight line that best fits the data and returns an array of constants corresponding to each x-value till we reach constant value ‘b’. A LINEST function that is built inside an INDEX function gives specific values that are called in the function as outputs. For our purpose, we can rewrite (Eqn 3.1) as:
	
	
	(3.2)


On differentiating Eqn. 3.2 with ‘H’ we get:
	
	
	(3.3)


Where P = pressure data from sensors, H = height of the foam column. 
P can be written as hydrostatic pressure head:
dP = 𝜌 * g * dH 										  (3.4)
Substituting Eqn. 3.4 in eqn. 3.3, we get:

	
	
	(3.4)

	
	
	(3.5)


Eqn. 3.5 can be used to calculate the density of foam at any height in the vertical test section. 
For calculating the average foam density between two segments by substituting ‘H’ as average height by substituting H=(h1+h2)/2, Eqn.3.5 can be modified as:
	
	
	(3.6)


where h1 = Starting height of the foam column segment and h2 = Ending height of the column segment for the vertical foam column. 
With the help of these constants (C1 and C2), average density (𝜌avg) of the trapped foam is calculated for each segment where there is no liquid loading observed. Only the top 3 segments are considered in the regression analysis because the bottom segments can gain liquid from the drainage of upper segments and consequently exhibit pressure profiles that are different from those of the upper foam-containing segments. 
After this, the quality of foam is calculated with the following:
𝜌avg = Average Density, 𝜌liq = Liquid density, 𝜌gas = Gas density
	
	
	    (3.7)


The liquid volume (Vliq)is calculated using the foam quality and the volume of the foam segment (Vsegment) in the vertical column:
	
	
	    (3.8)


As the liquid drains from the foam structure, the volume of gas in the foam increases. The drained liquid is given by:
	
	
	(3.9)


	
	
	 (3.10)


And total drained volume is calculated by:
Where i is the time at which the drainage was calculated. For our experiments, the time duration for the drainage tests lasted up to a minimum of 2 hours. 
Final drainage volume is given by:
	
	
	     (3.11)


[bookmark: _Toc99805641][bookmark: _Toc102015438]3.5.2 Foam Image Analysis
[bookmark: OLE_LINK9][bookmark: OLE_LINK10]Raw images taken from the optical microscope are calibrated for their magnification to provide the correct scale for the respective picture (Fig. 3.14). Magnification was kept constant for all 27 tests to maintain consistency. The raw image is then analyzed using the ImageJ software, where the brightness and threshold of the image were adjusted for the best possible image quality. Once the bubble boundaries are seen clearly, the scale is set for the image, and bubble size is measured for each bubble. A maximum of 100 bubbles are included in the bubble size analysis to give an accurate size distribution at 30, 60, 90, and 120 minutes for each test. The data obtained from these images were related to the drainage data obtained from the stability test to check for any correlation between them.   
[image: A picture containing tiled

Description automatically generated] [image: ]
(a)                                                                (b)
[bookmark: _Toc102015490]Figure 3.14: (a) Raw image taken from the digital microscope (left) and (b) Image analyzed in ImageJ (Right)


4. [bookmark: _Toc99805642][bookmark: _Toc102015439]CHAPTER FOUR
[bookmark: _Toc99805643][bookmark: _Toc102015440]RESULTS AND DISCUSSIONS
[bookmark: OLE_LINK11]In this section, experimental results are discussed discuss. Drainage measurements are analyzed to understand the stability of aqueous foams and the effects of pressure, quality, and oil contaminant concentration on foam drainage. The bubble structure of foam was examined in each test at an interval of 30 minutes for 2 hours. The examination was performed to understand the relationship between the foam drainage and the bubble size. The test setup, experimental procedure and test conditions were kept constant to minimize experimental error. The homogeneity of foam was maintained while varying foam quality for each test by constantly monitoring the density and flow rate of the foam along with the differential pressure measurements obtained from the pressure transducers along the vertical test section.
[bookmark: _Toc99805644][bookmark: _Toc102015441]4.1 Stability Test
Multiple stability tests were performed to check the repeatability of the drainage tests. From (Fig. 4.1), results for drainage tests for 40% foams at a system pressure of 250 psi are compared.  

[bookmark: _Toc102015491]Figure 4.1: Repeatability of drainage tests for foam quality of 40% at system pressure of 250 psi
It is seen that the tests give same results under similar conditions and the error percentage between the drainage measurements of the tests at any given time of the drainage test is less than  2.5 %. Similarly, tests were conducted for different quality of foams for varying conditions and same results within the error percentage would be obtained repeatedly.
	As the liquid phase drains from the foam structure, the foam quality increases continuously throughout the 2-hour period of the drainage test. For foam of 40 % quality, not much change is seen in the foam quality profile with increase in pressure (Fig. 4.2a). But for 50% quality foams, with the increase in pressure a decline is observed in the foam quality profile (Fig. 4.2b).
	[bookmark: _Hlk102012938]
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[bookmark: _Toc102015492]Figure 4.2: Foam quality profile for the drainage test for pure aqueous foams of different foam qualities (a) 40%, (b) 50%, and (c) 60%
This observation indicated the increase in stability of 50% foam at higher pressures. Same result is observed for foams of 60% quality (Fig. 4.2c).
	By looking at the density profile of pure aqueous foams, it is observed that for stable foams the change is density is lower as compared to unstable foams. Continuous monitoring of density is done for the 2-hour period with the help of pressure sensors which have an error percentage of  0.5%. For 50% and 60% foam qualities, it is observed that with the increase in pressure, the change in density is least (Fig. 4.3). This is due to less amount of liquid drainage from the foam system. The overall foam density decreases with increase in foam quality.
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[bookmark: _Toc102015493][bookmark: _Toc99805645]Figure 4.3: Foam density profile for the drainage test for pure aqueous foams of different foam qualities (a) 40%, (b) 50%, and (c) 60%
[bookmark: _Toc102015442]4.1.1 Aqueous Foam
[bookmark: OLE_LINK12][bookmark: OLE_LINK13]The initial experiments were conducted with pure aqueous foams (i.e. with no impurities). These tests studied the effects of pressure and quality on aqueous foams' drainage. Drainage of trapped foams in the vertical section is the measurement of foam stability. 
First, the effect of varying foam quality can be examined when the system pressure is kept constant (Fig. 4.1).  Results show the effect of foam quality on foam drainage at different pressures. At 100 psi (Fig. 4.1a), all foam qualities have approximately 98% drainage at the end of 120 minutes. Although, the foam quality of 60% has a delay of 10 minutes to reach their half-life stage (i.e., drainage of 50%) compared to 40% and 50% foams. This half-life extension implies that the effect of gravitational drainage at low pressure is higher for low-quality foams compared to those of high quality.  
	[bookmark: _Hlk101999086] (a)
	 (b)

	
(c)
[bookmark: _Toc102015494]Figure 4.4: Foam drainage showing the effect of foam quality at different pressures (a) 100 psi, (b) 250 psi, and (c) 400 psi
 



[bookmark: OLE_LINK14]At later stage, the effects of coalescence and coarsening were similar for all the three qualities. As the system pressure was increased to 250 psi (Fig. 4.1b), the drainage of 60% quality foam increased after 90 minutes compared to those of 40 and 50% quality foams. Overall, the drainage of 40% foam quality was the least (87.6%) at the end of 120 minutes and those of 50 and 60 % quality foams were close to 92%, which are 6% lower than their drainage at system pressure of 100 psi. At 400 psi system pressure, a distinction was observed in the drainage behavior of different quality foams (Fig. 4.1c). The 40% quality foam drained about 90% at the end of 120 minutes and the drainages were lower for 50 and 60% quality foams.  The half-life of the foams varied significantly.  There was a difference of 35 minutes between 40% and 60% quality foams. This difference demonstrates that increased foam quality at high pressure increases the stability of high-quality foams. 
At lower system pressures, low-quality aqueous foams show similar drainage as high-quality foams but have a difference in the half-life time. In other words, high-quality foams are delayed in reaching their half-life time at all pressures, making them more stable than lower quality foams. 
The effect of pressure on drainage was investigated at different foam qualities (Fig. 4.2). For 40% quality foams (Fig. 4.2a), the least drainage was observed at system pressure of 250 psi followed by 400 psi. The 40% quality foam was the least stable at a system pressure of 100 psi.  The initial drainage rate at 400 psi was low until the foam reached the half-life point and after that, the drainage rate increased considerably until it reached 80% drainage. At 50% and 60% foam qualities, a decrease in the drainage was noticed with system pressure. At higher foam quality of 60% (Fig. 4.2c), there is a clear increase in stability of foams. At foam qualities lower than 50%, a clear pattern with the change in system pressure was not observed. However, at higher foam qualities, increase in pressure extends the half-life of the foam. Thus, it can be said that increase in pressure compresses the gas molecules present in the bubbles which stops the expansion of gas bubbles in the foam structure and gives foam much needed stability.
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(c)
[bookmark: _Toc102015495]Figure 4.5: Foam drainage showing the effect of pressure at different foam qualities (a) 40%, (b) 50%, and (c) 60%


[bookmark: _Toc99805646][bookmark: _Toc102015443]4.1.2 Aqueous Foam with 10% Oil
To simulate downhole foam contamination with oil, light mineral oil at 10% concentration v/v was added to the base liquid. The presence of oil could create a layer film of water-oil emulsion around the bubbles. And the stability of this pseudo emulsion film determines the stability of the foam. The effect of pressure on the drainage of contaminated foam was studied at different qualities. At 100 psi (Fig. 4.3a), the highest drainage was observed with 60% quality foam which was close to the drainage of 40% quality foam. 50% quality foam had the least drainage. Although the 60% quality foam was the least stable at the 120-minute mark but had the best half-life time amongst the other foams of lower qualities. 
At the intermediate pressure (250 psi), results were similar to the ones observed at 100 psi (Fig. 4.3b) except minor differences. A 6% reduction in the drainages of 40% and 50% quality foams quality were observed while only 2% drainage reduction was recorded for 60% quality foam. The drainage behavior of 60% quality foam have been high throughout these tests. For system pressure of 400 psi, 50% quality foam was most stable showing the lowest drainage of 82.6%. 
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(c)
[bookmark: _Toc102015496]Figure 4.6: Foam drainage showing the effect of foam quality at different pressures (a) 100 psi, (b) 250 psi, and (c) 400 psi (10% oil contamination)
 



The effect of pressure on the drainage of 10% oil-contaminated foam was studied considering various qualities. For 40% foams (Fig. 4.4a), system pressure of 100 psi gave the least stable foams whereas system pressure of 400 psi had the most stable foams with the final drainage of 88 %. Comparing different quality foams, 50% quality showed slightly better stability regardless of the system pressure (Fig. 4.4b). At 60% foam quality, the effect of pressure on drainage was minimal (Fig. 4.4c).
	 (a)
	 (b)

	 
(c)


[bookmark: _Toc102015497]Figure 4.7: Foam drainage showing the effect of pressure at different foam qualities (a) 40%, (b) 50%, and (c) 60% (10% oil contamination)
Overall, with 10% oil contamination, the increase in pressure reduced drainage and improved foam stability for all qualities tested. The foam drainage curves for all qualities have a similar slope and follow each other through the drainage period.
[bookmark: _Toc99805647][bookmark: _Toc102015444]4.1.3 Aqueous Foam with 20% Oil
For the last 9 tests, the mineral oil concentration was increased from 10 to 20% v/v. The contamination is expected to impact the stability of the foam structure by creating a pseudo emulsion film. 
The effect of pressure on the drainage of 20% oil-contaminated foam was investigated varying its quality (Fig. 4.5). For system pressure of 100 psi (Fig. 4.5a), 40% quality foam has the lowest drainage of 93.3 %. A 1% reduction in drainage was observed for 60% quality foam and 50% quality foam were least stable at 95.3 %. There was no a substantial difference in drainage between the three foams. After increasing the pressure to 250 psi (Fig. 4.5b), 50% quality foam exhibited a slightly better stability. In the early drainage stage, 60% foam has a lower drainage than 40% foam but 60% foams become unstable after 80 minutes and drainage kept increasing till the end of 120 minutes whereas the 40% foam stabilizes itself. The drainage for 40 % and 60% foams are 86% and 88.5% respectively. Similar drainage pattern can be seen when the system pressure has been increased to 400 psi (Fig. 4.5c). Lowest drainage of 75.7 % is observed for the 50% quality foam at 400 psi pressure with 20% mineral oil concentration. This is the most stable foam that is observed over the 27 experiments that have been carried out in this study. For 40 and 60 % quality foams, the half-life of 60% quality foam was better. Still, after 80 minutes the 60% quality foam exhibited higher drainage and the 40% quality foam has stabilized and drainage reduces significantly similar to drainage at 100 psi.
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[bookmark: _Toc102015498]Figure 4.8: Foam drainage showing the effect of foam quality at different pressures (a) 100 psi, (b) 250 psi, and (c) 400 psi (20% oil contamination)
Results presented in Fig. 4.5 are rearrange for different qualities in Fig. 4.6. For 40% quality foams (Fig. 4.6a), the one generated at 100 psi was the least stable showing the final drainage of 93.3%. Then, its drainage dropped by 9% at 250 psi. Further increase in the pressure to 400 psi reduced the drainage to 80%, which is the lowest for 40% quality foams. Results obtained at 60% foam quality (Fig. 4.6c) are consistent with the ones observed at 40% quality.
For 50% quality foams (Fig. 4.6b), there is noticeable difference in the drainage measured at different pressures. The drainage decreased with pressure indicating a notable increase in stability at 400 psi. The improvement in stability could be attributed to two factors: a) compression of gas molecules in the bubbles restricting the rapid expansion of gas, and b) the stability of pseudo emulsion film resulting from the addition of 20% mineral oil stabilizing the bubbles in foam structure and slow down bubble film rupturing. Overall, the effect of quality study demonstrated that 50% foams were more stable than 40% and 60 % quality foams. 
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[bookmark: _Toc102015499]Figure 4.9: Foam drainage showing the effect of pressure at different foam qualities (a) 40%, (b) 50%, and (c) 60% (20% oil contamination)
[bookmark: _Toc99805648][bookmark: _Toc102015445]4.1.4 Effect of Oil Contamination
The effect of oil concentration on the drainage of 40%, 50% and 60% foam quality are compared in this section. Oil contaminant affects the stability of foam structure due to the formation of pseudo emulsion film formed on the bubble boundary. The comparison is made for the trapped foam at system pressure of 100 and 400 psi (Fig. 4.7). For foams of 40% qualities (Fig. 4.7a), we can see that at 0% oil concentration there is minor improvement in the foam stability at 400 psi as compared to 100 psi. When 10% v/v mineral oil is added, there is a 10% reduction in the drainage rate for 400 psi. Foams at 400 psi, become more stable when 20% v/v oil concentration is added to the base liquid mixture. Addition of oil to 40% foams at 100 psi, did not impact the stability of the foams majorly whereas the drainage reduced significantly for experiments conducted at 400 psi.
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[bookmark: _Toc102015500]Figure 4.10: Comparison of results of drainage test at 100 psi and 400 psi for foam qualities of (a)40% (b) 50% and (c) 60%
Now, comparing the drainage tests for 50% at 100 psi (Fig. 4.7b), not much difference is seen on addition of mineral oil at different concentrations but at 400 psi the drainage rate reduces with the increase in oil concentration. The reduction in drainage rate at100 psi and 400 psi for 50% foams for pure foams and 10% oil contaminated foams is identical. Addition of 20 % mineral oil, stabilizes the foam structure at 400 psi but impacts negatively to stability at 100 psi. For 60% foam quality at 100 psi (Fig. 4.7c), there is only a slight increase in stability with addition of mineral oil but at 400 psi addition of oil destabilizes the foam structure. For pure aqueous foams of 60% foams, the drainage rate is least for foams at 400 psi without any added contamination. Overall, the foam structures are more stable at higher pressure and increasing the addition of oil decreases the drainage rate except for pure foams of 60% quality.
[bookmark: _Toc99805649][bookmark: _Toc102015446]4.2 Bubble Size Distribution
The second study was conducted to understand the relationship of bubble size in the foam structure with both the varying effects of quality and pressure. The bubble size distribution is important to establish a relationship between foam drainage and the bubble size distribution. Therefore, different factors that can affect the bubble size are experimentally studied. While the generated foam was trapped in the vertical column and its bubble structure was monitored through a viewport installed at the column's entrance. The images captured from the viewport are analyzed and their average bubble size is noted at interval of 30 minutes. In this section, the results of the bubble size analysis are presented.
[bookmark: _Toc99805650][bookmark: _Toc102015447]4.2.1 Aqueous Foams
[bookmark: OLE_LINK19][bookmark: OLE_LINK20][bookmark: OLE_LINK17][bookmark: OLE_LINK18]The effects of quality and pressure on bubble size are discussed in this section. As anticipated, the average bubble size decreased with pressure and increased with foam quality. However, it is important to note that the impact of quality on bubble size diminished as the pressure increased. Also, the rate of change of bubble size (the slope of bubble size versus time plot) significantly reduced with pressure indicating the reduction of drainage and improvement of foam stability with pressure. 
At 100 psi, drainage was the least for 40% foam quality (Fig. 4.1a), and the bubble size was the minimum throughout the test (Fig. 4.8a). At 30 minutes, the average bubble size was 78 µm and increased to 92 µm at 60 minutes, and finally, the average bubble size was 132 µm. For 50% foam, there has been an increase in the overall bubble size when compared to 40% quality bubbles. This increase in bubble size is due to an increase in the volume of gas to achieve the desired foam quality. The average bubble size for 50% foam was 101 µm at 30 minutes and 168.6 µm at the end of the experiment. Interestingly, for 60% quality foam, the average bubble size was 213 µm at 90 minutes and 125 µm at the beginning of the test. This pattern continued at the end of the test as the average bubble size increased to 268 µm. 
As the pressure is increased to 250 psi (4.8b), there is an approximately 30% reduction in the average bubble size of the foams at all three qualities. The average bubble sizes of 60% quality foams at 100 and 250 psi have slightly higher slopes than other foam qualities at the same pressure, which makes the foam less stable at these pressures. This observation is consistent with drainage measurements (Fig. 4.1). As the system pressure was increased to 400 psi, the bubble size did not change significantly with time, demonstrating the improvement in the stability of the foams. 
	 (a)
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(c)


[bookmark: _Toc102015501]Figure 4.11: Average bubble size showing the effect of foam quality at different pressures (a) 100 psi, (b) 250 psi, and (c) 400 psi
[bookmark: _Toc99805651][bookmark: _Toc102015448]4.2.2 Aqueous Foams with 10% Oil
When 10 % mineral oil was added, some changes in the average bubble size distribution patterns was observed as compared to pure aqueous foams as discussed in the previous section. The bubble size appears to have slightly shrunk (Figs. 4.8 and 4.9) due to oil particles in the foam structure. The effect of foam quality on bubble size distribution was studied at different (40%, 50% and 60%) foam qualities. Initially, the system pressure was set at 100 psi and there was hardly any change in the average bubble size of 40% quality foam with and without oil contaminant. Foam with 50% quality was very stable as it exhibited a very slow rate of bubble size growth. At 30 mins, the average bubble size was 97.6 µm and it reached 134 µm at 120 minutes. Although 60% foams (Fig. 4.9a), had a higher slope than foams of other qualities, it was more stable than pure aqueous foams at 100 psi. Like the clean aqueous foam, with increasing pressure, the impact of foam quality on drainage diminished as indicated by the overlapping/bundling of average bubble size plots of different quality foams.
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[bookmark: _Toc102015502]Figure 4.12: Average bubble size showing the effect of foam quality at different pressures (a) 100 psi, (b) 250 psi, and (c) 400 psi (with 10% oil contamination)
[bookmark: _Toc99805652][bookmark: _Toc102015449]4.2.3 Aqueous Foams with 20% Oil
The mineral oil contamination was increased to 20% to study the oil-water interaction in foam structure at elevated oil concentration (Fig. 4.10). With increasing oil concentration, the impact of foam quality on drainage reduced regardless of the pressure. The reduction is indicated by the crowding of the average bubble size plots of different quality foams. Moreover, the impact of pressure on the drainage significantly reduced with the increase in oil concentration. Adding 20% oil contaminant also decreased the average bubble size of the foams, indicating the formation of  stable pseudo emulsion films around the bubbles. 
	 (a)
	 (b)

	
(c)


[bookmark: _Toc102015503]Figure 4.13: Average bubble size showing the effect of foam quality at different pressures (a) 100 psi, (b) 250 psi, and (c) 400 psi (with 20% oil contamination)


5. [bookmark: _Toc99805653][bookmark: _Toc102015450]CHAPTER FIVE
[bookmark: _Toc99805654][bookmark: _Toc102015451]Conclusion and Recommendations
In this study, a total of 27 tests for measuring drainage of liquid phase from the homogenously generated trapped foam column. Each drainage test lasted for 2 hours, and pressure data was collected with a data acquisition system. In addition to that, 108 images (4 images per drainage test) were analyzed to get data for average bubble size distribution. These images were captured with a digital microscope and a method was developed to measure the bubble diameter for each image. This section has been divided into two subsections (a) Conclusions and (b) Recommendations. First, the conclusions for three sets of foam drainage tests based on varying mineral oil contamination will be presented followed by recommendations for further experimentation to improve the understanding of the drainage behavior of foams and impact on bubble size.
[bookmark: _Toc99805655][bookmark: _Toc102015452]5.1 Conclusions 
The outcomes of foam stability investigation conducted by varying foam qualities, system pressure, and mineral oil concentration are summarized here. All tests were conducted at ambient temperatures and with the same foam generation technique using a closed flow loop to achieve consistency in the measurements. 
· Bubble size in the foam structure varies with foam quality at constant pressure, as foam quality depends on the amount of gas volume present in the foam structure. The higher the foam quality is, the larger the bubble size of the foam structure. Nonetheless, with the addition of contaminant oil, the effect of foam quality on the bubble size reduced noticeably.  
· With time, foam bubble size increased, confirming the coarsening and coalescence of foam bubbles. When the foam structure is unstable, the bubble growth rate increases due to the exacerbation of bubble coalescence and coarsening.
· An increase in pressure reduces the average bubble size of foams. However, with the addition of contaminant oil, the impact of pressure on the foam bubble size diminished significantly. 
· Increasing the oil concentration, decreases the difference in average bubble size between varying foam qualities at a constant pressure which means that the difference in the initial bubble size and final bubble size for varying foam qualities diminishes with the increase in oil concentrations. 
[bookmark: _Toc99805656][bookmark: _Toc102015453]5.2 Recommendations 
Based on the outcomes of the current investigation, the following recommendations are made for future studies:
· It would be impactful to study the effect of temperature on the bubble size distribution and drainage of foam. 
· The effect of addition of other downhole contaminants like salt, clay at different concentrations can have different impacts on the foam structure, which affects the bubble size distribution.
· Stabilizing agents like polymers, fused nanoparticles, and fiber can be added to the liquid surfactant mixture to understand their effect on the stability of foam under varying pressure conditions. The effect of these stabilizing agents on the bubble size in the foam structure would be interesting to study. 
· Since these tests were conducted in a vertical column, similar tests can be conducted in inclined columns to study the effect of inclination on foam drainage.
· Foam quality can be tested between 40-60% at intervals of 5%, and the surfactant concentration can be varied from 1-3% v/v at an interval of 0.5 % to check for any improvement in the stability of the aqueous foams.
[bookmark: _Toc99805657][bookmark: _Toc102015454]Nomenclature
µ = Liquid viscosity
µs = Surface shear viscosity
A = Cross sectional area
Deff = Diffusion efficient of gas
ꝺԑ = Geometric constant for bubble
E = Entering coefficient
E = Gibb’s elastic modulus
f(ɸ) = Fraction of bubble area covered by thin films
fb = Lamella rupture frequency 
g = Acceleration due to gravity
G = Pressure gradient driving the flow
h = Film thickness
H = Foam Height
K = Dimensionless permeability constant
k = foamability of foam
K1 = Dimensionless number
K1/2 = Dimensionless number
K3 = Permeability constant
K4 = Permeability constant
Kc0 = Dimensionless permeability
L = Channel length
M = First mobility parameter
m = Nature of viscous dissipation
N = Second mobility parameter
ɳ = Viscosity
N’ = Number of steps
p = Liquid pressure
ɸ = Liquid volume fraction
R = Radius of bubble
r’ = Radius of curvature of channels
Ravg = Average bubble Radius
S0 = Spreading oil coefficient
Si = Surface area of bubble i
Stot = Surface area of total foam
Sw = Spreading water coefficient
t = time 
Tcoars = Coarsening time
Tdrain = Drainage time
uo = Maximum flow speed
V(t) = Volume of liquid at time ‘t’
Vf = Final volume of liquid at time, t = 0
z = Height of the container
Z =Position of the grid in foam column
α = Liquid fraction exponent
γ = Surface tension
Δt = Time interval
ϒ = Surface tension 
ϒF = Foaming aqueous solution surface tension
ϒOF = Foaming aqueous solution/oil interfacial tension
ϒog = Surface tension between oil-gas phase
ϒwg = Surface tension between water-gas phase
ϒwo = Surface tension between water-oil phase
є = Capillary rise 
Ԑ = Liquid volume fraction 
Ԑc = Critical liquid fraction after
𝜌avg = Average Density
𝜌liq = Liquid density
𝜌gas = Gas density
Vliq = Liquid volume in column
Vtotal = Total foam volume in column
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[bookmark: _Toc102015458]A.2 Effect of pressure with 20% oil concentration
	
 (a)
	
 (b)

	
(c)



[bookmark: _Toc102015627]Appendix A 2: Foam quality profile for the drainage test for aqueous foams of different foam qualities with 20 % oil contamination (a) 40%, (b) 50%, and (c) 60%
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100 psi	0	11.683333333333334	23.933333333333334	36.033333333333331	47.85	59.68333333333333	71.5	83.35	95.2	107.05	118.78333333333333	131.19999999999999	65.120756772062165	69.467654658921106	73.559800356221245	77.546064006758726	80.998385217940765	84.053634741801915	86.414062442696036	88.604109117607166	90.930684633105358	92.798585692072493	93.734761835891902	94.679283584623946	250 psi	0	11.733333333333333	23.633333333333333	35.483333333333334	47.366666666666667	59.25	71.11666666666666	83.016666666666666	94.88333333333334	106.76666666666667	118.51666666666667	130.38333333333333	81.486392733162688	83.798133927696583	86.114638012379544	87.989405670318376	89.445993935202083	90.525745586528316	91.688684817448916	92.863867003393437	93.732287828864088	94.439825225195321	95.109118879473911	95.874572376744908	400 psi	0	11.683333333333334	24.066666666666666	36.016666666666666	47.866666666666667	59.733333333333334	71.566666666666663	83.416666666666671	95.266666666666666	107.1	118.85	130.71666666666667	83.206754028926937	85.325684175195747	87.058000016527302	88.77619595519009	90.226964316553364	91.152588708973653	92.103264646760351	93.036677575124742	93.678639161417593	94.269272377317492	94.99173738555325	95.626523710384035	Time (mins)


Quality (%)




100 psi	0	12.033333333333333	24.15	36	47.85	59.716666666666669	71.566666666666663	83.433333333333337	95.266666666666666	107.13333333333334	118.85	130.69999999999999	36.556506445614495	47.161846707840297	55.85463520257543	62.402456818336773	67.051552982476011	70.756009125118339	73.704619682873115	76.481907622523593	79.288604602936175	81.701112969133248	83.644678342245513	84.964404214596868	250 psi	0	11.866666666666667	24.216666666666665	36.083333333333336	47.966666666666669	59.833333333333336	71.7	83.566666666666663	95.416666666666671	107.28333333333333	119.03333333333333	130.88333333333333	36.125465947179222	44.623877624495869	51.592348999459027	57.161848312892893	61.504768562890114	64.91236842029285	67.594342421371607	70.030765056549228	72.358355579847	74.497834060577489	76.415262800805763	78.328105075631555	400 psi	0	11.55	23.133333333333333	34.716666666666669	46.233333333333334	57.75	69.266666666666666	80.783333333333331	92.283333333333331	103.8	115.2	126.68333333333334	36.449219133374008	44.080482119332068	49.833184853263191	54.714531484762489	58.57364484326957	61.714543631100852	64.281714992148295	66.644020107715988	68.91061450601363	70.304999932471915	71.902084562066847	73.613542880319741	Time (mins)


Quality (%)




100 psi	0	11.816666666666666	23.733333333333334	35.65	47.6	59.56666666666667	71.533333333333331	83.483333333333334	95.45	107.41666666666667	119.26666666666667	131.23333333333332	51.709549644220743	58.838259818456017	64.803431582827258	70.042390267512133	74.242656487689345	77.681129308189981	80.640751279375721	83.232891227472479	85.635976692327091	87.775834158401338	89.605138097447096	91.112433385630538	250 psi	0	11.816666666666666	24.216666666666665	36.43333333333333	48.416666666666664	60.383333333333333	72.333333333333329	84.266666666666666	96.233333333333334	108.16666666666667	120.01666666666667	131.94999999999999	50.771586318650208	55.363150932076046	59.322882121595057	62.840706487029905	65.921914662063003	68.813608890388267	71.340459378918268	73.535432870256855	75.513045819344867	77.316096910278659	78.954078799580913	80.863282222984907	400 psi	0	11.883333333333333	24.466666666666665	36.416666666666664	48.35	60.3	72.233333333333334	84.183333333333337	96.13333333333334	108.1	119.93333333333334	131.88333333333333	51.219286445665425	55.079016254518478	58.557726809089104	61.595684903370895	64.383204883401646	66.776707916830489	69.01946207371779	71.051686060129455	72.84037048557488	74.529305792255514	75.993592345441513	77.373071402074473	Time (mins)


Quality (%)




100 psi	0	11.75	23.65	35.549999999999997	47.45	59.35	71.25	83.15	95.066666666666663	106.96666666666667	118.75	130.65	68.46423852386333	72.260006839001804	75.614525897090431	78.839627895052857	82.00931565418918	84.482529605075669	86.479708094807251	88.299511507624359	90.150489401751244	91.719855055458353	92.872474675862335	93.760072086958573	250 psi	0	11.716666666666667	23.633333333333333	35.516666666666666	47.4	59.266666666666666	71.150000000000006	83.033333333333331	94.9	106.78333333333333	118.55	130.44999999999999	65.764694840061793	68.658003443326152	71.649822421444426	74.313683874553149	76.968785256651046	79.396831550708683	81.664702612298782	83.606450480834468	85.221669482712997	86.933274319189152	88.417563946287132	90.407548061246274	400 psi	0	11.883333333333333	24.333333333333332	36.233333333333334	48.1	59.983333333333334	71.86666666666666	83.75	95.63333333333334	107.51666666666667	119.3	131.21666666666667	73.695650478271119	75.832195016902475	77.997385560605807	79.647141198180833	81.570753185249458	83.22357448906466	84.849941995868562	86.160939703450779	87.332197536918159	88.49937275316266	89.421156804348016	90.322093609932267	Time (mins)


Quality (%)




100 psi	0	11.783333333333333	24.033333333333335	36.15	48	59.85	71.683333333333337	83.55	95.416666666666671	107.26666666666667	119.01666666666667	130.86666666666667	0.64195441991574498	0.54342561194833972	0.45172774412603567	0.38061624542715206	0.31104265500100542	0.26322738156458614	0.2309271875506983	0.19884040532221478	0.17068493684623243	0.14650810032897377	0.13742563611137509	0.12639186564751223	250 psi	0	11.533333333333333	23.066666666666666	34.633333333333333	46.25	57.866666666666667	69.5	81.11666666666666	92.733333333333334	104.35	115.85	127.63333333333334	0.64647387552238622	0.57048352846896799	0.50605005386154056	0.45104401091110197	0.40771948044906947	0.36259773809242213	0.32448571236511364	0.28869054476866285	0.2678839712053866	0.24464260582119676	0.22504671380577984	0.20458468522355744	400 psi	0	11.683333333333334	23.466666666666665	35.25	47.05	58.85	70.650000000000006	82.45	94.25	106.05	117.75	129.56666666666666	0.6359064734473624	0.56226522705654913	0.50506944933901554	0.45627164143030885	0.41772175630066183	0.38773190617873332	0.35194512155791058	0.31870898820421473	0.29387184860872173	0.27199283751394027	0.25456125574187494	0.23704338584817169	Time (mins)


Density (g/cc)




100 psi	0	11.966666666666667	24.366666666666667	36.233333333333334	48.116666666666667	60	71.916666666666671	83.816666666666663	95.733333333333334	107.63333333333334	119.41666666666667	131.31666666666666	0.52385373217063658	0.43859017625943031	0.37862577103730216	0.3285230951568372	0.29127953629323211	0.26099077566740453	0.23217667237371126	0.20374712263270886	0.17903112315601374	0.15602231066681505	0.13862214727432237	0.12173024594415295	250 psi	0	11.883333333333333	24.45	36.533333333333331	48.516666666666666	60.483333333333334	72.466666666666669	84.433333333333337	96.433333333333337	108.41666666666667	120.26666666666667	132.23333333333332	0.51716346497801435	0.44455413278818867	0.39805002076091012	0.36017078344813663	0.33041252129783105	0.30257896030804027	0.27990364595114076	0.25954855887550754	0.24137884920785371	0.22149214489645846	0.20299087408030686	0.18626191268786105	400 psi	0	11.733333333333333	24.1	36.216666666666669	48.083333333333336	59.95	71.816666666666663	83.683333333333337	95.566666666666663	107.45	119.21666666666667	131.1	0.51872030701696137	0.46026417141093079	0.42106042061225141	0.38886385558949943	0.35947252287301279	0.33545365832482626	0.31259951971355571	0.29420401537597124	0.27743952364904995	0.261210727674275	0.24531114185765218	0.2310045527025533	Time (mins)


Density (g/cc)




100 psi	0	11.683333333333334	23.933333333333334	36.033333333333331	47.85	59.68333333333333	71.5	83.35	95.2	107.05	118.78333333333333	131.19999999999999	0.35344102303052854	0.3102823438315786	0.26965300125625541	0.23007492084721712	0.19579814979732227	0.16546375099037225	0.14202797113845178	0.12028383903933874	9.718416453143916E-2	7.8638492496434398E-2	6.9343559209191316E-2	5.9965765616847688E-2	250 psi	0	11.733333333333333	23.633333333333333	35.483333333333334	47.366666666666667	59.25	71.11666666666666	83.016666666666666	94.88333333333334	106.76666666666667	118.51666666666667	130.38333333333333	0.19855993504527536	0.17582335350125317	0.15303992768222516	0.13460109558821312	0.12027516760851498	0.10965552665315217	9.8217714013446311E-2	8.6659488696967005E-2	7.8118341894060472E-2	7.1159525853074876E-2	6.4576847055213146E-2	5.704841095691205E-2	400 psi	0	11.683333333333334	24.066666666666666	36.016666666666666	47.866666666666667	59.733333333333334	71.566666666666663	83.416666666666671	95.266666666666666	107.1	118.85	130.71666666666667	0.18940735587053556	0.16876493074489554	0.15188886708059085	0.13515035822626173	0.1210171045525517	0.11199975575101284	0.10273835706872701	9.364513305707424E-2	8.7391201561540108E-2	8.1637306390716091E-2	7.4599117866822523E-2	6.8415087117071907E-2	Time (mins)


Density (g/cc)




100 psi	0	12.033333333333333	24.15	36	47.85	59.716666666666669	71.566666666666663	83.433333333333337	95.266666666666666	107.13333333333334	118.85	130.69999999999999	0.63704449117835515	0.53174814189975439	0.44544078438791446	0.38042997899933972	0.33427088919883324	0.29749076727551649	0.26821514579623412	0.24064052077620604	0.21277390468833227	0.18882103591811156	0.16952412197543035	0.15642107077941433	250 psi	0	11.866666666666667	24.216666666666665	36.083333333333336	47.966666666666669	59.833333333333336	71.7	83.566666666666663	95.416666666666671	107.28333333333333	119.03333333333333	130.88333333333333	0.64469655847896923	0.56111244856525644	0.49257570317668858	0.43779821528198687	0.39508445448699636	0.3615698153005556	0.33519189690784851	0.31122904066278062	0.28833657680948038	0.26729424427942511	0.24843582924138646	0.22962252329465471	400 psi	0	11.55	23.133333333333333	34.716666666666669	46.233333333333334	57.75	69.266666666666666	80.783333333333331	92.283333333333331	103.8	115.2	126.68333333333334	0.64491501611149993	0.57057194487855012	0.5145296370826361	0.4669760013337414	0.42938086933063407	0.39878251847457169	0.37377336812649475	0.35076000614385006	0.32867904928010327	0.31509507303971951	0.29953641956368293	0.28286354799573687	Time (mins)


Density (g/cc)




100 psi	0	11.816666666666666	23.733333333333334	35.65	47.6	59.56666666666667	71.533333333333331	83.483333333333334	95.45	107.41666666666667	119.26666666666667	131.23333333333332	0.48659574650608384	0.41581752177662529	0.35659162292967433	0.30457601476634322	0.26287318505533641	0.22873390935647048	0.19934895978341541	0.17361259804441687	0.14975328564169016	0.12850746291625445	0.11034500685734289	9.5379650988860587E-2	250 psi	0	11.816666666666666	24.216666666666665	36.43333333333333	48.416666666666664	60.383333333333333	72.333333333333329	84.266666666666666	96.233333333333334	108.16666666666667	120.01666666666667	131.94999999999999	0.50064811961526934	0.45548887622995982	0.41654388044246266	0.38194515428255449	0.35164066297903196	0.32320009109401543	0.29834785317142293	0.27675971264306731	0.2573093701108794	0.23957588928093743	0.22346590738425687	0.20468839049655729	400 psi	0	11.883333333333333	24.466666666666665	36.416666666666664	48.35	60.3	72.233333333333334	84.183333333333337	96.13333333333334	108.1	119.93333333333334	131.88333333333333	0.50102636120160871	0.46342522379519313	0.42953594137455964	0.39994042940996261	0.37278466281929257	0.34946737355303326	0.3276186661568572	0.30782092456924437	0.29039572327571783	0.2739422688418397	0.25967732217059208	0.24623856243182615	Time (mins)


Density (g/cc)




100 psi	0	11.683333333333334	23.933333333333334	36.033333333333331	47.85	59.68333333333333	71.5	83.35	95.2	107.05	118.78333333333333	131.19999999999999	0.35344102303052854	0.3102823438315786	0.26965300125625541	0.23007492084721712	0.19579814979732227	0.16546375099037225	0.14202797113845178	0.12028383903933874	9.718416453143916E-2	7.8638492496434398E-2	6.9343559209191316E-2	5.9965765616847688E-2	250 psi	0	11.733333333333333	23.633333333333333	35.483333333333334	47.366666666666667	59.25	71.11666666666666	83.016666666666666	94.88333333333334	106.76666666666667	118.51666666666667	130.38333333333333	0.19855993504527536	0.17582335350125317	0.15303992768222516	0.13460109558821312	0.12027516760851498	0.10965552665315217	9.8217714013446311E-2	8.6659488696967005E-2	7.8118341894060472E-2	7.1159525853074876E-2	6.4576847055213146E-2	5.704841095691205E-2	400 psi	0	11.683333333333334	24.066666666666666	36.016666666666666	47.866666666666667	59.733333333333334	71.566666666666663	83.416666666666671	95.266666666666666	107.1	118.85	130.71666666666667	0.18940735587053556	0.16876493074489554	0.15188886708059085	0.13515035822626173	0.1210171045525517	0.11199975575101284	0.10273835706872701	9.364513305707424E-2	8.7391201561540108E-2	8.1637306390716091E-2	7.4599117866822523E-2	6.8415087117071907E-2	Time (mins)


Density (g/cc)




0.93981863149216804	1.97856553998351	2.9431162407254701	4.00659521846661	4.9464138499587804	5.9356966199505301	6.8755152514426996	7.9884583676834202	8.9282769991755906	9.96702390766694	10.9810387469084	11.9208573784006	12.9348722176422	13.9983511953833	14.962901896125301	19.958779884583599	24.9793899422918	29.975267930750199	2.30179028132993	6.9053708439897798	12.0204603580562	21.227621483375898	35.294117647058798	59.846547314577997	78.772378516624002	99.744245524296602	115.60102301790199	125.831202046035	133.50383631713501	140.40920716112501	145.78005115089499	151.15089514066401	156.01023017902801	171.35549872122701	178.26086956521701	180.56265984654701	Time (mins)


Drained volume (cm3)
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Normalized density




Flow rate	0	8	16	24	32	40	48	56	64	72	80	88	96	104	112	120	128	136	144	152	160	168	176	184	192	200	208	216	224	232	240	248	256	264	272	280	288	296	304	312	320	328	336	344	352	360	368	376	384	392	400	408	416	424	432	440	448	456	464	472	480	488	496	504	512	520	528	536	544	552	560	568	576	584	592	600	608	616	624	632	640	648	656	664	672	680	688	696	704	712	720	728	736	744	752	760	768	776	784	792	800	808	816	824	832	840	848	856	864	872	880	888	896	904	912	920	928	936	944	952	960	968	976	984	992	1000	1008	1016	1024	1032	1040	1048	1056	1064	1072	0.12669072591107683	0.23653158294144422	0.36009108808410856	0.27574155774798875	0.32359727613556105	0.35015617702501395	0.32725552348911197	0.33633241145577414	0.36004432842908557	0.35714895377600703	0.41668661108324506	0.4	0.36670890840920262	0.35633611550088723	0.3609760225480157	0.30135565073832965	0.295704597233654	0.32218039583167518	0.35592096519072108	0.36532634891060506	0.36234361812814359	0.33937734536757053	0.31622331169291878	0.31990659363766566	0.33071750225268232	0.34625364629264593	0.35926138542847047	0.35871137335814179	0.34693021078206193	0.33191703127077393	0.32784832555775406	0.33057444660007135	0.33656247393165822	0.34480138838448177	0.35015628951342165	0.34688832661145425	0.34246736344915779	0.33779506862122427	0.3351413545909277	0.33636872448996952	0.33875028761850717	0.34226553556365086	0.34363368174493497	0.34333005777073827	0.34013460548853419	0.33835553323282302	0.33662996401616457	0.33706147842945594	0.33839335005941923	0.3397267728453221	0.33984599871679039	0.33983208567686812	0.33886533661777801	0.33764781833508845	0.33724255812415121	0.33753350051046943	0.33720288227860368	0.33776672450266015	0.33783911967379404	0.33700231248713225	0.33678790070104997	0.33654695645181326	0.33610600781336614	0.33584320825056652	0.33591529555869054	0.33618448031874698	0.3363690619551935	0.33613737727805842	0.33596864762645923	0.33580481122060352	0.33515420787163835	0.33582854627466591	0.33530334973915948	0.33551010935328546	0.33587839936090585	0.33585095810982574	0.33559224957280825	0.33567806934735728	0.33535237100322562	0.33557308510037026	0.33545969382500701	0.33567891597063754	0.33543793915896686	0.33577907801719059	0.33576155646755262	0.33530391514142049	0.3355516175757936	0.33541573453929502	0.33569047267443636	0.33614219355804825	0.33502219088410662	0.33560525974524563	0.335628231062224	0.3355097067631943	0.33566305214490449	0.33549056005208461	0.33559135262576573	0.33554085421129204	0.33498985046684054	0.33483776909960833	0.33538761835776792	0.33529496935277298	0.33540903259836335	0.33579509873464947	0.33562210932465736	0.3351756398735603	0.33527618082843541	0.33522359249775163	0.33535153622082942	0.3352937645427197	0.33531007832208354	0.33517407391651405	0.33532031180697891	0.33470755488682319	0.33511413831666298	0.33495055945005664	0.335173748292175	0.33527019230082628	0.33511793628053926	0.33516755550929961	0.33504407283966015	0.33489898647526467	0.33482217465401048	0.33507453943686832	0.3348232166518938	0.33473785275141893	0.33500156998280922	0.3350550167776582	0.33506856867058671	0.33450806853633325	0.33466452215036685	0.33470192158576545	0.33471639114728463	0.33483031822269665	0.33466636340798989	Time (secs)


Flowrate (gpm)



Pressure Profile

t=0	0	0.20954999999999999	0.42544999999999999	0.64134999999999998	0.85407499999999992	1.0794999999999999	1.30175	1.5176499999999999	1.7335499999999999	1.93675	-5.6131778743133687E-3	1.2683975375199679	2.3456749484604535	3.2787337707826771	4.3461205021866558	5.4565061763933667	6.5156864717763199	7.3625333957382626	8.8449662379890057	9.864194910784267	t=1 hour	0	0.20954999999999999	0.42544999999999999	0.64134999999999998	0.85407499999999992	1.0794999999999999	1.30175	1.5176499999999999	1.7335499999999999	1.93675	-7.5477284640190767E-3	0.60350310663650886	1.3097080448758986	1.9574538086033204	2.8139619194443153	3.7641236349622442	4.7089951464490198	5.479037308035176	7.6133834210818279	9.5270885685669562	t=2 hr	0	0.20954999999999999	0.42544999999999999	0.64134999999999998	0.85407499999999992	1.0794999999999999	1.30175	1.5176499999999999	1.7335499999999999	1.93675	-9.2499999999999995E-3	0.44650000000000001	0.87575000000000003	1.3727499999999999	2.0682499999999999	2.8462499999999999	3.60425	5.3312499999999998	7.7137500000000001	9.6295000000000002	Depth (m)


Pressure (kPa)



Test-1	0	11.95	23.916666666666668	35.766666666666666	47.616666666666667	59.466666666666669	71.316666666666663	83.166666666666671	95.033333333333331	106.88333333333334	118.61666666666666	0	25.058075279071236	43.134827727817949	55.234372574462434	63.422575126492241	69.407776413735746	74.168136295375646	78.526008775761284	81.813520501668307	84.717707703548783	87.64108003526583	Test-2	0	11.95	23.916666666666668	35.766666666666666	47.616666666666667	59.466666666666669	71.316666666666663	83.166666666666671	95.033333333333331	106.88333333333334	118.61666666666666	0	22.924202687027496	40.549714294646272	53.539220299661871	62.83887029512907	69.046694952993576	73.847636718845493	77.14847208426184	80.454402554144224	82.370623972748632	85.03936265739533	Time (mins)


Drainage %



100 psi	0	11.766666666666667	24.15	36.583333333333336	48.733333333333334	60.616666666666667	72.466666666666669	84.333333333333329	96.183333333333337	108.05	118	33.176081157416583	44.594160645005033	54.616439036810249	61.635292330440095	66.573960459745095	70.423217825172458	73.74153737231029	76.840834016526159	79.678240753608748	81.943805687708348	83	250 psi	0	11.95	23.916666666666668	35.766666666666666	47.616666666666667	59.466666666666669	71.316666666666663	83.166666666666671	95.033333333333331	106.88333333333334	118.61666666666666	33.452305758169381	42.390323838617824	49.817049486487434	55.474854178051693	59.752438188153704	63.192312346366464	66.177096787515325	69.161773196029827	71.620330648906844	73.984794339068927	76.604987991749198	400 psi	0	11.783333333333333	23.683333333333334	36.016666666666666	48.05	59.95	71.816666666666663	83.733333333333334	95.61666666666666	107.53333333333333	119.3	33	44.786249324404046	51.918910972202134	60.210205513974159	66.778415068082992	71.124711064380634	74.292455369422456	77.159110932163927	78.88662179813781	79.916565576100382	80.99903436048514	Time (mins)


Quality (%)




100 psi	0	11.816666666666666	24.15	36.283333333333331	48.15	60.033333333333331	71.933333333333337	84.25	96.766666666666666	109.05	120.85	50.788719719326266	59.398794879203876	65.908781551013291	71.023725353654854	74.97096828365234	76.082337372702455	79.525099950643408	83.928525183056394	87.72581245512238	90.68866546759223	92.551860816504629	250 psi	0	11.916666666666666	23.833333333333332	35.716666666666669	47.616666666666667	59.516666666666666	71.433333333333337	83.35	95.266666666666666	107.18333333333334	118.96666666666667	51.434925438706259	59.715549913475385	64.150310252336382	68.351338231455401	71.721395078225598	74.419841607770394	76.350615581521581	78.975789608000156	81.206963053174988	83.611456794238549	86.189246073005592	400 psi	0	11.766666666666667	23.683333333333334	35.56666666666667	47.45	59.333333333333336	71.233333333333334	83.15	95.05	106.95	118.71666666666667	49.323608196635114	56.445245327372128	60.41881077317278	63.931439466413579	67.205077403996611	69.938057999758129	72.479201407042922	74.160019151507228	75.9460706085422	77.849976854020298	79.315183021822207	Time (mins)


Quality (%)




100 psi	0	11.766666666666667	23.95	36.35	48.666666666666664	60.55	72.400000000000006	84.283333333333331	96.15	108.03333333333333	119.78333333333333	58.921518830973895	62.916047850643366	67.506464708147789	72.398001870088265	77.080722238303423	81.413669161841426	84.980019833748059	88.361101538279769	91.155225601700423	93.284468510337732	94.40677534583692	250 psi	0	11.65	23.866666666666667	35.9	47.733333333333334	59.56666666666667	71.400000000000006	83.233333333333334	95.083333333333329	106.91666666666667	118.63333333333334	64.581160696153546	66.93618856001639	69.912908995965878	72.767237309959413	75.61496925045445	78.352366999007856	81.024745421854462	83.453111583732507	86.081848865766787	88.415085616326422	89.978798276324852	400 psi	0	11.7	23.983333333333334	36.016666666666666	47.866666666666667	59.7	71.55	83.416666666666671	95.25	107.11666666666666	118.85	60.282017692780833	61.847693379442269	63.635155295247145	65.938309297035062	68.397654278104326	70.758770652063149	73.108102796803067	74.968305222843995	76.87319382702195	78.83597518980929	80.949437132679776	Time (mins)


Quality (%)




100 psi	0	11.766666666666667	24.15	36.583333333333336	48.733333333333334	60.616666666666667	72.466666666666669	84.333333333333329	96.183333333333337	108.05	0.67060743522873278	0.55724171040628279	0.45773435844797689	0.38804686048304188	0.3390127218833951	0.30079492424639592	0.26784860424024248	0.23707687849658807	0.20890535703230648	0.18641143314907282	250 psi	0	11.95	23.916666666666668	35.766666666666666	47.616666666666667	59.466666666666669	71.316666666666663	83.166666666666671	95.033333333333331	106.88333333333334	118.61666666666666	0.67098779071610992	0.58308003641879835	0.51003623995181824	0.45439024548060841	0.41231908375755111	0.37848701834975013	0.34913087978286694	0.31977580374530401	0.29559524575716289	0.27234012462752938	0.24656983218036574	400 psi	0	11.783333333333333	23.683333333333334	36.016666666666666	48.05	59.95	71.816666666666663	83.733333333333334	95.61666666666666	107.53333333333333	119.3	0.62596703488059524	0.56369642483722904	0.49421068257693773	0.4134376438457949	0.3494507426405089	0.30710952160713689	0.27624964415948133	0.24832294590607729	0.23149369187550511	0.22146007309026647	0.21091476046075319	Time (mins)


Density (g/cc)




100 psi	0	11.816666666666666	24.15	36.283333333333331	48.15	60.033333333333331	71.933333333333337	84.25	96.766666666666666	109.05	120.85	0.49573831308107896	0.41025218449559209	0.34561702773070996	0.29483271568919095	0.25564205702405629	0.24460770028635917	0.21042583323383668	0.16670591573662583	0.12900410919159674	9.9587079850880111E-2	8.108812900324662E-2	250 psi	0	11.916666666666666	23.833333333333332	35.716666666666669	47.616666666666667	59.516666666666666	71.433333333333337	83.35	95.266666666666666	107.18333333333334	118.96666666666667	130.88333333333333	0.49412400522471583	0.41268188962320118	0.36906485744368078	0.3277466443834095	0.29460125056261466	0.26806132052795145	0.24907165161472328	0.22325237588376787	0.20130819930594709	0.17765937211670579	0.15230613781929572	0.13265811107286177	400 psi	0	11.766666666666667	23.683333333333334	35.56666666666667	47.45	59.333333333333336	71.233333333333334	83.15	95.05	106.95	118.71666666666667	0.5194938866114569	0.45011554419555411	0.41140543034814625	0.37718572049972199	0.34529423689701549	0.31866978803673807	0.29391419965136462	0.27753982577167452	0.26014027461737832	0.24159259281308443	0.2273186873397324	Time (mins)


Density (g/cc)




100 psi	0	11.766666666666667	23.95	36.35	48.666666666666664	60.55	72.400000000000006	84.283333333333331	96.15	108.03333333333333	119.78333333333333	0.41499087502641219	0.37533073094251573	0.32975424543513621	0.28118805210445269	0.23469512049886965	0.19167495505528184	0.1562660292958136	0.12269656793982894	9.4954783514711635E-2	7.3814348652341447E-2	6.2671395232034965E-2	250 psi	0	11.65	23.866666666666667	35.9	47.733333333333334	59.56666666666667	71.400000000000006	83.233333333333334	95.083333333333329	106.91666666666667	118.63333333333334	130.44999999999999	0.36482733021862224	0.34166501291780599	0.31238818595908235	0.28431511765110079	0.25630692640820663	0.22938390090882527	0.2031003575471351	0.17921673883201497	0.15336241754721633	0.13041442156650521	0.11503489703774741	0.10926921464822212	400 psi	0	11.7	23.983333333333334	36.016666666666666	47.866666666666667	59.7	71.55	83.416666666666671	95.25	107.11666666666666	118.85	0.41273805611906583	0.39748538571374165	0.38007209399815239	0.35763497679613315	0.33367626125318067	0.3106744798833741	0.28778749940483001	0.26966557624200171	0.2511083243884335	0.23198708653607478	0.21139793215153044	Time (mins)


Density (g/cc)




40%	0	11.766666666666667	24.15	36.583333333333336	48.733333333333334	60.616666666666667	72.466666666666669	84.333333333333329	96.183333333333337	108.05	0	31.254037777741811	53.875331636658565	67.03903601142477	74.978925082582009	80.409840865442391	84.559025376765533	87.988923063769619	90.751767870065521	92.698895615349741	50%	0	11.816666666666666	24.15	36.283333333333331	48.15	60.033333333333331	71.933333333333337	84.25	96.766666666666666	109.05	120.85	0	31.931133084731716	52.009450849494044	65.32984596548576	74.132243170646476	76.378463494971143	82.689315018791348	89.334477489660273	93.77905757246036	96.419905153355558	97.70931042226411	60%	0	11.766666666666667	23.95	36.35	48.666666666666664	60.55	72.400000000000006	84.283333333333331	96.15	108.03333333333333	119.78333333333333	0	18.502691016646502	37.430141210161686	54.85056822578683	68.870431521872248	79.528080205966063	86.630660156262152	91.972228479746946	95.363985725237995	97.327411936292151	98.146059588018261	Time (mins)


Drainage %




40%	0	11.95	23.916666666666668	35.766666666666666	47.616666666666667	59.466666666666669	71.316666666666663	83.166666666666671	95.033333333333331	106.88333333333334	118.61666666666666	0	25.058075279071236	43.134827727817949	55.234372574462434	63.422575126492241	69.407776413735746	74.168136295375646	78.526008775761284	81.813520501668307	84.717707703548783	87.64108003526583	50%	0	11.916666666666666	23.833333333333332	35.716666666666669	47.616666666666667	59.516666666666666	71.433333333333337	83.35	95.266666666666666	107.18333333333334	118.96666666666667	0	31.193928965725505	45.509262812509071	57.531924340779064	66.094680499289382	72.256685894296723	76.286723687282105	81.259064403543761	85.025724625331733	88.612390104386691	91.913014676963741	60%	0	11.65	23.866666666666667	35.9	47.733333333333334	59.56666666666667	71.400000000000006	83.233333333333334	95.083333333333329	106.91666666666667	118.63333333333334	0	12.856062114005077	27.840793426879145	40.882677898741385	52.600041095538977	62.644703905256037	71.298369276996226	78.174508806625113	84.558323629603223	89.301644944226368	91.994822632323704	Time (mins)


Drainage %




40%	0	11.783333333333333	23.683333333333334	36.016666666666666	48.05	59.95	71.816666666666663	83.733333333333334	95.61666666666666	107.53333333333333	119.3	0	19.674854744801497	39.087614005800738	58.284215813047702	70.919778127170503	78.031029929862513	82.586814887278663	86.253788267038914	88.254473894875062	89.372454204121937	90.487200020823082	50%	0	11.766666666666667	23.683333333333334	35.56666666666667	47.45	59.333333333333336	71.233333333333334	83.15	95.05	106.95	118.71666666666667	0	26.131416126945517	38.994877061146546	49.342208727902062	58.120465095655582	64.809722247635889	70.507560744824687	74.00002056634581	77.470025864815071	80.895441826536	83.339347941277893	60%	0	11.7	23.983333333333334	36.016666666666666	47.866666666666667	59.7	71.55	83.416666666666671	95.25	107.11666666666666	118.85	0	7.728571650199358	16.171997339036203	26.454171277219473	36.691170555934193	45.797802020745642	54.15747517061714	60.280282296217059	66.095529587204908	71.606288327375296	76.993991936283152	Time (mins)


Drainage %




100 psi	0	11.766666666666667	24.15	36.583333333333336	48.733333333333334	60.616666666666667	72.466666666666669	84.333333333333329	96.183333333333337	108.05	0	31.254037777741811	53.875331636658565	67.03903601142477	74.978925082582009	80.409840865442391	84.559025376765533	87.988923063769619	90.751767870065521	92.698895615349741	250 psi	0	11.95	23.916666666666668	35.766666666666666	47.616666666666667	59.466666666666669	71.316666666666663	83.166666666666671	95.033333333333331	106.88333333333334	118.61666666666666	0	25.058075279071236	43.134827727817949	55.234372574462434	63.422575126492241	69.407776413735746	74.168136295375646	78.526008775761284	81.813520501668307	84.717707703548783	87.64108003526583	400 psi	0	11.783333333333333	23.683333333333334	36.016666666666666	48.05	59.95	71.816666666666663	83.733333333333334	95.61666666666666	107.53333333333333	119.3	0	19.674854744801497	39.087614005800738	58.284215813047702	70.919778127170503	78.031029929862513	82.586814887278663	86.253788267038914	88.254473894875062	89.372454204121937	90.487200020823082	Time (mins)


Drainage %




100 psi	0	11.816666666666666	24.15	36.283333333333331	48.15	60.033333333333331	71.933333333333337	84.25	96.766666666666666	109.05	120.85	0	31.931133084731716	52.009450849494044	65.32984596548576	74.132243170646476	76.378463494971143	82.689315018791348	89.334477489660273	93.77905757246036	96.419905153355558	97.70931042226411	250 psi	0	11.916666666666666	23.833333333333332	35.716666666666669	47.616666666666667	59.516666666666666	71.433333333333337	83.35	95.266666666666666	107.18333333333334	118.96666666666667	0	31.193928965725505	45.509262812509071	57.531924340779064	66.094680499289382	72.256685894296723	76.286723687282105	81.259064403543761	85.025724625331733	88.612390104386691	91.913014676963741	400 psi	0	11.766666666666667	23.683333333333334	35.56666666666667	47.45	59.333333333333336	71.233333333333334	83.15	95.05	106.95	118.71666666666667	0	26.131416126945517	38.994877061146546	49.342208727902062	58.120465095655582	64.809722247635889	70.507560744824687	74.00002056634581	77.470025864815071	80.895441826536	83.339347941277893	Time (mins)


Drainage %




100 psi	0	11.766666666666667	23.95	36.35	48.666666666666664	60.55	72.400000000000006	84.283333333333331	96.15	108.03333333333333	119.78333333333333	0	18.502691016646502	37.430141210161686	54.85056822578683	68.870431521872248	79.528080205966063	86.630660156262152	91.972228479746946	95.363985725237995	97.327411936292151	98.146059588018261	250 psi	0	11.65	23.866666666666667	35.9	47.733333333333334	59.56666666666667	71.400000000000006	83.233333333333334	95.083333333333329	106.91666666666667	118.63333333333334	0	12.856062114005077	27.840793426879145	40.882677898741385	52.600041095538977	62.644703905256037	71.298369276996226	78.174508806625113	84.558323629603223	89.301644944226368	91.994822632323704	400 psi	0	11.7	23.983333333333334	36.016666666666666	47.866666666666667	59.7	71.55	83.416666666666671	95.25	107.11666666666666	118.85	0	7.728571650199358	16.171997339036203	26.454171277219473	36.691170555934193	45.797802020745642	54.15747517061714	60.280282296217059	66.095529587204908	71.606288327375296	76.993991936283152	Time (mins)


Drainage %




40%	0	11.783333333333333	24.033333333333335	36.15	48	59.85	71.683333333333337	83.55	95.416666666666671	107.26666666666667	119.01666666666667	130.86666666666667	0	28.632723710013764	50.951883642282937	65.38742434313518	77.081943732148787	83.726311559973652	87.572583611882138	90.880783964618743	93.362769744540401	95.180068155928495	95.787810512746347	96.471044633395977	50%	0	11.966666666666667	24.366666666666667	36.233333333333334	48.116666666666667	60	71.916666666666671	83.816666666666663	95.733333333333334	107.63333333333334	119.41666666666667	131.31666666666666	0	30.279286871600537	48.312514970183841	61.31454858062537	69.761133566141524	75.86430888655471	81.032502392648269	85.522191700205724	88.93345047519378	91.697808037146856	93.524976204699385	95.081817525488205	60%	0	11.683333333333334	23.933333333333334	36.033333333333331	47.85	59.68333333333333	71.5	83.35	95.2	107.05	118.78333333333333	131.19999999999999	0	23.372223340031155	42.53606619529404	58.557031702343522	70.321160728247222	79.09792950528886	84.827920092670652	89.325133381407625	93.23893827711494	95.737135901145962	96.773430215953425	97.672947840609751	Time (mins)


Drainage %




40%	0	11.533333333333333	23.066666666666666	34.633333333333333	46.25	57.866666666666667	69.5	81.11666666666666	92.733333333333334	104.35	115.85	127.63333333333334	0	22.669006625779414	39.610767852421233	52.418433570847476	61.432813954445741	69.815629061807826	76.096918109570737	81.329817415494716	84.074811042482821	86.883092259124211	89.039389099336645	91.084477052812275	50%	0	11.883333333333333	24.45	36.533333333333331	48.516666666666666	60.483333333333334	72.466666666666669	84.433333333333337	96.433333333333337	108.41666666666667	120.26666666666667	132.23333333333332	0	26.900684079525139	41.920164283053808	52.879029262193932	60.685516852386726	67.347668523546005	72.318298303015055	76.430923269113407	79.822782776454801	83.233271793162928	86.122856213350659	88.500538960561741	60%	0	11.733333333333333	23.633333333333333	35.483333333333334	47.366666666666667	59.25	71.11666666666666	83.016666666666666	94.88333333333334	106.76666666666667	118.51666666666667	130.38333333333333	0	23.414247773022645	43.748731702801678	57.913103345278053	67.502302978856889	73.811658713009649	79.84617836998504	85.142567104274576	88.538644184173293	90.980243926558984	93.021017324303543	95.034581579342642	Time (mins)


Drainage %




40%	0	11.683333333333334	23.466666666666665	35.25	47.05	58.85	70.650000000000006	82.45	94.25	106.05	117.75	129.56666666666666	0	22.683868962300419	38.291541479365137	50.217989369453534	58.735148735425945	64.808837629797893	71.424143610616497	76.951634362045823	80.694784147985843	83.717523615169384	85.941721832860594	88.012446188275177	50%	0	11.733333333333333	24.1	36.216666666666669	48.083333333333336	59.95	71.816666666666663	83.683333333333337	95.566666666666663	107.45	119.21666666666667	131.1	0	22.312282417371708	35.700250091276644	45.749107359478266	54.177388713101017	60.537050475779587	66.147408416017598	70.350920455380589	73.939127624206606	77.192295376629545	80.169220212810131	82.670017131959867	60%	0	11.683333333333334	24.066666666666666	36.016666666666666	47.866666666666667	59.733333333333334	71.566666666666663	83.416666666666671	95.266666666666666	107.1	118.85	130.71666666666667	0	23.643427520424122	40.60724218575595	55.33052448275614	66.131990676973345	72.243600134551187	77.888109816972957	82.806523019212435	85.830586806105032	88.35471192922563	91.105841003817957	93.217586643678146	Time (mins)


Drainage %




100 psi	0	11.783333333333333	24.033333333333335	36.15	48	59.85	71.683333333333337	83.55	95.416666666666671	107.26666666666667	119.01666666666667	130.86666666666667	0	28.632723710013764	50.951883642282937	65.38742434313518	77.081943732148787	83.726311559973652	87.572583611882138	90.880783964618743	93.362769744540401	95.180068155928495	95.787810512746347	96.471044633395977	250 psi	0	11.533333333333333	23.066666666666666	34.633333333333333	46.25	57.866666666666667	69.5	81.11666666666666	92.733333333333334	104.35	115.85	127.63333333333334	0	22.669006625779414	39.610767852421233	52.418433570847476	61.432813954445741	69.815629061807826	76.096918109570737	81.329817415494716	84.074811042482821	86.883092259124211	89.039389099336645	91.084477052812275	400 psi	0	11.683333333333334	23.466666666666665	35.25	47.05	58.85	70.650000000000006	82.45	94.25	106.05	117.75	129.56666666666666	0	22.683868962300419	38.291541479365137	50.217989369453534	58.735148735425945	64.808837629797893	71.424143610616497	76.951634362045823	80.694784147985843	83.717523615169384	85.941721832860594	88.012446188275177	Time (mins)


Drainage %




100 psi	0	11.966666666666667	24.366666666666667	36.233333333333334	48.116666666666667	60	71.916666666666671	83.816666666666663	95.733333333333334	107.63333333333334	119.41666666666667	131.31666666666666	0	30.279286871600537	48.312514970183841	61.31454858062537	69.761133566141524	75.86430888655471	81.032502392648269	85.522191700205724	88.93345047519378	91.697808037146856	93.524976204699385	95.081817525488205	250 psi	0	11.883333333333333	24.45	36.533333333333331	48.516666666666666	60.483333333333334	72.466666666666669	84.433333333333337	96.433333333333337	108.41666666666667	120.26666666666667	132.23333333333332	0	26.900684079525139	41.920164283053808	52.879029262193932	60.685516852386726	67.347668523546005	72.318298303015055	76.430923269113407	79.822782776454801	83.233271793162928	86.122856213350659	88.500538960561741	400 psi	0	11.733333333333333	24.1	36.216666666666669	48.083333333333336	59.95	71.816666666666663	83.683333333333337	95.566666666666663	107.45	119.21666666666667	131.1	0	22.312282417371708	35.700250091276644	45.749107359478266	54.177388713101017	60.537050475779587	66.147408416017598	70.350920455380589	73.939127624206606	77.192295376629545	80.169220212810131	82.670017131959867	Time (mins)


Drainage %




100 psi	0	11.683333333333334	23.933333333333334	36.033333333333331	47.85	59.68333333333333	71.5	83.35	95.2	107.05	118.78333333333333	131.19999999999999	0	23.372223340031155	42.53606619529404	58.557031702343522	70.321160728247222	79.09792950528886	84.827920092670652	89.325133381407625	93.23893827711494	95.737135901145962	96.773430215953425	97.672947840609751	250 psi	0	11.733333333333333	23.633333333333333	35.483333333333334	47.366666666666667	59.25	71.11666666666666	83.016666666666666	94.88333333333334	106.76666666666667	118.51666666666667	130.38333333333333	0	23.414247773022645	43.748731702801678	57.913103345278053	67.502302978856889	73.811658713009649	79.84617836998504	85.142567104274576	88.538644184173293	90.980243926558984	93.021017324303543	95.034581579342642	400 psi	0	11.683333333333334	24.066666666666666	36.016666666666666	47.866666666666667	59.733333333333334	71.566666666666663	83.416666666666671	95.266666666666666	107.1	118.85	130.71666666666667	0	23.643427520424122	40.60724218575595	55.33052448275614	66.131990676973345	72.243600134551187	77.888109816972957	82.806523019212435	85.830586806105032	88.35471192922563	91.105841003817957	93.217586643678146	Time (mins)


Drainage %




40%	0	12.033333333333333	24.15	36	47.85	59.716666666666669	71.566666666666663	83.433333333333337	95.266666666666666	107.13333333333334	118.85	130.69999999999999	0	30.638083930953545	51.583204646363832	64.880788680268623	73.02908255553848	78.752927484875528	82.821519995740928	86.25863091968958	89.342765053176251	91.6809224514611	93.354249996294527	94.383482659407477	50%	0	11.816666666666666	23.733333333333334	35.65	47.6	59.56666666666667	71.533333333333331	83.483333333333334	95.45	107.41666666666667	119.26666666666667	131.23333333333332	0	27.34509441743883	46.877545352635117	61.514972052302319	71.550173078167475	78.63898323864727	83.92857123143888	87.944260583870701	91.152314209860577	93.592096613728103	95.36643844542732	96.612781392198059	60%	0	11.75	23.65	35.549999999999997	47.45	59.35	71.25	83.15	95.066666666666663	106.96666666666667	118.75	130.65	0	22.624039151393795	40.206253909957773	54.976427021455301	67.454666722759626	75.787746809305787	81.619154180980118	86.234203554037364	90.245103644188191	93.10603246059263	94.891764700834642	96.0848130828645	Time (mins)


Drainage %




40%	0	11.866666666666667	24.216666666666665	36.083333333333336	47.966666666666669	59.833333333333336	71.7	83.566666666666663	95.416666666666671	107.28333333333333	119.03333333333333	130.88333333333333	0	24.839511655594947	42.565541939945668	55.02139741752454	63.678951270388055	69.824629001940522	74.261324944559064	77.986159140452642	81.272825309000211	84.059620947202717	86.36652417187365	88.488331294561178	50%	0	11.816666666666666	24.216666666666665	36.43333333333333	48.416666666666664	60.383333333333333	72.333333333333329	84.266666666666666	96.233333333333334	108.16666666666667	120.01666666666667	131.94999999999999	0	17.784182952004343	31.723906400347946	43.022523070467685	52.079792561070683	59.867283309244215	66.107253223982084	71.099995744083117	75.257826140662345	78.767365514435326	81.72303007989224	84.888651507807651	60%	0	11.716666666666667	23.633333333333333	35.516666666666666	47.4	59.266666666666666	71.150000000000006	83.033333333333331	94.9	106.78333333333333	118.55	130.44999999999999	0	16.188249700331923	31.425419360368657	43.706890380174293	54.743049946407865	63.782404005593285	71.31680601870525	77.070341480212974	81.366160778113553	85.432496175539157	88.554061301458887	92.149255255382428	Time (mins)


Drainage %




40%	0	11.55	23.133333333333333	34.716666666666669	46.233333333333334	57.75	69.266666666666666	80.783333333333331	92.283333333333331	103.8	115.2	126.68333333333334	0	23	38	49	58	64	68	72	76	78	80	83	50%	0	11.883333333333333	24.466666666666665	36.416666666666664	48.35	60.3	72.233333333333334	84.183333333333337	96.13333333333334	108.1	119.93333333333334	131.88333333333333	0	15.198756741721123	27.824327186076587	38.018261844238957	46.689423563097016	53.613774913410673	59.6650418185232	64.78317087776189	69.000735819373631	72.736270375830259	75.780896919702982	78.484327989642168	60%	0	11.883333333333333	24.333333333333332	36.233333333333334	48.1	59.983333333333334	71.86666666666666	83.75	95.63333333333334	107.51666666666667	119.3	131.21666666666667	0	15.585066553191968	30.032969253475557	40.131868196820072	50.913729138054698	59.323485444534128	66.827862419571417	72.320510896593319	76.807507127812087	80.884400546464931	83.825858937517268	86.46345906690685	Time (mins)


Drainage %




100 psi	0	12.033333333333333	24.15	36	47.85	59.716666666666669	71.566666666666663	83.433333333333337	95.266666666666666	107.13333333333334	118.85	130.69999999999999	0	30.638083930953545	51.583204646363832	64.880788680268623	73.02908255553848	78.752927484875528	82.821519995740928	86.25863091968958	89.342765053176251	91.6809224514611	93.354249996294527	94.383482659407477	250 psi	0	11.866666666666667	24.216666666666665	36.083333333333336	47.966666666666669	59.833333333333336	71.7	83.566666666666663	95.416666666666671	107.28333333333333	119.03333333333333	130.88333333333333	0	24.839511655594947	42.565541939945668	55.02139741752454	63.678951270388055	69.824629001940522	74.261324944559064	77.986159140452642	81.272825309000211	84.059620947202717	86.36652417187365	88.488331294561178	400 psi	0	11.55	23.133333333333333	34.716666666666669	46.233333333333334	57.75	69.266666666666666	80.783333333333331	92.283333333333331	103.8	115.2	126.68333333333334	0	23	38	49	58	64	68	72	76	78	80	83	Time (mins)


Drainage %




100 psi	0	11.816666666666666	23.733333333333334	35.65	47.6	59.56666666666667	71.533333333333331	83.483333333333334	95.45	107.41666666666667	119.26666666666667	131.23333333333332	0	27.34509441743883	46.877545352635117	61.514972052302319	71.550173078167475	78.63898323864727	83.92857123143888	87.944260583870701	91.152314209860577	93.592096613728103	95.36643844542732	96.612781392198059	250 psi	0	11.816666666666666	24.216666666666665	36.43333333333333	48.416666666666664	60.383333333333333	72.333333333333329	84.266666666666666	96.233333333333334	108.16666666666667	120.01666666666667	131.94999999999999	0	17.784182952004343	31.723906400347946	43.022523070467685	52.079792561070683	59.867283309244215	66.107253223982084	71.099995744083117	75.257826140662345	78.767365514435326	81.72303007989224	84.888651507807651	400 psi	0	11.883333333333333	24.466666666666665	36.416666666666664	48.35	60.3	72.233333333333334	84.183333333333337	96.13333333333334	108.1	119.93333333333334	131.88333333333333	0	15.198756741721123	27.824327186076587	38.018261844238957	46.689423563097016	53.613774913410673	59.6650418185232	64.78317087776189	69.000735819373631	72.736270375830259	75.780896919702982	78.484327989642168	Time (mins)


Drainage %




100 psi	0	11.75	23.65	35.549999999999997	47.45	59.35	71.25	83.15	95.066666666666663	106.96666666666667	118.75	130.65	0	22.624039151393795	40.206253909957773	54.976427021455301	67.454666722759626	75.787746809305787	81.619154180980118	86.234203554037364	90.245103644188191	93.10603246059263	94.891764700834642	96.0848130828645	250 psi	0	11.716666666666667	23.633333333333333	35.516666666666666	47.4	59.266666666666666	71.150000000000006	83.033333333333331	94.9	106.78333333333333	118.55	130.44999999999999	0	16.188249700331923	31.425419360368657	43.706890380174293	54.743049946407865	63.782404005593285	71.31680601870525	77.070341480212974	81.366160778113553	85.432496175539157	88.554061301458887	92.149255255382428	400 psi	0	11.883333333333333	24.333333333333332	36.233333333333334	48.1	59.983333333333334	71.86666666666666	83.75	95.63333333333334	107.51666666666667	119.3	131.21666666666667	0	15.585066553191968	30.032969253475557	40.131868196820072	50.913729138054698	59.323485444534128	66.827862419571417	72.320510896593319	76.807507127812087	80.884400546464931	83.825858937517268	86.46345906690685	Time (mins)


Drainage %




100 psi	0% oil	10% oil 	20 % oil	95	95.787810512746347	93.354249996294527	 400 psi	0% oil	10% oil 	20 % oil	90.487200020823082	85.941721832860594	80	
Drainage %




100 psi	0% oil	10% oil 	20 % oil	97.70931042226411	93.524976204699385	95.36643844542732	 400 psi	0% oil	10% oil 	20 % oil	83.339347941277893	80.169220212810131	75.780896919702982	
Drainage %




100 psi	0% oil	10% oil 	20 % oil	98.146059588018261	96.773430215953425	94.891764700834642	 400 psi	0% oil	10% oil 	20 % oil	76.993991936283152	93.217586643678146	83.825858937517268	
Drainage %




40%	30	60	90	120	77.951100000000011	92.926780000000022	104.74184999999997	131.74949999999998	50%	30	60	90	120	100.95819000000003	127.08156976744183	143.47934328358204	168.64325999999997	60%	30	60	90	120	125.71138947368424	156.43272413793105	213.12690625000002	267.72980000000001	Time (mins)


Bubble size (um)




40%	30	60	90	120	56.158699999999996	76.287954545454554	94.003430000000023	104.56480999999999	50%	30	60	90	120	68.618939999999995	92.321889999999968	104.72322000000003	117.98912000000001	60%	30	60	90	120	83.662209999999973	100.48661000000006	126.78412222222227	146.32411111111105	TIme (mins)


Bubble size (um)




40%	30	60	90	120	53.409662921348314	72.703780000000037	87.262	95.968109999999982	50%	30	60	90	120	58.892659999999978	80.068250000000006	95.333749999999952	109.71638000000006	60%	30	60	90	120	74.009960000000021	92.692890000000048	108.20554000000004	115.16835	Time (mins)


Bubble size (um)




40%	30	60	90	120	79.104210000000009	100.04308999999995	108.1765737704918	127.18077777777778	50%	30	60	90	120	97.625779999999963	118.21353999999992	128.62041249999996	134.66309859154933	60%	30	60	90	120	107.03590999999999	139.51568253968262	180.0803333333333	193.40952631578944	Time (mins)


Bubble size (um)




40%	30	60	90	120	66.647560000000041	81.674569999999989	96.015529999999984	104.57911999999995	50%	30	60	90	120	75.422780000000017	100.19665999999998	111.09647	129.77287058823532	60%	30	60	90	120	70.061549999999983	94.35993000000002	112.42831764705878	129.67065789473682	Time (mins)


Bubble size (um)




40%	30	60	90	120	56.175580000000011	70.36681999999999	82.341209999999975	91.061599999999984	50%	30	60	90	120	63.124419999999965	81.987819999999999	95.509679999999989	116.18917999999999	60%	30	60	90	120	67.815689999999989	85.703549999999993	102.79900999999998	117.12828735632186	Time (mins)


Bubble size (um)




40%	30	60	90	120	71.313770000000019	98.369069999999979	106.37393749999998	125.12221739130433	50%	30	60	90	120	80.98248000000001	94.683890000000034	103.4361098901099	109.48114285714284	60%	30	60	90	120	90.070959999999999	118.36587058823527	136.49986666666666	126.03163043478268	Time (mins)


Bubble size (um)




40%	30	60	90	120	63.612839999999984	81.073239999999956	85.696220000000011	95.170479999999984	50%	30	60	90	120	65.554069999999996	88.791819999999959	99.688100000000034	120.33748051948054	60%	30	60	90	120	72.748049999999978	98.589421052631621	130.53155932203387	136.76538775510204	Time (mins)


Bubble size (um)




40%	30	60	90	120	52.193210000000029	67.222380000000015	78.703459999999993	85.353059999999999	50%	30	60	90	120	55.930059999999997	74.96823999999998	94.91968999999996	102.73395000000004	60%	30	60	90	120	65.028120000000015	82.937360000000012	97.530569999999983	109.6533260869565	Time (mins)


Bubble size (um)
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